## Slide 1
Measured and Simulated Strain in the Large Scale Coil with Considering Radial Compressibility
Shannon Griffin, Yu Suetomi, Ernesto Bosque, Kwangmin Kim, Jun Lu, Hongyu Bai
Iain Dixon
National High Magnetic Field Laboratory at Florida State University
MT29, Boston, MA
Hubertus Weijers Memorial: High Field Magnet, Jul 5, 2025, 5:15 PM
Momentum D

## Slide 2
LSC insert
45T outsert
Background on the Large Scale Coil
Bore size (radius) | Coil length | Stored energy
13 cm | 19 cm | 212.6 kJ
70 cm
Notes: -The Large Scale Coil development and testing is part of the development of the 40T project
-Both the LSC and 40T are high field, insulated high-temperature superconducting magnets, constructed from REBCO tapes, would with SS and copper co-wind
-The 40T will be a user magnet
-REBCO tapes will experience strain due to high Lorentz forces
-The things we learn from the LSC experiments contribute to an improved 40T design
-The LSC is tested with the 45T outsert

## Slide 3
LSC
outsert
2D, axisymmetric model of the LSC with the 45T outsert
Test Conditions: Background field: 11.5 T
Tests were preformed over the course of several days.
Goals:
  Learn from measured results to refine our simulation models.
  Optimize 40T magnet design.
Background on the Large Scale Coil
Notes: - Shown here is a comsol simulation of the LSC, displaying the magnetic field, at full field
The LSC is tested in a background field of 11.5 T
Reaches a field of 19.2 T
Strain gauges on inboard and outboard location on outmost turn of the overbanding
Inboard- closer to the midplane
Outboard- further form the midplane
Goals are to learn from comparisons of experimental results to simulated results and to refine our models

## Slide 4
LSC
2D, axisymmetric model of the LSC with the 45T outsert
outsert
Background on the Large Scale Coil
Winding pack
Cu
SS
REBCO
mandrel
Cu
…..
22 double pancake coils
Notes: -Simulations are 2D, axisymmetric
-Pancakes in the LSC are mirrored about the midplane, so half of the LSC is modeled

## Slide 5
LSC
2D, axisymmetric model of the LSC with the 45T outsert
outsert
Background on the Large Scale Coil
Stainless steel over-banding
The over-banding is thicker on disks further away from the midplane.
There is an increase in screening currents as you move further from the midplane.
Therefore, these pancakes are designed with more structural support
Notes: -Simulations are 2D, axisymmetric
-Pancakes in the LSC are mirrored about the midplane, so half of the LSC is modeled

## Slide 6
LSC
2D, axisymmetric model of the LSC with the 45T outsert
Background on the Large Scale Coil
outsert
Experimental results are from disk 1 & disk 33
Strain gauges were placed on the “inboard” and “outboard” locations on the outermost over-band of these disks.
Notes: -In this study, data from the strain gauges on disks 1 and 33 are compared to measured data
-stars denote their location in the LSC

## Slide 7
Calculates -Current density
-Magnetic field
Electromagnetic model
Calculates Displacements (stress, strain, tilting angle)
Elastic structural model
Coupling analysis during charging process (time stepping)
Lorentz force
Tape tilting angle
Structural analysis during winding process (steady)
Structural analysis during cooling process (steady)
Tape width
Step1.
Step2.
Step3.
Homogenized bulk assumed winding pack
Fully discrete winding pack
(Frictionless contact boundary)
Coupling analysis during charging process (time stepping)
Radial build of winding
Current density dist.
Mandrel
Radial build of winding
Tape width
Hoop strain dist.
FLOSSS (Florida Screening Strain Software)
T-A method
Simulation Model: ‘FLOSSS’
Notes: The simulation is performed by 3 steps, stady state structural analysis of winding process and cooling process and
Time stepping coupling analysis during charging process.
This is coupled of electromagnetic model and elastic structural model. This step is numerically solved with feedback of these parameters at each time step.

## Slide 8
Chart: D1 inboard/outboard strain [%]
Chart: Insert Current [A]
Measured and Simulated Strain
Dual Operation to 612 A:
First, outsert is charged (generates a background field of 11.5 T).
  Strain is close to 0 during outsert charging.
Then, insert is charged to 612 A.
Measured strain was compensated by compensation gauge
Predicted strain is greater than measured strain on the inboard and outboard locations of the disks.
Inboard
Outboard
Coil’s end
Coil’s midplane
Notes: -Data from various experimental runs were compared, dual operation to 612 A for disks 1 and 33 were chosen for repeatability
-all measured data is compensated by the compensation gauge
-Simulated inboard and outboard strain is consistently higher than measured inboard and outboard strain
-for disk 33: difference between inboard and outboard strain is small
tilt angle at the end of the over-banding is much less for measured data
-Simulated data is taken form the same point on the disks as inboard and outboard strain gauge locations

## Slide 9
Chart: Insert Current [A]
Measured and Simulated Strain
Tilt at the end of the over-banding is greater for predicted strain
Chart: D1 inboard/outboard strain [%]
Dual Operation to 612 A:
First, outsert is charged (generates a background field of 11.5 T).
  Strain is close to 0 during outsert charging.
Then, insert is charged to 612 A.
Measured strain was compensated by compensation gauge
Inboard
Outboard
Coil’s end
Coil’s midplane
Notes: -Data from various experimental runs were compared, dual operation to 612 A for disks 1 and 33 were chosen for repeatability
-all measured data is compensated by the compensation gauge
-Simulated inboard and outboard strain is consistently higher than measured inboard and outboard strain
-for disk 33: difference between inboard and outboard strain is small
tilt angle at the end of the over-banding is much less for measured data

## Slide 10
Simulations consistently predict higher strain than what is measured
Compressibility of winding pack?
  Macroscopic profile distribution
   application of “Gap offset” method
Compressibility of stainless-steel over-banding?
  Microscopic roughness
  application of compressibility model
Axial clamping?
  Axial Pressure
  application of uniform current density assumption
  application of edge friction
Effective radial modulus should be dominated by… macroscopic thickness distribution of REBCO tapes
Effective radial modulus should be dominated by… microscopic roughness on steel tapes.
The effective radial modulus should not be the same as the material property.
Evidence of radial compressibility on REBCO tapes:
Yan, Y., Kim, J., Bong, U., Jang, W., Kim, G., Park, J., & Hahn, S. (2023). Measurement and analysis of winding stresses in dry-wound pancake coils considering nonlinear compressive behaviors. Superconductor Science and Technology, 36(11), 115019. https://doi.org/10.1088/1361-6668/
Xue, S., Kwon, J., Guo, Y., Garg, T., Sumption, M. D., & Collings, E. W. (2023). Compressive Stress-Strain Behavior of Rebco coated conductors and Cables. IEEE Transactions on Applied Superconductivity, 33(5), 1–6. https://doi.org/10.1109/tasc.2023.3247370
Park, J., Kim, J., Yan, Y., & Hahn, S. (2024). Diameter Change of Dry Wound rebco solenoid pancake coil by winding tension. IEEE Transactions on Applied Superconductivity, 34(5), 1–5. https://doi.org/10.1109/tasc.2024.3362772
Discrepancy between measured data and simulations?
Actual contact area
Assumed contact area
Assumed contact area
Actual contact area
Notes: Why is there a discrepancy between measured and simulated results?
There are a few potential culprits that will be examined in this study
Compressibility of the winding pack due to macroscopic roughness
   gap_off method will be applied to address this
Compressibility of the stainless steel over-banding due to microscopic roughness
   compressibility model will be applied to address this
Axial clamping due to axial pressure
   Application of uniform current density and edge friction will be applied to address this

## Slide 11
Chart: Measured tape profile, disk 1 (SP 1129)
Top (above REBCO) | 17.042 | 15.528 | 15.528 | 15.528 | 14.77 | 15.338 | 18.179 | 18.936 | 19.883 | 21.019 | 21.208 | 22.913 | 24.617 | 26.321 | 26.889 | 26.134 | 28.783 | 28.025 | 26.51 | 27.457 | 28.972 | 28.025 | 29.161 | 26.7 | 26.51 | 28.404 | 24.806 | 24.996 | 22.723 | 21.208 | 21.019 | 19.883 | 18.179 | 16.664 | 16.474 | 14.013 | 15.149 | 15.149 | 15.717 | 17.042
Bottom (below REBCO) | 17.989 | 15.9066 | 16.664 | 17.042 | 18.368 | 16.853 | 17.989 | 20.262 | 20.451 | 21.208 | 21.208 | 22.723 | 23.102 | 24.996 | 24.238 | 24.427 | 25.753 | 27.457 | 26.511 | 28.404 | 27.078 | 26.7 | 27.836 | 27.457 | 25.374 | 24.617 | 24.238 | 23.291 | 22.344 | 21.587 | 21.966 | 20.072 | 18.368 | 17.61 | 16.664 | 15.528 | 15.528 | 15.906 | 16.285 | 17.61
Chart: Measured tape profile, disk 33 (SP1142)
Top | 17.334 | 16.67 | 23.672 | 14.501 | 15.847 | 15.004 | 15.17 | 14.337 | 17.02 | 15.333 | 17.013 | 16.168 | 17.667 | 17.334 | 18.007 | 18.679 | 17.513 | 16.847 | 17.341 | 18.012 | 18.019 | 18.501 | 18.007 | 18.012 | 17.705 | 17.334 | 17.17 | 18.17 | 17.17 | 18.216 | 17.883 | 16.568 | 16.18 | 17.513 | 17.529 | 16.697 | 17.174 | 19.518 | 16.863 | 18.86 | 17.846 | 18.028
Bottom | 18.003 | 17.341 | 15.847 | 15.841 | 16.337 | 15.168 | 17.001 | 15.168 | 17.5 | 15.167 | 17.003 | 16.333 | 16.667 | 17.334 | 17.667 | 20.167 | 16.67 | 17.167 | 18.833 | 20.501 | 19.167 | 17.337 | 18.336 | 18.186 | 18.333 | 22.167 | 18.667 | 16.837 | 19.34 | 18.007 | 17.17 | 18.012 | 18.003 | 17.334 | 18.019 | 15.847 | 15.333 | 16.188 | 17.84 | 18.012 | 17.5 | 17.833
REBCO tapes have an uneven profile – they are not perfectly flat as assumed for simulations
Penalty method with gap offset
For more information on this topic, please refer to my colleague, Dr. Yu Suetomi’s talk: Screening current induced stress and strain analysis considering thickness variation along the width of REBCO tape
Macroscopic profile distribution on REBCO tapes
Applied to REBCO tapes in the winding pack
Notes: On the tape used for disk 1 there is a significant change in thickness along the tape width
In comparison, on the tape used for disks 12 and 33 there is not that much variation along the tape width
 tape thickness profile is used to derive a function which is input into FLOSSS
 function is implemented into contact physics in the solid mechanics model
 This simulates a gap along the width where the REBCO is the thinnest
 more radially compressible where REBCO is thinner, radially stiffer where REBCO is thicker
For more information on this see Yu Suetomi’s talk and paper!!

## Slide 12
Compressibility model
  Fitted to experimental data in the above study by Yufan Yan
Microscopic roughness on stainless steel tapes
SS tapes have an uneven profile – they are not perfectly flat as assumed for simulations
Applied to SS over-banding
Penalty Method
=gap distance, =penalty factor
Notes: -Stainless steel tapes are assumed to be perfectly flat in our simulations
-in reality, they have a microscopic roughness
-this causes the elastic modulus of a stack of stainless steel tapes to be lower than that of stainless steel
-Yufan Yan has done some work in regards to fitting a compressibility model to data from experiments
-I applied this model to the stainless steel over banding in the LSC model

## Slide 13
Gap offset applied to REBCO + compressibility model applied to over-banding
Disk 1
Chart: Inboard Strain [%]
D1_IN, gap_off+low mod OB | 0 | 0.097023
D1 In, gap_off | 0 | 0.20632
Chart: Insert Current [A]
D1_OUT, gap_off+low mod OB | 0 | 0.14585
D1 Out, gap_off | 0 | 0.24848
Penalty method with gap offset decreases inboard and outboard strain in disk 1
  REBCO used in disk 1 has a large thickness variation
The application of the compressibility model on the stainless steel over-banding decreases simulated inboard and outboard strain.
Disk 1
Inboard
Outboard
Coil’s end
Coil’s midplane
Inboard strain gauge
Outboard strain gauge
Strain gauge location
Measured tape profile
Measured
Simulated
Hard contact
w/ winding compressibility of REBCO
w/ winding compressibility of REBCO &
winding compressibility of OB
Notes: -Results for disk 1 that account for macroscopic thickness variation in the REBCO, and microscopic roughness on SS -Decreases inboard and outboard strain
-this makes sense because disk 1 has both a large amount of overbanding compared to other disks, and has a large thickness distribution in the tape used to manufacture this disk

## Slide 14
Gap offset applied to REBCO + compressibility model applied to over-banding
Disk 33
Chart: Inboard Strain [%]
D33_IN, gap_off+low mod OB | 0 | 0.30495
D33 In, gap_off | 0 | 0.32538
Chart: Insert Current [A]
D_33_OUT, gap_off+low mod OB | 0 | 0.40816
D33 Out, gap_off | 0 | 0.42858
Penalty method with gap offset doesn’t really decrease inboard and outboard strain in disk 33
  REBCO used in disk 33 is relatively flat
The decrease of simulated inboard and outboard strain due to the application of the compressibility model on the stainless steel over-banding is less apparent in disk 33.
  less over-banding on these disks
Disk 33
Inboard strain gauge
Outboard strain gauge
Inboard
Outboard
Coil’s end
Coil’s midplane
Strain gauge location
Measured tape profile
Measured
Simulated
Hard contact
w/ winding compressibility of REBCO
w/ winding compressibility of REBCO &
winding compressibility of OB
Notes: -results where macroscopic thickness distribution on REBCO and microscopic roughness on over-banding are accounted for on disk 33
-accounting for these don’t make as much of a difference for disk 33
-disk 33 has mess overbanding than disk 1, and the REBCO tape profile is relatively flat,

## Slide 15
[%]
Original simulation (Hard contact)
Simulation w/ gap offset
Simulation w/ gap offset and OB winding compressibility
Max: 0.35%, Min-0.18%
Max: 0.54%, Min-0.34%
Max: 0.59%, Min-0.33%
Hoop strain in REBCO tapes
Outboard strain gauge location
Strain is harder to distribute to outer radius of the over-band
Strain concentrates due to gap between tapes
I = 586 A under BM field
Simulated Strain in Disk 1
Notes: -Taking a closer look at the strain distribution for three cases:
the original simulation where tapes are assumed to be perfectly flat, macroscopic thickness distribution on REBCO, and both macroscopic and miscroscopic roughness
-when the REBCO tape profile is applied, the strain concentrates, due to the uneven tape profile causing gaps between the tapes
-when the compressibility model is applied to the overbanding, strain doesn’t distribute very well to the outer radius of the over band
-this causes a lower strain on the inboard and outboard edges of the overbanding ( a better match to measured data), but higher strain in the winding pack
-Remind the audience what gap_offset and OB winding compressibility is!!
-Most important: less strain measured at the inboard and outboard gauges means higher strain in the winding pack!!!!

## Slide 16
Chart: Disk number from coil end
| 44 | 43 | 42 | 41 | 40 | 39 | 38 | 37 | 36 | 35 | 34 | 33 | 32 | 31 | 30 | 29 | 28 | 27 | 26 | 25 | 24 | 23 | 22 | 21 | 20 | 19 | 18 | 17 | 16 | 15 | 14 | 13 | 12 | 11 | 10 | 9 | 8 | 7 | 6 | 5 | 4 | 3 | 2 | 1
w/ WT, w/o gap offset at 645 A | 0.35 | 0.34761 | 0.35219 | 0.35077 | 0.35342 | 0.36227 | 0.3573 | 0.38424 | 0.38416 | 0.47948 | 0.47394 | 0.5306 | 0.52669 | 0.5369 | 0.52691 | 0.50793 | 0.51237 | 0.49679 | 0.48391 | 0.46403 | 0.45734 | 0.48187 | 0.47047 | 0.5002 | 0.46659 | 0.46553 | 0.48637 | 0.50803 | 0.48935 | 0.51776 | 0.54176 | 0.52033 | 0.5304 | 0.47348 | 0.47793 | 0.38463 | 0.38017 | 0.35485 | 0.36317 | 0.35419 | 0.34924 | 0.34562 | 0.35153 | 0.35884
w/o WT, w/ gap offset at 600 A | 0.41542 | 0.42059 | 0.51448 | 0.5771 | 0.53565 | 0.57099 | 0.62354 | 0.73899 | 0.50475 | 0.46265 | 0.48922 | 0.40692 | 0.5323 | 0.55431
Discussion: Max strain in the winding pack
Chart: SP 1127
total | 77.333 | 74.333 | 70.5 | 72.001 | 68.9997 | 73.667 | 76 | 78.001 | 80.001 | 83.334 | 83.333 | 87.334 | 89.5 | 90 | 92.334 | 94.501 | 96.666 | 97.67 | 99.5 | 97.667 | 96.833 | 98.833 | 96.667 | 94.5 | 94.499 | 90.833 | 88.333 | 88.499 | 85.5 | 82.167 | 81.667 | 79.5 | 77.5 | 74.833 | 72.167 | 68.001 | 68.5 | 69.999 | 71.167 | 75.667
Chart: SP 1119
total | 86.666 | 83 | 81.166 | 80.667 | 79.833 | 80.667 | 82.833 | 83.333 | 83.001 | 85.667 | 87.497 | 87.997 | 89 | 89.497 | 89.833 | 90.997 | 91.833 | 91.837 | 94.334 | 93.167 | 93.167 | 93.167 | 91.833 | 92.501 | 96.001 | 91.167 | 89.5 | 89.336 | 89.497 | 84.666 | 85.001 | 83.836 | 84.667 | 81.333 | 82.833 | 82.667 | 87.166 | 84.001 | 80.5 | 83.166 | 83.167 | 86.833
inner
outer
Chart: SP1105
Total | 96.509 | 88.501 | 86.004 | 84.341 | 83.506 | 82.167 | 82.5 | 83.167 | 81.168 | 82.167 | 81.002 | 82.667 | 80.834 | 81.501 | 79.834 | 80.835 | 79.669 | 81.503 | 80.5 | 82.003 | 80.5 | 82.5 | 80.334 | 84.001 | 83.167 | 85.001 | 83.833 | 84.667 | 85.667 | 85.503 | 85.334 | 86.506 | 86.669 | 87.516 | 89.002 | 94.72 | 97 | 111.168
inner, outer
Notes: -here is a plot of tensile hoop strain on the REBO tapes in various disks, with and without the macroscopic thickness distribution of the REBCO applied
-Increase in strain varies for each disk
-here are the profiles of inner and outer tapes used to make the disks

## Slide 17
Chart: Disk number from coil end
| 44 | 43 | 42 | 41 | 40 | 39 | 38 | 37 | 36 | 35 | 34 | 33 | 32 | 31 | 30 | 29 | 28 | 27 | 26 | 25 | 24 | 23 | 22 | 21 | 20 | 19 | 18 | 17 | 16 | 15 | 14 | 13 | 12 | 11 | 10 | 9 | 8 | 7 | 6 | 5 | 4 | 3 | 2 | 1
w/ WT, w/o gap offset at 645 A | 0.35 | 0.34761 | 0.35219 | 0.35077 | 0.35342 | 0.36227 | 0.3573 | 0.38424 | 0.38416 | 0.47948 | 0.47394 | 0.5306 | 0.52669 | 0.5369 | 0.52691 | 0.50793 | 0.51237 | 0.49679 | 0.48391 | 0.46403 | 0.45734 | 0.48187 | 0.47047 | 0.5002 | 0.46659 | 0.46553 | 0.48637 | 0.50803 | 0.48935 | 0.51776 | 0.54176 | 0.52033 | 0.5304 | 0.47348 | 0.47793 | 0.38463 | 0.38017 | 0.35485 | 0.36317 | 0.35419 | 0.34924 | 0.34562 | 0.35153 | 0.35884
w/o WT, w/ gap offset at 600 A | 0.41542 | 0.42059 | 0.51448 | 0.5771 | 0.53565 | 0.57099 | 0.62354 | 0.73899 | 0.50475 | 0.46265 | 0.48922 | 0.40692 | 0.5323 | 0.55431
Discussion: Max strain in the winding pack
Chart: SP 1127
total | 77.333 | 74.333 | 70.5 | 72.001 | 68.9997 | 73.667 | 76 | 78.001 | 80.001 | 83.334 | 83.333 | 87.334 | 89.5 | 90 | 92.334 | 94.501 | 96.666 | 97.67 | 99.5 | 97.667 | 96.833 | 98.833 | 96.667 | 94.5 | 94.499 | 90.833 | 88.333 | 88.499 | 85.5 | 82.167 | 81.667 | 79.5 | 77.5 | 74.833 | 72.167 | 68.001 | 68.5 | 69.999 | 71.167 | 75.667
Chart: SP 1119
total | 86.666 | 83 | 81.166 | 80.667 | 79.833 | 80.667 | 82.833 | 83.333 | 83.001 | 85.667 | 87.497 | 87.997 | 89 | 89.497 | 89.833 | 90.997 | 91.833 | 91.837 | 94.334 | 93.167 | 93.167 | 93.167 | 91.833 | 92.501 | 96.001 | 91.167 | 89.5 | 89.336 | 89.497 | 84.666 | 85.001 | 83.836 | 84.667 | 81.333 | 82.833 | 82.667 | 87.166 | 84.001 | 80.5 | 83.166 | 83.167 | 86.833
inner
outer
Chart: SP1105
Total | 96.509 | 88.501 | 86.004 | 84.341 | 83.506 | 82.167 | 82.5 | 83.167 | 81.168 | 82.167 | 81.002 | 82.667 | 80.834 | 81.501 | 79.834 | 80.835 | 79.669 | 81.503 | 80.5 | 82.003 | 80.5 | 82.5 | 80.334 | 84.001 | 83.167 | 85.001 | 83.833 | 84.667 | 85.667 | 85.503 | 85.334 | 86.506 | 86.669 | 87.516 | 89.002 | 94.72 | 97 | 111.168
inner, outer
Tapes that are thick in the center and thin at the edges lead to high strain in the winding pack
Notes: -tapes that are very thick in the center and thin at the edges cause large strain in in the winding pack

## Slide 18
Chart: Disk number from coil end
| 44 | 43 | 42 | 41 | 40 | 39 | 38 | 37 | 36 | 35 | 34 | 33 | 32 | 31 | 30 | 29 | 28 | 27 | 26 | 25 | 24 | 23 | 22 | 21 | 20 | 19 | 18 | 17 | 16 | 15 | 14 | 13 | 12 | 11 | 10 | 9 | 8 | 7 | 6 | 5 | 4 | 3 | 2 | 1
w/ WT, w/o gap offset at 645 A | 0.35 | 0.34761 | 0.35219 | 0.35077 | 0.35342 | 0.36227 | 0.3573 | 0.38424 | 0.38416 | 0.47948 | 0.47394 | 0.5306 | 0.52669 | 0.5369 | 0.52691 | 0.50793 | 0.51237 | 0.49679 | 0.48391 | 0.46403 | 0.45734 | 0.48187 | 0.47047 | 0.5002 | 0.46659 | 0.46553 | 0.48637 | 0.50803 | 0.48935 | 0.51776 | 0.54176 | 0.52033 | 0.5304 | 0.47348 | 0.47793 | 0.38463 | 0.38017 | 0.35485 | 0.36317 | 0.35419 | 0.34924 | 0.34562 | 0.35153 | 0.35884
w/o WT, w/ gap offset at 600 A | 0.41542 | 0.42059 | 0.51448 | 0.5771 | 0.53565 | 0.57099 | 0.62354 | 0.73899 | 0.50475 | 0.46265 | 0.48922 | 0.40692 | 0.5323 | 0.55431
Discussion: Max strain in the winding pack
Tapes that are thick in the center and thin at the edges lead to high strain in the winding pack
Considering the macroscopic roughness of the REBCO tapes using the gap offset method, leads to higher strain in the winding pack for disks which use tapes with a large thickness difference, such as in module 11.
  Radial compressibility of disks leads to concerns of high strain on REBCO tapes!
However, module 11 was not damaged during testing
This indicates that for disks closer to the midplane, edge friction due to axial clamping may reduce strain in the winding pack.
Notes: -Mention mod 11 was not damaged even though high strain was predicted
-axial clamping may help reduce strain
-use this as a segway into axial clamping

## Slide 19
Chart: Insert Current [A]
D33_IN, gap_off+low mod OB+edge frict. | 0 | 0.34603
D_33_OUT, gap_off+low mod OB+edge frict. | 0 | 0.37883
Simplified friction equation:
Axial forces are exported from a separate COMSOL simulation which simulates SM of the whole coil with homogenized disk
Tilt at the end of the OB is very similar for measured results and results with edge friction! (difference between outboard and inboard strain)
Edge Friction + Axial Clamping
Disk 33
Simulated, w/ winding compressibility of REBCO & OB
& Edge friction
Measured outboard
Measured inboard
Simulated, Hard contact
Outboard
Inboard
Outboard
Inboard
Fz
Fed
Fed
FLorentz
FLorentz
Edge friction
Difference in magnitude may be due to microscopic roughness on REBCO tape surfaces.
Penalty method with gap offset on winding pack and compressibility model on over-banding are also included
Stationary study where Lorentz forces are taken from time of interest.
Notes: -Next I implemented an edge friction force
Axial forces are imported from another COMSOL model which simulated the solid mechanics of the whole coil with homogenized disks
I used the simplified friction equation for convergence
Results are shown against original simulated results and measured results.
Tilt at the end of the ovebanding is very similar to measured results
There is still a difference in magnitude…….simulated strain is still higher than measured, this is also the case for disk 1
The difference in magnitude may be due to the macroscopic roughness on the REBCO tape

## Slide 20
Implementing the gap offset method, PLUS modeling the stainless-steel over-banding with a compressibility model produces results closer to measured strain, particularly for disk 1.
  Disk 1: large thickness difference in REBCO tape profile, thick over-banding.
Radial compressibility increases strain in the winding pack.
Edge friction may help reduce strain for tapes near the midplane.
Radial compressibility is a factor that we need to consider when designing dry-wound REBCO coils.
The over-banding does not support the loads as once thought.
This supports the need to use distributed reinforcement in the 40 T, rather than lumped over-banding.
Other factors to consider in SM simulations:
  Microscopic roughness on tapes could mean disks are even more radially compressible.
    This could explain why predicted strain is still higher than measured strain.
    There is on going work, measuring the compressibility of tape stacks, for implementation into FLOSSS
Discussion

## Slide 21
THANK YOU!
This work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-2131790, DMR-2128556, and the State of Florida.