## Slide 1
Corrections only after layers 6, 8, 10, 12
Data after layer 6 Data after layer 12
Construction of a Superconducting “Direct Wind” R&D Magnet for the EIC Interaction Region
M. D. Anerella, Y. Bai, J. Becker, A. Ben-Yahia, A. Drees, J. Escallier, P. Joshi, F. Kurian, A. Marone, C. Runyan, V. Teotia, W. Wahl, P. Xu, Brookhaven National Laboratory, Upton, NY 11973, U.S.A.. H. Witte, MIT, LNS
Abstract- Brookhaven National Laboratory (BNL) was chosen to host the international Electron-Ion Collider (EIC), which will collide high energy and highly polarized hadron and electron beams with a center of mass energy up to 140 GeV. The Interaction Region (IR) requires several large aperture, relatively high field superconducting dipole and quadrupole magnets, some of which are very closely spaced. A value engineering effort is underway as part of the EIC Project to construct and test a Direct Wind magnet (coil comprised of NbTi conductor deposited directly onto a support tube, in this instance tapered, and secured mechanically against Lorentz forces afterwards) to replace two Rutherford cable collared magnets. This magnet exceeds the combination of aperture, number of coil layers, and magnetic field, as compared to existing accelerator and R&D Direct Wind magnets to date. Furthermore, construction has been completed using a newly commissioned winding machine, upgraded in anticipation of upcoming EIC production coil fabrication. Construction issues, lessons learned, and results shall be discussed, including the planned and accomplished corrections to multipoles made in successive coil layers based on warm magnetic measurements of preceding layers.
*Work supported by Brookhaven Science Associates, LLC under Contract No. DE-SC0012704 with the US Department of Energy.
Structural Analysis
Fabrication Status
An R&D magnet has been designed & built to a design which represents a cost savings and a technical improvement over (2) Rutherford cable magnets in the EIC IR which it would replace. It is the most challenging Direct Wind magnet built to date and is scheduled to be tested this summer.
SUMMARY
EIC Interaction Region Overview
One tapered direct wind magnet replaces 2 Rutherford cable magnets
(Q1ApF and Q1BpF)
Mechanical Design
Coil fabrication complete
Magnet assembly, wiring complete
Q1ABpF – New Magnet Concept
Multipole Corrections During Construction
Lessons Learned
b3
a3
b4
Wiring file errors
  Wires overlapping
  Corner radii too small
  Incorrect taper
Very large number of filler parts required
  Immediate term – increase labor resources to match need
  Short term – design/build/use stamping die to cut shapes
  Long term – identify & purchase programmable planar cutter
Cable twist pitch
  Two varieties used, the smaller of the two proved more flexible
  Order production cable to preferred configuration
Delamination after initial cure of layer 10
  Greatest number of DW coil layers to date
  Successfully remediated
  Procedure revised to ward against future occurrence, all layers, all coils
  Add pre-winding software checks of wiring files
a4
b3
b4
a3
a4