## Slide 1: Relation between strain energy release rate and heat generated at cryogenic temperatures
the case for CTD-101K epoxy magnet impregnant
to improve understanding of stability of superconducting magnets
Jan van Steenlandt, Anna Kario, Simon Otten, Sander Wessel, Laurent Warnet, Hans van Oort and Herman ten Kate
University of Twente, The Netherlands, May 20, 2025.
1

## Slide 2: Why heat and strain energy release rate?
Stability of Nb3Sn superconducting magnet windings highly depends on the type of magnet impregnant [1]
How to improve this stability?
Possible explanation: heat generated during fractures of the impregnant in the vicinity of Nb3Sn, how much energy it takes to propagate?
How to quantify this?
Current ramp number [-]
Cable current [kA]
Limit of short strands
Notes: The training is magnet architecture specific, in this case I show an example for CCT magnets

## Slide 3: Motivation - Nb3Sn cable/impregnants training study at Twente and PSI
Training curves measured using the BOX facility.
BOX facility sample holder.
BOX (Bonding Experiment) = small scale cable test facility to investigate different impregnants and surface treatments.
So far: large spread in training curves with pure epoxy resin impregnants and surface treatments, but also reduced training for particle filled epoxy resin and paraffine….
Trying to understand at strand level, interfaces with resin.
470 mm
Notes: The training is magnet architecture specific, in this case I show an example for CCT magnets

## Slide 4: How did we measure this relation?
The release of mechanical energy is governed by the (critical) strain energy release rate
→ Which fraction of is dissipated and transferred into thermal energy?
How to measure this in a condition relevant for Nb3Sn magnets?
We modified the so-called Compact Tension Double Cantilever Beam experiment (CT-DCB) based on ISO standard.
Included a representative dummy Nb3Sn wire in the interface to see debonding at its surface…..
: 40 mm
: 20 mm
: 20 mm
Notes: The training is magnet architecture specific, in this case I show an example for CCT magnets

## Slide 5: Preparations for the experiment
A working Nb3Sn strand is represented as:
a 0.85 mm Ø copper tube
insulated with S-2 fiberglass
chemically treated with cabling lubricant
heat treated at 665 °C in Ar atmosphere
positioned parallel to the crack propagation in its plane
the tube allows a temperature sensor close to the fracture.
Notes: The training is magnet architecture specific, in this case I show an example for CCT magnets

## Slide 6: Making the sample…..
CTD-101K:
DGEBA* based
Common magnet impregnant
* diglycidyl ether of bisphenol A
Notes: The training is magnet architecture specific, in this case I show an example for CCT magnets

## Slide 7: Setup of the experiment
Custom made cryogenic tensile stress-strain setup
Slowly submerged in liquid nitrogen at 77 K
Specimen loaded in mode I (⊥ to the crack plane)
Low loading rate of 1 µm/s
Measurands:
  Mechanical energy release
      Force load → S-type load cell
      Displacement → Cantilever extensometers
  Thermal heat load
      Temperature → type E thermocouple
  Setup compliance measured at cold with unnotched sample (solid block of CTD-101K)

## Slide 8: Examination of the sample after the test
Microscope image of the fracture surface after the test
Multiple crack arrest lines
Top view

## Slide 9: Measured load vs displacement at successive force ramps
Unstable crack propagation observed
Also with crack arrest
Several load cycles performed, each one shows decreasing slope
Only ramps 1, 3 and 4 show significant energy release and show a thermal response.
Error ± 1 α

## Slide 10: Determining the strain energy release
For determining the strain energy release rate, the crack length needs to be measured:
  Initial length measured on the fracture surfaces after test
  Crack length during each ramp based on slope and calculated using the compliance method:
  Calibration functions 𝑓𝜑 for CT-DCB specimens listed in the ISO standard [2].
Measured initial crack length at five locations using a microscope image of the fractured surfaces and digital image analysis software.
: crack length relative to
: slope
: Young’s modulus

## Slide 11: Measured strain energy release rate
Strain energy release rate is obtained for each ramp according to ISO 13586 standard [2] with:
Calibration factor 𝜑 for CT-DCB specimens.
Error ± 1 α
Slope and relative crack length are averages between subsequent ramps.
Load [N]
Displacement [μm]
For two specimens & all ramps, we found:
G = 230 ± 30 J/m²
Values comparable to Evans et al. [3], which measured for a DGEBA-based epoxy at 77 K.

## Slide 12: Measured temperature response due to cracking
Temperature rise in 10 to 50 mK range
Temperature rise is initially steep
Sharper for ramp 3, where the crack tip was located closer to the thermocouple in the tube
The Cu tube has a uniform temperature after 0.5 s followed by an exponential decay during cooldown.
Error ± 1α

## Slide 13: Results for the thermal energy release
Total surface thermal heat load deposited during each fracture event in J/m²:
First ramp close to half the measured strain energy release rate (230 J/m²) (two surfaces!)
Deviates for later ramps, likely due to a non-uniform crack front.
Specimen | Ramp | [mK] | [J/m²]
1 | 1 | 24 ± 5 | 90 ± 30
 | 3 | 22 ± 4 | 260 ± 80
 | 4 | 15 ± 4 | 600 ± 220
2 | 1 | 24 ± 4 | 100 ± 30
 | 3 | 24 ± 5 | 220 ± 80
Specimen | Ramp |  | 
1 | 1 | 24 ± 5 | 90 ± 30
 | 3 | 22 ± 4 | 260 ± 80
 | 4 | 15 ± 4 | 600 ± 220
2 | 1 | 24 ± 4 | 100 ± 30
 | 3 | 24 ± 5 | 220 ± 80
Temperature [K]
Time [s]
: volumetric heat capacity of copper at 77 K
: total tube volume
: average of tube diameter and half its perimeter (actual deposited area likely in between)
Evidence of 100% conversion

## Slide 14: Implications for the stability of impregnated superconducting coils
The previous results imply that:
the strain energy release rate at 4.2 K = thermal heat load on the fractured surfaces near the superconductor
Sufficient heat load to destabilize?
Case study: Nb3Sn cable with 21 strands and 25 kA current in a background magnetic field of 7.5 T [1]
Evans et al. [3]: for a DGEBA*-based epoxy at 4.2 K is 61 ± 6 J/m²
Length of most critical strand vulnerable to heat load
* diglycidyl ether of bisphenol A

## Slide 15: Stability model, method and results (simple model for illustration)
A of 61 ± 6 J/m² leads to a hot spot temperature in Nb3Sn wire of 11 K.
Nb3Sn will share current and heat is generated.
The length of strand that can recover through thermal conduction, i.e. , is some 2 mm 6 mm (what could be exposed)
Derivation based on Wilson (1983) [4]
: averaged in field volumetric specific heat and thermal conductivity of Nb3Sn wire at = 4.2 K
: strand cross section
: current density shared with copper within the wire
: in field resistivity of copper within the wire at = 4.2 K
More than sufficient to destabilize the Nb3Sn cable !

## Slide 16: Conclusion
Successfully a custom made test rig was made for determining strain energy release rate G (adjusted ISO standard, now including a dummy Nb3Sn/Cu wire at the crack interface).
Heat generated during fracture of epoxy magnet impregnant, can be measured at 77 K.
It seems to match half the strain energy release rate :
can be integrally modelled as a heat load on the fractured surfaces.
For an impregnated Nb3Sn cable in usual operational condition, such a heat load is more than sufficient to destabilize:
⇒ at 4.2 K of impregnants to be considered for stability.

## Slide 17: References
[1] Daly, M. et al. (2021). BOX: An efficient benchmark facility for the study and mitigation of interface-induced training in accelerator type high-field superconducting magnets. Superconductor Science and Technology, 34(11). https://doi.org/10.1088/1361-6668/ac2002
[2] S.N. (2018). Plastics — Determination of fracture toughness (GIC and KIC) — Linear elastic fracture mechanics (LEFM) approach. ISO 13586. Second edition.
[3] D. Evans and Z. Zhang. (2000). The Work of Fracture of Epoxide Resins at Temperatures to 4K. Advances in Cryogenic Engineering Materials, Springer, Boston, MA.
[4] M. N. Wilson. (1983). Superconducting Magnets. Oxford University Press.