## Slide 1: AC Loss in Round Superconductor wires and Flat Helical Wrap Conductors in a range of frequencies
Mike Sumption, M. Majoros, E.W. Collings
Center for Superconducting and Magnetic Materials, MSE, The Ohio State University
T. Haugan, AFRL
3Or-3B02
This work was supported by NASA (Cheeta), Raytheon, and the Air Force Summer Faculty Program

## Slide 2: What are the components of loss of a ROUND SC
Coupling loss
Hysteretic Loss
Total loss
Eddy Current loss
Transport Current loss
Because of large Lp/d ratio, and also f2 like dependence, coupling loss dominates at high frequency
But this is just at LOW FREQUENCIES
What if we wanted to know loss at high f, for example for harmonics analysis?
What is the effect of skin depth?
Let’s keep to round ones for now (YBCO later!)

## Slide 3: Skin Depth Effect in Ordinary Conductors
The skin depth begins to appear when  = 2X, where X is the wire depth. The critical frequency is
But, at high frequency, the currents are constrained to a surface region, depth (smaller area, higher R)
Here d is the wire diameter
Here losses are normalized to total conductor,
w = d, and the losses go as f1/2
Room T
At low frequencies we have the standard eddy current expression

## Slide 4: Superconducting Composites have several critical frequencies
There are three critical frequencies, fc1, fc2, and fc3
fc3 corresponds to the fc of metal wires, when the skin depth is less that the thickness of the outer sheath, here X. Here the loss is the same as that of a metal wire
At frequencies below fc3, but above an fc2, the skin depth is greater than X, but less than the wire radius
Between fc2 and fc1, some screening still modifies the loss, until below fc1, the “low freq loss expressions” apply
Partial screening

## Slide 5
If f > fc3, we have results same as metallic conductor
z
x
y

B only penetrates into outer Stabilizer shell
B does not penetrate into filamentary array
 < tos
Outer Stabilizer
Filamentary array
B, dB/dt
Eddy current flowing within skin depth of outer stabilizer only
X = tos
Self-field B sizeable compared to external B

## Slide 6
If fc2 < f < fc3, in some ways similar*, except B penetrates partially into array,  = m
z
x
y

B penetrates partially into filamentary array as well as Stabilizer shell
Currents flow in eddy current pattern, treat filamentary array as region of very low resistivity only
tos <  < Ro
Outer Stabilizer
Filamentary array
B, dB/dt
Eddy current flowing within outer stabilizer AND in filamentary region
X = tos
Self-field B sizeable compared to external B
* Does interact with hysteretic contributions, with added complications

## Slide 7: But what about between fc1 and fc2?
Quasistatic ramp, no eddy currents, filament hysteresis only
Low/modest ramp rate, eddy currents, adds weak background slope and gradient across whole composite
Very fast ramp, complete coupling, loss is “hysteretic-like” one fat filament
Let’s reminder ourselves what fc1 is
For one thing, its where Qcoup peaks…
It’s also the place where filaments re-couple
But, we really need to look in much greater detail here

## Slide 8: Coupling currents, shielding, and saturated regions I
An applied dB/dt creates coupling currents which flow “up one side of strand and down the other”
But twist drives currents to centerline at front (or back) of conductor
Charge accumulation drives currents to back (front) of conductor, completing circuit and creating an opposing B
Currents in filaments are superconducting
Filaments crossing matrix create coupling loss

## Slide 9: Coupling currents, shielding, and saturated regions II
Currents in the filaments tends to flow at the critical current in in thin shell region
This region is called the saturated region
The currents completing the path through the matrix flow in the inner region
The thickness of this saturated region at the conductor edges is
Here x is limited to x < Ba/(Jc)
(see left)
Once the total coupling current exceeds a critical value (Jc times the area of the first filamentary layer in from the periphery) this layer of filaments will be “saturated” with current.

## Slide 10: Coupling currents, and saturated regions III
If we take x to be df, then we can define a critical ramp rate
If we take x to be ds, then we can define a saturation critical ramp rate
Remembering our definition of fc1
And since B(t) = Basin(t), dB/dt = 2fBa
Then
and
But the Bp of a layer of filaments df thick is dfJc/2
Which leads to
A similar treatment of leads to
Thus, fc1 is the frequency at which the maximum filamentary saturation happens for a given Ba
(or)
fc1 is where all the filaments that can re-couple do so
(although, for large Ba, we can saturate before fc1)

## Slide 11: Coupling currents, and saturated regions IV
Q* = Q/Ba2
f/fc
2Bpf
Bps
2nBpf
Ba = 2Bps
fc1
Note filament recouple at fc1/2 for Ba=2Bps

## Slide 12: Additional screening above fc1
Q* = Q/Ba2
f/fc
We might ask, why can we have reduced loss at high frequency? Note that the equation below is coupling loss only
However, the graph at right includes both coupling and Saturated region loss
Our Bean-like profiles are 2-D, and our filament layers are porous to flux
This flux is further shielded as we increase f above fc1
Since coupling currents are driven by dB/dt, this shielding reduces loss
Low loss, low M
High loss, high M
Low loss, high M
Zero loss, max M
How can increased M lead to lower loss?

## Slide 13: Coupling & Eddy loss ignoring saturated filament regions
From f = 0 to fc2
For f < fc3
For fc2 < f < fc3
For f > fc3
Coupling Currents
Normalized to strand volume…
Shell eddy currents*
* The shell also contributes to coupling, accounted for by an effective matrix  (conductance contribution)

## Slide 14: AC loss calculations at high frequency including filamentary saturation effects
Loss in Saturation layer
The Eddy or coupling loss
Filament hysteretic loss, here set to zero
Fraction of strand saturated
Fraction of strand unsaturated
Using the appropriate expression for Coupling loss (Here Pe)
(or)
Below fc2
Above fc2
Ba > Bpf
Ba < Bpf

## Slide 15: Loss of Selected MgB2 strand over wide frequency range with various Ba (I)
Property | Conductor 1
 | MgB2, Cu matrix, Cu shell
m,eff, m | 1.54E-10
Lp, cm | 1
X, mm | 0.1
 | 0.15
R0, mm | 0.5
s, m | 1.54E-10
df, m | 50
Jc, A/m2 | 4.6E+9
B0, T | 0.5
Bp, T | 0.092
fc1, Hz | 15.4
fc2, Hz | 78.1
fcs, Hz | 1,952
, T/s | 34.2
, T/s | 173
, T/s | 4,335
, T/s (Hz) | 2.0 (0.9)
, T/s (Hz) | 20.0 (9.0)
Property | Conductor 1
 | MgB2, Cu matrix, Cu shell
m,eff, m | 1.54E-10
Lp, cm | 1
X, mm | 0.1
 | 0.15
R0, mm | 0.5
s, m | 1.54E-10
df, m | 50
Jc, A/m2 | 4.6E+9
B0, T | 0.5
Bp, T | 0.092
fc1, Hz | 15.4
fc2, Hz | 78.1
fcs, Hz | 1,952
 | 34.2
 | 173
 | 4,335
 | 2.0 (0.9)
 | 20.0 (9.0)
(1 – Below fc1, below dB/dtc)
(2 - Below dB/dtcs)
(3 - Above dB/dtcs)
(4 - Above dB/dtcs)
(5 - Above fc3)
Here individual filament hysteresis = 0

## Slide 16: Loss of Selected MgB2 strand over wide frequency range with various Ba (II)
Possible errors in loss
Here individual filament hysteresis = 0

## Slide 17: Loss of Selected MgB2 strand over wide frequency range with various Ba (II)
Property | Conductor 1
 | MgB2, Cu matrix, Cu shell
m,eff, m | 1.54E-10
Lp, cm | 1
X, mm | 0.1
 | 0.15
R0, mm | 0.5
s, m | 1.54E-10
df, m | 50
Jc, A/m2 | 4.6E+9
B0, T | 0.5
Bp, T | 0.092
fc1, Hz | 15.4
fc2, Hz | 78.1
fcs, Hz | 1,952
, T/s | 34.2
, T/s | 173
, T/s | 4,335
, T/s (Hz) | 2.0 (0.9)
, T/s (Hz) | 20.0 (9.0)
Property | Conductor 1
 | MgB2, Cu matrix, Cu shell
m,eff, m | 1.54E-10
Lp, cm | 1
X, mm | 0.1
 | 0.15
R0, mm | 0.5
s, m | 1.54E-10
df, m | 50
Jc, A/m2 | 4.6E+9
B0, T | 0.5
Bp, T | 0.092
fc1, Hz | 15.4
fc2, Hz | 78.1
fcs, Hz | 1,952
 | 34.2
 | 173
 | 4,335
 | 2.0 (0.9)
 | 20.0 (9.0)
Here individual filament hysteresis = 0

## Slide 18: Including the effects of Flux Creep (or Power Law)
But, in using this formulation, we have merely applied the LTSC formulation to HTS without thinking about thermal activation – but we should!
Hysteretic
Eddy and coupling
LTSC Cables
Pt  Ph+Pc
To a first approx
Ph
Pc
t = t2
t = t1
t = t0
In reality, with time, flux creep drives us away from the critical state, if f < fc
However, at high frequencies (above fc) creep effects can be seen as adding to loss. Essentially we are probing losses for Jc values higher than those we “measured” at some fixed electric field criterion

## Slide 19: Including the effects of Flux Creep (or Power Law)
thus and then
If we account for the fact that the SC transition has an n-value
here JPL is the current density that flows under an electric field E
We note that n  U0/kbT
(Since E = xdB/dt)
If we use an average dB/dt defined as dB/dt = 2Bmf, then
This is a simple and approximate approach, but agrees with the result from Thakur in the limit of Bm >> Bp

## Slide 20: Including the effects of Flux Creep (or Power Law) II
At f = fc JPL (PLM)Jc (CSM)
f/fc < 1 (f/f0)1/2-1 < 1
f/fc > 1 (f/f0)1/2-1 > 1
Middle term negative
Middle term positive
CSM, hysteretic + eddy current
PLM, hysteretic-creep + eddy current
If we take a Bmax field of, say 0.5 T, assuming we use an Ic defined by Ec = 1 V/cm, and for a 0.1 mm wide filament, fc = (Ec)/wBmax = 10-4 V/m/(*0.0001 m*0.5 T)  0.6 Hz

## Slide 21: Alternatively, Losses in coated conductor TAPES below the skin depth, ignoring flux creep
Hysteretic Loss
Eddy Current loss
But for Bmax > Bp, N 1
Transport Current Loss
Ignoring transport current and for Bm > Bp
But, flux creep influences on loss can be important
F. Grilli, E. Pardo, A. Stenvall, D. N. Nguyen, W. Yuan, and F. Gömöry, IEEE Trans. Appl. Supercond. 24 (2014) 8200433.
M. Kapolka, V. M. R. Zermeno, S. Zou, A. Morandi, P. L. Ribani, Member, E. Pardo, and F. Grilli, IEEE Trans. Appl. Supercond. 28 (2018) 8201206
L. Pust, Supercond. Sci. Technol. 3 (1990) 598-601.
K. P. Thakur, A. Raj, E. H. Brandt, and P. Sastry, Supercond. Sci. Technol. 24 (2011) 045006, doi:10.1088/0953-2048/24/4/045006.
E.H. Brandt, Phys. Rev B 55 (1997) 14514.

## Slide 22: Losses for coated conductor TAPES with helical wrap (e.g. CORC) WITH flux creep
/2
(/2)2
B
B
Hysteretic loss correction
Eddy loss correction goes as square, since Qe  (dB/dt)2

## Slide 23: Coupling currents in typical multifilamentary strands
matrix
filament
filament
B, dB/dt
Slow ramping, hysteresis only
matrix
filament
filament
B, dB/dt
fast ramping, Hyst+coupling
The critical ramp rate needed to fully re-couple

## Slide 24: Coupling currents in conductors with tapes
matrix
filament
filament
B, dB/dt
Slow ramping, hysteresis only
The critical ramp rate needed to fully re-couple
matrix
filament
B, dB/dt
Slow ramping, hysteresis only
filament
This is a very fast ramp!
i.e., coupling of coated conductor structures requires a very fast ramp, because the currents to be coupled are large!!

## Slide 25: Summary
We showed loss expressions for superconductors below the skin depth regimes
We then showed the loss expressions for superconductor in high frequencies in various skin depth regimes
Some particular cases were explored, over a wide range of f
We gave the corrections due to power law (flux creep) effects
We discussed (shortly) coated conductor loss and creep modifications
Ramp rates needed to fully couple coated conductor tapes in cable configurations quite large, because currents to be coupled large