## Slide 1
T. Prikhna1,2,4, A. Kethamkuzhi2, R. Vlad2, M. Karpets1,3, R. Kluge4, S. Ponomarov5,, V. Moshchil1, X. Obradors2,, B. Büchner4 , J. Gutierrez2 , Sabine Wurmehl4,, and T. Puig2
1 V. Bakul Institute for Superhard Materials of the National Academy of Sciences of Ukraine,
2, Avtozavodska Str., Kyiv 07074, Ukraine
2 Institut de Ciencia de Materials de Barcelona, CSIC, Campus UAB, 08193 Bellaterra, Spain
3 National Technical University of Ukraine «Igor Sikorsky Kyiv Polytechnic Institute”,
Peremogy Avenue 37, 03056 Kyiv, Ukraine
4 Leibniz-Institut für Festkörper- und Werkstoffforschung Dresden e. V.,
Helmholtzstrasse 20 01069 Dresden, Germany.
5 V.E. Lashkaryov Institute of Semiconductor Physics of the National Academy of Sciences of Ukraine,
41, Nauky Ave., Kyiv 03028, Ukraine
We acknowledge funds from MICIU/AEI/FEDER for SUPERENERTECH (PID2021–127297OB-C21), FUNFUTURE “Severo Ochoa” (CEX2019–000917-S); MUGSUP (UCRAN20088) project from CSIC scientific cooperation with Ukraine; Catalan Government 2021 SGR 00440; NAS of Ukraine Project III-7-24 (0788)
M2Or4B-03, 20.05.2025, 17.00-17.15 (Naples 4/5)
Growth & Characterization of REBCO and Iron-based Superconductors
Charge carrier density and critical current density variations of superconducting layers of GdBCO and EuBCO coated conductors as a result of high pressure oxygenation

## Slide 2
Content
Motivation
Experimental ( 1-160 bar oxygen pressure, 300-800 oC temperature, 3, 6 or 12 h holding time)
Characteristics before and after treatment (Tc, Jc, carrier density, nH, c-lattice parameter of RE123 (RE=Gd, Eu)
Study of the materials structures (SEM EDS and Auger spectroscopy).
Conclusions
M2Or4B-03, 20.05.2025, 17.00 (Naples 4/5)
Growth & Characterization of REBCO and Iron-based Superconductors

## Slide 3
Ic
Tirr
Hirr
Overdoped
Nancomposite
REBCO
Jc of REBCO films is expected to increase in the overdoped state
It should be a robust and homogeneous process to increase Jc in Coated Conductors.
popt
Optimal Doping (~p = 0.16): maximum Tc (~93 K)
Overdoped Regime (p > 0.16): Tc decreases despite increasing hole concentration
Underdoped Regime (p < 0.16): Tc also decreases; pseudogap opens
What is overdoping?
- Increase of nH(100 K);
- Reduction of c-lattice
parameters of RE123
(RE=Y, Eu, Gd)
p- hole doping per CuO2 planes of RE123
(the structure of the CuO chains remains unaffected)

## Slide 4
1. Motivation
The overdoping for YBa2Cu3O7-δ (Y123) thin films (as a result of treatment via Ag layer when heated under oxygen partial pressure below 1 bar at low temperatures) was confirmed by a sudden increase of charge carrier density, nH, associated to the reconstruction of the Fermi-surface at the Quantum Critical Point (QCP). The authors (Stangl, A., Palau, A., Deutscher, G., Obradors, X., 2021, . Sci Rep., 11, 8176.) achieved the highest ever reported in YBCO films critical current density Jc, equal to 90 MA·cm−2 at 5 K which corresponds to about a fifths of the depairing current.
The Miura, M. et al. ( 2022, NPG Asia Materials , 14, 85) demonstrated that thermodynamic improvements of superconductors can work in parallel with already successful artificial pinning centers and that a maximum critical current density Jc ~ 0.3 Jd (despairing current ) appears to be the current upper limit for the enhancement in Jc. They concluded that variation in λ and ξ leads to an intrinsic improvement in Jc via Jd, allowing extremely high values of Jc of 130 MA/cm2 at 4.2 K, consistent with an enhancement in Jd of a factor of 2 for nanoparticle-doped (Y,Gd)123 coated conductors (CCs). The combination of thermodynamic and pinning optimization route for the (Y,Gd)123 CCs resulted in high vortex-pinning force ~3.17 TN/m3 at 4.2 K and 18 T (H||c) .
The idea to apply such high oxygen pressure (100-160 bar) and annealing temperature (600-800 oC) was caused by our experience with melt-texturing YBCO for which such conditions allowed essentially decrease the time, , of oxygenation, increase JC (especially in high magnetic fields) due to increase of twin density, reduce anisotropy of JC, decrease mico- and macrocracking (and thus improve mechanical properties). [3-5]

## Slide 5
Experimental
FYSC : Ag (2μm)/ GdBCO (1.8μm)// CeO2 (700 nm)/ MgO/Y2O3/Al2O3/ Hastelloy (75 μm);
FESC : EuBCO (2.5μm)+BaHfO3 nanorods (BHO)/ CeO2 (700 nm)/ /MgO/Y2O3//Al2O3/ Hastelloy (50 μm);
FESC : Ag (2μm)/ EuBCO (2.5μm)+BaHfO3 nanorods / CeO2 (700 nm)//MgO/Y2O3/Al2O3/ Hastelloy 50 μm).
Architecture of the studied types of commercial Fujikura coated conductors,
model numbers FYSC-S12 and FESC-SCH12:
The transition temperature, TC, and critical current density, Jc, were estimated by SQUID magnetometer.
Tc was estimated as well using transport measurements.
Charge carrier density, nH, were found from the Hall effect at 100 K by Quatum Design PPMS (before the nH study Ag layer was removed by etching from CC re-oxygenated via Ag layer)
Commercial tape (Fujikura)
Cu layer etched in HCl: H2O2=1:1
Cu layer etched in HCl: H2O2=1:1
Ag layer etched in NH3: H2O2:MeOH 1:1:5
Type 1
Type 2
Cu
Ag
REBCO
REBCO
REBCO
Ag

## Slide 6
Mode 1
Mode 2
Mode1
O2 pressure decreased
when cooling
Mode 2
O2 pressure was kept constant up to cooling down to room temperature
Oxygenations conditions
1-160 bar O2
TS=300-800 oC
Ramp =
5 ºC/min
= 3,, 6 or
12 h
Leibniz-Institut für Festkörper- und Werkstoffforschung Dresden e. V.,
Helmholtzstrasse 20 01069 Dresden, Germany.
Experimental
PO2
T
PO2
T
Mode 1
Mode 2

## Slide 7
JAMP−9500F, JEOL, Japan – Scanning Auger Microscopy which is combination of HRSEM (secondary electron mode, resolution 3 nm) and Local Auger-electron Spectroscopy (resolution 5 - 8 nm)
Study of materials structures
The c-lattice parameters of RE123 superconducting phases (RE=Gd, Eu) of GdBCO_CC and EuBCO_CC were estimated from X-ray diffraction patterns obtained using Ultima IV (Japan, Rigaku) in CuKα radiation λ = 1.54184 Å, in 2θ = 8–88° range, with scanning step 0.05°, and the acquisition time at one point 2–4 s. The obtained diffractograms were refined by the Rietveld method.
The materials microstructures were examined by SEM EDS and Auger spectroscopy using JAMP−9500F, JEOL, Japan.
10 Å- Auer electrons

## Slide 8
Characterization
No | p(O2), bar |  |  |  | Ts, oC | , h |  | Mode 1 or 2 |  |  |  | Jc (0 T, 77K), MA/cm2 | c-parameter, nm |  |  | nH(100 K), 1021 cm-3 |  |  |  |  | Tc, K |  |  | 
(1) Ag (2μm)/ GdBCO (1.8μm)/ CeO2 (700 nm)/ MgO/Y2O3/Al2O3/Hastelloy (75 μm) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
1 | Starting |  |  |  |  |  |  |  |  |  | 2.57 |  |  | 1.17351 |  |  |  |  | 6.55 | 92.75 |  |  |  | 
2 | 10 |  |  | 300 |  |  | 3 |  | 1 |  | 2.23 |  |  | 1.17318 |  |  |  |  | 5.09 | 92.71 |  |  |  | 
3 | 5 |  |  | 300 |  |  | 3 |  | 1 |  | 2.49 |  |  | 1.17343 |  |  |  |  | 6.18 | 92.60 |  |  |  | 
4 | 100 |  |  | 600 |  |  | 3 |  | 1 |  | 2.67 |  |  | 1.17310 |  |  |  |  | 6.91 | 92.77 |  |  |  | 
5 | 160 |  |  | 800 |  |  | 3 |  | 1 |  | 2.49 |  |  | 1.1,7300 |  |  |  |  | - | 92.74 |  |  |  | 
6 | 2 |  |  | 300 |  |  | 3 |  | 1 |  | 2.47 |  |  | 1.17289 |  |  |  |  | 6.22 | 93.26 |  |  |  | 
7 | 1 |  |  | 300 |  |  | 3 |  | 1 |  | 2.19 |  |  | 1.17320 |  |  |  |  | 5.27 | 92.76 |  |  |  | 
8 | 100 |  |  | 600 |  |  | 6 |  | 1 |  | 2.36 |  |  | - |  |  |  |  | 7.05 | - |  |  |  | 
9 | 100 |  |  | 600 |  |  | 12 |  | 1 |  | 2.65 |  |  | - |  |  |  |  | 8.21 | - |  |  |  | 
(2) EuBCO (2.5μm)+BHO Nanorods/ CeO2 (700 nm)/MgO/Y2O3/Al2O3)/ Hastelloy (50 μm) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
10 | Starting |  |  |  |  |  |  |  |  | 1.38-1.21 |  |  |  |  | 1.17419 |  | 6.05 |  |  |  |  | 92.35 |  | 
11 | 10 |  |  | 300 |  |  | 3 |  | 1 | 0.87 |  |  |  |  | 1.174631 |  | 3.77 |  |  |  |  | 91.65 |  | 
12 | 5 |  |  | 300 |  |  | 3 |  | 1 | 0.99 |  |  |  |  | 1.17384 |  | 3.85 |  |  |  |  | - |  | 
13 | 100 |  |  | 600 |  |  | 3 |  | 1 | 0.77 |  |  |  |  | 1.17425 |  | 4.02 |  |  |  |  | - |  | 
14 | 160 |  |  | 800 |  |  | 3 |  | 1 | 1.31 |  |  |  |  | 1.17341 |  | - |  |  |  |  | - |  | 
15 | 2 |  |  | 300 |  |  | 3 |  | 1 | 1.09 |  |  |  |  | 1.17341 |  | 4.43 |  |  |  |  | - |  | 
16 | 1 |  |  | 300 |  |  | 3 |  | 1 | 1.09 |  |  |  |  | 1.17341 |  | 4.33 |  |  |  |  | 91.65 |  | 
17 | 100 |  |  | 600 |  |  | 3 |  | 1 | 0.97 |  |  |  |  | 1.17433 |  | 4.92 |  |  |  |  | 92.22 |  | 
(3) Ag (2μm)/ EuBCO (2.5μm)+BHO Nanorods/ CeO2 (700 nm)/MgO/Y2O3/Al2O3)/ Hastelloy (50 μm) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
18 |  | 160 | 600 |  |  |  | 3 |  | 2 |  | 1.32 |  |  |  | 1.17488 |  |  | 6.25 |  |  | 93.04 |  |  | 
19 |  | 160 | 800 |  |  |  | 3 |  | 2 |  | 0.69 |  |  |  | 1.17471 |  |  | 6.69 |  |  | 92.09 |  |  | 

## Slide 9
Gd_CC03
Gd_CC01
Gd_CC00
No 1 Starting GdBCO
No 1 Starting GdBCO
No 2 GdBCO
10 bar 300 oC
No 2 GdBCO
10 bar 300 oC
No 4 GdBCO
100 bar 600 oC
No 4 GdBCO
100 bar 600 oC

## Slide 10
Comparison of normalized resistivity of GdBCO_CC
O2 pressure decreased
as furnace
cooled
O2 pressure was kept constant up to cooling down to room temperature
Mode 1
Signatures of overdoping are observed
Mode 2

## Slide 11
No | Regime PO2/TS//mode |  | c, nm of RE123 | Jc (0 T), MA/cm2 |  | Tc, K | nH 1021, cm-3
 |  |  |  | 77 K | 5 K | SQUID DС | (at 100 K)
Ag (2μm)/GdBCO (1.8μm)/CeO2 (700 nm)/ MgO/Y2O3/Al2O3/Hastelloy (75 μm) |  |  |  |  |  |  | 
1 | Initial I (Gd123+Ag) | 1.17351 |  | 2.57 | - | 92.75 92.58 | 6.55
2 | 100 bar/250 oC/3 h/2 | 1.1.7213 |  | 2.20 | 26.63 | 93.02 91.15 | -
3 | 160 bar/250 oC/3 h/2 | 1.17284 |  | 1.92 | 23.37 | 92.79 91.15 | 5.37
4 | 1 bar/300 oC/3 h/1 | 1.17320 |  | 2.19 | - | 92.76 92.18 | 5.27
5 | 2 bar/300 oC/3 h/1 | 1.7289 |  | 2.47 | - | 93.26 91.63 | 6.22
6 | 5 bar/ 300 oC/3 h/1 | 1.17343 |  | 2.49 | - | 92.60 92.17 | 6.18
7 | 10 bar,/300 oC/3 h/1 | 1.17318 |  | 2.23 | - | 92.71 92.25 | 5.09
8 | 100 bar/300 oC/3 h/2 | 1.17374 |  | 2.12 | 26.12 | 92.55 92.23 | 5.34
9 | 160 bar/450 oC/3 h/2 | 1.17334 |  | 2.02 | 24.56 | 93.06 92.23 | 5.49
10 | 100 bar/600 oC/3 h/1 | 1.17310 |  | 2.67 | - | 92.77 92.23 | 6.91
11 | 100 bar/600 oC/3 h/ 2 | 1.17141 |  | 2.22 | 25.16 | __-__ - | -
12 | 100 bar/600 oC/ 12 h/1 | 1.17310 |  | 2.65 | - | __-_ 92.22 | 8.21
13 | 160 bar/600 oC/3 h/2 | 1.17312 |  | 1.98 | 23.67 | 92.65 92.22 | 6.84
14 | 160 bar/800 oC/3 h/1 | 1,17300 |  | 2.49 | - | 92.74 92.17 | -
15 | 160 bar/800 oC/3 h/2 | 1.17246 |  | 2.62 | 28.94 | 92.76 92.75 | 6.27
Regime of Oxygenation (p, Ts, , , Oxygenation Mode): and Results of Study of Jc(0 T) at 77 K and 5 K, Tc, nH(100 K), c- parameter of Gd 123

## Slide 12
Figure (a, f) – Images in SEI (secondary electrons) mode of GdBCO_CC and EuBCO+BHO_CC (materials without Cu and Ag layers, which were removed by etching in acids), respectively, and Auger maps of elements distributionover these images: (b-e) – Eu, Ba, Cu, O; (g-j) – Gd, Ba, Cu, O.
GdBCO_CC starting ( Ag layer etched)
EuBCO+BHO_CC – starting (Ag layer etched)
Gd
Figure (a) – SEM of EuBCO+BHO_CC after re-oxygenation at 800 C, under 160 bar oxygen pressure for 3 h, and (b-e) - Auger maps of elements Eu, Ba, Cu, O distribution over this image. Before repeated oxygenation the Cu and Ag layers was removed by etching in acids after re-oxygenation.
EuBCO+BHO_CC after re- oxygenation at 800 C, 160 bar , 3 h)

## Slide 13
Figure. Dependences of critical current density Jc at 77 K in 0 T field vs. c-lattice parameter (on the left y-axis) and carrier densities nH (on the right y-axis) at 100 K in comparison between initial samples and the treaded ones for GdBCO_CC (with Ag protected layer) oxygenated at 300 ºC, under 1-100 bar O2 (a) and at 600 ºC under 100 bar O2 (b), for EuBCO_CC (without Ag) treated at 300 ºC under 1-10 bar O2 (c). Jc vs. O2 pressure for EuBCO_CC (without Ag) treated at 300-800 ºC (d).
a)
b)
c)
d)
Transition temperature, Tc (K), charge carrier density at 100 K, nH /1021 (cm-3) (values next to the data points), and estimated doping, p, for GdBCO_CC (with Ag layer) after treatment using Mode 2
(100 and 160 bar O2).

## Slide 14
No | p(O2), bar | Ts, oC | , h | Rate of Ts, and p(O2) decrease (Mode 1 or 2) | Jc (0 T), MA/cm2 |  |  | c-para-meter, nm | nH (100 K), 1021 cm-3 | Tc, K |  | 
 |  |  |  |  | Before at 77 K | After at 77K | After at 5K |  |  |  |  | 
Ag (2μm)/ GdBCO (1.8μm)/CeO2 (700 nm)/MgO/Y2O3/Al2O3 /Hastelloy (75 μm) |  |  |  |  |  |  |  |  |  |  |  | 
A | Reference GdBCO_CC sample for c, Tc and nH |  |  |  | 2.57 1.95 | - | - 23.69 | 1.1735(1) - | 6.55 6.93 | 92.58 91.45 |  | 
1 | 100 | 600 | 3 | with furnace (1) | 2.04 | 2.22 | 24.79 | 1.1715(5) | 6.5 | 92.72 |  | 
2 | 100 | 600 | 6 | with furnace (2) | 2.14 | 2.49 | 24.98 | 1.1718(8) | 7.86 | 92.79 |  | 
3 | 100 | 600 | 12 | with furnace (1) | 2.10 | 2.42 | satu-rated | 1.1720(6) | 7.73 | 93.25 |  | 
4 | 160 | 800 | 3 | with furnace (1) | 2.12 | 2.70 | satu-rated | 1.1,727(1) | 7.3 | 92.63 |  | 
5 | 160 | 800 | 6 | with furnace (1) | 1.87 | 2.29 | 23.14 | 1.1725(3) | 6.74 | 92.35 |  | 
6 | 160 | 800 | 12 | with furnace (1) | 1.79 | 1.11 | 22.73 | 1.1724(8) | 3.25 | 92.63 |  | 
Regimes of oxygenation (oxygen pressure, p, maximal heating temperature, Ts, holding time at maximal temperature, ) and Jc in 0 T before (at 77 K) and after (at 77 and 5 K) re-oxygenation; transport Tc, nH(100 K), and c-parameter after re-oxygenation

## Slide 15
GdBCO_CC with Ag: critical current density JC at 77 K in 0 T field vs. dwell time before and after re-oxygenation under 100 bar at 600 oC (a) and under 160 bar at 800 oC (b) depending on on dwell time
(a) (b)
(a) (b)
c-lattice parameters of GdBa2Cu3O7- after re-oxygenation vs. charge carrier density nH estimated at 100 K.; (b) - Transition temperature, Tc (K), charge carrier density at 100 K, nH /1021 (cm-3) (values next to the data points), and estimated doping, p, for GdBCO_CC after re-oxygenation under 100 bar at 600 oC and under 160 bar O2 at 800 oC). The c-parameter, Tc , nH and p of the reference sample A is as well presented.
After treatment at 160 bar O2 at 800 oC for 3 h JC(77K,0T) of GdBCO_CC was increased for 21.5 % (from 2.12 to 2.70 MA/cm2) while heating for 6 h resulted in JC(77K,0T) increase to less extend - for 18 %, and after 12 h dwell the Gd123 structure partly decomposed and critical current density decreased from 1.79 to 1.11 MA/cm2. Treatment of samples at 600 oC under 100 bar O2 for 3, 6, and 12 h resulted in JC(77K,0T) increase for 8, 14 and 13 %, respectively.
The re-oxygenation under 160 bar at 800 oC for 3 h result in nH = 7.3×1021 cm-3 and p=0.174; c-parameter decreased to 1.1727(1) nm.
The analysis of obtained results allowed us to conclude that optimal doping of CuO planes of Gd123 is around p=0.1740- 0.1745.

## Slide 16
(a) - Normalized resistivity and (b) - resistivity, , and (c) - Tc estimated magnetically vs. temperature of the GdBCO_CC samples after re-oxygenation 1 (a) and 2 (b).
(a) (b) (c)
Behaviour of normalized resistivity before superconducting transition evidenced about overdoping

## Slide 17
Sample No | Conditions |  |  |  |  | Architecture | Jc After |  |  |  |  | 
 | Pressure O2, bar | Rate of heating, oC/min | Temperature, oC | Holding time, h | Mode of oxygenation |  | Jc ( 77K) MA/cm2 After | Jc ( 5K) MA/cm2 After | c axis parameter Measured at ICMAB, calculated by Kyiv | Charge carrier density nH (100K) X 1021 cm-3 | Tc (K) by SQUID | Tc (K) by Transport
Y13284 | 100 | 5 | 600 | 3 | 1 | YBCO/STO | 0.13 | 15.1 |  |  | 89.8 | 
Y13291 | 100 | 5 | 600 | 6 | 2 | YBCO/STO | 3.82 | 35.3 |  |  | 91.6 | 
Y13283 | 160 | 5 | 800 | 3 | 1 | YBCO/STO | 1.19 | 11.7 |  |  | 92.2 | 
Y13282 | 160 | 5 | 800 | 6 | 1 | YBCO/STO | 4.09 | 38.2 |  |  | 91.8 | 
5th batch – YBCO on STO (initial samples are not oxygenated)
YBCO/STO
Best values of Jc (3.8-4 MA/cm2) obtained ever for YBCO/STO using high pressure oxygenations at 100, 160 bar.
On going!

## Slide 18
Conclusions
The evidences of overdoping were observed about what were witnessed an increase of nH(100 K), reduction of c-lattice parameters of RE123 (RE=Eu, Gd) of superconducting layers, behavior of normalized resistivity before superconducting transition, and Jc variation.
2. After treatment at 160 bar O2 at 800 oC for 3 h JC(77K,0T) of GdBCO_CC was increased for 21.5 % from 2.12 to 2.70 MA/cm2, (nH = 7.3×1021 cm-3 , p=0.174; c-parameter decreased to 1.1727(1) nm), while heating for 6 h under same pressure-temperature conditions leaded to JC(77K,0T) increase for 18 % only. After 12 h heating JC(77K,0T) decrease from 1.79 to 1.11 MA/cm2 because of superconducting structure decomposition. Treatment of the samples at 600 oC under 100 bar O2 for 3, 6, and 12 h resulted in increase in JC(77K,0T) for 8, 14 and 13 %, respectively.
4. The c-parameter of Gd123 as a result high pressure – high temperature treatment under 100 bar oxygen pressure can be decrease from 1.1735(1) down to 1.1715(5) nm, but the increase in critical current density was for 8% only. Decrease of c-parameter down to 1.1718(8) nm and attaining nH = 7.86×1021 cm-3 (which was the highest for the last batch of GdBCO_CC) resulted in 14 % increase of JC(77K,0T). Seems optimal doping of CuO planes of Gd123 is around p=0.1740- 0.1745.
5. For EuBCO_СС with HBO nanorods after treatment a decrease in c-parameters of Eu123 was observed: from 1.1738(8) to 1.1734(5) nm (for the Ag-coated sample under 100 bar O2 at 300 °C) and from 1.1740(2) to 1.1736(3) nm (for the sample without Ag under 160 bar O2 at 800 oC), but we failed to increase nH(100 K) and Jc of the studied samples. JC(77K,0T) remained on the same level or slightly decreased.