## Slide 1: Inconel 625 flange development for Cu-based superconducting radio frequency cavities
Shreyas Balachandran1, Oleksandr Hryhorenko2
Adam O’Brien2, Gregory Grose2, Aniket Ingrole3, Jun Lu3, Anne-Marie Valente-Feliciano2
Department of Mechanical Engineering, FAMU- FSU College of Engineering, Tallahassee, FL.
Thomas Jefferson National Lab Facility, Newport News, VA.
Magnet Science and Technology, National High Magnetic Field Lab, Tallahassee, FL.
Acknowledgement: The work was performed under the DOE- ACCELERATE program. Additional support for the National High Magnetic Field Laboratory facilities is from the NSF: NSF-DMR-2128556, and the State of Florida. This work is authored by Jefferson Science Associates, LLC, under U.S. DOE Contract No. DE-AC05-06OR23177.

## Slide 2
Beyond SRF Nb- Alternative materials: Focus on Nb3Sn
4W
at ~4 K
Posen, S., Lee, J., Seidman, D. N., Romanenko, A., Tennis, B., Melnychuk, O. S., & Sergatskov, D. A. (2021). Advances in Nb3Sn superconducting radiofrequency cavities towards first practical accelerator applications. Superconductor Science and Technology, 34(2), 025007.

## Slide 3: Cryocooled Nb3Sn on Nb successfully tested in Jefferson Lab- 1MW, 1MeV compact electron accelerator possible.
10 MeV, 1 MW system in the works!

## Slide 4: Nb3Sn on Cu for SRF applications
Cu melts at ~1100°C.
Cu-based Nb3Sn is a widely studied system.
Cost of RRR 100 Cu ~ 1/20 of RRR 300 Nb
Cu
Nb3Sn
~ 5 times improvement in thermal conductivity at 4K with Cu
Cu
Nb3Sn
Nb
Current
Proposed

## Slide 5: Techniques available to deposit Nb3Sn on Cu
Process | Hold Temperature (°C) | Hold Time (h) | References
CVD | 850-950 | 1-2 | Personal communication with Ultramet.
Magnetron sputtering- Subsequent heat treatments to obtain higher Tc | 850 | 5 | L. Xiao et al., “The Study of Deposition Method of Nb3Sn Film on Cu Substrate,” presented at the 18th Int. Conf. on RF Superconductivity (SRF’17), Lanzhou, China, July 17-21, 2017, JACOW, Geneva, Switzerland, Jan. 2018, pp. 131–133. doi: 10.18429/JACoW-SRF2017-MOPB036.
 | > 750 | 24 | E. A. Ilyina et al., “Development of sputtered Nb3Sn films on copper substrates for superconducting radiofrequency applications,” Supercond. Sci. Technol., vol. 32, no. 3, p. 035002, Jan. 2019, doi: 10.1088/1361-6668/aaf61f.

## Slide 6
Problem: Cu structure after heat treatment

## Slide 7: Materials and Methods
Element | Weight percent
Chromium | 22.0
Molybdenum | 9
Niobium + Tantalum | 1.2
Iron | 1.8
Aluminum | 0.3
Titanium | 0.26
Silicon | 0.16
Manganese | 0.3
Carbon | 0.04
Sulphur + Phosphorus | <0.005
Nickel | Bal.
Cu- C10100, off the shelf- 3.1 mm sheet
Inconel 625- 3.1mm sheet and 1 in. plate
Sample ID | Weld speed (mm/s) | Beam Offset (mm) | Energy per unit length (W/mm)
O1-C | 6.8 | 0.4 | 328
O2-C | 6.8 | 0.6 | 328
O3-C | 6.8 | 0.9 | 328
O4-C | 6.8 | 1.1 | 328
V1-C | 7.6 | 1.0 | 328
V2-C | 6.8 | 1.0 | 369
V3-C | 5.9 | 1.0 | 422
V4-C | 5.1 | 1.0 | 492
O7-I | 7.2 | 0.4 | 328
O8-I | 7.2 | 1.0 | 328
Welding parameters for 3mm thick sheets of Cu and Inconel 625. Beam current = 50 mA, beam Voltage = 50 kV, and oscillation diameter of 2mm, 10 kHz.
Beam
Offset
In Cu
In A-625

## Slide 8: Result- Beam offset in Cu leads to better welds.
0.4 mm
0.6 mm
0.9 mm
1.1 mm
V= 7.6 mm/s
V= 6.8 mm/s
V= 5.9 mm/s
V= 5.1 mm/s
O = 1 mm
Cu
Alloy 625
Cu
Alloy 625
Offset in Cu, v = 6.8 mm/s
Offset in Inconel 625, v = 6.8 mm/s
1.0 mm
0.4 mm
Varying speed, Offset in Cu = 1mm
3 mm

## Slide 9: Result- Quantification of the fusion zone -Ni, Cr, Mo distribution
There is diffusion of Ni and Cr in Cu. There is a slight Cu diffusion on the Inconel edge in the 0.4mm offset sample.
The Inconel particle density in the fusion zone depends on the Cu offset.

## Slide 10: Result- Quantifying the fusion zone after heat treatments- Offset 1mm in Cu.
As welded
750℃ / 50h
950℃ / 2h

## Slide 11: Result: Alloy 625 microstructure does not change with heat treatment

## Slide 12: Result: Hardness values of regions around the fusion zone.

## Slide 13: Result: Hardness values of regions around the fusion zone after 950℃/2h.

## Slide 14: Mechanical testing in progress (77K) - Fracture in Cu
Offset in Cu 1mm
Offset in Cu 0.4 mm

## Slide 15: Conclusions
Cu welds well with Inconel 625.
  Offsets in Cu were easier to weld than offsets in Inconel 625.
The welds last heat treatments in the range of 750℃ - 950℃.
  Preliminary testing indicates Cu is the weak spot but…
  Fatigue properties need exploration.
Inconel 625 maintains its microstructure in the temperature range explored.
  Precipitation is expected.

## Slide 16
Inconel Flange welded to Cu tube