## Slide 1: Design, fabrication, and testing of the quadrupole triplet magnet for the HRS project
Xiaoji Du, Yamen Al-Mahmoud, Yoonhyuck Choi, David Greene, Junseong Kim, Ryan Koschay, Hai Nguyen, John Wenstrom, Ting Xu, Danlu Zhang, Hengkang Zheng
Facility for Rare Isotope Beams, Michigan State University, East Lansing, MI 48824, USA

## Slide 2: Outline
Introduction of HRS project in FRIB
Quadrupole triplet magnet for HRS project
Magnet design
Magnet fabrication
Magnet cold test
Summary

## Slide 3: Introduction of HRS project in FRIB
High Rigidity Spectrometer (HRS) is a key expansion of FRIB user facility and will improve beam efficiency and provide high rigidity (8 Tm) rare isotope beams
HRS project divided into two sub-projects: High Transmission Beamline (HTBL) and Spectrometer Section (SPS)
HRS

## Slide 4: Quadrupole triplet magnet for HRS project
Functional Requirements for the Quadrupole Magnets of the HTBL
Parameter | QHA | QHB
Quantity (in 8 quadrupole triplets) | 16 | 8
Effective field length (nominal) (m) | 0.40 | 0.79
Pole-tip radius (m) | 0.15 | 0.15
Warm-bore radius (m) | 0.10 | 0.10
Quadrupole maximum field strength (T@poletip, base requirement) | 2.34 | 2.48
Quadrupole maximum field strength (T@poletip, with 10% tuning margin) | 2.57 | 2.73
Quadrupole gradient integral (T, base requirement) | 6.24 | 13.06
Quadrupole gradient integral (T, with 10% tuning margin) | 6.86 | 14.37
Quadrupole good-field region radius (m) | 0.10 | 0.10
Maximum higher-order-field contamination (%) | 1 | 1
Sextupole maximum field strength (T/m2, base requirement) | 10 | 10
Sextupole maximum field strength (T/m2, with 10% tuning margin) | 11 | 11
Octupole maximum field strength (T/m3, base requirement) | 50 | 50
Octupole maximum field strength (T/m3, with 10% tuning margin) | 55 | 55

## Slide 5: Magnet design
Coil-dominated quadrupole triplet (CDQT)
Iron-dominated quadrupole triplet (IDQT)
Lower weight
Decreased helium consumption
Reduced cool-down time
Improved mechanical performance
Shortened secondary beam tuning time

## Slide 6: Magnet design
Quadrupole design (discrete cosine theta coil)
Shape function
2D plot of coil geometry
Quadrupole gradient along beam axis
Harmonic decomposition analysis
Property | Value
Multipole Order | 2
Number of super-layers | 4
Number of Layers per super-layers | 2
Number of Turns | 20, 21, 23, 24
Length of cable [m] | 731.47
Min wire spacing in arcs [mm] | 3.4
Min wire spacing in straights [mm] | 3.8
Tip-to-Tip length [m] | 0.5
Effective Length, L0 (m) | 0.40
Radius of Aperture, R0 (m) | 0.10
Quad. MAX gradient, G2 (T/m) | 17.4
Quad. MAX grad. integral, Gi2 (T) | 6.98
Maximum non-quadrupole content | 0.12%
Bmax in coil [T] | 2.9
Total magnetic stored energy [kJ] | 70
Total Inductance [H] | 0.69

## Slide 7: Magnet design
Quench protection circuit for quadrupole
HTS Leads
HTS Leads
Room Temperature
In Cryo Vessel
PS (500A)
Slow Dump Resistor (0.16 Ohm)
Cold Diodes (4V)
SC Coil
SC Coil
SC Coil
SC Coil

## Slide 8: Magnet design
Sextupole coil (QHA)
Operating Current [A] | 36
Diameter of wire [mm] | 0.6
Inner Radius [m] | 0.1798
Outer Radius [m] | 0.1874
Number of Turns | 969
Racial Thickness [mm] | 7.6
Packing factor | 0.562
straight section length [mm] | 302.714
Total length [mm] | 490
Start angle [degree] | 0.0797
End angle [degree] | 20.1077
Coil angle [degree] | 20.028
Max field on wire [T] | 0.658
Reference radius [m] | 0.1
Field Gradient [T/m^2] | 11.2566
Effective length [mm] | 409.2489
Integrated Strength [T/m] | 4.6068
Non_uniform | 0.3322%

## Slide 9: Magnet design
Octupole coil (QHA)
Operating Current [A] | 36
Diameter of wire [mm] | 0.6
Inner Radius [m] | 0.1892
Outer Radius [m] | 0.1975
Number of Turns | 819
Racial Thickness [mm] | 8.3
straight section length [mm] | 341.90
Packing factor | 0.554
Total length [mm] | 490
Start angle [degree] | 0.0755
End angle [degree] | 14.9935
Coil angle [degree] | 14.918
Max field on wire [T] | 0.664
Reference radius [m] | 0.1
Field Gradient [T/m^3] | 56.0406
Effective length [mm] | 427.93
Integrated Strength [T/m^2] | 23.98
Non_uniform | 0.0878%

## Slide 10: Magnet design
Dipole
Operating Current [A] | 36
Diameter of wire [mm] | 0.6
Inner Radius [m] | 0.1993
Outer Radius [m] | 0.2076
Number of Turns | 866
Racial Thickness [mm] | 8.3
straight section length [mm] | 341.90
Packing factor | 0.554
Total length [mm] | 490
Start angle [degree] | 0.075
End angle [degree] | 15.075
Coil angle [degree] | 15
Ratio of co-winding | 0.33
Max field on wire [T] | 0.686
Reference radius [m] | 0.1
Field Strength [T] | 0.06488
Effective length [mm] | ~428
Integrated Strength [Tm] | ~0.0278
Non_uniform [%] | 5.669

## Slide 11: Magnet design
Force calculation
Dipole | Sext | Octu
1 | 1 | 1
1 | 1 | -1
1 | -1 | 1
1 | -1 | -1
-1 | 1 | 1
-1 | 1 | -1
-1 | -1 | 1
-1 | -1 | -1
Polarity (1 for +36 A; -1 for -36 A)
8 different cases totally (Setting quadrupole to 450 A)

## Slide 12: Magnet design
The maximum segment net force always appears on quadrupole. The order of magnitude of max/min force remains roughly unchanged when changing polarities.
Polarity |  |  |  | Dipole |  | Quadrupole |  |  |  |  |  |  |  | Sextupole |  | Octupole | 
 |  |  |  |  |  | Layer_1 |  | Layer_2 |  | Layer_3 |  | Layer_4 |  |  |  |  | 
Dipole | Sext | Octu |  | F_x (N/m) | F_y (N/m) | F_x (N/m) | F_y (N/m) | F_x (N/m) | F_y (N/m) | F_x (N/m) | F_y (N/m) | F_x (N/m) | F_y (N/m) | F_x (N/m) | F_y (N/m) | F_x (N/m) | F_y (N/m)
1 | 1 | 1 | maximum net force of segment | 45164 | 20379 | 167670 | 143560 | 106640 | 110040 | 108290 | 129400 | 119810 | 145030 | -29698 | 39337 | 34499 | 45521
1 | 1 | -1 |  | 31209 | 14702 | 154510 | 156720 | 111510 | 93830 | 132320 | 105370 | 149850 | 114990 | -49599 | 27608 | 51732 | 41570
1 | -1 | 1 |  | 44422 | 23369 | 141190 | 142860 | 74790 | 110030 | 70438 | 129400 | 75246 | 145050 | 43944 | 39337 | 49671 | 45521
1 | -1 | -1 |  | 18929 | 14702 | 128030 | 155890 | 79675 | 93484 | 94468 | 105370 | 105290 | 115010 | 63845 | 27608 | 36560 | 41570
-1 | 1 | 1 |  | 45164 | 34366 | 166720 | 153740 | 106150 | 99413 | 108160 | 118290 | 119660 | 133400 | -29698 | 38234 | 34499 | 50231
-1 | 1 | -1 |  | 31209 | 36802 | 153680 | 166900 | 111400 | 104480 | 132190 | 94259 | 149700 | 103360 | -49599 | 26505 | 51732 | 43460
-1 | -1 | 1 |  | 44422 | 34366 | 140420 | 152970 | 74515 | 99422 | 70567 | 118290 | 75390 | 133370 | 43944 | 38234 | 49671 | 50231
-1 | -1 | -1 |  | 30467 | 36802 | 127380 | 166000 | 79785 | 104060 | 94597 | 94257 | 105430 | 103330 | 63845 | 26505 | 36560 | 43460
1 | 1 | 1 | minimum net force of segment | -44422 | -34366 | -140420 | -152970 | -74515 | -99422 | -70567 | -118290 | -75390 | -133370 | -43944 | -38234 | -49671 | -50231
1 | 1 | -1 |  | -30467 | -36802 | -127380 | -166000 | -79785 | -104060 | -94597 | -94257 | -105430 | -103330 | -63845 | -26505 | -36560 | -43460
1 | -1 | 1 |  | -45164 | -34366 | -166720 | -153740 | -106150 | -99413 | -108160 | -118290 | -119660 | -133400 | 29698 | -38234 | -34499 | -50231
1 | -1 | -1 |  | -31209 | -36802 | -153680 | -166900 | -111400 | -104480 | -132190 | -94259 | -149700 | -103360 | 49599 | -26505 | -51732 | -43460
-1 | 1 | 1 |  | -44422 | -23369 | -141190 | -142860 | -74791 | -110030 | -70438 | -129400 | -75246 | -145050 | -43944 | -39337 | -49671 | -45521
-1 | 1 | -1 |  | -30467 | -14702 | -128030 | -155890 | -79675 | -93484 | -94468 | -105370 | -105290 | -115010 | -63845 | -27608 | -36560 | -41570
-1 | -1 | 1 |  | -45164 | -23369 | -167670 | -143560 | -106640 | -110040 | -108290 | -129400 | -119810 | -145030 | 29698 | -39337 | -34499 | -45521
-1 | -1 | -1 |  | -31209 | -14702 | -154510 | -156720 | -111510 | -93830 | -132320 | -105370 | -149850 | -114990 | 49599 | -27608 | -51732 | -41570

## Slide 13: Magnet design
Overbending structure
M1Po3C-02: Structural analysis and field mapping test setup of the quadrupole triplet magnet for HRS project
Hengkang Zheng, Xiaoji Du, Yamen Al-Mahmoud, Yoonhyuck Choi, David Greene, Junseong Kim, Ryan Koschay, Hai Nguyen, John Wenstrom, Danlu Zhang, Ting Xu

## Slide 14: Magnet Fabrication
Quadrupole coil fabrication
The quadrupole is discrete cosine-theta NbTi coil wound on anodized Aluminum bobbin, There are 4 layers with G-10 inter-layer separators and aluminum outer cylinder.
Coil winding
G-10 pieces overbending
Vacuum Pressure Impregnation

## Slide 15: Magnet Fabrication
Multipole coil fabrication
Coil winding
Side clamp bars and end pieces assembly
Curing
Inspection

## Slide 16: Quadrupole coil testing
The single-layer prototype
  In-house fabrication, and cold testing have been completed.
The full-scale quadrupole coils
  Fabricated by vendors.
  2 long and 6 short coils have been fabricated.
  1 long and 1 short coil have passed cold testing，with no quench occurrences.
  The remaining coils are currently waiting for testing.
Quadrupole coil LHe test set up

## Slide 17: Summary
A discrete cosine theta quadrupole triplet was designed for HRS project.
Quench protection circuit was designed to ensure the safe operation of superconducting magnets.
The quadrupole coils have been fabricated and has passed individual cold testing.
The multipole coils, which is paired with the long quadrupole coil, have also been fabricated.
Next step: assemble the multipole and quadrupole coils together and carry out cold testing.
References:
  [1] Yoonhyuck Choi, et al., “The High Transmission Beamline Superconducting Magnets for High Rigidity Spectrometer Project at FRIB: Design Status”, IEEE Transactions on Applied Superconductivity, vol. 35, no. 5, August 2025.
  [2] D. Greene, et al., "Design of Coil-Dominated Quadrupole Triplet for High Rigidity Isotope Beams," IEEE Transactions on Applied Superconductivity, vol. 33, no. 5, pp. 1-5, 2023.
  [3] D. Greene, et al., “Status of coil-dominated discrete-cosine-theta quadrupole prototype for High Rigidity isotope beams”, 15th IPAC, 2024, doi: 10.18429/JACoW-IPAC2024-WEPS67