## Slide 1: Week 27: R134a with z5 material
Presenter: Amin Bouzaiene, Maria Cristina Arena, Hsuan-Chu Chen

## Slide 2: Experimental design
Conditions
  Flowrate: 1-100 L/hr (conversion factor ~3) at room temp with gas supply pressure 3 barg
Procedures (with cycles)
  Using vacuum pump to keep the cartridge nearly vacuum (-0.92 barg)
  Insert R134a with gas cylinder
  As the pressure of the cartridge increases to 0 barg, stop inserting gas, and turn on the vacuum pump

## Slide 3: R134a PSA cycles
In the first cycle it takes 45 minutes
We experienced that :
Cartridge was heating up and the heat wave was moving in the length of the bed from the beginning to the end of the cycle. exothermic reason
Maximum volume of gas adsorbed
Vacuum do not regenerate the cartridge at each cycle.

## Slide 4: Results (z5 experiments)
The volume of R134a adsorbed decreases drastically between the first and second cycle and the cartridge is hot R134a is adsorbed in the molecular sites of the sieve
After the 3th cycle, the volume of R134a remains nearly constant the adsorbent is saturated
The difference of the volume between the first experiment and the saturation
The void volume in the bed we could assume that it is 1.15 L
The mass of the adsorbent is 260g
The amount of gas adsorbed/g adsorbent = 2.4 mmol/g
Converted volume = Volume measured by the flowmeter calibrated in air/ conversion factor
Chart: R134a adsorption in z10
| 1 | 2 | 3 | 4 | 5 | 6 | 7
 | 17.2094 | 2.0547 | 1.6284 | 1.5353 | 1.7071 | 1.1869 | 1.1542

## Slide 5: R134a literature compared with experimental results
260 g of adsorbent material and 16 liters of gas adsorbed
The amount of gas adsorbed/g adsorbent = 2.51 mmol/g at a pressure of 1 bar it is comparable with literature findings

## Slide 6: Regeneration with vacuum for 45 minutes
GOAL : try to see if keeping under vacuum the cartridge for a time equal to the time of adsorption of the first cycle, the regeneration takes place or not.
1st cycle after thermal regeneration volume of gas adsorbed was 16.1 L
After vacuum for 45 minutes volume adsorbed is 0.7 L
RESULT: the regeneration with vacuum pressure is NOT effective.