## Slide 1: Radiation-detected magnetic resonance RD-NMR and RD-MRI
Magdalena Kowalska
CERN, Switzerland
kowalska@cern.ch

## Slide 2: Principles of RD-NMR

## Slide 3: Conventional NMR and MRI: principle
NMR/MRI elements:
  Stable probe nuclei with spin different from 0
  Sample/ environment containing these nuclei (liquid or solid)
  Strong static magnetic field (several Tesla)
  Weaker magnetic field oscillating at radio-frequency (MHz)
Principle:
  Perturb spins of probe nuclei (with oscillating field or other means)
  record resonance frequency and pace of response -> info about local environment
Radiofrequency
B

## Slide 4: Conventional NMR and MRI: applications
NMR Spectroscopy
  static magnetic field very homogenous: no spatial resolution
  100s of micro-liters of samples needed for good signal
  studies of structure and dynamics of compounds, in physics, chemistry & biology
MRI Imaging
  Static magnetic field with a strong gradient in 1-3 dimensions: < mm spatial resolution
  Space-resolved studies of materials; medical diagnosis via anatomical information
25Mg NMR
radiofrequency

## Slide 5: Conventional NMR/MRI: challenges
Very low sensitivity:
  Small degree of spin ‘polarization’ (relative difference in spins up and down; 10-5)
  Inefficient detection (inductive pickup)
Limited number of nuclei with good NMR properties:
  Many nuclei with spin 0 (no signal) or > ½ (broad resonances)
  Small spin polarization due to nuclear properties
High magnetic field required -> heavy and expensive superconducting magnets
Limited gradient of magnetic field
Our reply to these challenges => radiation-detected NMR/MRI:
  (Hyper)polarisation of spins of unstable nuclei + detection of asymmetry in decay radiation
ISOLDE-CERN: central laboratory for technique development
Result:
Many probe nuclei (1016-1017) , large samples (100s of microliters)
Long measurement time (minutes) – on samples and patients
Limited resolution: rather mm than micrometers or below
Large, non-portable and expensive setups

## Slide 6: Present RD-NMR probe nuclei
300 stable isotopes, over 3000 known unstable isotopes
Our past and upcoming RD-NMR probes
neutrons
protons
beta-NMR/MRI
gamma-NMR/MRI

## Slide 7: Radiation-detected NMR: hyperpolarisation
Criteria (element-dependent) :
  Speed and degree of polarisation
  Type of production facility
Optical pumping:
laser
Spin Exchange Optical pumping
(SEOP): laser + atomic collisions
Production mechanism
(heavy-ion reactions)
Capture of polarised neutrons
being explored:
‘Chemical’ methods
(pH2, DNP)
Low temperature (mK) nuclear orientation
Short-lived nuclei
(t1/2 = ms to s):
In-beam polarisation at production side
Long-lived nuclei (t1/2 = min to day):
polarisation decoupled from production

## Slide 8: Radiation-detected NMR: decay asymmetry
Gamma decay,
spin >1/2
B0
Beta decay
spin >0
b detector
g detector
Decay anisotropy
L. Dupond
g detector
b detector
beta-NMR/MRI
gamma-NMR/MRI
Procedure (RD-NMR):
Stopped in mm’s of material: 1-2D studies
Can pass cm’s of material: 1-2D studies

## Slide 9: Examples

## Slide 10: Use of polarised unstable nuclei
b decay
g decay
gamma-MRI
Cell on a chip, preclinical studies,
medical diagnosis
  Decay asymmetry parameter:
  Unitarity of CKM
  quark mixing matrix
  Fundamental interactions
Spin and parity of
nuclear states connected by
emitted radiation
  Nuclear structure
Material science
Spin relaxation and
beta-NMR
Chemistry
Biology
Polarised
radioactive
nuclei
beta-MRI
?

## Slide 11: Sensitivity and new nuclei
=> shorter measuring time
=> studies not possible before
Stable K NMR: usually 39K (I=3/2), low receptivity and Q line broadening
In ionic liquids and deep eutectic solvent (glycholine) -> almost no signal
b-NMR:
0.1 M KCl in D2O
128 scans,
acquisition time ~10 min
9.4 T
KCl in EMIM-DCA (+ H2O traces)
16 000 scans, acquisition time >10 h
30 min
acquisition
EMIM-DCA IL,
109 nuclei of 47K

## Slide 12: Sub-micrometer resolution
Beam of polarized nuclei -> implanted into sample at defined depth
Observe environment in layers and measure diffusion
Example:
  Lithium diffusion in solid-state battery materials
  Other laser-polarized short-lived nuclei
-More elements feasible
=> Studies of thin layers and interfaces in bulk material

## Slide 13: Real-time measurement
0 3.6 7.2 ppm
Ion implantation into sample defines t0
Study of dynamic processes
Examples:
  DNA G-quadruplex interaction with Na and K
  Protein binding to metal ions (e.g. Cu)
ERC Grant 2015-21, collaboration with: Poznan, Ljubljana, Geneva

## Slide 14: Portable and cost-efficient setups
Polarisation inside sample => para-hydrogen, dynamic nuclear polarization, SEOP
No need for superconducting magnet => compact setup
Longer-lived nuclei, e.g. PET isotopes
  300 ul of SABRE Ir catalyst
  300 ul of 13 N [Ammonia] in H2O
  pH2 created at LN2 temperature
CERN Medical Applications Fund: With Mainz, HUG-Geneva
FET-OPEN project: with HEPIA, Madrid, RS2D, Maastricht, Leuven
RD-ZULF-NMR setup
Gamma-MRI setup

## Slide 15: Team and expertise
Team:
  Nuclear and atomic physicists
  Chemical engineers
  Engineers
Expertise: hyperpolarization techniques, NMR and RD-NMR, detectors, rf

## Slide 16: b-NMR: metal ions in chemistry and biology
NMR can provide info on location & evolution of metal-ion binding to (bio)molecules
  Challenges: almost invisible signals due to small abundance, spin >1/2, and small sensitivity
  Result: metal-ion-NMR used very rarely => sensitive NMR approach is needed
‘green solvents’: ionic liquids and prospects for car battery material
Na and K binding to DNA G-quadruplexes (present e.g. in telomeres):
  Binding crucial to their formation, stability, and polymorphism
With:
Ljubljana
Geneva
Leipzig
Poznan
With:
Geneva
Leipzig
Bratislava
Poznan
EMIM-DCA IL,
109 nuclei of 47K

## Slide 17: RD-ZULF-NMR
Zero to Ultra-Low Field NMR (ZULF-NMR):
  Studies in mT fields -> Very portable
  Excitations with Hz frequencies -> signals from samples in metallic containers
  Hyperpolarisation needed, e.g. para-H2, Dynamic Nuclear Polarisation (DNP)
  Relatively low sensitivity
Radiation-detected NMR (RD-NMR):
  Unstable probe nuclei (often short-lived)
  Extremely high sensitivity
  Studies in > 0.1 to several T fields -> large setups
RD-ZULF-NMR: combine advantages of both techniques
  Proof-of-principle:
  Parahydrogen hyperpolarisation
  (SABRE) of 13N-labelled NH3
  solution (used for PET)
With:
Mainz
Postdoc from Prag
Student from Tampere

## Slide 18: g-MRI with long-lived polarised nuclei
Addressing limitations of present molecular imaging:
  Low MRI sensitivity
  Low PET/SPECT spatial resolution
Simultaneous exploitation of gamma (γ) detection sensitivity + spatial resolution and flexibility of MRI
  Use of polarised unstable tracers
  Increase MRI sensitivity and nuclear medicine resolution
  positioning given by MRI sequences
  tracer amount given by degree of asymmetry of γ-emission
Work on prototype MRI device ongoing
EU FET-OPEN

## Slide 19: g-MRI and lung & brain imaging with Xe isomers
Imaging using long-lived 129m,131m,133mXe long-lived nuclear states (isomers):
Xe: biologically neutral, yet binding to biomolecules and passing blood-brain barrier
Stable 129Xe used for MRI lung (and brain) imaging
Unstable 133Xe used for SPECT brain imaging
Gain: higher MRI sensitivity or higher nuclear-medicine resolution
Polarisation using spin-exchange optical pumping (SEOP) known from stable 129Xe studies

## Slide 20: Radiation-detected (RD-)NMR
Gamma decay,
spin >1/2
b detector
b detector
g detector
g detector
beta-NMR
gamma-NMR
Beta decay, I>0
B0
NMR signals from only 106 unstable probe nuclei already recorded
Use of single nuclei feasible in principle
RD-NMR: NMR detected via decay radiation emitted by unstable probe nuclei
Principle: spin-oriented unstable nuclei emit decay radiation that is anisotropic
- signal proportional to degree of polarisation (Mz)
-> ingredients: radioactive nuclei with spin > 0 + hyperpolarisation

## Slide 21: ISOLDE radionuclei
Nearly 1300 isotopes available from over 75 chemical elements
Over 1000 used for experiments
-> by far largest choice among such facilities
Production
(ions/s)
neutrons
protons

## Slide 22: Isotope production for RD-NMR
Short- and long-lived nuclei: ISOLDE - CERN’s lab for production and studies of unstable nuclei (> 1300 ion beams produced)
(at SC, 1956-91)
Longer-lived nuclei: nuclear reactors (e.g. ILL, MARIA) or medical cyclotrons (e.g. HUG in Geneva)

## Slide 23: Hyperpolarisation for RD-NMR
Criteria (element-dependent) :
  Speed and degree of polarisation
  Type of production facility
Optical pumping:
laser
Spin Exchange Optical pumping
(SEOP): laser + atomic collisions
Production mechanism
(heavy-ion reactions)
Capture of polarised neutrons
being explored:
‘Chemical’ methods
(pH2, DNP)
Low temperature (mK) nuclear orientation
Short-lived nuclei
(t1/2 = ms to s):
In-beam polarisation at production side
Long-lived nuclei (t1/2 = min to day):
polarisation decoupled from production

## Slide 24: Use of polarised unstable nuclei
b decay
g decay
gamma-MRI
Cell on a chip, preclinical studies,
medical diagnosis
  Decay asymmetry parameter:
  Unitarity of CKM
  quark mixing matrix
  Fundamental interactions
Spin and parity of
nuclear states connected by
emitted radiation
  Nuclear structure
Material science
Spin relaxation and
beta-NMR
Chemistry
Biology
Polarised
radioactive
nuclei
beta-MRI
?

## Slide 25: Chemistry, biology, and material science with beta-NMR on optically-pumped short-lived nuclei

## Slide 26: b-NMR on optically-pumped short-lived nuclei
J. Croese et al., Nucl. Inst. Meth. A, 1020 (‘21) 165862
M. Jankowski et al, to be submitted
b-NMR at 0.1, 0.5, 1.2 or 4.7 T
M. Kowalska et al., J. Phys. G: Nucl. Part. Phys. 44 (2017) 084005
W. Gins et al., Nucl. Instrum. Meth. A 925 (2019) 24
At the radioactive-ion beam facility ISOLDE at CERN
Laser beam
+
+
neutralisation (optional)
b-asymmetry + b-NMR
Optical pumping
Short-lived ions from ISOLDE
+
B
SC magnet
b detectors
B
sample + rf coil
betaDropNMR

## Slide 27: RD-NMR nuclei for optical pumping
  Already polarized or Planned, considered
g-MRI (with Geneva, Madrid, Leuven, Strasbourg, Maastricht):
CERN MA project, 2017-2021
EU FET-Open project, 2022-
RD-ZULF-NMR (with Mainz):
Patent applications filed
CERN MA project, 2022-
b-NMR, betaDropNMR:
ERC Starting Grant
ERC Proof of Concept application
b-NMR, PreSOBEN:
ERC Consolidator Grant

## Slide 28: RD-NMR probe nuclei
300 stable nuclei
3000 known unstable nuclei
neutrons
protons

## Slide 29: Liquid b-NMR on I=1/2 potassium nuclei
Stable K NMR: usually 39K (I=3/2), low receptivity and Q line broadening
In ionic liquids and deep eutectic solvent (glycholine) -> almost no signal
b-NMR:
0.1 M KCl in D2O
128 scans,
acquisition time ~10 min
9.4 T
KCl in EMIM-DCA (+ H2O traces)
16 000 scans, acquisition time >10 h
M. Jankowski et al.,
in preparation
30 min
acquisition
EMIM-DCA IL,
109 nuclei of 47K
KCl crystal,
1010 nuclei of 47K

## Slide 30: DNA G-quadruplex binding to potassium
b-NMR advantages:
  Sensitivity: metal ions are easily visible, cleaner spectra
  Smaller or no quadrupole moments -> longer T1 and narrower spectra
  Real-time: folding intermediates
DNA G-quadruplexes:
  present e.g in telomers, crucial: binding to alkali metals
B. Karg
Our study:
  Beamline- (vacuum-) compatible solvent: glycholine
  Liquid dispenser in vacuum
  Short G-rich DNA strands (ht, c-myc)

## Slide 31
Pure glycholine
beam
container
RF coils
Design:
In collaboration with M. Baranowski, M. Kozak (Poznan), J. Plavec (Ljiubliana); funded by ERC (2015-21)
107 of 47K nuclei
30 min scan
DNA G-quadruplex binding to 47K
After 3h
in vacuum
Glycholine + c-MYC folded around Na+

## Slide 32: Li diffusion in all solid-state batteries
load-lock
LN2 trap
Sample temp control:
-30 to 200 deg
Bellow system to
load/remove sample
Sample exchange point
Lithium diffusion in solid-state battery materials
  Depth-controlled implantation
  Measurement of T1 relaxation time for implantation in different layers
  Triggered by G. Rees, Oxford; collaboration with Z. Salman (PSI); funded by CERN Knowledge Transfer Fund (2024-26)
Beamline upgrades ongoing, 1st measurements planned for 2025

## Slide 33: Distribution of B field & neutrons in unstable nuclei
Offset in magnetic moment from HFS (hyperfine anomaly)
Very small, down to 10-6
Required: accurate m from NMR and HFS
PreSOBEN
B
NMR
HFS
M. Bissell
Compare nuclear magnetic moment derived from NMR & atomic hyperfine structure
47K b-NMR
in EMIM-DCA
Combined with atomic (J. Ginges, Brisbane) and nuclear (J. Dobaczewski, York) theory:
+ NMR shielding from quantum chemistry (A. Antusek, Bratislava)
Radius of
magnetic field distribution
in 47K vs stable 39K
Combined with atomic (J. Ginges, Brisbane) and nuclear (J. Dobaczewski, York) theory:
M. Bissell, in preparation
=> m (ratio) from HFS: 0.364(9) % difference

## Slide 34: Distribution of magnetic field & neutrons in nuclei
Determined through Magnetic Hyperfine Anomaly (Bohr-Weisskopf effect):
Effect of finite nuclear magnetisation on atomic hyperfine structure
Very small effect, down to 10-6 (up to 10-2 in rare cases)
Required:
Larmor frequency and magnetic moment with 10-5-10-6 accuracy (done)
  Precision: b-NMR in liquid hosts
  Absolute magnetic field: in-situ 1H or 2H probe
  Accuracy: ab initio quantum chemistry calculation of chemical shifts
magnetic hyperfine structure constant with 10-4-10-5 accuracy (upcoming)
  In-flight rf excitations within hyperfine structure
PreSOBEN
B
D= /
NMR
HFS
from M. Bissell
Differential anomaly

## Slide 35: Distribution of magnetisation in 47K vs stable 39K
Accessed through its effect on atomic hyperfine structure vs Larmor frequency
K chemical shift of EMIM-DCA to H2O
ca. 35 ppm (A. Antusek, Bratislava)
Hyperfine structure ratio:
47K b-NMR
in EMIM-DCA
M. Bissell et al., in preparation
Effect for 47K vs 39K
D = 0.364(9) %
Combined with atomic (J. Ginges, Brisbane) and nuclear (J. Dobaczewski, York) theory:
M. Bissell and M. Jankowski

## Slide 36: Chemistry and biology on PET isotopes with para-hydrogen and DNP polarisation

## Slide 37: RD-ZULF-NMR on long-lived PET isotopes
RD-ZULF-NMR: radiation-detected + zero-to-ultralow-field NMR:
  Combine ZULF-NMR portability with RD-NMR sensitivity
  Use easily available unstable isotopes
  Hyperopolarisation with SABRE (para-hydrogen)
  Suitable PET isotopes:
In collaboration with U Mainz: D. Budker, D. Barskiy, R. Kircher, and Geneva University Hospital (V. Bonvin, V. Garibotto, A. Grotzky)
Funded by CERN Medical Applications Fund (2022-24)
Medical Applications
Parahydrogen prepared from small H2 bottle
pH2 hyperpolarising chemical reaction
inside ZULF apparatus
Magnetic field pulse and signal acquisition via change of beta-decay asymmetry
Isotope production
as aqueous solution (like for PET)
beta-particle detectors
Proof of Concept

## Slide 38: SABRE optimization with natural-abundance 15N
Kircher, Xu, Barskiy. J. Am. Chem. Soc. 146 (2024), 514
At 1T
In SABRE-SHEATH
[15N]-NH3
(8 Scans)
D. Barskiy, R. Kircher

## Slide 39: Setup for RD-ZULF-NMR
In the lab at Geneva University Hospital cyclotron:
  Twinleaf SHEATH
  2 thin beta detectors + SiPM, easy DAQ
  pH2 created at LN2 temperature
  Semi-automatic liquid shuttling setup
  300 ul of SABRE Ir catalyst
  300 ul of 13 N [Ammonia] in H2O
  pH2 created at LN2 temperature

## Slide 40: First SABRE polarization tests on 13N
H2 bubbling with too much liquid
Tests with no polarisation
1st polarization tests
Preliminary
Data analysis ongoing

## Slide 41: PET isotopes polarized with DNP
DNP = dynamic nuclear polarization
Polarisation of electron spins at mK temperatures + polarization transfer to nuclei with microwaves
Invented for nuclear and particle physics for polarized targets
Discovered by NMR community later on
Polarisation of 18F using a portable DNP polarizer
  Polariser under design
  18F from medical cyclotron
Project funded with CERN knowledge transfer fund (2024-25)

## Slide 42: g-detected MRI
http://science.mq.edu.au/~dyves/research/hyper.html
Aim: combine advantages of nuclear medicine and MRI in one modality
Record MRI signals from PET/SPECT-type nuclei
Hyperpolarize spins and observe asymmetry of gamma decay
Result - high efficiency (g detection) and high resolution (MRI)
Gamma-MRI Equipment:
  I>1/2 gamma-emitting nuclei
  Spin-polarizer
  MRI magnet
  Gamma detectors inside B field
Shown to work in 2D by:
Y. Zheng, G.W. Miller, W.A. Tobias, G.D. Cates, Nature 537, 652 (2016)

## Slide 43: Stable 129Xe MRI
R.L. Eddy, G. Parraga, Eur. Resp. J. 2020 55: 1901987
Provides information on:
  pulmonary ventilation
  tissue microstructure
  gas exchange
Features:
  Sensitive
  Fast (< 10 s)
  Precise (3 mm)
  No proton background
  Chemical information
Applications:
  Respiratory diseases
  Emerging: functional images of highly perfused organs: kidneys, brain
J. Chacon-Caldera, Magn Reson Med. 2020;83(1):262
Y. Shepelytskyi, Magn Reson Med. 2022;88:83

## Slide 44: g-MRI with long-lived Xe isomers
EU FET-OPEN
Simultaneous exploitation of gamma (γ) detection sensitivity + spatial resolution and flexibility of MRI
  Use of polarised unstable tracers
  Increase MRI sensitivity and nuclear medicine resolution
  positioning given by MRI sequences
  tracer amount given by degree of asymmetry of γ-emission
Work on 0.1 T Gamma-MRI prototype ongoing

## Slide 45: g-detected MRI – spatial resolution
Gamma-MRI
  Higher sensitivity than conventional MRI: signal detection via gamma radiation
  Higher resolution than nuclear medicine techniques: position via rf pulses
Plot by K. Kulesz
No polarisation
Polarisation
Rf excitation in resonance with 1 voxel

## Slide 46: Acknowledgements
Funding:
Thank you for your attention
N. Azaryan, M. Becvar, M. Bissell, M. Chojnacki, D. Havranek, B. Karg, M. Jankowski, K. Vitulova, W. Lindberg, I. Michelon, D. Paulitsch, M. Pesek, M. Piersa-Silkowska, A. Sparks, S. Warren, T. Treczoks
Collaborators:
b-NMR at CERN: L. Vazquez, CERN; M. Baranowski, M. Kozak, Poznan; G. Rees, Oxford, M. Madurga, Knoxville; D. Zakoucky, Rez
RD-ZULF: D. Budker, D. Barskiy, R. Kircher, Mainz; A. Grotzky, V. Bonvin, V. Garibotto, Geneva Hospital
Conventional NMR: J Gravier, M Pupier, UNIGE
Theory: quantum chemistry: A. Wesolowski, UNIGE, A. Antusek, Bratislava; atomic physics: J. Ginges, B. Roberts, Brisbane; nuclear theory: J. Dobaczewski, York, M. Kortalainen, Jyvaskyla
CERN team:

## Slide 47: More studies planned for 2024
Distribution of magnetic field and ‘halo’ neutron in 11Be
  ‘halo nucleus’ where magnetisation is carried by last neutron -> determination of neutron-halo radius
  Optical pumping and b-NMR at ISOLDE
  M. Bissell, D. Paulitsch
Lithium diffusion in solid-state battery materials
  Optical pumping and b-NMR at ISOLDE
  Triggered by G. Rees, Oxford
  A. Sparks, N. Azaryan
b-NMR on PET isotope 18F
  18F shipped from Geneva Hospital Cyclotron
  DNP polarization at 2 K
  In collaboration with G. Reichertz, Bochum
  M. Pesek

## Slide 48: Radiation-detected NMR
Spin hyperpolarisation
+ signal detection via decay anisotropy
Beta-NMR
gamma-NMR
Gamma decay, I>1/2
Beta decay, I>0
B0
Observed decay asymmetry can be used to:
  Probe underlying decay mechanism
  Determine properties of involved nuclear states
  Derive differences in nuclear energy levels
Unstable probe nuclei with spin > 0 in magnetic field

## Slide 49: Hyperpolarisation for RD-NMR
Criteria (element-dependent) :
  Speed and degree of polarisation
  Type of production site
Optical pumping:
laser
Spin Exchange Optical pumping
(SEOP): laser + atomic collisions
Production mechanism
(heavy-ion reactions)
Capture of polarised neutrons
To be explored:
‘Chemical’ methods
(pH2, DNP)
Low temperature nuclear orientation
Short-lived nuclei
(t1/2 = ms to s):
In-beam polarisation at production side
Long-lived nuclei (t1/2 = min to day):
polarisation decoupled from production

## Slide 50: b-NMR on optically-pumped short-lived nuclei
Experimental setup at the radioactive-ion beam facility ISOLDE at CERN
  Polarisation online via optical-pumping (e.g. on alkali, alkali earths, excited noble gases)
Laser beam
+
+
neutralisation (optional)
b-asymmetry + b-NMR
Optical pumping
Short-lived ions from ISOLDE
+
B
SC magnet
b detectors
B
sample + rf coil
J. Croese et al.,
Nucl. Inst. Meth. A (2022)
M. Jankowski et al.,
To be submitted
betaDropNMR
PresOben

## Slide 51: ppm magnetic moments of unstable nuclei
Nuclear magnetic dipole moments:
- Determine orbits of last neutrons and protons
- Very sensitive to nuclear wavefunction
Experiments:
  stable isotopes: ppm precision from NMR
  short-lived nuclei: 10-3 – 10-4 precision
    Hyperfine structure from laser spectroscopy
    b-NMR in solid hosts
Calculations of shielding by electrons in B field:
  All nuclei => till recently: per-mill level
  Since recently: ab initio, coupled cluster approaches
Per-mill accuracy
  Enough to compare with nuclear-structure theory
  Not enough for fundamental tests
  Not enough to study the ‘magnetic radii’ of nuclei
  Not enough to combine b-NMR with NMR
m
Spin 3/2
Half-life: 9 ms
1000 ions/s
b-NMR
b-
E. Arnold et al., Phys. Lett. B 197, 311 (1987)
R. Neugart et al., Phys. Rev. Lett. 101, 132502 (2008)

## Slide 52: Potassium binding to DNA G-quadruplexes
Beamtime on 18-22 November
Fresh glycholine
Signal from 107 47K nuclei in total
Signal from 107 47K nuclei in total
Glycholine after 3h in vacuum
Sample with DNA pre-folded with 23Na
Data analysis ongoing by M. Jankowski

## Slide 53: Backup

## Slide 54: RD-NMR measurement
Polarisation + destruction of polarisation with rf -> decrease in decay asymmetry
Measurement principle,
example of beta-detected NMR
Frequency
β asymmetry
B0
RF coil
β detectors
β particles
M. Jankowski

## Slide 55: Spin polarization via optical pumping
Multiple excitation cycles with circularly-polarized laser light
Photon angular momentum transferred to electrons and then nuclei
  Works best for 1 valence electron
  nuclear spin-polarization of 10-90%
  Polarization buildup time < us
I =3/2
29
+
Mg
F
3
2
1
0
3p 2P3/2
fine
structure
hyperfine
structure
-2
-1
0
1
2
-2
-1
0
1
2
-3
3
Magnetic sublevels
frequency
D2-line
s+ light
3s 2S1/2
2
1

## Slide 56: Radiation-detected NMR at CERN
ISOLDE: CERN’s laboratory for production and studies of radioactive nuclei

## Slide 57: Elements polarized with lasers
Laser polarization works best for alkali and alkali-earth metals
  Radioactive half-lives: dozen ms to several s
Laser-polarized at ISOLDE:
  Already polarized
  Planned

## Slide 58: b-NMR setup at ISOLDE
magnetic mass
separator
1.4 GeV protons
target
Laser-polarization and b-NMR beamline at ISOLDE/CERN
Radioactive ion beam at 60keV

## Slide 59: Experimental setup 2016 - 2019
M. Kowalska et al., J. Phys. G: Nucl. Part. Phys. 44 (2017) 084005
W. Gins et al., Nucl. Instrum. Meth. A 925 (2019) 24
R. Harding et al., Phys. Rev. X Phys. Rev. X 10, 041061
J. Croese et al., Nucl. Inst. Meth. A (2022)
9
4
Design: F. Wienholtz, W. Gins, R. Harding
Polarisation detection
(scintillators + SiPMs)
b-asymmetry and b-NMR measurements at 0.5 and 1.2 T

## Slide 60: Experimental setup since 2021
4
2021 : 4.7 T superconducting magnet from ETHZ
Detection:
Scintillators + SiPMs
Sample + rf coil
+ B-field probe
Beam neutralisation (optional)
Circularly polarised laser light
polarisation via optical pumping
Ion beam from ISOLDE
J. Croese et al., Nucl. Instr. and Meth. A (2021), M. Jankowski et al., in preparation

## Slide 61: Projects

## Slide 62: ppm magnetic moments of unstable nuclei
Two orders of magnitude improvement over literature thanks to:
Extremely narrow resonances => liquid samples
In-situ NMR measurement of stable reference => vacuum-compatible 1H or 2H NMR probe
Increased field stability => 1H NMR feedback loop
Increased field homogeneity => shimming coils
ppm NMR shielding and reference moment => ab initio calculations (A. Antusek)
R. Harding et al., Phys. Rev. X 10, 041061 (2020)

## Slide 63: Magnetic dipole moments of stable nuclei
1H (proton): ppb accuracy
Heavier than 1H: ppm precision quoted in tables, but accuracy at per-mill level:
Experimental data at ppm level:
  NMR
  Atomic Beam Magnetic Resonance
Calculation of shielding by electrons in magnetic field:
  Problematic: most calculations from 60’s or 70’s – per-mill accuracy
  Only recently: ab initio calculations (coupled cluster approach), ppm accuracy
Recent example, highly-charged 208Bi and tests of QED in strong fields at GSI:
  7-sigma difference between measured and predicted HFS splitting
  discrepancy resolved by more accurate m(209Bi) with ab initio NMR shielding calculations
  => QED works even at such strong fields
M. G. H. Gustavsson, A.-M. Mårtensson-Pendrill, Phys. Rev. A 58 (1998)
K. Jackowski et al., J. Phys. Chem. A 114, 2471 (2010)
J. Ullmann et al., Nat. Comm. 8, 15484 (2017)
L. V. Skripnikov, Phys. Rev. Lett. 120, 093001 (2018)
A. Antusek et al., Phys. Rev. A 98, 052509 (2018)

## Slide 64: ppm-accuracy in nuclear magnetic moments
26Na
t1/2=1.1 s
about 1e8 nuclei
b decay
[MHz]
vacuum-compatible liquid hosts:
ionic liquids
Molecular tumbling in liquids => over 100 x narrower resonances than in solid hosts
R. Harding et al., Phys. Rev. X 10, 041061 (2020)

## Slide 65: Ab initio quantum chemistry calculations
New ab initio chemical calculations of Na shielding for reference m(23Na):
  m(23Na) from NMR measurement of NaCl in H2O:
  m(23Na) value from ABMR (atomic beam magnetic resonance) of Na atom beam in B-field:
A. Antušek et al., Chem. Phys. Letters 532, 1 (2012)
A. Antušek,
Bratislava
With old shielding
With new shielding
m(23Na) [mN]
relativistic DHF
paramagnetic shielding = 637.1+/- 0.1 ppm
Coupled cluster theory
NMR shielding: 582.0 +/- 2.6 ppm
Previous corrections inaccurate, as in e.g. 209Bi
R. Harding et al., Phys. Rev. X 10, 041061 (2020)

## Slide 66: ppm accuracy in frequency ratio & reference
26Na relative to stable 23Na
Accurate frequency ratio:
Accurate reference:
A. Antusek, Bratislava
m(23Na) /mN
R. Harding et al., Phys. Rev. X 10, 041061 (2020)

## Slide 67: Moments of radio-nuclei with ppm accuracy
2 orders of magnitude more precise than previously: ppm accuracy
Improved precision and accuracy for 27-31Na using 26Na moment as reference (b-NMR in solid hosts)
Direct comparison to conventional NMR
Experimental approach – speeds up b-NMR measurements
Magnetic dipole moments:
R. Harding et al., Phys. Rev. X (2020)
Next nucleus: 11Be
Will require reference merasurement of stable 9Be in ionic liquid

## Slide 68: New probe nuclei for NMR studies
Complementary NMR properties
+2.45534(8) mN
+ 86 mb
mI = +2.217494(5) mN
Q (b): 106 mb
Half-live
+3.89211(11) mN
- 7 mb
+2.849378(20) mN
- 5 mb
+2.41843(9) mN
+ 40 mb
+2.0681(5) mN
+2.29668(8) mN

## Slide 69: Liquid b-NMR on I=1/2 potassium nuclei
Stable K NMR: usually 39K (I=3/2), low receptivity and Q line broadening
In ionic liquids and deep eutectic solvent (glycholine) -> almost no signal
b-NMR:
0.1 M KCl in D2O
128 scans,
acquisition time ~10 min
9.4 T
KCl in EMIM-DCA (+ H2O traces)
16 000 scans, acquisition time >10 h
KCl crystal,
1010 nuclei of 47K
EMIM-DCA IL,
109 nuclei of 47K
M. Jankowski et al.,
in preparation

## Slide 70: b-NMR and DNA G-Quadruplexes
b-NMR advantages:
  Sensitivity: metal ions are easily visible, cleaner spectra
  Smaller quadrupole moments -> longer relaxation and narrower spectra
  Real-time: folding intermediates
DNA G-quadruplexes:
  present e.g in telomers, crucial: binding to alkali metals
B. Karg

## Slide 71: Potassium binding to DNA G-quadruplexes
Suitable vacuum-compatible solvent to fold G-quadruplex:
  Ionic liquids not suitable
  Deep Eutetic Solvent glycholine (glycerol + choline chloride) shown to fold GQ
b-NMR experiments in 2022: 47K implanted into glycholine + DNA
Pure glycholine
Glycholine + c-MYC folded around Na+
In presence of DNA: K resonance shifted and broadened: implanted K replaces Na inside G-quadruplex?
B. Karg

## Slide 72: Liquid dispenser system at high vacuum
Fresh droplet  avoid peak broadening
  Container with liquid sample inside beamline, but open from outside
T. Treczoks, N. Azaryan
container
RF coils
beam
Photos: M. Jankowski

## Slide 73: b-ZULF-NMR on long-lived PET nuclei
RD-ZULF-NMR: radiation-detected + zero-to-ultralow-field NMR:
  Combine ZULF-NMR portability with RD-NMR sensitivity
  Proof-of-principle polarisation experiment in May 2023
  Suitable candidates:
In collaboration with U Mainz: D. Budker, D. Barskyi and HUG (V. Garibotto, A. Grotzky)
Medical Applications Fund and ERC PoC
Parahydrogen prepared from small H2 bottle
pH2 hyperpolarising chemical reaction
inside ZULF apparatus
Magnetic field pulse and signal acquisition in beta-decay asymmetry
Isotope production
as aqueous solution (like for PET)
beta-particle detectors

## Slide 74: g-detected MRI
http://science.mq.edu.au/~dyves/research/hyper.html
Aim: combine advantages of nuclear medicine and MRI in one modality
Record MRI signals from PET/SPECT-type nuclei
Hyperpolarize spins and observe asymmetry of gamma decay
Result - high efficiency (g detection) and high resolution (MRI)
Gamma-MRI Equipment:
  I>1/2 gamma-emitting nuclei
  Spin-polarizer
  MRI magnet
  Gamma detectors inside B field
Shown to work in 2D by:
Y. Zheng, G.W. Miller, W.A. Tobias, G.D. Cates, Nature 537, 652 (2016)

## Slide 75: Stable 129Xe MRI
R.L. Eddy, G. Parraga, Eur. Resp. J. 2020 55: 1901987
Provides information on:
  pulmonary ventilation
  tissue microstructure
  gas exchange
Features:
  Sensitive
  Fast (< 10 s)
  Precise (3 mm)
  No proton background
  Chemical information
Applications:
  Respiratory diseases
  Emerging: functional images of highly perfused organs: kidneys, brain
J. Chacon-Caldera, Magn Reson Med. 2020;83(1):262
Y. Shepelytskyi, Magn Reson Med. 2022;88:83

## Slide 76: g-MRI with long-lived Xe isomers
EU FET-OPEN
Simultaneous exploitation of gamma (γ) detection sensitivity + spatial resolution and flexibility of MRI
  Use of polarised unstable tracers
  Increase MRI sensitivity and nuclear medicine resolution
  positioning given by MRI sequences
  tracer amount given by degree of asymmetry of γ-emission
Work on 0.1 T Gamma-MRI prototype ongoing

## Slide 77: g-detected MRI – spatial resolution
Gamma-MRI
  Higher sensitivity than conventional MRI: signal detection via gamma radiation
  Higher resolution than nuclear medicine techniques: position via rf pulses
Plot by K. Kulesz
No polarisation
Polarisation
Rf excitation in resonance with 1 voxel

## Slide 78: Summary and outlook
Radiation-detected NMR:
  Extremely sensitive
  Offering new (unstable) NMR nuclei
Interesting for:
  Physics – magnetic moments
  Chemistry – in zero-to-low magnetic field
  Biology: metal ions and biomolecules
  Medicine: new imaging technique
Many developments ongoing
  Collaboration with theory and across fields crucial

## Slide 79: Acknowledgements
Team: N. Azaryan, M. Bissell, M. Chojnacki,
M. Jankowski, I. Michelon, M. Pesek, M. Piersa,
T. Treczoks
Alumni: J. Croese, L. Dupond, K. Dziubinska,
R. Engel, W. Gins, R. Harding, B. Karg, K. Kulesz,
S. Warren, F. Wienholtz, E. Wistrom
Scientific collaborators:
b-NMR on short lived-isotopes
  UNIGE: NMR: J. Viger-Gravel, M. Pupier; Vzz calculations: T. Wesolowski, Y. Gimball-Zofka
  Slovak Academy of Sciences: NMR shieldings: A. Antusek, A. Hurajt
  Poznan U.: NMR: M. Baranowski, M. Kozak, J. Wolak
  Czech Academy of Sciences: online setups: D. Zakoucky
  Teheran U.: molecular dynamics: M. Maddah
  Leipzig U.: NMR: J. Matysik
  U. Tennessee: b-detectors: M. Madurga
Gamma-MRI
  CERN: isotope production: U. Koester, J. Schell, A. Mokhles Gerami
  HESSO/HEPIA: J-N. Hyacinthe, S. Pallada + team: Xe hyperpolarization
  U Complutense Madrid: J-M. Udias, L. Fraile + team: g-detectors
  RS2D: J. Rivoire + team: NMR console
  KU Leuven: D. Sakalariou + team: MRI magnet + gradients
  U Maastricht: simulations + encapsulation: R. Jolivet, K. Dziubinska-Kuehn
RD-ZULF-NMR:
  Mainz: ZULF-NMR: D. Budker, D. Barskyi
  HUG: isotope production: A. Grotzky
Funding:
BetaDropNMR
PreSoBEN

## Slide 80: liquid b-NMR to understand short-lived nuclei
Liquid b-NMR at ISOLDE facility + NMR shielding calculations:
  Accurate magnetic moments of short-lived nuclei
  + rf-laser spectroscopy => first precise studies of distribution of magnetisation and neutrons in unstable nuclei
Project just started:
  Planned studies on Be, Na, Mg, K, Rn, Fr, Ra isotopes
PreSOBEN

## Slide 81: Idea
81
What is Magnetic Hyperfine Anomaly? = Bohr-Weisskopf effect (e)
Effect of finite nuclear magnetisation on hyperfine structure
Probes distribution of nuclear magnetisation and, via it, unpaired neutrons
Very small effect, down to 10-6 (up to 10-2 in rare cases)
What do we require to determine it experimentally?
magnetic dipole moment down to 10-5-10-6 accuracy
magnetic hyperfine structure constant down to 10-4-10-5 accuracy
Measure Hyperfine Anomaly in unstable nuclei, not neglect it
2 orders of magnitude higher accuracy
than previously reachable for unstable nuclei
PreSOBEN

## Slide 82: Ingredients
I>0
Spin polarisation and asymmetric decay: Optical pumping
82
I>1/2
2
1
-2
-1
0
1
mF
-1
0
1
s-
2
F
Accurate magnetic moments: Radiation-detected NMR in liquids
  Rf-induced flip of nuclear spin in strong magnetic field
  Resonance detection: change in decay anisotropy
Accurate HFS constant A: Rf-laser double resonance
  Excitation within hyperfine multiplet in no or weak magnetic field
betaDropNMR
PreSOBEN

## Slide 83: rf-laser double resonance spectroscopy
Rf excitation within hyperfine (HF) multiplet
Rf excitation => narrow resonance
HF splitting measured directly not as a difference optical frequencies
Detection: fluorescence or change in decay asymmetry
Optical pumping into defined states
Transition to atomic excited state
Circular or linear light polarisation
kHz-wide resonance => hyperfine structure constant with 102-103 higher accuracy
Frequency offset (MHz)
26Na,
589-nm
laser
excitation,
Dec 2018
-300 -100 100 300 500
rf transition probability
26Na, rf transition,
Frequency offset (MHz)
simulation
aim
0
-5
-10
-15
b-decay asymmetry

## Slide 85: Beta-detected NMR
ultra-sensitive real-time NMR with short-lived nuclei
Hyperpolarisation via optical pumping: atomic hyperfine structure
= > up to 100 % of spin polarisation
Resonance detection in b decay asymmetry: property of the weak force
=> Every b particle hitting detectors counted
Result:
NMR spectra possible on 107 active nuclei
Probe nuclei with other NMR properties than stable ones
Real-time observation with time 0 = beam entering sample
B0
-2
-1
0
1
2
-2
-1
0
1
2
-3
3
Atomic magnetic sublevels

## Slide 86: Liquid-NMR chamber
Challenge: maintain liquid samples with high vacuum in polarization section
B-field direction (0.5 T)
+
+
+
+
  Polarized radioactive metal ions/ atoms
Notes: Detector solid angle coverage ~ 10%
100mW CW dye laser 10-15mm in diameter, degree of polarization 20-60%
Spins undergo adiabatic rotation

## Slide 87: b-NMR spectra recording
Same principles as continuous wave NMR
Short-lived I>0 beta-decaying nuclei brought from outside
Resonance: Change in beta decay asymmetry
B0
β particles
β-detectors
b-decay asymmetry
RF Coil
RF
From
J. Croese

## Slide 88: Accurate m of radio-nuclei
26Na relative to stable 23Na
26Na/23Na Larmor
Accurate frequency ratio:
Accurate reference:
Old precise experimental data: Atomic Beam Mag. Res. & NMR
NMR: New coupled cluster calculations of solvated 23Na+
ABMR: New DHF calculations of free Na atom
A. Antusek, Bratislava
m(23Na) /mN

## Slide 89: Experiment at ISOLDE-CERN
magnetic mass
separator
1.4 GeV protons
target
ISOLDE: CERN facility for production and research with radioactive nuclei