## Slide 1: Signal formation in LGAD detectors
Initial Ionization process and Landau distribution in PiN diodes
(bare with me in this step, it is interesting)
Space charge effects during e/h drift
Gain quenching in LGAD
Temporal resolution in LGADs
Landau distribution in LGADs
A novel method to measure LGAD gains
N. Cartiglia
Laboratory Innovative Silicon Sensors
Torino

## Slide 2: Landau distribution in PIN diodes
In each event, the impinging particle creates clusters of charges along its path.
These localized energy deposits follow some unknown “elemental distribution X”.
The sum of the energy deposits is the total energy deposition.
The total energy deposition follows a Landau distribution
Question: which distribution X is such that the sum of random numbers from this distribution is a Landau?
Each local deposition follows an “elemental distribution X”
(to be determined)
The total deposition follows a
Landau distribution
n = number of draws
Suppose: n = thickness in micron
?

## Slide 3: The central limit theorem does not apply
The sum (or average) of a large number of independent and identically distributed random variables, regardless of the original distribution of the data, as the sample size becomes large, will approach a normal (Gaussian) distribution,
Since the resulting distribution is a Landau and not a Gaussian,
the elemental distribution X does not have finite mean and variance.
provided that the variables have a finite mean and variance.

## Slide 4: Stable distributions
For a special class of functions, stable distributions, the sums of random variables result in a distribution of the same type.
the sum of random numbers from a Landau distribution is also distributed as a Landau distribution.
Properties of the distribution obtained by drawing n random numbers from a
The MPV increases proportionally to ln(n)
The FWHM remains constant
How does this compare with the measured results?
The Landau distribution is a stable distributions, therefore:

## Slide 5: The measured Landau distribution in PiN diodes
The MPV scales logarithmically:
This is consistent with the elemental distribution X to be a Landau
The FWHM decreases with thickness:
This is not consistent with the elemental distribution X to be a Landau.
==> Convolution of a Landau with a Gaussian of mean = 0.
The correct choice of the elemental distribution X is the convolution of a Landau with a Gaussian
(approx. of the Vavilov distribution)
Meroli S., Passeri D., Servoli. L. (2011). Energy loss measurement for charged particles in very thin silicon layers. JOURNAL OF INSTRUMENTATION, vol. 6 / 2011

## Slide 6: Starting point
In the WF2, the energy deposition in a sensor of arbitrary thickness is therefore obtained as a sum of deposits chosen randomly from an elemental distribution, the convolution of a Landau Gaussian.
The program correctly reproduces the measured MPV and the FWHM dependence on the sensor thickness.
6
Local deposition follows a LandauGaussian distribution
The total deposition follows a
Landau distribution
WF2 program:
https://www.to.infn.it/~cartigli/Weightfield2/index.html

## Slide 7: LGAD Temporal resolution vs sensor thickness
Data from: "Beam test results of 25 um and 35 um thick UFSD", F. Carnesecchi, S. Strazzi et al, Eur. Phys. J. Plus (2023) 138:99
"Optimization of the gain layer design of Ultra-Fast Silicon Detectors", F. Siviero et al, NIMA 1033 (2022) 166739
Let’s compare the measured temporal resolution of sensors of various thicknesses with the WF2 predictions
This plot reports the resolution due to non-uniform charge deposition; jitter is subtracted.
Problem: the predicted temporal resolution is much worse than the measured resolution.
This discrepancy increases with thickness.
The root of the problem: events in the high tail of the Landau distribution degrades the resolution.
The correct simulation of the initial Landau distribution leads to the wrong prediction of the temporal resolution
?

## Slide 8: Landau distribution and temporal resolution
The temporal resolution is degraded if one energy deposit is much larger than the average.
Thick sensors have worse temporal resolution because it is more likely that at least one energy deposit is much larger.
The events in the Landau tail spoil the temporal resolution.
WF2 Simulated energy deposits
15-micron thick sensor
80-micron thick sensor
Large energy deposits are more likely in thicker sensors

## Slide 9: What are we missing in the simulation?
Space charge effects
Gain saturation

## Slide 10: Space charge effects
Charge density decreases during drift, equalizing the current
(connected with the talk “Finding sharks..” M. Moll)
Electron drift
Longer distribution
WF2 simulation of a charge cloud drifting toward the electrode
With Space charge repulsion, the temporal resolution in WF2 is slightly closer to the measured resolution
y [um]
y [um]
x [um]
x [um]
During the e/h drift, the charge density decreases due to space charge effects

## Slide 11: Gain quenching
n++ electrode
p+ gain implant
LGAD
Efield
-
-
-
-
-
-
-
+
+
+
+
+
+
+
Carriers
Efield
The charge carriers in the gain layer produce a field that is opposite to the LGAD field, lowering the gain.
Due to gain quench, the gain is lower for large charge depositions
Gain quenching acts as a dumper, equalizing the current
The WF2 simulation with Space charge repulsion and gain quench agrees well the measured resolution
With Space charge repulsion and gain quench, the temporal resolution in WF2 is very similar to the measured resolution
The LGAD gain is not constant, it is smaller for large charge clusters

## Slide 12: LGAD signal formation: pictorial rappresentation
n++ electrode
p+ gain implant
Space Charge effects
n++ electrode
p+ gain implant
Initial energy deposition
Electrons drift
Gain Quenching
n++ electrode
p+ gain implant
Holes drift
LGAD signal formation needs to include these three mechanisms:
An initial non-uniform energy deposition obtained as sum of elemental deposits
Space Charge effects during the particle drift.
Gain Quench during multiplication.

## Slide 13: Effect of gain quench on the LGAD Landau distribution
Since the gain is lower for large charge deposits, the gain mechanism distorts the initial Landau distribution, decreasing the Landau high tail.
HPK2 beta measurement
Gain 9, rescaled by 7
Gain 62
Signal [mV]
Distortion
Entries
Initial Landau
Measured Landau
Reduced tail ==> smaller FWHM
Signal [mV]
Gain
Distortion
Entries
Low
High

## Slide 14: Measured LGAD Landau distribution as a function of gain
Gain quenching transforms the initial Landau distribution into a Gaussian distribution
200V
300V
350V
400V
450V
500V
510V
520V
530V
Landau
Gaussian

## Slide 15: LGAD Temporal resolution vs Landau position
What is the temporal resolution as a function of the event position in the Landau?
Data from: Ongoing study, C. Marinuzzi et al
"Optimization of the gain layer design of Ultra-Fast Silicon Detectors", F. Siviero et al, NIMA 1033 (2022) 166739
Landau distribution
Signal (mV)
Entries
MPV
Events in the tail have a worse temporal resolution ( as expected)

## Slide 16: Can we use gain quenching to our advantage?
n++ electrode
p+ gain implant
Higher LGAD
Efield
-
-
-
-
-
-
-
+
+
+
+
+
+
+
Carriers
Efield
n++ electrode
p+ gain implant
Lower
LGAD
Efield
-
-
-
-
-
-
-
+
+
+
+
+
+
+
Carriers
Efield
Gain layers with deeper implant work at lower values of the electric field and the change of the mean free path with Efield is higher.
Therefore, the field generated by the e/h has a more significant impact on Lambda.
Can we exploit this aspect to design LGADs that perform better?
Deep GL
Shallow GL

## Slide 17: Temporal resolution vs gain implant position
(signals with amplitude > 2*MPV in 80-micron thick sensors)
Unfortunately
WF2 predicts that, in our regime of operation, the gain implant depth does not affect the LGAD temporal resolution
gain ~ 16
Jitter = 0 in this study

## Slide 18: Landau method to measure gain
Can we use the distortion of the LGAD Landau to measure the LGAD gain?
Signal [mV]
Entries
# events > 1.5 MPV
# events > MPV
Consider a quantity that is sensitive to the magnitude of the Landau tail, for example
  (# of events >1.5*MPV)/(# of events >MPV)
Up to gain ~ 7-10, the ratio remains similar to that of the PiN Landau
At higher gain, there is a linear dependence from the gain
Self calibrating, no need to know anything about the electronics (it just needs to be linear)

## Slide 19: WF2 control panel
If you use WF2, be aware of these two options

## Slide 20: Summary
The following experimental quantities have been considered and correctly simulated in this study:
The initial energy deposition by a MIP
  The MPV and FWHM dependence upon sensor thickness
The reduction of the Landau tail as a function of the LGAD gain
The LGAD temporal resolution as a function of sensor thickness
The temporal resolution in bins of the Landau distribution
Seemingly uncorrelated effects find an explanation in the shared underlying process of gain quench and space charge repulsion.

## Slide 21: Extra

## Slide 22: WF2 Gain quench simulation
Gain quench increases:
When the gain increases
When the number of incoming electrons increases
Increasing signal charge
n++ electrode
p+ gain implant
LGAD
Efield
-
-
-
-
-
-
-
+
+
+
+
+
+
+
Charge
Efield
Increasing gain

## Slide 23: LGAD Temporal resolution vs Landau position
Events in the tail have a worse time resolution ( as expected)
Data from: Ongoing study, C. Marinuzzi et al
"Optimization of the gain layer design of Ultra-Fast Silicon Detectors", F. Siviero et al, NIMA 1033 (2022) 166739
Landau distribution
Signal (mV)
Entries
MPV

## Slide 24: WF2 prediction: LGAD Temporal resolution vs Landau position
The events in the tail of the distribution contains very large localized energy depositions.
The signal shape is irregular, so the temporal resolution is degraded.
In thicker sensors, the temporal resolution degradation for events in the tail of the Landau distribution is more severe.
This is “simply” because is more likely to have large energy deposits
Landau distribution
Signal (mV)
Entries
MPV

## Slide 25: Additional data on quenching

## Slide 26: LGAD Temporal resolution vs sensor thickness
Let’s compare the measured temporal resolution with the WF2 predictions, including:
Space charge
Gain quench
In the simulation,
Gain quench, making the signal smoother, has a very strong effect on the temporal resolution.
Space charge effects improve slightly the temporal resolution with respect of the initial deposition
Space charge effects, when added to gain quench, degrade slightly the resolution.
Including Gain Quench (and Space Charge effects to a lesser extent) in the simulation brings the predictions much closer to the measured values.
Gain Quench

## Slide 27: Signal formation in LGAD detectors
This contribution examines several PIN Diodes & LGAD properties and searches for the shared underlying physical processes at their root.
Observables:
The shape of the Landau distribution in PiN diodes
  The MPV and FWHM dependence upon the sensor thickness
The shape of the Landau distribution in LGAD as a function of gain
The temporal resolution of LGADs as a function of the sensor thickness
The temporal resolution in bins of the Landau distribution
The Weightfield2 program has been used to validate/confute various hypotheses.
WF2 program:
https://www.to.infn.it/~cartigli/Weightfield2/index.html

## Slide 28: WF2: LGAD Landau distribution as a function of gain
LGAD Landau distribution without gain quench
Gain = 17
Due to gain quench, the tail is reduced
WF2:
WF2 simulation for an 80-micron thick sensors
LGAD Landau distribution with gain quench
Gain = 17
WF2:
Sigma/MPV = 0.23
Sigma/MPV = 0.18
Sigma/MPV can be used to describe the importance of the Landau tail.

## Slide 29: Effect of gain quench on the LGAD Landau distribution
At low gain, the LGAD Landau distribution is compatible with the parametrization of the Landau for PIN diodes
Red: HPK2, beta run, gain 9
PiN prediction (Meroli et al.)

## Slide 30: Measured LGAD Landau distribution as a function of gain
50-micron thick sensors, CERN beam test
TI amplifier (SC board)
“Beam test results of a 16 ps timing system based on ultra-fast silicon detectors”,
N. Cartiglia et al, NIMA 850 (2017) 83 - 88

## Slide 31: Temporal resolution vs gain
Consider the temporal resolution for signals with amplitude > 2*MPV in 80-micron thick sensors. (these events are very irregular, so they are a good testing ground)
As the gain increases, quenching smooths the signal shape more and more, and the resolution improves.
Jitter = 0 in this study

## Slide 32: Properties of the Landau - II
The next step is to connect Landau's mathematical properties and the measured results.
In the following, the number of random numbers n and the sensor thickness play the same role, n = sensor thickness in micron
This will allow us to determine the elemental distribution to build any measured Landau.

## Slide 33: LGAD Landau distribution as a function of gain
Comparison Data - WF2 simulation
With Gain Quench, WF2 reproduces well the evolution of the ratio Sigma/MPV.
Without gain quench, Sigma/MPV is roughly constant, not matching the data.
Simulation without Gain Quench
Gain increases the tail
Simulation with Gain Quench

## Slide 34: Starting point of the WF2 simulation
In the WF2, the energy deposition in a sensor of arbitrary thickness is therefore obtained as a sum of deposits chosen randomly from an elemental distribution, the convolution of a Landau Gaussian.
The program correctly reproduces the measured MPV and the FWHM dependence on the sensor thickness.
In the following slides, the consequences of this step will be examined
34
Local deposition follows a LandauGaussian distribution
The total deposition follows a
Landau distribution
The correct choice of the elemental distribution X is the convolution of a Landau with a Gaussian
==> This distribution is a good approximation of the Vavilov distribution, which is known to reproduce the energy deposits in thin sensors.

## Slide 35: What read-out architecture is a better for LGADs?
These two plots compare the temporal resolution due to non-uniform ionization for a Trans-Impedance (TI) or Charge Sensitive Amplifier (CSA) for two different sensor thicknesses (30-micron and 80-micron).
For signals around the MPV (regular shape), the resolution is the same
In thin sensors (that have relatively uniform signals), the resolution is the same
In the tail of thick sensors (irregular signals), the TI architecture is much better
30-micron
80-micron
Large difference between TI and CSA

## Slide 36: LGAD Read-out architecture