## Slide 1: The SCALE Demonstrator Test
C. Barth, F. Pasdeloup, Y. Leclercq & A. Ballarino on behalf of WP6a
212th TE-TM

## Slide 2: Motivation: SCALE
CERN & Airbus UpNext collaboration:
‘Superconducting Technologies for Future Electric/Hybrid Planes Power Distribution Systems’
Development, construction and test of a superconducting powertrain transmission line SCALE (‘Super-Conductors for Aviation with Low Emissions’)
  rely on technologies of SC-link
  ≈ 7 m flexible, coaxial transmission line with trajectory representative of usage in a plane
  target performance: 0.5 – 1.0 kA in DC @ ≥ 20 K, 250 V – 500 V insulation voltage
  optimize superconductor cable of transmission line for low weight

## Slide 3: Motivation: SCALE
Components & trajectory of the power transmission line:
current leads
short-circuit
transmission line

## Slide 4: Motivation: SCALE
Mock-up of the power transmission line & trajectory:
current leads
aka ‘Fuel Cell’
short-circuit
aka ‘E-motor’
coaxial transmission line with representative trajectory
R = 350 mm
horizontal + vertical bend
horizontal + vertical bend
vertical bend
vertical bend
vertical access
R = 500 mm

## Slide 5: SCALE HTS cable
Based on WP6a HTS cable:
Cu braid as core for stabilization
2 REBCO layers (7 tapes each), separated by Cu buffer layer: 3 kA @ 50 K
Kapton tape layers for el. insulation (2 layers, each 50 % overlap): 10 kV air, 5 kV (gHe)
Optimizations of HTS cable for SCALE:
Coaxial: Kapton el. insulation layers between REBCO tape layers
Low weight: Kevlar rope instead of Cu braid core, multiple Cu tape layers required for electrical & mechanical stabilization (winding direction change between layers)
WP6a
SCALE

## Slide 6: SCALE HTS cable
Upgrade of HTS cabling machine:
Multiple passes needed:  full reel-to-reel operation
  grooves in caterpillar belts
  pulling caterpillar with force limiter
CW & CCW Cu buffer layers:  upgrade of Cu buffer head
  2x Cu tape source spools (CW & CCW), 2x radius measure laser
  stepper motor + rotational torque meter instead of prop. brake  more precise tension control (while stationary & in rotation)
   protect cable

## Slide 7: SCALE demonstrator
Schematic overview:
4x 600A HL-LHC current leads
(2 per polarity)
7m long flexible cryostat: 15 mm ID
ref. temp. sensor
13 mm OD, 284 g/m
cryogenic connection to SM18 ‘Diode’ test station
warm He gas return
SCALE coaxial HTS cable
injection of cold He gas
short-circuit:
aka ‘E-motor’
current injection:
aka ‘Fuel Cell’

## Slide 8: SCALE demonstrator
Schematic overview:
(short-circuit)
cold gHe injection (20 – 65 K)
short-circuit of the 2 coaxial layers
instrumentation feedthrough (IFS)
vacuum pumping port
vacuum volume over-pressure protection
cold gHe bypass
(needed for flow regulation)
capillary for instrumentation
gHe vessel
distance for thermal expansion compensation
temp. sensor for gHe temp. regulation

## Slide 9: SCALE demonstrator
Schematic overview:
(current leads)
4x 600A HL-LHC current leads
current lead cryostat
lead cryostat extension
splice cryostat
RT current connection
warm gHe
return
lower heat exchanger
resistive part
HL-LHC 600A HTS cables
2x HL-LHC 600A HTS cables to coaxial layer splices
ref. temp. sensor

## Slide 10: SCALE demonstrator
Realization:
current leads
short-circuit
current leads
transmission line
transmission line
splices

## Slide 11: SCALE demonstrator
Simplified schematic overview:
gHe temperature:
Oscillations on short-circuit side due to gHe temp. regulation
Splice side temp. (Tref) stable
<1 K temp. gradient along flexible cryostat (@ ≈0.6 g/s)
gHe flow: ≈0.6 g/s

## Slide 12: Test results
Reference temperature of 63 K:

## Slide 13: Test results
Reference temperature of 63 K:
No voltage at 2 kA

## Slide 14: Test results
Reference temperature of 66 K:

## Slide 15: Test results
Reference temperature of 66 K:
Stable at 2 kA
current re-distribution
during plateau
 stable

## Slide 16: Test results
Reference temperature of 70 K:

## Slide 17: Test results
Reference temperature of 70 K:
Unstable at 2 kA
heating
during plateau
 unstable

## Slide 18: Test results
Splice resistance:

## Slide 19: Summary
Successful cold powering test of SCALE demonstrator that by far exceeded the performance targets:
Low cable weight: 284 g/m
Homogenous resistance splice resistances <13 nΩ
63 K reference temperature (temperature of the splices on the current lead side): no voltage on the coaxial HTS cable at 2 kA
66 K reference temperature: ≈0.25 µV/cm on the coaxial cable, stable at 2 kA current plateau (voltage is slowly decreasing due to current re-distribution)
70 K reference temperature: ≈0.9 µV/cm on the coaxial cable after ramp to 2 kA (20 A/s), unstable at 2 kA current plateau (voltage is increasing due to local heating)

## Slide 20: Thank you for your attention
Acknowledgements: TE-MSC-HSD: M.-P. Careil, J. Hurte, J. Mazet, A. Saba, S. Morisi & P. Denis TE-MSC-LSC: A. C. Zurita TE-MSC-CMI: J. B. Deschamps TE-MSC-TM: P. Viret, J. Feuvrier, S. Juberg & F. J. Mangiarotti TE-CRG-ME: O. Pirotte TE-MPE-EP: J. Steckert EN-MME-FS: P. Moyret EN-MME-EDM: R. Betemps BE-CEM-MTA: P. Koziol the collaborators from industrial support