## Slide 1: Chemical and Structural Evolution of Rb2–2xK2xTi2O5 Layered Titanates When Exposed to Ambient Air
Journée UFR de Chimie / UFR de Physique - 2ème édition
15/11/2024
Narimane Meziani, David Bérardan , Méline Parent, Brigitte Leridon, Gwenaelle Rousse and Paola Giura

## Slide 2
General Formula: M₂Ti₂O₅, where M = {alkali element} (e.g., Rb₂Ti₂O₅ or RTO)
Layered Structure
Key Property: Large water absorption capacity
Promising Electrolyte for Supercapacitors
for hydrated Rb₂Ti₂O₅
Equivalent dielectric constant for hydrated Rb₂Ti₂O₅
ɛr
d
C(Farad)= 0A/d
High capacitance
Chemical and Structural Evolution of Layered Rb₂₋₂ₓK₂ₓTi₂O₅ Titanates
Crystal Structure and Properties of M₂Ti₂O₅
SDS. Coutinho, D. Berardan, G. Lang , and al. Solid State Ion. 2021; 364:115630

## Slide 3
Chemical and Structural Evolution of Layered Rb₂₋₂ₓK₂ₓTi₂O₅ Titanates
How does this material evolve when exposed to ambient air and humidity ?

## Slide 4
Chemical and Structural Evolution of Layered Rb₂₋₂ₓK₂ₓTi₂O₅ Titanates
Evolution Cycle of Rb₂Ti₂O₅
Hydration in ambiant air
Reaction with CO2 from air leading to degradation of crystalline compounds, and formation of MHCO3 (RbHCO3)

## Slide 5
Chemical and Structural Evolution of Layered Rb₂₋₂ₓK₂ₓTi₂O₅ Titanates
Evolution Cycle of Rb₂Ti₂O₅
Hydration in ambiant air
Reaction with CO2 from air leading to degradation of crystalline compounds, and formation of MHCO3 (RbHCO3)
380°C

## Slide 6
Chemical and Structural Evolution of Layered Rb₂₋₂ₓK₂ₓTi₂O₅ Titanates
Evolution Cycle of Rb₂Ti₂O₅
Hydration in ambiant air
Reaction with CO2 from air leading to degradation of crystalline compounds, and formation of MHCO3 (RbHCO3)
Thermal treatment at 380°C of the compound exposed to air for 96 hours formation of Rb2CO3
380°C
2RbHCO3 = Rb2CO3 + H2O + CO2

## Slide 7
Chemical and Structural Evolution of Layered Rb₂₋₂ₓK₂ₓTi₂O₅ Titanates
Evolution Cycle of Rb₂Ti₂O₅
Hydration in ambiant air
Reaction with CO2 from air leading to degradation of crystalline compounds, and formation of MHCO3 (RbHCO3)
Thermal treatment at 380°C of the compound exposed to air for 96 hours formation of Rb2CO3
Thermal treatment at 900°C formation of Rb₂Ti₂O₅ (M₂Ti₂O₅).
1st Reaction
900°C
2nd Reaction
Formation of Rb₂Ti₂O₅
2RbHCO3 = Rb2CO3 + H2O + CO2
380°C

## Slide 8
Chemical and Structural Evolution of Layered Rb₂₋₂ₓK₂ₓTi₂O₅ Titanates
Evolution Cycle of Rb₂Ti₂O₅
Hydration in ambiant air
Reaction with CO2 from air leading to degradation of crystalline compounds, and formation of MHCO3 (RbHCO3)
Thermal treatment at 380°C of the compound exposed to air for 96 hours formation of Rb2CO3
Thermal treatment at 900°C formation of Rb₂Ti₂O₅ (M₂Ti₂O₅).
1st Reaction
900°C
2nd Reaction
Formation of Rb₂Ti₂O₅
2RbHCO3 = Rb2CO3 + H2O + CO2
380°C

## Slide 9
Inorg. Chem. 2024, 63, 38, 17513
What if we conduct hydration experiments without CO₂ ?
Chemical and Structural Evolution of Layered Rb₂₋₂ₓK₂ₓTi₂O₅ Titanates
Evolution Cycle of Layered Rb₂₋₂ₓK₂ₓTi₂O₅ Titanates

## Slide 10
What if we conduct hydration experiments without CO₂ ?
Thank you for your attention !
Chemical and Structural Evolution of Layered Rb₂₋₂ₓK₂ₓTi₂O₅ Titanates
Evolution Cycle of Layered Rb₂₋₂ₓK₂ₓTi₂O₅ Titanates
Inorg. Chem. 2024, 63, 38, 17513