## Slide 1: Nanocatalyseurs ultra-modèles à base de ZrO2 pour la réaction d'hydrogénation catalytique du CO2: structure cristalline et réaction en mode operando
UFR de Chimie: Guilhem SIMON, Ahmed NAÏTABDI, Axel Wilson
UFR de Physique: Romain BERNARD, Geoffroy PRÉVOT

## Slide 2: Analyse du projet : diapositive 3
Project plan
Ultra-model Nanocatalysts
ZrO2 ultrathin films grown on Cu2O/Cu(111)
STM image: (100100 nm2)
Putting CO2 to use. Creating value from emission
Model Nanocatalysts
ZrO2 strengths:
Practical Nanocatalysts
Supported Nanoparticles
Design method: Physical
Benchmark and industrial catalysts
Nanopowders
O2 plasma
treatment
Size-selected nanoparticles
Cu(111)
Cu2O/Cu(111)
ZrO2
Design method: Chemical
Gap 1
Gap 2
Size control
Composition
Thermodynamic
Stability
Dual sites:
strong Lewis acidity (Zr+4)
and strong Lewis basicity
(Ovac: Zr3+)
CO2 hydrogenation under realistic reaction conditions
Up to 50 bar @350 °C:
Electronic properties and morphology are thickness dependent
Operando Raman spectroscopy, XPS
Reaction as a function of the thickness
Electronic properties
XRD (Grazing Incidence @Synchrotron
Structures as a function of
the thickness
ZrO2
ZrO2
ZrO2
Raman setup

## Slide 3: Analyse du projet : diapositive 2
Electronic properties and in situ investigations
XPS
High concentration of Zr3+ in thin films
Large accumulation of CO (ZrCO) on thick films
2 ML (Thin)
Cubic
6 ML(Thick)
Monoclinic
After reaction
Before reaction
Tetragonal
Electronic properties are thickness dependent
In situ Raman spectroscopy
Cubic
Reaction conditions: (D2 + CO2)
30 bar @ 300°C
Real time monitoring of the gas phase:
-Reactants
-Reaction products @ 250°C
Catalytic efficiency
Cubic
Monoclinic
Both Cubic and Monoclinic are active for CO2 HR
Cubic: via formates
Monoclinic: via rWGS

## Slide 4: Analyse du projet : diapositive 2
Surface structure: ZrO2/Cu2O/Cu(111)
x
y
z

Surface X-ray diffraction experiments
Scanning tunneling microscopy
reconstruction (25.1 Å x 9.2 Å)