## Slide 1: Novel strategies for the synthesis of efficient ZnO supported Pd-based nanocatalysts Journée UFR de Chimie / UFR de Physique - 2ème édition 15.11.2024.
Andrija Kokanović
Thesis supervisors: dr Slavica Stankic, dr Igor M. Opsenica
Institut des NanoSciences de Paris

## Slide 2
Heterogeneous catalysis – ZnO supported Pd/PdZn nanoparticles.
Gas-phase centered synthesis methodologies.
Novel materials.
Potential environmental remediation and industrial application.
Introduction – context and motivation

## Slide 3
Material
Strategy and approach
Gas-phase synthesis
Gas-phase synthesis of the support + chemical deposition
One step gas-phase synthesis
Catalyst
XRD
Electron microscopy
XPS
FTIR-CO
ICP-QMS
SBET
Thermal annealing
or
Characterization
Application
Conversion of organic pollutants
or
industrially important reactions

## Slide 4
Strategy and approach
Innovative vs conventional synthesis
Ar
O2
Zn pieces
T
T
oxidation
zone
Zn(g)
O2
collection zone (r.t.)
CVS-ZnO
100 nm
CSV-ZnO
400 nm
Pd/CVS-ZnO
100 nm
PdZn/ZnO
Zn(g)
O2
PdCl2, NaBH4, H2O
1) Pd(acac)2, acetone
2) O2, 400 °C
3) H2, 400 °C

## Slide 5
Strategy and approach
Ar
O2
Zn pieces
Pd(acac)2
T1
T2
oxidation
zone
Zn(g)
Pd(X)(g)
O2
collection zone (r.t.)
PdZn-ZnO
100 nm
MOCVS-PdZn-ZnO
One step procedure.
No post synthesis workup.
Induction of morphological changes by thermal annealing.

## Slide 6
Strategy and approach
Ar
O2
Zn pieces
Pd(acac)2
T1
T2
oxidation
zone
Zn(g)
Pd(X)(g)
O2
collection zone (r.t.)
PdNiZn-ZnO
MOCVS-PdNiZn-ZnO
Ni(TMHD)2
Ni(X)(g)
PdZn – 41.5 ° and 43.6 °
NiZn – ~43.5 °

## Slide 7
My results - Pd/CVS-ZnO
1. A. Kokanović, V. Ajdačić, N. T. Jovanović, S. Stankic, I. M. Opsenica, ACS Appl. Nano Mater. 2023, 6, 15820–15828.
100 nm
400 nm
5 nm
ZnO
Pd
0,219 nm
(111)
CVS-ZnO
Pd/CVS-ZnO
XRD
HRTEM

## Slide 8
My results - MOCVS-PdZn-ZnO
2. A. Kokanović, D. Pupavac, S. Chenot, S. Guilet, I. M. Opsenica, S. Stankic, Catal. Sci. Technol. 2024, Advance Article.
100 nm
Zn(s)
Pd(acac)2(s)
250 °C
650 °C
30 mbar, Ar:O2/10:9, 1 h
PdZn (111)
PdZn (200)
MOCVS-PdZn-ZnO
10 nm
2.19 Å
2.81 Å
PdZn (111)
ZnO (100)
Pd 3d5/2
335.0 eV Pd(0)
336.2 eV Pd in PdZn
XRD
HRTEM
XPS

## Slide 9
Innovative approach to heterogeneous catalysts synthesis.
Possibility of increasing catalytic system complexity.
Materials applicable in environmentally friendly and industrially important chemical reactions.
Conclusion

## Slide 10: Thank you for your attention!
I would like to express my gratitude toward my colleagues: Stephane Chenot, Stephane Guilet, Dunja Pupavac, Vladimir Ajdačić, Nataša T. Jovanović;
supervisors: S. Stankic, Igor M. Opsenica;
research groups: Low-dimensional Oxydes (Institut des NanoSciences de Paris, CNRS/Sorbonne Université) and OpsenicaLab (Faculty of Chemistry – University of Belgrade).