## Slide 1
Magnetic compression
Introduction
Switchable adhesion
Fabrication of model magnetic foams
Magnetic elastomer foams as low Poisson’s ratio actuators
for switchable adhesion
Maxime Bès1, Samuel Lamont2, Jean-Claude Mancer1, Ludovic Olanier1, Franck Vernerey2, Artem Kovalenko1
1 Laboratoire Sciences et Ingénierie de la Matière Molle, ESPCI Paris, PSL University, Sorbonne Université, UMR7615-CNRS, F-75005 Paris, France
2 Department of Mechanical Engineering and Material Science & Engineering Program, University of Colorado at Boulder, Boulder, Colorado, USA.
artem.kovalenko@espci.fr
Soft magnetic composites exhibit fast and programmable macroscopic deformations in magnetic fields and are promising for applications in soft untethered robotics or for design of surfaces with switchable adhesion or wetting. In practice, because of incompressible nature of the soft non-porous actuators their compression or elongation are limited, and bending and folding remain preferred actuation modes. Here, we explore the potential of magnetic foams as compressible actuators with low Poisson’s ratio.
Magnetic foam actuators
Conclusions
We fabricated model soft magnetic PDMS foams with open porosity and low Poisson’s ratio.
Magnetically-induced compression is stronger for thicker foams.
We showed a proof-of-concept of a magnetically-triggered adhesive detachment.
Acknowledgments
Magnetic compression modeling
Funding:
ANR MAGELAn
Jérôme Robert (IPCMS), Jérôme Fresnais (Phenix), Etienne Barthel (SIMM), Bruno Bresson (SIMM)
Non-porous magnetic actuators
easy
☹difficult
easy, with no lateral expansion
What determines the strain?
How can we use these actuators?
Kim, Y.; Zhao, X. Chem. Rev. 2022, 122 (5), 5317–5364
Control of porosity
pore
Microstructure characterization
200 µm
Fe microparticles
open
pores
Mechanical properties
Compression curves
Poisson’s ratio
Chart: Position (top to bottom)
| 0 | 5.5555555555555552E-2 | 0.1111111111111111 | 0.16666666666666666 | 0.22222222222222221 | 0.27777777777777779 | 0.33333333333333331 | 0.3888888888888889 | 0.44444444444444442 | 0.5 | 0.55555555555555558 | 0.61111111111111116 | 0.66666666666666663 | 0.72222222222222221 | 0.77777777777777779 | 0.83333333333333337 | 0.88888888888888884 | 0.94444444444444442 | 1
Experiment (DIC) | 1.0093 | 0.99746 | 0.95335 | 0.90367 | 0.88649 | 0.87264 | 0.81332 | 0.73608 | 0.70246 | 0.71526 | 0.72015 | 0.69742 | 0.66156 | 0.62211 | 0.57586 | 0.56898 | 0.56413 | 0.49099 | 0.39358
L0
Δ
Strain field (DIC)
Total strain
ε≈0.6
Increase
ε≈0
Observations:
Macroscopic deformation in a field of a permanent magnet;
The total strain increases with the sample height;
High strain gradient from the top to the bottom of the sample
Cause: gravity-like action of magnetic force (= body force)
See the modeling part for more details…
Flash for a video on foam-magnet interaction
Video
Mechanical equilibrium
Magnetic force
Approximations
H
sample ≈ const (H)
Strain gradient
Effect of L0
optimum
sample height
Working principle
Adhesion tests (Tack)
field on
field off
Magnet
a
d