## Slide 1
The 8th International Conference on MPGDs
Robust photocathodes and spatial resolution studies of
resistive PICOSEC Micromegas precise-timing detectors
Djunes Janssens and Marta Lisowska
On behalf of the PICOSEC Micromegas Collaboration
djunes.janssens@cern.ch
October 15th, 2024

## Slide 2
  To enable the sub-25 ps PICOSEC Micromegas precise-timing detector to perform effectively under the demanding conditions of physics experiments, we are adapting its design to improve robustness.
  Outline:
  Resistive Plane PICOSEC Micromegas
    Single-Channel Prototype
    Increased Readout Granularity for Spatial Resolution
    Multi-Pad Prototype with Vertical Charge Evacuation
  Robust Photocathodes
    DLC
    B4C
    Graphene
  Towards an Applicable Detector
  Conclusion
Introduction
The general progress overview can be found in Yue Meng’s presentation of this morning.

## Slide 3: Resistive plane PICOSEC Micromegas

## Slide 4: Resistive PICOSEC Micromegas
A resistive layer is introduced in both single- and 100-channel readout structures to enhance the detector's robustness while maintaining a timing resolution of under 25 ps. These slightly conductive materials offer:
More stable operation by quenching discharges
Potentially improved position reconstruction through increased signal sharing
J. Bortfeldt et al., NIM A 903 (2018) 317
A. Utrobicic, RD51 Collaboration meeting (14-06-2022)
A. Utrobicic et al., JINST 18 (2023) C07012 [2304.00056].
M. Lisowska et al., JINST 18 (2023) C07018 [2303.18141].

## Slide 5: Resistive PICOSEC Micromegas
J. Bortfeldt et al., NIM A 903 (2018) 317
A. Utrobicic, RD51 Collaboration meeting (14-06-2022)
A. Utrobicic et al., JINST 18 (2023) C07012 [2304.00056].
M. Lisowska et al., JINST 18 (2023) C07018 [2303.18141].
A resistive layer is introduced in both single- and 100-channel readout structures to enhance the detector's robustness while maintaining a timing resolution of under 25 ps. These slightly conductive materials offer:
More stable operation by quenching discharges
Potentially improved position reconstruction through increased signal sharing

## Slide 6: Resistive PICOSEC Micromegas
mimimum for protection
rate capability
  Minimum surface resistivity for timing: D. Janssens’ presentation of yesterday
  D. Janssens, PhD dissertation, https://cds.cern.ch/record/2890572
mimimum for timing
pad’s center
pad’s edge
A surface resistivity of 20 MΩ/□ was chosen to ensure that:
the leading edge of the signal is minimally affected by the delayed component,
the rate capability estimation,
the protection against discharges.
Relative signal amplitude reduction
Induced signal on the edge of a 1 x 1 cm2 pad

## Slide 7: Resistive PICOSEC Micromegas
Simulated amplification drop from Φ = 6 · 105 cm−2s−1 pion beam
Simulated voltage drop for Φ = 6 · 105 cm−2s−1 pion beam
  Minimum surface resistivity for timing: D. Janssens’ presentation of yesterday
  D. Janssens, PhD dissertation, https://cds.cern.ch/record/2890572
mimimum for protection
rate capability
mimimum for timing
A surface resistivity of 20 MΩ/□ was chosen to ensure that:
the leading edge of the signal is minimally affected by the delayed component,
the rate capability estimation,
the protection against discharges.

## Slide 8: Single channel resistive PICOSEC Micromegas
PICOSEC amplifier design: A. Utrobičić, et al., JINST 18 (2023) C07012
Based on the RF pulse amplifier: C. Hoarau, et al., JINST 16 (2021) T04005
Chamber and Micromegas board design: A. Utrobičić, et al., arXiv:2406.05657 [physics.ins-det]
LeCroy WR8104 oscilloscope
RF current amplifier cards
Single-pad prototype design
After production, the timing performance of the resistive single-pad detector for fully contained events was measured using custom-built current amplifiers and a 10 GS/s sampling oscilloscope.
outer board with spring loaded pins
Micromegas board
spacer
radiator with a photocathode
PEEK insert
aluminium vessel
aluminium flange
quartz window
1 inch
radiator with a photocathode
Micromegas board
1 cm

## Slide 9: Single channel resistive PICOSEC Micromegas
This prototype, along with several others, was tested in both the lab and the CERN SPS H4 beamline using 150 GeV/c muons.
By utilizing tracking information from GEMs and timing information from MCP-PMTs, the timing performance could be measured.

## Slide 10: Single channel resistive PICOSEC Micromegas
The detector with 10 mm 𝜙 active area demonstrated equivalent performance compared to a non-resistive prototype, achieving a time resolution of σ = 12.5 ± 1.4 ps.
Signal waveform
Single-pad resistive
MM 20 MΩ/□ + Ti + CsI
σ = 12.5 ± 1.4 ps
Time difference distribution
M. Lisowska, PhD dissertation, (available soon).
D. Janssens, PhD dissertation, https://cds.cern.ch/record/2890572

## Slide 11: Increase readout granularity for spatial resolution
To investigate potential improvements in spatial resolution, two sets of resistive PICOSEC Micromegas prototypes with increased granularity and a 15 mm active area were produced and tested.
19 pads with 3.5 mm pitch
37 pads with 2.2 mm pitch
Backside contact pads
The pads were read out using a SAMPIC waveform TDC, while an MCP-PMT (timing reference) scanned across the active area (self-triggered in coincidence with the reference).

## Slide 12: Increase readout granularity for spatial resolution
For the 3.5 mm readout pad pitch, comparable timing performance was observed on the central pad, despite only having partially contained events, with most charge centered around the particle trajectory.
2D signal amplitude map for 3.5 mm pitch
4 mm
Both timing and spatial resolution are worse for the high granularity readout, most likely due to the smaller signal amplitudes.
acceptance region
µm

## Slide 13: Multi-pad prototype with vertical charge evacuation
mimimum for protection
rate capability
mimimum for timing
The rate capability of resistive MPGDs is highly dependent on the charge evacuation scheme used. Various promising 'fast evacuation' configurations can be found within our community.
To enhance the rate capability of the 10 x 10 cm² resistive multi-pad design, a vertical charge evacuation configuration was developed, in contrast to the previous single DLC layer with horizontal evacuation.
G. Bencivenni, et al., JINST 14 (2019) P05014.
M. Iodice et al., Journal of Physics: Conference Series 1498 (2020) 012028.
M. Iodice et al., JINST 15 (2020) C09043.

## Slide 14: Multi-pad prototype with vertical charge evacuation
Cathode voltage scan for pad # 56
While the observed planarity of the MM board was ~ 15 µm after bulking, thowever, his does not fully explain the magnitude of the non-uniform response observed across the active area.
 Possibly exacerbated by photocathode degradation!
pad 19:
<V> = 91.8 mV
σt = 22,1 ps
pad 12:
<V> = 97.2 mV
σt = 21.5 ps
pad 89:
<V> = 99.3 mV
σt = 19.1 ps
pad 82:
<V> = 104.2 mV
σt = 19.1 ps
pad 56:
<V> = 50.6 mV
σt = 29.1 ps
Measured quantities for 150 GeV/c muons
Mean amplitude for SPE [V]

## Slide 15: Robust photocathodes

## Slide 16: Number of photoelectrons
Right plot and equation: L. Sohl, PhD dissertation, https://universite-paris-saclay.hal.science/tel-03167728/.
Given a particle crossing the radiator, the choice of photocathode affects the number of photoelectrons (PEs) produced, which is determined by its quantum efficiency. This, in turn, influences the time resolution, which depends on:
timing resolution for single PE
number of PEs
timing resolution

## Slide 17: Number of photoelectrons
  SPE PH spectrum
  150 GeV/c muon PH spectrum
  noise spectrum (Gaussian)
signal PH spectrum (Pólya)
amplitude
Charge-sensitive amplifier
pre-trigger
region
The average number of photoelectrons (NPE) is obtained by comparing the pulse heights of single photoelectron (SPE) events, measured with a UV LED, to those from multiple photoelectron measurements using a muon beam.
A photocathode with 3 nm Cr and 18 nm CsI produces over 12 photoelectrons per muon when combined with a 3 mm MgF₂ crystal.
L. Sohl, PhD dissertation, https://universite-paris-saclay.hal.science/tel-03167728/.
M. L. V. Fernandez, summer student seminar, https://indi.to/9RPK3.
M. Lisowska, PhD dissertation, (available soon).

## Slide 18: Alternative Photocathodes to CsI
Ageing studies for CsI
CsI photocathode after air exposure
CsI photocathode damaged by IBF
CsI is highly susceptible to degradation from:
Diamond-Like Carbon (DLC)
Boron Carbide (B4C)
Nanodiamonds
Carbon nano-structures
Graphene
IBF and air exposure observations: L. Sohl, PhD dissertation, https://universite-paris-saclay.hal.science/tel-03167728/.
Air exposure observations: M. Lisowska, PhD dissertation, (available soon).
QE ageing studies: M. Lisowska’s master thesis, https://cds.cern.ch/record/2885929.
humidity from assembly or possible outgassing of materials, e.g., Kapton
ion backflow (IBF)
discharges
To increase robustness, different alternatives to CsI are being investigated:

## Slide 19: DLC as Alternative Photocathodes
DLC photocathodes, ranging in thickness from 1.5 nm to 3.5 nm, were characterized during the test beam measurements.
The detector with a 1.5 nm DLC layer deposited directly on the radiator exhibited a time resolution of σ = 31.9 ± 1.3 ps, while thicker samples showed approximately 4 ps worse resolution.
Single-pad MM 3 mm MgF2
+ 1.5 nm DLC
σ = 31.9 ± 1.3 ps
96.8% efficiency
NPE ≈ 3.0
Pulsed DC magnetron vacuum deposition machine
Surface resistivity as a function of layer thickness
Time difference distribution
X. Wang, et al., arXiv:2406.08712.
M. Lisowska, et al., arXiv:2407.09953 [physics.ins-det].
M. Lisowska, PhD dissertation, (available soon).

## Slide 20: B4C as Alternative Photocathodes
Single-pad MM 3 mm MgF2 + 3 nm Cr + B4C 3 mm
σ = 34.5 ± 1.5 ps
95.4% efficiency
NPE ≈ 3.4
B4C sample in the sputtering machine
C.-C. Lai, ESS
B4C photocathodes deposited at CEA-Saclay and ESS have demonstrated promising results.
A detector with a 9 nm B4C layer and 3 nm Cr resulted in a time resolution of σ = 34.5 ± 1.5 ps, with thicker samples showing slightly worse resolution by up to ~10 ps.
Time difference distribution
M. Lisowska, et al., arXiv:2407.09953 [physics.ins-det].
M. Lisowska, PhD dissertation, (available soon).
L. Sohl, PhD dissertation, https://universite-paris-saclay.hal.science/tel-03167728/.
M. Lisowska, et al., JINST 18 (2023) C07018.

## Slide 21: Graphene as Protective Layer
In studies using graphene as a photocathode, a 2.5–3 nm Ti layer produced a surprisingly large number of PEs.
Adding graphene partially screens the photoelectron (PE) emission from the Ti, with the monolayer (ML) screening approximately 30%, and the bilayer (BL) and trilayer (TL) screening about 50% of the PEs.
VA = 275 V
Cathode voltage scan
Number of photoelectrons per muon crossing
 Graphene could be considered as a protective layer.
More on graphene in MPGDs can be found in G. Orlandini’s MPGD 2022 presention: https://indi.to/rqqnb.

## Slide 22: Towards an applicable detector

## Slide 23: B4C as an Alternative Photocathodes
Single-pad detector with the embedded amplifier
The first measurement combining a single-pad 15 mm resistive Micromegas + DLC photocathode + embedded amplifier in the outer PCB:
 showed stable performance and achieved a time resolution of σ = 31.4 ± 0.6 ps for fully contained events.
Time difference distribution
VC = -530 V
VA = 275 V
973 mbar
Time resolution distribution
M. Lisowska, PhD dissertation, (available soon).

## Slide 24: Summary
  To enable the sub-25 ps PICOSEC Micromegas precise-timing detector to perform effectively under the demanding conditions of physics experiments, we are adapting its design to improve robustness.
  The Resistive Micromegas with a single-pad and 20 MΩ/□ showed equivalent precision to a non-resistive prototype, with time resolution of σ = 12.5 ± 1.4 ps.
  With increasing the granularity of the readout offers the possibility for sub-mm spatial reconstruction, with a pad pitch of 3.5 mm yielding σ = 0.5 mm with minimal timing degradation in the center of the pad.
  The vertical charge evacuation design, while promising (< 20 ps), needs further investigation to work out non-uniform response.
  Intensive studies for alternative photocathodes resulted in achieving a time resolution of σ = 31.9 ± 1.3 ps for DLC, 34.5 ± 1.5 ps for B4C, and 36.3 ± 0.3 ps for Ti + a monolayer of graphene.
  Outlook:
  Robust photocathodes: ageing studies of the DLC and B4C, response to IBF
  Rate-capability: double-layer DLC Micromegas for vertical charge evacuation

## Slide 25: PICOSEC Micromegas Collaboration
PICOSEC micromegas collaboration: https://picosec-mm.web.cern.ch

## Slide 26
  Thank you for your attention!