## Slide 1
What is the status of 2212 wire, cable and coil at Solid Material Solutions?
Alexander Otto
President
Guidance from CERN: The proposed title of your talk is:
“Progress on BSCCO 2212 wire and cable”, with focus on low pressure heat treatment.
HTS Landscape
Objectives
Standard HTS-2212 wire
Low loss HTS-2212
(Wire, Cable. Coil)
Applications
Solid Material Solutions (SMS)
55 Middlesex Street, #205
Chelmsford, MA USA 01863
978-455-7182
Developments
  High Je low loss wire and cable
    Designs
    Property validation
    Scale up and production
  Coils
    Racetrack and solenoid
    Performance
    Production
  Summary and Discussion
Solid Material Solutions (SMS)
Chelmsford, MA USA 01863 978-455-7182
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 2
2212 wire, cable and coils for ac, fast-ramp and some high field applications
  Fast ramp-able with low loss
  Fine filamentary and transposed
  Mechanically robust with inorganic bonding
  High temperature margin
  Normal zone propagation in field with 2212’s shorter distance to Hirr
  Competitive Jc / Je and cost / price
Product development, utilization with sufficient revenue growth
Mission
Address unmet HTS opportunities and demand
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 3: Value Progression for our 2212
-Cost / performance
-Proven designs
-Production volume
Cable
Standard designs for dc use
Low loss, small f for ac use
Wire
Coil
Magnet
Component
End user system
- Large Iop range
- Many designs
-High Jop
-Resists burnout
-Robust
-Affordable
-Easily cooled
-Accelerators
-Instruments
-Motors and generators
-Ion beam therapy
-MRI and NMR
-Fusion reactors…
Drop in forms
Field Boosting?
Our focus
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 4
HTS Conductor features for fast ramp / ac use
See for example Martin Wilson’s book
POWER LOSS
dB/dt - induced voltages drive current in conductive loops
For inter-strand coupling losses …
Short cable pitch
Increased inter-strand resistance
ac dB/dt  V, I
Loop Examples
HTS with these features and high Jop
HOW REDUCE LOSS for 1 T/s to 3,000 T/s?
- Make loops smaller
- Increase resistances in loops
- Reduce number of loops
HOW APPLY TO CONDUCTOR?
- Smaller diameter wire
- Small, unmerged filaments
- Optimally higher resistance between filaments and strands
- Wire axial twist and cabling to short pitch
- Transposed strands in cable
Current, I = V/R
In HTS
~0 resistance to Jc
Inter filament with twist,
Matrix resistance
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 5
∅ 1 mm standard wire
with 990 filaments
2-stack
∅ 0.16 mm low loss wire
With 36 filaments
1-stack
2212 wires with low loss and high Je developed
36 filament mainline wire design
f 0.16 mm, capability to f 0.12 mm
Functionally ~unmerged ~ 10 mm filaments
5 mm and 10 mm short twist pitches
Inter-filament resistance increased ~5X
High Jc / Je (1 – 1.5 kA/mm2 Je at 4.2K, 5T)
Validated by Robinson Research Institute and other facilities
Powder-in-Tube Process
similar to Nb3Sn, MgB2, Bi2223
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 6
Scaled up to produce 3 km piece lengths
~ 3 km
Drawing, take up view
Axial twisting
3 km piece length process for f 0.16 mm low loss wire qualified (we do not sell this wire)
20 km buffer in inventory, 5mm and 10 mm pitch (cables and coils require a lot of wire)
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC
3,000 m

## Slide 7
Jc (T) well behaved and rises ~ 32-fold to ~ 21 kA/mm2 at 4.2K from 63.2 K
Jc (T)
Data from Robinson Research Institute (RRI) for 12.K to 65K and SMS for 4.2 K
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 8
Ic / Je (.01T to 8T, 12.5K – 65K) Generated by RRI
8
Excellent fit equations developed by A. Godeke
For Ic / Je (T, B) by physics analysis of data
Vital for developing good coil designs
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC
Results show:
  - Usefully high Je / Jc levels by 1 atm reaction
  - Accurate scaling from low cost 63 K Ic tests
Data
Calculations by fit equations
Wire test
fixture
to avoid
damage

## Slide 9
Jc Comparisons at similar conditions
9
RRI tested SMS wire Jc(T, 7T) is very close to data for OP-BOST wire Jc(T, 7T)
No overlapping test regime data yet for later, better OP-BOST or SMS wire
Jiang et al. IEEE Trans Appl Supercond. 2019 August ; 29(5): doi:10.1109/TASC.2019.2895197. and Ashley Francis data
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 10
New Jc Advancement Study Yielding Promising Results
10
Lots of headroom for Jc advances in 2212 wires
Testing Jc(B,T) vital – so far only have 63.2K data that was scaled here with RRI based factors
Extensive optimizations as for 1G and 2G not yet done for 2212 (needs $)
Jiang et al. IEEE Trans Appl Supercond. 2019 August ; 29(5): doi:10.1109/TASC.2019.2895197. and Ashley Francis data
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 11
Wire Loss Tested at Ohio State University (OSU)
- Losses reducing features are effective
Mainline
No Twist
Twist, 5 mm pitch
Loss per cycle versus wire diameter
- Loss decreases 4X with half the wire∅ and shorter twist pitch
- Analysis of loss and fabrication factors led to selection of f 0.16 mm baseline
Power loss tests for energized coil ongoing at OSU
    Vital for coil and cooling development, designs and usage regimes
    Plan to apply test method developments to test recently built best mode coils
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 12
Total loss comparison analysis of HTS “Wire” Options
Transport loss data required for coil cooling design, validate magnetization data
2212 loss similar to MgB2 and LTS low loss designs
Perp
field
2212 low loss design
Based on magnetization data and analysis for ~ 150 Hz – long lengths terminated
4 mm 2G
4 mm 1G
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC
~independent of field direction
Wire
Cable
Perfect par field

## Slide 13
Cable designs and cabling line developed
Fine wire cabling line developed
Higher wire count line being built
Baseline cable design
  Rutherford
  16-strand
  extending to higher strand counts
Roll consolidation
Coilability
~55 cables produced
Bare- and coated-wire cable designs
16-strand cables with increasing amounts of roll consolidation
1.45 mm
Typical cable top view
1.5 mm
13
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 14
Coil Development: Wind-and-React
    Racetrack
    Cylindrical
    Saddle
  88 coils produced
  Many with high performance
Coil for subscale 140 kW motor test bed
Numerous test coils fabricated
Integrated into application initiatives
Set up to test
Bonded wind pack
with insulation, reinforcement
63.2K test
Ic with coil field effect removed ~ 19.8 A
11.6 A
Average end to end wire Jc here ~ 70% of RRI wire Jc
63.2K
65K
60K
Field T
.
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 15: Series Fabrication and Ic of Racetrack Pancakes and Stacks 4-stack pancake coil – serially connected
- Series made pancake coils
- Bare / coated wire cables
- To application specification
- Pancake coil I-V data are very similar, Ic ~ 10 A
- Field adjusted Ic ~ 16 A at 63 K, 1 A/wire
- Je(SF, 4.2K) ~ 1.6 kA/mm2 (60% of RRI data)
Low loss
cable jumpers
Coated wire cables
Bare wire cables
Stack of 4 racetrack pancakes
- Very uniform geometry to tight specs
- Strong sintered structure
- For 1 T at > 300 Hz, > 15K
- Front two before Ic tests
- Wrapped are Ic tested
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 16: Stack and Constituent Coil Performance Comparisons 4-stack of racetrack pancake – serially connected – coated and bare wire cables used
No Ic decrease except for self field effects with very uniform coil to coil I-V’s and Ic’s
Coated wire cable 4-stack Ic’s show effect on current sharing
Method developed / validated for pancake stacks, jumpers, tight geometric tolerances
Uncoated wire cable in coil
Coated wire cable in coil
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 17
Low loss 2212 Wind and React Wire-Wound Solenoid Test Coils
Primary Challenges (to enable long wire coils and data)
Many turns and layers without losing build
End reversal of wind and terminations
Thin, effective insulation without sticking
  Coil CE3T
  3600 turns with 0.16 mm f low loss insulated 2212 wire
  Build compromised in last few layers, but reacted anyway
   Good Ic at 63 K, 245 m wire, 10 – 25 K tests planned
  68 mm
  20 mm
245 m
wire
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 18
React-and-wind 2212 Cable and Coil Development
    Bend properties of some SMS cable designs show utility to winding smaller ID coils than expected (to ~ 6 cm)
    Fine wire Rutherford cable is only 1.4X thickness of 1G tape but also has same of better bend properties
With standard 16-strand Rutherford cable
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 19: Long length cable 1 atm reaction and Ic testing Scalable racetrack pancake approach for react-and-wind (> f52 mm) developed
78 turn Ic test mandrel coil with 16-strand cable
35 m cable on reaction mandrel after reaction
Reaction set up
+- 1 degree C plane
Relatively low-cost scalability by adding series modules for much longer cables
f10 cm 28 cm
30 cm module
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 20: Cable End-to-End Ic in Racetrack Coil form
- Constant n value over very large I-V range
- Corrected Ic matches Ic’s of short samples cuts from cable ends
- End-to-end Ic in useful regime – many further optimization options
I-V for 33.5 m cable length
Log – Log I-V
Test format
Racetrack coil
78 turns
Ic at 63.5K
with coil field 5.0 A
field adjusted 15 A
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC
9 mm
26 turns
50 mm f
Epoxy potted
Insert pancake test coil module with reacted cable

## Slide 21
Summary and Discussion Ideas
Summary of SMS 2212 Development Status
High Je, low loss wire designs and their manufacture to 3,000 m piece lengths and by 1 atm reaction
Baseline low-loss 16-strand cable and fabrication with higher strand count
Coil designs and wind and react for them established, and also nascent react and wind capability
Discussion Ideas
Introduction of SMS 2212 into CERN initiatives and its potential usefulness to CERN needs
  Ramp induced loss and field boosting in accelerator dipoles as compared to other HTS
    Filaments to < 10 mm and possibly 6 mm (what are ramp rates and loss requirements?)
    Are all other required loss-reducing features required?
  No need for training, and stability / quench characteristics?
  Mechanical properties – including compression
  Jop / Iop trade offs – optimal cable designs with reinforcement
  Scalability of SMS 2212 conductor tech, plus possibility of reacted 2212 cables for coil winding
  Cost? – similar to PIT in general x a silver / complexity factor ~ 2 x that of high quality NB3Sn in high volume (Also no rare earths)?
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC

## Slide 22
.
Coiling React-and-Wind Set up and Development
Wind stations set up, qualified
5 cm ID pancakes wound, potted, Ic tested with good results
25 cm ID solenoid wound with good results, shipped
(higher field usage require wind and react for 5 cm ID regime)
25 cm ID solenoid coil winding set up for reacted cable
HiTAT at CERN 23 – 24 October 2025 Alexander Otto Solid Material Solutions LLC
Test level wet wind solenoid
Winding set up