## Slide 1: REBCO FReTC Conductors Rutherford-Type Cables
1Massachusetts Institute of Technology,
Plasma Science and Fusion Center,
Cambridge, MA 02139, USA.
Makoto Takayasu1, Luisa Chiesa2, and Vyacheslav Solovyov33
3Brookhaven Technology,
Group, Stony Brook,
NY 11794, USA.
2Tufts University, Mechanical,
Engineering Department,
Medford, MA 02155, USA.
Acknowledgment
This work was partially supported by the U. S. Department of Energy (DOE), Office of Fusion Energy Science under DE-FC02-93ER54186, DE-SC0019905 and DE-SC0024864, and the DOE Office of High Energy Physics under Grant DE-SC0023458.
This work would not be possible without the generous support of Eni and MIT PSFC.
The REBCO/copper cable used for this project was supplied by Dr. A.E. Haight, CTD.
FReTC-CICC
2nd HiTAT Workshop, CERN
October 23 - 24, 2025

## Slide 2
1. REBCO Rutherford-Type Cable Review
2. FReTC
FReTC cabling: Method I
  Method II
3. FReTC Fabrication Device
4. FReTC Characteristics:
Current density, hysteresis loss, and bending
5. Summary
Outline
FReTC

## Slide 3: REBCO Rutherford-Type Cable Review
A. Kario et al., Supercond. Sci. Technol., 26, 085019, 2013.
D. Uglietti et al., Supercond. Sci. Technol., 28, 124005, 2015.
20 strands x 16 tapes, 60 kA at 12 T
Roebel Cable
11 HTS-CroCo strands (each 20 x 6 mm W + 10 x 4 mm W tapes)
W.H. Fietz et al., IEEE Trans. Appl. Supercond, 26, 4800705, 2016.
HTS-CroCo Cable
Y. He et al., IEEE Transactions on Applied Superconductivity, 35, 4800207, 2025.
North China Electric Power University
Quasi-Isotropic strands

## Slide 4
4 mm width copper dummy tape with Nomex Tape.
2.5 mm width Nomex lacing tape
Rutherford-Type Cabling Methods
Tightly winding on a round-edge-former.
Method I
Suitable for wide tapes.
Method II
Winding around a flat round-edge former.
Simple and easy.
12 sub-cables
2 mm-60 tape FReTC
(Flat Round-edge-former Tape Cable)
FReTC
M. Takayasu, Supercond. Sci. Technol., vol. 34, 2021.
M. Takayasu, IEEE Trans. Appl. Supercond., vol. 34, 2024.
Fabrication
Difficult and complicate.
Suitable for large cables.

## Slide 5
Fabricated 400 Tape FReTC
Former: 19.1 mm width, 4.8 mm round edge copper rod
4 mm wide, 1.2 m long 400 tapes (10 sub-cables x 40 tapes).
Former cross-section
Schematic view of FReTC cross-section
Ic = 60 kA (150 A x 400 tapes at 18 T and 20 K)
(Tape Ic = 150 A at 18 T, 20 K)
Cable: 10 sub-cables of 40 Tapes (5 REBCO tapes and 35 copper tapes)*
If all tapes are REBCO,
* The stacked tape dummy cables were previously used for a CTD project (Dr. A.E. Haight).

## Slide 6
3 m FReTC cabling
FReTC Fabrication Device
Stacked REBCO tape subcables
3 m-FReTC cabling machine
DSCN2496

## Slide 7
FReTC Fabrication Device (cont’d)
DSCN2511
pre-winding
Subcable feeders
One full twist-pitch
Rotate a former, and move to the left.
Demo fabrication of a 4 mm wide 400 tapes FReTC for a 60 kA FReTC.
28 mm
Cabling speed : 1 m / 30 min.
Twist-pitch = 250 mm
Fabricated 400 Tape FReTC Top view

## Slide 8
Top view
Top view
Other Fabricated FReTC Samples
BTG 2 mm, 42 tape
BTG 4 mm tape striated to
1 mm filaments
Former cross-section
Former: 12.7 mm wide, 4.8 mm round edge aluminum rod
REBCO tapes: 42 tapes
(14 stacks of 3 taps)
REBCO tapes: 28 tapes
(7 stacks of 4 tapes)
REBCO tapes : BTG exfoliated 4 mm and 2 mm
Twist-pitch = 200 mm
(BTG : Brookhaven Technology Group, Inc.)

## Slide 9
Characteristics of FReTC
Hysteresis Loss
REBCO tapes are parallel to the magnetic field. Therefore, hysteresis loss can be reduced.
TSTC
Tapes are parallel to
former surfaces
Bending characteristics are similar to TSTC conductors.
Modeling
Critical Bending
Critical Twist-Pitch
Lpf is the FReTC twist-pitch.
Field
= the inverse aspect ration

## Slide 10
FReTC Compared with TSTC : Current Density JE
50 kA Cables at 18 T and 20 K
Current Density JE
* Cooling channel space
of 4 mm x 4 mm is added.
REBCO Tape:
4 mm wide, 90 mm thick
Ic = 150 A at 18 T, 20 K)

## Slide 11
Characteristics of FReTC (cont’d)
Transverse forces
Good structure supports against electromagnetic transverse forces.
CICC
(Cable-In-Conduit Conductor)
Direct cooling
Conduction cooling

## Slide 12
Typical Rutherford-type cables
Differences of FReTC from other REBCO Rutherford-type cables
Roebel Cable
16 tapes x 20 strands
FReTC
12 sub-cables
2 mm-60 tape FReTC
Full-size cable fabrication from tape spools.
All tapes face the former surface.

## Slide 13
REBCO Rutherford-type cabling of FReTC could provide cost-effective high-current cables.
- Mechanical support structure against electro-mechanical forces
- Easy fabrication
- Minimizing AC losses
- Design flexibility
- Excellent tape usage
Summary
Need more work

## Slide 14: Thank you for your attention