## Slide 2
High Field Magnet program targets and requirements
Ezio Todesco
Thanks to B. Auchmann for feedback

## Slide 3
11 collaborating institutes
33 workpackages, half from CERN
HFM forum
HFM WG
www.cern.ch/hfm
Five RD lines
  Nb3Sn conductor
  Nb3Sn magnets
  HTS
  Integration & sust.
  Infrastructures
  Plus societal impact

## Slide 4: Main target for HFM R&D
Baseline for FCC-hh: Future Circular Collider with 85 TeV c.o.m. energy (42.5 TeV + 42.5 TeV)
  Baseline is 14 T dipole (operational field) in Nb3Sn, operating at 1.9 K, with 20% loadline margin
  Note that previous baseline was at 16 T and 100 TeV
There is a HTS option
  HTS allows opening the way towards higher field, and (possibly) simpler manufacturing, and (possibly) lower costs
  We keep for HTS the field range from 14 to 20 T giving 85 to 120 TeV
  However, note that synchrotron radiation scales with E4: so 50% more energy gives 4 times more synchrotron radiation
  This radiation falls not on the magnet, but on the beam screen and therefore 20 TeV does not seem compatible with the target of sustainability
    However we keep it as a strategic goal of the program
FCC-hh parameters | Nb3Sn | HTS option
Dipole field (T) | 14.0 | 14-20
Temperature (K) | 1.9 | 4.5-20
Tunnel length (km) | 90.7 | 90.7
Arc length (km) | 76.9 | 76.9
Arc filling factor (adim) | 0.83 | 0.83
Energy c.o.m (TeV) | 85 | 85-120
Non Cu jc 16 T 4.2 K | 1200 | TBD
Loadline margin | 80% | TBD
E. Todesco, “Status and perspectives of high Field magnets for particle accelerators”
Plenary talk at ASC, IEEE TAS 35 (2025) 4002914

## Slide 5: Which margins
The baseline for Nb3Sn is to be at 80% of loadline, corresponding to 20% loadline fraction, 60% current margin, 4.5 K temperature margin and 20 mJ/cm3 enthalpy margin
What about HTS ? Critical current surface slope is very different from Nb3Sn
  20% loadline margin would imply half current margin (30% rather than 60%), double temperature margin (9 K rather than 4.5 K, when operating at 4.5 K) – and physics is quite different !
  Today, we do not have a clear view on the margins required for HTS dipole operation in an accelerator
  The concept of short sample is also more complex than in Nb3Sn

## Slide 6: Sustainability
The importance of the aspect related to the energy consumption of the accelerator has become more and more significant in the past years
  At 85 TeV, half of the consumption is due to the synchrotron radiation (independent of the magnet temperature) and half by the magnet operating at 1.9 K and with losses during ramp assumed to be 10 kJ/m per cycle
First aspect:
  The hysteresis losses during the ramp are a dominant parameter for the accelerator
  Concern about large filaments of HTS, and striation + twist techniques should be studied
Second aspect:
  As operating at 4.5 K with Nb3Sn would give 25-30% saving, in the hypothesis of matching with HTS the budget of hysteresis losses (to be verified) operating at 4.5 K would give similar saving
  Operating at 20 K would give a larger saving, but not beyond 50% since half of the budget is for synchrotron radiation – but cryogenics infrastructure could be simpler
Third aspect
  If we were able to go to 120 TeV, we would be largely dominated by synchrotron radiation losses on the beam screen, independently of the temperature of the magnets

## Slide 7: Sustainability for FCC-hh
Baseline: 90 km, 85 TeV, 14 T, Nb3Sn at 1.9 K with 10 kJ/m
85 TeV, 14 T, 4.5 K Nb3Sn/HTS option with 10 kJ/m
85 TeV, 14 T, 20 K HTS option, with 10 kJ/m
120 TeV, 20 T, 20 K, with 10 kJ/m*
Previous FCC baseline, 100 km, 100 TeV, 16 T, with 10 kJ/m
  20 T stays as a strategic objective for HFM
  Operation at 20 K is interesting, but does not reduces energy consumption by factors 5-10 of the accelerator as it is sometimes stated
  *higher field likely to have larger losses – so this budget could be optimistic
  +M. Benedikt, slide 22, FCC week, 2025 Wien https://indico.cern.ch/event/1408515/contributions/6506636/
Synchrotron radiation
Magnet
<4.0 TWh+
<2.5 TWh+
<2.0 TWh+

## Slide 8: HTS for accelerator dipoles: advancement in the last ten years
Apertures
  C1, C2, C3: 65 mm
  Feather2, cosq: 40 mm
  IHEP: 20 mm
Cables
  Bin5 (BSCCO): Rutherford
  Feather2, Cosq: Roebel
  IHEP, CERN 2025: tapes
  CEA 2025: MI tapes
  C1/C2/C3: CORC ®
Design
  Feather2: aligned block
  C1, C2, C3, Bin5: CCT
  IHEP: racetracks with gap

## Slide 9: Requirements on field quality: a new paradigm ?
Today, an HTS superconductor is available, developed and strongly supported by fusion community, matching the requirements in critical current and with a decreasing cost
  Many colleagues advocate a change of paradigm: rather than developing a conductor targeting accelerator needs, adapt the accelerator to the existing tape
  This option should be carefully explored – but our baseline is developing a high current density twisted cable based on tape
I recall that during the preliminary phases of HL-LHC,
strands with different number of subelements were used
(108/127, 132/169) – at the end the larger filament was
kept since smaller filaments were not needed and were
much more expensive – final optimization should be done
on cost vs performance
Deep Throat advice to R. Redford in All the president’s men (Wildwood Enterprise, 1976)

## Slide 10: Requirements on field
A lot of emphasis on multipoles, but first requirement is on generation of main component
Dipole: stability and reproducibility with 0.001-0.01% (10-100 ppm)
  Residuals are cured by orbit correctors and feedback system
  Note that linearity of TF is not needed, any reproducible effect can be implemented in the control system
      Note that Tevatron dipoles had iron very far from the coil also to minimize the saturation – later experience shows that this is not an issue
    What is critical is the reproducibility
Similar values for the quadrupole
  Residuals are cured by tune correctors and feedback system
see also E. Todesco, «The magnetic model of the LHC at 6.5 TeV», IEEE TAS 26 (2016) 4005707

## Slide 11: Requirements on harmonics
Quadrupolar component in the dipoles during ramp : during EuroCirCol we had a requirement of <20 units
  This is a relevant parameter, since due to high field and large saturation, it would be helpful to release this constraint
  This depends on the conversion from b2 to units of tune, and the precision of correction with tuning magnets
  I personally believe we could try to work with much higher b2 components
  see also D. Tommasini, et al., «The 16 T Dipole Development Program for FCC and HE-LHC», IEEE TAS 29 (2019) 4003109

## Slide 12: Requirements on harmonics
Sextupolar component in the dipoles during ramp: we had a requirement of 20 units
  This is a relevant parameter, since it is related to superconductor hysteresis, and to the magnet design (cross-talk between aperture, partially corrected by iron, but not all along the ramp die to saturation)
  This depends on the conversion from b3 to units of chromaticity, and the precision of chromaticity correction with sextupoles
  In the LHC 1 unit of b3 of 40 units of chroma, we should tune chroma with less than 5 units, and therefore b3 should be corrected with a 0.1 units precision, with a 7 units swing of b3 during ramp this means that our correction has order of 1% error (already very good)
  Feedback system to correct chromaticity are much less effective (on line measurement is not trivial)
So 20 units of b3 looks quite challenging to me

## Slide 13: Conclusions
The possibility of adapting the accelerator (main) magnets to the available REBCO tape should be carefully studied
  This is a change of paradigm, but we should not exclude it a priori
Stability and reproducibility of main components (dipole and quadrupoles) are the fist requirement
  Today requirement is 0.01% to 0.001% (10 to 100 ppm), over a large range of fields (for dipoles from 1 to 14 T) – could we release it ?
Requirements on b2 and b3 are stringent (less than 20 units in absolute value, all along the ramp) and due to the precision of correction via tuning quadrupoles and sectupole correctors
  Could we release it via better correction ? Today is already very precise
More work to be done in close connection to the beam dynamics experts