## Slide 1: REBCO cable and magnet activities in the USA
Luisa Chiesa, Tushar Garg, Vadim Kashikhin, Claudia Navarro, Emily Romancew, Mike Sumption, Venkat Selvamanickam, Makoto Takayasu, Danko van der Laan
With special coordination by Xiaorong Wang (LBNL) and Yuhu Zhai (PPPL)
Speaking on behalf of the contributors above – Lance Cooley

## Slide 2: Cables with “run of the mill” tapes share current effectively
DOE Advanced Mfg. Office grant from 2015 resulted in “variable Ic” cables now tested as a magnet
10 m CORC cable
25 m CORC cable
Weiss, J.D., et al., 2025 Superconductor Science and Technology, 38(8), p.085007. https://doi.org/10.1088/1361-6668/adedbd

## Slide 3
25 K
Current sharing seems to be robust; Inter-layer transitions are evident

## Slide 4
Series-connected low-inductance CORC® insert for 40 T
4
Initial iteration of 40 T solenoid
50 mm bore
12 T LTS outsert (Oxford Instruments – i.e. the present 32 T and 40 T outsert )
Three CORC® coils connected in series
Stainless steel overbanding over each coil
Operating at 11.2 kA at 80 - 88 % of Ic
 | unit | Coil 1 | Coil 2 | Coil 3
cable type |  | A-U x 3 | B-V | C-U / 2
cables per layer |  | 42 | 30 | 25
number of layers |  | 8 | 6 | 3
height | mm | 176.4 | 210 | 212.5
inner radius | mm | 28.0 | 72.3 | 125.3
outer radius (sc) | mm | 63.4 | 115.5 | 151.3
 | kA | 11.2 |  | 
background field | T | 12 |  | 
field contribution | T | 8.65 | 11.0 | 8.33
 | % | 0.88 | 0.86 | 0.79
 | MPa | 39.8 | 6.5 | 0.1
 | MPa | 495 | 624 | 544
 | MPa | 417 | 875 | 1117
 | unit | Coil 1 | Coil 2 | Coil 3
cable type |  | A-U x 3 | B-V | C-U / 2
cables per layer |  | 42 | 30 | 25
number of layers |  | 8 | 6 | 3
height | mm | 176.4 | 210 | 212.5
inner radius | mm | 28.0 | 72.3 | 125.3
outer radius (sc) | mm | 63.4 | 115.5 | 151.3
 | kA | 11.2 |  | 
background field | T | 12 |  | 
field contribution | T | 8.65 | 11.0 | 8.33
 | % | 0.88 | 0.86 | 0.79
 | MPa | 39.8 | 6.5 | 0.1
 | MPa | 495 | 624 | 544
 | MPa | 417 | 875 | 1117
12 T
28 T
+
Slides provided by D. van der Laan

## Slide 5
Demonstration of series-connected CORC® solenoids
5
Series-connection of inner and middle coil
Inner coil wound from three parallel CORC® wires
3 turns per layer, 2 layers
Middle coil based on a single CORC® cable
46 turns, 4 layers (magnet from 2019)
5.14 T at 10 kA
150 mm
60 mm
90 mm
Results
Hall sensors show even current distribution between the three parallel CORC® wires
Peak axial field of 5.14 T reached at 10 kA
Slides provided by D. van der Laan
This will be tested at ASC

## Slide 6
20 T Large-bore CORC® solenoids
6
Initial iterations of large-bore 20 T solenoids
Single CORC® coil
1.2 m bore as needed for the muon collider target and capture solenoids
 | unit | Value
number of layers (r) |  | 13
turns per layer (z) |  | 54
inner radius | m | 0.60
outer radius (sc) | m | 0.80
height | m | 0.837
self inductance | H | 0.556
 | kA | 25.2
max @4.2 K |  | 0.56
 | MPa | 324
 | MPa | 25
 | MPa | 865
 | unit | Value
number of layers (r) |  | 13
turns per layer (z) |  | 54
inner radius | m | 0.60
outer radius (sc) | m | 0.80
height | m | 0.837
self inductance | H | 0.556
 | kA | 25.2
 |  | 0.56
 | MPa | 324
 | MPa | 25
 | MPa | 865
 | unit | Value
number of layers (r) |  | 12
turns per layer (z) |  | 20
inner radius | m | 0.60
outer radius (sc) | m | 1.06
height | m | 0.84
self inductance | H | 0.0746
 | kA | 80.0
max @4.2 K |  | 0.68
 | MPa | 268
 | MPa | 20.4
 | MPa | 732
 | unit | Value
number of layers (r) |  | 12
turns per layer (z) |  | 20
inner radius | m | 0.60
outer radius (sc) | m | 1.06
height | m | 0.84
self inductance | H | 0.0746
 | kA | 80.0
 |  | 0.68
 | MPa | 268
 | MPa | 20.4
 | MPa | 732
Two options are considered
6-around-1 CORC®-CICC
Jacketed CORC® cable
Slides provided by D. van der Laan
Dummy cables
CORC cable

## Slide 7: REBCO Flat Round edge former Tape Cables for High-Current and High-Field Applications
More details see Makoto’s presentation at this workshop
Figure 2: (a) Displacement sum result for single-tape FReTC (RB = 200 mm)
(b) Equivalent strain result at wrapped tape edge
(a)
(b)
REBCO Tape Subcable
Copper tape
Objective: Develop parametric modeling tool for the optimization of Rutherford-type REBCO tape cables
Status
One sub-cable single-twist-pitch parametric model for the FReTC developed in collaboration with M. Takayasu (single tape wrapped around large former shown at left)
  Parametric model can be extended to a multi-tape subcable
Preliminary model results show strain maximum at tape edges
Can the parametric model adapt to cable specifications of interest to accelerator magnets? 200 mm  20 mm bend radius w/ thin REBCO
Modeling effort at Tufts University by Claudia Navarro and Luisa Chiesa

## Slide 8: Collaboration on model development
Figure 1: Helical wrap with 30 mm radius (a) Tape (shell) deformation (b) Sliding distance
FNAL REBCO Tape Cable
Claudia Navarro1, Emily Romancew2, Vadim Kashikhin3
1Tufts University (Medford, MA), 2Northern Illinois University (DeKalb, IL), 3FNAL (Batavia, IL)
Detail: Experimentally validate scalability of parametric modeling tools for FNAL bend radius
Status
Additional model (fig. 1) is under development by E. Romancew for the evaluation of the longitudinal strain in a REBCO layer for a cable under bending
This model aims to include strain effects from tape wrapping (around the former) in the helical cable bending model
Alternative bending approach can be evaluated for geometry generated by the FReTC parametric model (fig. 2)
This alternative model should also be validated by experimental data
Figure 2: (a) FNAL Tape Cable geometry imported from FReTC parametric model into helical wrapping model (b) Mesh for tape wrap
(b)
(a)
Slides provided by Claudia Navarro

## Slide 9: Fermilab / AMPeers / NIU Rutherford-type cable
Figure 5: Setup for critical current testing on straight cable with wrapped REBCO
Slides provided by Emily Romancew

## Slide 10: Develop 6-around-1 cable for magnet applications
Castaneda et al. 2024. “A 6-around-1 Cable Using High-Temperature Superconducting STAR ® Wires for Magnet Applications.” SuST.
A short video on the cabling
Retained ~ 90% of straight-cable Ic in the solenoid coil
Wind into a 6-turn solenoid coil, bend radius 30 mm
Hairpin test
Coil

## Slide 11: Conduction-cooled REBCO dipole magnet “C2” test at OSU
T. Garg et al., Thermal Performance of a Conduction-Cooled CCT Dipole ReBCO Magnet: Cyclic Cool-Down and Thermal Gradient Measurements, 2025, submitted to IEEE TAS.
4-layer CCT dipole magnet using CORC® wires developed by US MDP
Previously tested at 4.2 K
Shipped to OSU for conduction-cooled test
613 mm
75 kg
Cooling Straps
Cooling strap
Power I/O
Joint 3-4
Cooling strap
Joint 1-2
Joint 2-3
Temp. Sens. A-C-B
Cooling strap
Cold copper ring

## Slide 12: Cooldown performance shows the magnet is superconducting
Voltage in each layer with 0.5 A current
Measured temperature during the cooldown
Next step is the powering test
~30 K @ 40 h
sensor C

## Slide 13: PPPL HTS Activities
Y. Zhai and PPPL Team

## Slide 14: R2R Characterization for Commercial HTS Conductors
Develop Continuous HTS Inspection System at PPPL (1) Industrial standard needed for inspecting HTS performance consistency
Winding Improvement with R2R Measurements
Upgraded to Enable Low-T High-B Measurements
Mock-Up 5 DP coils

## Slide 15: Large Bore, Fast Ramp Dummy Load Coil for Cable Qualification
The HTS cable samples (e.g., 11" long) are subjected to a linearly increasing magnetic field with values between 0.2 T/s, 1 T/s or higher (up to 10 T/s).
Test stand has a horizontal clear bore size of 20.55” (522 mm) for cryostat assy
C. Sanabria, SuST, 2024

## Slide 16: Conceptual Design Consideration for 30T for Quantum Physics
Parameters | Coil 1 (Insert) | Coil 2 (Outsert)
Material | REBCO + SUS304 Co-Winding | 
Conductor (Width; Thickness) | 6 mm; 75 um | 4 mm; 60 um
Co-Winding SUS304 Thickness | 50 um | 50 um
Winding ID 2a1; OD 2a2 | 104 mm; 179 mm | 200 mm; 256.3 mm
Coil Height 2b | 120 mm | 148 mm
# of Turns/Double-Pancake | 600 | 512
# of Double-Pancakes | 20 | 37
SUS304 Overband | 2 mm | 5 mm
Transport Current | 254.7 A | 
Conductor Current Density | 566.0 A/mm2 | 1061.3 A/mm2
Winding Pack Current Density | 339.6 A/mm2 | 578.9 A/mm2
Winding Pack Hoop Stress | 581 MPa | 389 MPa
Central Field Contribution | 13.78 T | 16.22 T
Conductor Length Required | 5.4 km | 13.6 km
Stress level critical even without considering screening current.
Will propose the 30-T magnet once we finalize approach to manage the screening-current stress and quench in Phase 2.

## Slide 17: Summary thoughts
Everybody needs thin REBCO
  ACT is presently sourcing conductor with excellent performance from Shanghai SC
  AMPEERS is presently developing 20 µm substrates (or thinner)
  SuperPower is being encouraged to restore 30 µm production with new “HM” additive
Fusion cable activities are behind confidentiality walls
  These cables generally aim for large bend radii, where a few (like FReTC) could be scaled for accelerator magnet purposes
  Fusion is driving transformative expansion of test facilities that will also benefit HEP
HEP-MDP works continuously to help university programs and SBIRs be allied & aligned with the accelerator magnet community’s needs and priorities
University programs and SBIRs are generating and testing new ideas essential to the technology development of REBCO for HEP applications
  Stronger and robust support is critical to sustain a healthy and robust ecosystem