## Slide 1: MIEL (Microscope for the Injection and Emission of Light)
Fabrice Retiere (TRIUMF)
Work done within the PHoton for Astro-particle and Applied Research (PHORWARD) group at TRIUMF
Collaboration with U.Sherbrooke (QC, Canada) for the Photon to Digital Converter

## Slide 2: Setup – phase 1
Built in 2020-2021
Two papers:
  K. Raymond, “Stimulated Secondary Emission of Single Photon Avalanche Diodes”, IEEE TED and https://arxiv.org/abs/2402.09634
  Also J. McLaughlin at al., “Characterisation of SiPM Photon Emission in the Dark”, IEEE TED and https://arxiv.org/abs/2107.13753 but the light transmission is overestimated

## Slide 3: Main motivation of work up to now is external cross-talk
Big issue for “monolithic calorimeter”
  Original work was for the nEXO experiment, a liquid Xenon TPC with scintillation detection
  Especially worrisome for the ones that work at low threshold, dark matter search detectors in liquid Argon and liquid Xenon
The upshots are:
  External cross-talk with Hamamatsu VUV4 MPPC is on the order of 5% in liquid Xenon for with about 50% photo-coverage
  But full simulation package still does not exist. It is a 3 parts problem: emission + transport + (IR) detection
  It may be higher for FBK VUV SiPM
Also an issue for new design especially BSI SiPMs
MIEL provides a wealth of information about the emission part

## Slide 4: Imaging in the dark shows defect locations
Stitched images of 3x3 mn2 SiPM

## Slide 5: The spatial distribution of cross-talk FBK SiPM case (no metallic trenches)
We have not modeled transport within the SiPM in much detail
Anyone interested. It is a very interesting, yet challenging problem

## Slide 6: Spectra at room temperature
FBK VUV=HD3 SiPM
Hamamatsu VUV4

## Slide 7: Modeling optics and assuming isotropic emission, one calculate photon emission
Temperature spread likely due to incorrect
after-pulsing correction
Hamamatsu VUV4 MPPC
FBK VUV-HD3

## Slide 8: Remaining issue with light emission characterization
Experimental
  Objective used has NA=0.45 i.e. incidence angle <26 degrees. Fraction of emitted photon detected estimated to be 10%
  We have another objective with NA=0.78 but still would capture a small fraction of emitted photons.
  There is a question about angular spectrum of light emission
Modeling
  Isotropic assumption may not be correct. Affect yield estimate
  Understanding the parameters that drive light emission may help reduce it
  We have a pseudo-collaboration with ANSYS/Lumerical but short of manpower

## Slide 9: MIEL phase 2 – light injection optimization
Installed LightConversion I-OPA in February 2023
Wavelength tunable from 300 to 2000nm
Pulse width 180fs

## Slide 10: Preliminary results with Sherbrooke PDC
Fire a single SPAD
Best timing resolution about 20ps
The best resolution is not at shortest wavelength
  Indicate low field close to surface
  May be the case for VUV SiPM
Tail in 100ps scale allow studying electric field

## Slide 11: Further studies
Optics is interesting at these short time scale
Can see reflections of window

## Slide 12: Scope of future work
Map timing response and PDE vs wavelength and over-voltage: additional model constraints
Develop Two-photon absorption technique for SPAD
  Allow probing response in 3D
  Has been done at CERN for tracking detector, producing about 10,000 e-
  Working at single photon level is likely trickier
Improve automation for faster turn around and data taking
PIQSCL: New setup at conceptual design stage combining capabilities to characterize single photons and tracking detectors
  I am interested in learning about characterization needs

## Slide 13: Light emission is most likely a worse issue in BSI than FSI SPADs

## Slide 14: The end

## Slide 15: Aim: back-side illuminated SPAD arrays
Versatility
  Visible to IR via thickness control
  Deep UV through Back-side surface processing
    Unconventional Anti-reflective coating: black silicon, graphene, 3D structures
  Non-photon detection
    Minimum ionizing
    keV scale electron (hybrid photo-detector)
    Dark matter
15
CMOS (in 2D or 3D)
Aka. electronics
Molecular bonding
Ultra-thin contact 1-5nm
Thin passivation ~100nm
e-
Low drift field region
Drift field region
Avalanche region
photon
CMOS
Aka. electronics
Molecular bonding
Ultra-thin contact 1-5nm
Thin passivation ~100nm
Low drift field region
Drift field region
Avalanche region
photon
Front Side illumination (ala Sherbrooke)
e-
Back side illumination
e-
h
e-

## Slide 16: Asset: MIEL
FBK Reflected Light and Laser Spot
2D Emission Map
IX-83 Microscope
Vacuum Chamber
SPAD
Cooled X-Y Stage
Vacuum Window
Dichroic Mirror
Emission Filter
Emitted Light
SiPM Surface
Objective
Spectroscopy
Imaging
A)
B)
Diffraction
Grating
Spectrometer and Cryogenically Cooled Camera
300 - 1500nm
Tunable laser

## Slide 17: Assets: simulations
Collaboration with ANSYS – Lumerical
Development of ”Quanta Level Avalanche Diode Simulator” (QLADS)
  Mixing charge carrier and photon transport
  U. Alberta, TRIUMF, U. Victoria
  Current focus on non-photon applications: Minimum Ionizing, keV electrons and dark matter
Example: QLADS used with diffusion region on top for MIP detection (ASGAP concept)

## Slide 18: Light emission to crosstalks
Light emission assumptions:
  At p-n junction – maximum field
  Isotropic
External cross-talk
  Photon escaping the SiPM surface
Internal cross-talk
  Photons being absorbed in a neibhoring SPAD
We measure photons escaping with objective acceptance
Single Photon Avalanche Diode