## Slide 1: The µ-RWELL technology for the IDEA MUON and pre-shower system
G. Bencivenni (*)
On behalf of
Bologna, Ferrara, LNF, Torino WP5-RDFCC
(*) Laboratori Nazionali di Frascati – INFN, Frascati (IT)
2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 2: IDEA apparatus & the μ-RWELL
Tiles: 50x50 cm2 with X-Y readout
Efficiency >98%
Space resolution:
100μm (preshower)
500μm (muon)
Preshower:
130m2, 520 det., 3x105 chs. (0.4 mm strip pitch)
Muon:
1500m2, 6000 det., 5x106 chs., (1.2mm strip pitch)
Requirements
Instrumented surface/FEE
Reliability  high gain
Easy Manufacturing
Mass production → Technology Transfer to Industry
FEE cost reduction → custom made ASIC
GOALS
Pre-shower
Muon
detector
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024
2
Pre-shower: high resolution detector after the magnet to maximize the energy resolution of the dual readout calorimeter and tag π0 and 𝛾.
Muon system: reconstruct and tag the muon using three layers within the iron return yoke, and reconstruct the LLP.

## Slide 3: The μ-RWELL: the layout
The μ-RWELL is a resistive MPGD, with a GEM derived amplification stage, composed of two elements:
  Cathode
  μ-RWELL PCB
  a WELL patterned kapton foil (with Cu-layer on top) acting as amplification stage
  a resisitive DLC film with ρ50÷100 MΩ/□
  a standard readout PCB with pad/strip segmentation
G. Bencivenni et al., The micro-Resistive WELL detector: a compact spark-protected single amplification-stage MPGD, 2015 JINST 10 P02008
3
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 4: The μ-RWELL: principle of operation
Applying a suitable voltage between the top Cu-layer and the DLC the “WELL” acts as a multiplication channel for the ionization produced in the conversion/drift gas gap.
The charge induced on the resistive foil is dispersed with a
time constant, τ  C [M.S. Dixit et al., NIMA 566 (2006) 281]:
the DLC surface resistivity  
the capacitance per unit area, which depends on the distance between the resistive foil and the pad/strip readout plane  t
the dielectric constant of the insulating medium  r
The main effect of the introduction of the resistive stage is the suppression of the transition from streamer to spark, with a consequent reduction of the spark-amplitude
As a drawback, the capability to stand high particle fluxes is reduced, but appropriate grounding schemes of the resistive layer solves this problem (see High-Rate layouts)
4
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 5
The R&D steps
R&D on high-rate layout
2014
2017
2018
2019
2020
2021
2022
2023
2009
R&D start
DRL
R&D on low-rate layout
SRL
SG
2015
2016
TT @ ELTOS
R&D on large area and 2D readout
2024
DLC Resistivity
Readout segmentation + 2D readout
2D readout
TIGER FEE
IDEA slice test: DC+ preshower+ dual_calo+muon
Initial Concept in the 2009, but we really started the R&D on this new MPGD on the 2014
PEP-Groove
PEP-Dot
5
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 6: 1-D Tracking studies
Resistivity scan
With a 0.4 mm strip pitch and 0.15 mm strip width, no effects were observed within this resistivity range.
Additionally, DLC resistivity uniformity is not a critical parameter for spatial resolution.
Increasing the r/out strip pitch will reduce the spatial resolution: X  12pitch
R/O pitch scan
6
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 7: 1-D tracking (inclined tracks)
CC
μTPC
For inclined tracks and/or in presence of high B fields, the charge centroid (CC) method gives a very broad spatial resolution on the anode-strip plane (typical effect observed on MPGDs).
Implementing the μTPC mode[1], using the knowledge of the drift time of the electrons each ionization cluster is projected inside the conversion gap, and the track segment in the gas gap is reconstructed.
[1] introduced for ATLAS MMs by T. Alexopoulos
Combining the CC and μTPC reconstruction (through a wheighted average) a resolution well below 100 μm could be reached over a wide incidence angle range.
M. Giovannetti et al., On the space resolution fo the μ-RWELL, 2020 JINST 16 P08036
1D Strip R/O: 400um pitch
7
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 8: 2-D Tracking layouts
The charge sharing is performed through the capacitive coupling between a stack of layers of pads and the r/out board.
- 1.2 mm X-Y strip pitch.
Reduce the FEE channels, but the total charge is shared between the X & Y r/out.
Operation at lower gas gain wrt the «COMPASS» r/out (X-Y r/out decoupled)
- 0.4 mm (0.8mm) X-Y strip pitch for pre-shower (Muon).
The TOP-readout layout allows to work at low gas gain wrt the «COMPASS» r/out (X-Y r/out decoupled).
- 0.8 mm X-Y strip pitch.
X strips patterned on the TOP of the amplification stage introduces dead zone in the active area.
N.2 u-RWELLs 1D (21D)
u-RWELL - Capacitive Sharing r/out
u-RWELL TOP r/out
Common Cathode
Drift gap
Drift gap
X-strips
Y-strips
Drift gap
Chatode
Y-strips
X-strips
Drift gap
Y-strips
X-strips
Chatode
8
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 9: 2D layouts performance
0.4 mm X-Y strip pitch X = 85µm Y = 121µm
1.2 mm X-Y strip pitch X = 142 µm Y = 147 µm
PROFILE 2D
RESIDUAL 2D
0.8 mm X-Y strip pitch X = 173 µm Y = 250 µm
n.2 1D μ-RWELL [2×1D]
Capacitive Sharing
Top R/O
9
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024
0.4 mm X-Y strip pitch

## Slide 10: 2D layouts performance
2D layouts – 10x10 cm2
2D layouts – 10x10 cm2
2x1D: spatial resolution < 200µm (pitch 0.8 mm), low voltage operating point 520V, efficiency  95%
CS: spatial resolution <200µm (with pitch 1.2 mm), high voltage operating point, ≥ 600V, efficiency  98%
Top r/out: spatial resolution < 200µm (pitch 0.8 mm), low voltage operating point 520V, efficiency 70%
10
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 11: New technology solutions
µ-RGroove  evolution of the top/r-out layout, where the amplification stage is based on «grooves» rather than «wells». This design could facilitate the implementation of the strip readout on the top, without introducing dead-zones ( Z. Yi in RD51).
µ-RWELL with CS layout with pad readout  new design in which the readout PCB is segmented into pads instead of strips. This choice allows for collecting all the charge on a single readout electrode with an increase of FFE channels (30%). With a pad size of  1 cm², a spatial resolution of  300 µm has been achieved (M. Iodice in RD51).
GEM + µ-RWELL with CS layout with strip/pad readout  a hybrid design featuring a GEM pre-amplification stage to lower the operating point, greatly enhancing detector stability while maintaining high spatial performance with millimeter strip-pitches
M. Iodice
2D-readout (XY) μRGroove
X strips
Y strips
Z. Yi
Drift Gap: 6mm
Transfer Gap: 3mm
Cathode
11
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 12: GEM + µ-RWELL
60k
3 different gains for the μ-RWELL
3 different detectors
μ-RWELL gain @ 3500
μ-RWELL 3500
μ-RWELL 2000
μ-RWELL 1000
A very stable detector: it doesn’t show any hint of instabilities even at a gain of 60k.
We stopped because the FEE saturates.
GEM gain
@ 450V ≈ 20
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 13: Tracking technologies comparison
13
Pre-shower
Muon
well below 10 µm
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 14
Technology Transfer to Industry
14
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 15: Detector Manufacturing & TT
The μ-RWELL_PCB is a rigid-flex PCB based on SBU technology, that is compatible with standard industrial processes.
The ELTOS is the industrial partner involved in the manufacturing of the µ-RWELL.
The ELTOS SpA was founded in 1980 in Arezzo, Italy.
The Company has a large experience in the construction of MPGDs, including technologies such as Thick-GEM (THGEM) and MicroMegas.
The involvement of a private industry in this R&D opens the way for the use of μ-RWELL technology across various fields of applications.
15
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 16: Detector Manufacturing flow chart
LAYOUT design
DLC foil production
Final detector
manufacturing
Feedback from tests
PCB production
16
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 17: Detector manufacturing steps
3
4
5- 6
1
7
0
Step 0 – Detector PCB design @ LNF
Step 1 – CERN_INFN DLC (C.I.D) sputtering machine installed @ CERN
  In operation since Nov. 2022
  Production by LNF-INFN technical crew
Step 2 – Producing readout PCB by ELTOS
  pad/strip readout
Step 3 – DLC patterning by ELTOS
  photo-resist → patterning with BRUSHING-machine
Step 4 – DLC foil gluing on PCB by ELTOS
  Large press available, up to 16 PCBs workable simultaneously
Step 5 – Top copper patterning by CERN
  Cu amplification holes image and HV connections by Cu etching
Step 6 – Amplification stage patterning by CERN
    PI etching → amplification-holes
Step 7 – Electrical cleaning and detector closure @ CERN
17
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 18: DLC sputtering
The graphite target
The three external cathodes
220 +/- 30 MOHm/sq
The CID (CERN-INFN-DLC) sputtering machine, a joint project between CERN and INFN, is used for preparing the base material of the detector. The potential of the DLC sputtering machine is:
Flexible substrates up to 1.7×0.6m2
Rigid substrates up to 0.2×0.6m2
In 2023, the activity on CID focused on the tuning of the machine on small foils: good results in terms of reproducibility and uniformity.
In 2024, the challenge has been the sputtering of large foils:
DLC+Cu sputtering on 0.8×0.6m2 successfully done (May/June 2024)
DLC on 1.7×0.6m2 large 0/50/0 Apical foils successfully done (June 2024)
DLC on 1.7×0.6m2 large 5/50/0 Apical foils still to be done (July 2024)
C.I.D.
18
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 19: Electrical Hot Cleaning
The 16 co-produced prototypes have been extensively tested with X-rays:
15/16 are fine
1/16 needs to be re-cleaned
Production yield > 93%
At the end of the manufacturing process at CERN, a conditioning procedure is performed:
Standard PCB washing
Electrical cleaning in dry air (90°C in an oven) from 300 V to 700 V (each step with current < 1 nA)
Detector closure and final test at 600 V in ambient air
@ CERN
@ LNF
Pilot co-production test
19
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 20: Co-production pilot results
Characterized with X-ray gun → Gas gain measurement
16 co-produced protos have been delivered and tested
10/16 (LNF) + 5/16 (CERN) are fine
1/16 should be re-cleaned
20
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 21: Max-gain vs resistivity
16 co-produced protos have been delivered and tested
10/16 (LNF) + 5/16 (CERN) are fine
1/16 should be re-cleaned
The maximum gain is larger for  ≥ 40 MOhm/square
21
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 22: Max-gain: large size vs small size
CS_01 13 MOhm/sq, area 46x38 cm2
M2R1 260 MOhm/sq, area 30x25 cm2
22
For large-size detectors, the max-gain increases with the DLC resistivity, although, compared to the small-size detectors, the gain curve for the larger size is shifted towards lower values.
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 23
Summary
The μ-RWELL is a well-established technology with excellent performance.
Several 2D readout layouts have been tested, demonstrating spatial resolution up to 100 µm over a large particle incidence angle range (0°- 45°).
New layouts to improve stability, maximize gain, and enhance overall detector performance are under study.
A significant effort is being made to well define and simplify the manufacturing process and facilitate the technology transfer to industry.
The DLC sputtering process — a crucial manufacturing step— is now fully under our control.
23
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 24
MANY THANKS
24
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 25: SPARE SLIDES

## Slide 26: References
26
G. Bencivenni et al., The micro-Resistive WELL detector: a compact spark-protected single amplification-stage MPGD, 2015 JINST 10 P02008
G. Bencivenni et al., The μ-RWEL detector, 2017 JINST 12 C06027
G. Bencivenni et al., Performance of μ-RWELL detector vs resistivity of the resistive stage, Nucl. Instrum. Meth. A 886 (2018) 36.
G. Bencivenni et al., The μ-RWELL layouts for high particle rate, 2019 JINST 14 P05014
G. Bencivenni et al., On the space resolution of the μ-RWELL, 2020 JINST 16 P08036
A.Ochi et al., Carbon sputtering Technology for MPDG detectors, PoS(TIPP2014)351 (2014)..
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 27: Front end electronics: TIGER
Readout chain
The full readout chain is well known.
A complete setup is under deployment in Beijing for the BESIII CGEM-IT where a cosmic ray data taking is ongoing since Dec. 2019
TIGER chip features
64 channels
Event rate 100 kHz/ch
Input dynamic range up to 50 fC
Time resolution < 5 ns
ENC < 2000 e- rms with 100 pF input capacitance
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024
27

## Slide 28
WP5 2024 – Front-end electronics
Detector under test:
Active area = 400x50 mm2
Resistivity = 80 MΩ/□
Strip pitch = 0.4-1.6 mm
Strip width = 0.15 mm
1D readout
The data taking consisted of HV scan, Drift scan and Thr. scan, with Ar:CO2:CF4
Data analysis is ongoing, and will be the task of the next months
charge [fQ]
charge [fQ]
time [ns]
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024
28

## Slide 29
Pitch scan comparison TIGER - APV
Similar results are obtained with TIGER electronics and APV, even though small differences are present in the two setups (noise, threshold): 1-2 fC with APV and 2-4 fC with TIGER. The grounding scheme must be improved in future setups. A spatial resolution of 100 µm is achieved with a 0.4 mm strip pitch, a shift between the efficiency plateaus of 0.4 mm and 0.8 mm pitch is observed, as expected (due to larger noise on the 0.8 mm detector)
WP5 2024 – Front-end electronics
APV
TIGER
TIGER
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024
29

## Slide 30
Testing CF4-free gas mixtures
The gas mixtures based on CF4 are effective for fast electron drift but are not considered eco-friendly.
Alternatives to CF4 are needed. Here, we compare the performance of a μ-RWELL using Ar:CO2 (70/30) and Ar:CO2:CF4 (45:15:40). A shift in the working point of approximately 50-100V is observed due to the different Argon ratios, along with a reduction in the plateau width of about 50V.
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024
30

## Slide 31
Comparing the time performance of the two gas mixtures:
12 ns is achieved with Ar with Ar:CO2
7.8 ns is achieved with Ar:CO2:CF4
The contribution of the electronics (approximately 2 ns) and time-walk are included.
Preliminary
Preliminary
Testing CF4-free gas mixtures
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024
31

## Slide 32: Spot Effect for SRL – Manufacturer plot
From the mathematical model of the resistive stage of a μ-RWELL:
1. detectors with same size but different resistivity exhibit a rate capability scaling as the inverse of their resistivity.
2. for the SRL, increasing the active area from 10x10 cm2 to 50x50 cm2 the rate capability should go down few kHz/cm2
3. By using a DLC ground sectoring every 10 cm, large (50x50cm2) detectors could achieve rate capability up to 100kHz/cm2 (with X-ray)
10x10 cm2
× 1/3
50x50 cm2
Different primary ionization ⇒
Rate Cap.m.i.p. = 3×Rate Cap.X-ray
32
G. Bencivenni, LNF-INFN,

## Slide 33: Irradiation test of DLC and μ-RWELL
GIF++ - Full area, Flux ~ 200 kHz/cm2
PSI-1, beam spot ~ 9 cm2
Φ ~ 10 MHz/cm2
X-Ray gun- spot 50 cm2
Φ ~ 700 kHz/cm2
90mC/cm2
125mC/cm2
175mC/cm2
500mC/cm2
600mC/cm2
μ-RWELL DETECTORS
Bare DLC foils
DLC foils: monitoring of the resistivity of two foils under x-ray irradiation.
μ-RWELL detectors: prototypes irradiated with different radiation.
33
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 34: μ-RWELL + GEM
L. Shekhtman, Nuclear Inst. and Methods in Physics Research, A 936 (2019) 401–404
Drift Gap: Shekhtman 3mm – LNF+Roma2 6mm
Transfer Gap: Shekhtman 3mm – LNF+Roma2 3mm
Cathode
Developed for CMD3 upgrade disks (4 sectors 50×50cm2)
The GEM must be stretched: sizes larger than 50×50cm2 could be critical (depending on the gas gaps size).
34
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 35: μ-RWELL + GEM: gas gain
G~2000
G~60000
μ-RWELL + GEM
μ-RWELL
L. Shekhtman, Nuclear Inst. and Methods in Physics Research, A 936 (2019) 401–404
35
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 36: Low Mass μ-RWELL
36
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 37: Technology spread
In the last years there has been a significant spread of the technology among several research groups working on Nuclear and Sub-Nuclear experiments
CLAS12 @ JLAB (USA): the upgrade of the muon spectrometer
EPIC @EIC (BNL - USA): endcap tracker disks based on a hybrid GEMtechnology
X17 @ n_TOF EAR2 (CERN):TPC with a amplification stage, for the detection of the X17 boson
TACTIC @ YORK Univ. (UK): radial TPC for detection of nuclear reactions with astrophysical significance
Muon collider: R&D for a digital hadron calorimeter
CMD3 (RU): GEM+ RWELL disk for the upgrade of the tracking system
UKRI (UK): thermal neutron detection with pressurized 3He-based gas mixtures
3
4
7
5
1
6
2
37
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 38: High-rate layouts evolution
Extensive R&D has been performed to optimize the DLC grounding, enabling the detector to withstand up to 1MHz/cm2
Single Resistive Layer
Single DLC layer with edge conductive line
2-D current evacuation
rate capability < 100 kHz/cm2
Easy for industry
Two stacked resistive layers with a double matrix of conductive vias
3-D current evacuation
Rate capability > 10MHz/cm2
Complex manufacturing not easily engineered
Double Resistive Layer
Single DLC layer
2-D current evacuation through conductive grid on the DLC layer
rate capability > 10MHz/cm2
Easily engineered, BUT complex Cu+DLC sputtering/alignment
Silver Grid
Single DLC layer
2-D current evacuation: conductive grid by etching from the top Cu, through the kapton foil down to the DLC
No grid alignment issues, scalable to large size – large dead zone (>15%)
Easily engineered, because based on SBU technology
PEP Groove (Patterning – Etching -Plating)
38
2014 - 2016
2017
2018 - 2020
2021/22
G. Bencivenni et al., The μ-RWELL layouts for high particle rate, 2019 JINST 14 P05014
38
G. Bencivenni, LNF-INFN

## Slide 39: High-rate layouts: PEP layouts comparison
2022
2023
PEP-Groove:
DLC grounding through conductive groove to ground line
Pad R/O = 9×9mm2
Grounding:
- Groove pitch = 9mm
- width = 1.1mm
→ 84% geometric acceptance
PEP-DOT:
DLC grounding through conductive dots
connecting the DLC with pad r/outs
Pad R/O = 9×9mm2
Grounding:
- Dot pitch = 9mm
- dot rim = 1.3mm
→ 97% geometric acceptance
DOCA 0.48 mm
Dead area 1.1 mm
Cu 0.142 mm
GND 0.35 mm
0.23 mm
Dead area 1.305 mm
Cu 0.094 mm
GND 0.767 mm
0.175 mm
DOCA 0.535 mm
DOT  plated blind vias
39
G. Bencivenni, LNF-INFN,

## Slide 40: Groove vs DOT (X-ray characterization)
2022
2023
PEP-Groove layout
PEP-DOT layout
Both layouts exhibit satisfactory performance:
gas gain up to 104
rate capability (@ 90% gain drop) > 10 MHz/cm2 , measured with different irradiation spot size.
40
G. Bencivenni, LNF-INFN,

## Slide 41: Groove vs DOT (test beam characterization)
PEP-Groove layout
PEP-Dot layout
DOT
Groove
DOT
Groove
APV25 based Fee
41
G. Bencivenni, LNF-INFN,

## Slide 42: PEP DOT – time performance (preliminary)
DOT layout
σt ~7ns
CF4 gas mixture
Thr = 6.5 fC
HV = 620 V
Gas Gain = 6000
TB-2023 at H8C with preliminary version of the FATIC chip (developed by Bari Group) in the framework of the R&D for the LHCb-Muon upgrade. A new test beam foreseen next Nov. ‘24 with an updated version of the ASIC, aiming to reduce the FEE thr down 3 – 3.5 fC
FATIC based Fee
42
G. Bencivenni, LNF-INFN,

## Slide 43: Detector washing and electrical cleaning
At LNF, we are installing a detector washing station with a stainless-steel tank and a high-pressure car-washing machine using deionized water.
After washing, the detector is placed in an oven at 90°C. After 24 hours, it is gradually powered by increasing voltage from 300V to 680V, following Rui's guidelines.
43
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 44: The DOCA
Cross-section of a μ-RWELL with a conductive line on the DLC (High-Rate scheme).
The concept of DOCA (Distance-Of-Closest-Approach) before discharge is fundamental for the stability of the detector.
The DOCA is defined as the distance between the edges of the conductive lines and its closest amplification hole.
The DOCA (before discharge) as a function of the DLC resistivity, for different voltages.
The study has been performed with a custom tool, with two thin conductive movable tips.
A study born with
the SG μ-RWELL
44
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024

## Slide 45: Prepreg thickness optimization
28µm thick prepreg maximize both the amplitude of the signal induced on the pad readout, and S/N ratio (measurement done with APV25)
45
G. Bencivenni, LNF-INFN – 2nd FCC Italy-France Workshop, Venezia 4th Nov 2024