## Slide 1: Nb3Sn High Field Magnet (HFM) activities at Saclay
2nd FCC Italy & France Workshop
E. Rochepault, V. Calvelli, G. Campagna, M. Durante, H. Felice, J. Faucheux, T. Guillo, G. Lenoir, G. Minier, S. Perraud, Y. Perron, F. Rondeaux - CEA
J.C. Perez - CERN

## Slide 2: Development Plan towards 16 T Nb3Sn Dipoles
16 T
demo
12-14 T demo
Subscales
Powered samples
Non-powered samples
F2D2
SMC
R2D2

## Slide 3: Non-Powered samples
0

## Slide 4: Magnet scale - Subscale dipole
Characterize the mechanical behavior of Nb3Sn coils in their structure
coil segment
Cool-down to 77K
Instrumented coil segment
Mechanical loading in a structure
Courtesy of E. Rochepault and G. Campagna

## Slide 5: Cable scale - 10-stack campain
Campain performed by M. Durante in 2000
Restarted in 2022
Objective
  Independent test
  Validated on old conductor (FRESCA2)
  Test of all new conductor for HFM program
R&D investigation
  Characterization of mechanical behavior (strain rate, hold, unloadings and cyclic behavior)
  Investigation of damage (impregnation matrix and conductors)
  Validation of mechanical models
Adapted from S. Perraud

## Slide 6: Strand and sub-element characterization
Tensile test on strands at RT and 77 K
  Data for the identification and the validation of mechanical models
  Investigation of mechanical behavior of strands (strain rate, hold, cyclic behavior)
Nano-indentation at RT
  Local elastic modulus and nano-hardness
Perspectives
  Transverse tests on strands
  Nano-indentation at cryogenic temperatures
  Micro and nano-mechanical testing
Test of a Nb3Sn strand
Clamping setup
Inner part cryostat
Outer part cryostat
@CEA Paris-Saclay
Nano-indentation in Nb3Sn phase of a PIT strand [Lenoir 17]

## Slide 7: Cable scale - Mesh Generator

## Slide 8: Strand scale - Mesh Generator
60/91
60/91
162/169
162/169
Micrographies from S. Hopkins and C. Sanabria
Numerical models from Y. Perron

## Slide 9: Thermomechanical behavior during HT
Model
Experiment
Subelement
Filament
Filament
Work performed during PhD of
M. Abdel-Hafiz @ CEA/LMPS, Univ. Paris-Saclay
Subelement
1st diffusion stage
2nd diffusion stage

## Slide 10: Powered samples
1

## Slide 11: deBOnding eXperiment n°1 - deBOX1
New instrumentation: two pick-up coils and a 7 kN load cell for cryogenic use
Twente sample holder : 11 T background, 100 kA transformer, up to 200 MPa compression
PhD Thesis Guillaume Campagna

## Slide 12: SMC-11T
2

## Slide 13: SMC-CEA#101
SMC-CEA #101 fabricated at Saclay in 2021
Assembled and tested at CERN in 2022
95 % SS @ 4.2 K
No sign of mechanical degradation or loss of pre-stress

## Slide 14: SMC-CEA#102
Introduction of the CTD flexibilizer
2 shortcuts detected after impregnation
repaired, electrical tests passed !
Assembled and tested at CERN in 2024
99 % SS @ 4.2 K
No sign of mechanical degradation or loss of pre-stress

## Slide 15: R2D2
3

## Slide 16: Conductor production and qualification
2 Nb3Sn RRP conductors for grading
Same cables for all magnets
Strand characterization @ CERN
Cable production @ CERN
Cable and strand characterization @ Saclay
Parameter | Unit | HF cable | LF cable
Strand type |  | DEM-1.1 | DEM-0.7
Strand layout |  | RRP® 162/169 | RRP® 60/91
Strand diameter | mm | 1.1 | 0.7
Number of strands |  | 21 | 34
Cable mid-thickness | mm | 1.969 ± 0.010 | 1.253 ± 0.010
Cable width | mm | 12.579 ± 0.050 | 12.579 ± 0.050
Pitch | mm | 84 ± 3 | 79 ± 3
Core |  | No core | No core
LF
HF
Cocascope 3D FEM
LF
HF

## Slide 17: Overview of the R2D2 design
CEA conceptual design validated by an external committee
Fabrication, assembly and pre-stress at Saclay
Tests at cold at CERN
Main goal: demonstrate feasibility of grading
  Winding two cables on top of each other
  Heat treating two different cables together
  Jonctions of the 2 cables  1st option: external Nb3Sn-NbTi joints
Aperture | None
Outer diameter | 480 mm
Structure length | 2.0 m
Nominal central field | 11.1 T
Ultimate central field | 12.0 T
Nominal peak field | 12.7 T
Ultimate peak field | 13.7 T
R2D2 = Research Racetrack Dipole Demonstrator

## Slide 18: Fabrication of R2D2 Nb3Sn coil CR01
CR01:
Winding
Heat treatment
Junctions
Impregnation
Electrical shortcut, identified
CR02:
Winding
Heat treatment pending

## Slide 19: R2D2 structure procurement
Shell segments received at CERN
Structure components (yoke, pads, rods, endplates)
Machining ongoing
Delivery expected ~November
Connection box:
    3D design finalized
    Mockup ongoing
Magnet schedule :
  Dummy assembly at Saclay to validate the mechanical behavior of the structure  Q4 2024
  Selection of the 2 best coils for assembly  Q1 2025
  Delivery at CERN for cold tests  mid-2025

## Slide 20: FD/F2D2
4

## Slide 21: F2D2 16T demonstrator magnet
Conceptual design stage
Fabrication, assembly and pre-stress at Saclay
Tests at cold at CERN
Main goal: demonstrate all technologies
  Representative of high field magnets: grading, joints, flared-ends, high field and high stress
  Representative of accelerator magnets: 50 mm bore, field quality
Aperture | 50 mm
Outer diameter | 650 mm
Structure length | 2.0 m
Nominal central field | 15.5 T
SS central field | 17.8 T
Nominal peak field | 16.2 T
SS peak field | 18.6 T
F2D2 = Future Flared Dipole Demonstrator

## Slide 22: FD 14T demonstrator magnet
Conceptual design stage
Fabrication, assembly and pre-stress at Saclay
Tests at cold at CERN
Main goal: demonstrate key technologies
  Representative of high field magnets: grading, joints, flared-ends, high field and high stress
  Some simplifications: 1 type of coils, no bore
Aperture | None
Outer diameter | 650 mm
Structure length | 2.0 m
Nominal central field | 14.0 T
SS central field | 17.2 T
Nominal peak field | 14.7 T
SS peak field | 17.9 T
FD = Flared Dipole

## Slide 23: Conclusion
Non-powered samples
Characterization of materials
Modelling activities
Powered samples
Behavior of Nb3Sn cables at low or no pre-stress
Behavior of HFM Nb3Sn cables under stress
Short Model coil SMC :
2 coils manufactured at Saclay: successful tests!
Development of fabrication processes, infrastructure, experience
Demonstrator magnet R2D2
 Proof of concept of the grading technologies
Coil fabrication ongoing
Structure components being machined
Demonstrator magnet F2D2
 Design of a 14+ T accelerator-type magnet
FD: 14+ T dipole as an intermediate assembly to validate the concepts

## Slide 25: Backup slides

## Slide 26: CEA plan towards 20 T HTS dipoles
Phase 1 2023-2025:
Racetrack MI
Phase 2 :
magnet MI 16 T+
« EuCARD V2 »
Phase 3 :
« EuCARD V3 »
MI cold bore 16 T+
magnet
Ongoing Project
Phase one objectives :
Adapt and validate the numerical tools for electromagnetic + thermal + quench models
Characterize specific parameters of MI windings (Turn-to-turn thermal conduction…)
Develop the technologies from winding to assembly including electrical connections
Evaluate the options of conduction cooled dipole
Fabricate and test one racetrack coil for models benchmark
Courtesy T. Lécrevisse