## Slide 1
LOW SEY COATINGS
Pedro Costa Pinto and Mauro Taborelli
TE-VSC-SCC
Velo workshop 28.11.2024

## Slide 2
The secondary electron yield
Low SEY with Non Evaporable Getter coatings
Low SEY with amorphous carbon coatings

## Slide 3
The secondary electron yield: SEY
number of emitted electrons (secondary)
number of impinging electrons (primary)
δmax or SEYmax = maximum value as a function of primary energy
Emax = primary energy of the maximum
secondaries
Primary e-
N
0 500 1000 1500 2000 2500 3000
Primary Energy [eV]
2.5
0.5
2.3
2.1
1.9
1.7
1.5
1.3
1.1
0.9
0.7
Copper as rec.
Emax
δmax
SEY
N.Hilleret
The electrons in that energy range escape from less than 20 nm: SEY depends on surface properties
SEY=

## Slide 4
The NEG TiZrV can act as a pump, but when activated it has also a low SEY
Operation of the getter:
Once saturated, or exposed to air the gettering activity ceases and no more gas is pumped.
Getter
Room temperature
(RT)
Activation temperature
(Tactivation)
Non Evaporable Getters (NEG) for accelerator applications
A Non Evaporable Getter (NEG) can be regenerated by heating to its activation temperature during a certain time.
Notes: Appropriate situation with the CERN logotype
Mixture of different logotypes
All of them are circulating
All CERN clubs were also very creatives

## Slide 5
Back to room temperature (RT) the NEG recovers its pumping capabilities.
Room temperature
(RT)
Activation temperature
(Tactivation)
NEGetter
The NEG TiZrV can act as a pump, but when activated it has also a low SEY
Operation of the getter:
Once saturated, or exposed to air the gettering activity ceases and no more gas is pumped.
A Non Evaporable Getter (NEG) can be regenerated by heating to its activation temperature during a certain time.
Non Evaporable Getters (NEG) for accelerator applications
Notes: Appropriate situation with the CERN logotype
Mixture of different logotypes
All of them are circulating
All CERN clubs were also very creatives

## Slide 6
SEY of Non Evaporable Getter (NEG) coatings
TiZrV NEG can provide a surface with sufficiently low δmax :
activation
at 200C 2h
-Thermal activation is necessary: 2h at 200C or 24h at 180C
Henrist et al.
Appl.Surf.Sci,
2001

## Slide 7
Low SEY without thermal activation: a-C coating
Thin film amorphous carbon coatings with SEY1
after air exposure, without any bake-out; robust for 1 year (clean) air exposure
Low SEY for thickness above 50 nm (on a smooth surface)
sp2 character (XPS), nanocrystalline graphite to amorphous (Raman)
NO PUMPING EFFECT
After air exposure
40
30
20
10
0
runs

## Slide 8
Up to 2018: coated 20 dipoles + 15 quadrupoles. Showed no issue in operation.
Long Shutdown 2 (2019-20): all 90 focussing quadrupoles and adjacent short straight sections by June 2020. In operation, suppresses e-cloud
At present: Applied preventively on spare dipoles, since the dynamic pressure recovery after emergency replacements is faster
Scaling up to a series: e-cloud mitigation in SPS

## Slide 9
LHC standalone magnet: coating in-situ
Treatment in the tunnel
only 150 mm for access
Beamscreen
20K
coating
~ O 50 mm
Cold bore
1.9K

## Slide 10
Development of adapted coating method
Titanium target
pump hydrogen
enhance adhesion
Graphite target
direction
100
mm
Ti and C cathodes to reduce outgassing and increase adhesion
Develop a “modular sputtering source” that can be inserted and pulled by cables all along a magnet
Reduce outgassing during coating, H2 is crucial (especially with the double wall of beamscreen and cold bore)
C

## Slide 11
10 meters
Development of adapted coating method: 10 m travel
Threshold HL-LHC
Successfully applied to Q5L8 quadrupole in situ in 2021, to be applied to Pt2 and Pt8 triplet magnets in LS3

## Slide 12
Implementation of coatings in a project
Adapted coating system.

## Slide 13
Implementation of coatings in a project
Adapted coating system.
Low SEY: limit impurities in the films (oxygen in NEG, hydrogen in carbon). Ex: by bakeout before coating, add sublayers, doping, discharge parameters

## Slide 14
Implementation of coatings in a project
Adhesion: surface preparation is crucial (wet chemistry, plasma treatments, sublayers). Preliminary test on representative surfaces and conditions.
Low SEY: limit impurities in the films (oxygen in NEG, hydrogen in carbon). Ex: by bakeout before coating, add sublayers, doping, discharge parameters
Adapted coating system.

## Slide 15
Implementation of coatings in a project
Include the coating constrains from
early stages of the design.
Adhesion: surface preparation is crucial (wet chemistry, plasma treatments, sublayers). Preliminary test on representative surfaces and conditions.
Low SEY: limit impurities in the films (oxygen in NEG, hydrogen in carbon). Ex: by bakeout before coating, add sublayers, doping, discharge parameters
Adapted coating system.

## Slide 16: THANK YOU FOR YOUR ATTENTION

## Slide 17
+
+
+
+
Proton bunch (charge +)
Electron (charge -)
The beam is perturbed by the electron multiplication: emittance growth, beam instability
Cryogenic parts of the accelerator are submitted to heat load
The pressure rises due to electron stimulated desorption and provokes noise in the experiments
E-cloud is more pronounced for high beam currents and short bunch spacing
E-cloud is suppressed by a sufficiently low secondary electron yield of the walls (typically below 1.1-1.3)
Gas molecule
Electron cloud or why slow electrons matter
e-cloud

## Slide 18
Pumping action of TiZrV NEG: sticking probability of H2 and CO upon thermal activation
The NEG pumps H2, CO, CO2, N2…. It does not pump CH4 and noble gases which do react with the surface
The sticking probability is the ratio between sticking and impinging molecules. It shows the pumping efficiency
The sticking probability increases when the NEG is activated (all measurements made at the same T, after thermal activation)

## Slide 19
electron gun
Ip = Is + Ic
d = Ic / (Is + Ic)
Sample
Ip
Ic
A
Is
A
Ic
Measurement of TEY on materials in the lab
electron gun
Sample
Ip
Ic
A
Is
Faraday cup
Ip = Is with Faraday cup
d = 1-Is/Ip
Gun is closer to sample:
better adapted for low Ep
The two currents are not measured simultaneously
Measurements done at low dose (below 10-6 C/mm2) to avoid conditioning of the surface
e-cloud

## Slide 20
20
XPS C1s
δmax is influenced by the hydrogen in the discharge gas
The intensity at high BE decreases with H2, but we don’t know the mechanism
Reduce and control H2 outgassing during the coating process
SEY max
δmax
Thin films

## Slide 21
TiZrV alloy is deposited by DC-magnetron sputtering with a single target made of intertwisted wires of titanium, zirconium and vanadium
Coating method for vacuum pipes
Before coating
after coating
typically < 300G
Coating after pumping and bake out
B-field
coil
Vacuum chamber
Skip?
Notes: Appropriate situation with the CERN logotype
Mixture of different logotypes
All of them are circulating
All CERN clubs were also very creatives

## Slide 22
2 StSt tubes
measured in
clean-room (REF 1,2)
coated with carbon
left in the lab. with covers
both measured again in clean-room
No dust and particles: test in optical particle counter
-No difference in particles between coated and uncoated tube
-No increase after shaking and gentle hammering of the chamber
-No increase for a chamber left in air for months
-Same result for size above 5 µm
In addition:scotch-tape test for adhesion
3 µm < Size < 5 µm
intake cycles
3µm < D <5µm
Cycles
N particles
REF1
Tube no coating
REF2
Tube after coating