## Slide 2: ActiWiz – notre couteau Suisse pour les calculs d’inventaires des radionuclides
C. Theis & H. Vincke
ARRAD WG1 - libération de matériaux et de bâtiments 17/10/2024, CERN

## Slide 3: Contents
Introduction
Calculation methodologies for nuclide inventories
Overview of ActiWiz 3 & its application in practice

## Slide 4
Activated material
Design
Construction
Operation
Maintenance &
Dismantling

## Slide 5: Material activation
beam
secondary particles
Isotope production &
build-up
Decay

## Slide 6: The challenge we faced….
Multitude of usually unknown parameters
material composition
irradiation & cooling period
radiation field
Full laboratory analysis (g-spec & radiochemical) is not a sustainable option due to huge material flow
We need a tool that can calculate all of this for us efficiently

## Slide 7: Methods of computing nuclide inventories
Disadvantages
Requires fluence spectra as input (Monte Carlo)
Does not yield spatial information
Advantages
Very high statistical significance & short computation times
Analysis & reporting tailored to characterization
Hybrid (deterministic & MC)
Combine the power of modern intranuclear-cascade models with analytical computation speed
Disadvantages
Calculation times can be very long
Difficult to achieve sufficient statistics for thin layers
Advantages
Yields spatial distributions of nuclides & residual dose rate
Monte Carlo
State-of-the-art method for many problems in science

## Slide 8: Pi,j,k(E) provides the amount of isotope i produced in a single element j, for a single radiation type k and a given energy (group) E
neutrons < 20 MeV: JEFF 3.3
neutrons > 20 MeV, p, pi+, pi-, photons up to 100 TeV: 100 CPU years of generic CERN-FLUKA calculations
Foundation of ActiWiz: Basic nuclide production rates Pi,j,k(E)
Data for 85 constituents (mainly elements of natural composition) and 5 particle types have been produced.  in total 17 million basic isotope production data values

## Slide 9: Nuclide inventory calculation in ActiWiz
decay
build-up
Build-up & decay
(Bateman)
Nuclide inventory for a given irradiation and cool down history within seconds for most cases
Production rate Pi of each radio-nuclide i , based on particle fluences Fk, the material composition nj and Pi,j,k(E)

## Slide 10: Nuclide inventory analysis
Radiotoxicity
(EU, CH, US, A, Japan, IAEA limits)
g emission spectra
Radiological dominating isotopes
Isotope production sources
Shielding calculator
Alpha/beta analysis
Evolution of rad. hazard with add. cooling time
Residual dose rate calculator

## Slide 11: ActiWiz 3 overview
84 built-in radiation fields
CERN accelerators & LHC experiments
External radiation fields
Import via fluence spectra
Parameters
Arbitrary material compounds (85 chemical elements)
Arbitrary irradiation/cooling patterns (512 bits FP precision)
Fully integrated GUI
+ python scripting engine

## Slide 12: A short demo Long term irradiation at the Super Proton Synchrotron (SPS) 1) key nuclides in materials 2) difficult to measure nuclides

## Slide 13
Steel equipment is located next to a target in the SPS and is irradiated by the secondary radiation field
Radiation field that is produced is used as input to calculate nuclide inventory produced in steel equipment
Nuclide inventory produced in steel (304L) located close to a target in the SPS (400 GeV)
Long term irradiation of 20 years, various cooling times
Which isotopes are dominant in the nuclide inventory?
How does this change for different cooling time?

## Slide 15: Analysis of radionuclides as a function of cooling times
Which isotopes are dominant at what cooling time?
Example: radiotoxicity (according to Swiss LL) of stainless steel in Super Proton Synchrotron (after 20 years of irradiation)
Allows for defining key nuclides for operational and waste characterization

## Slide 16: Analyzing difficult to measure isotopes in equipment
Steel 304L and Indium are irradiated next to the SPS (same radiation field as before) over 20 years.
Question:
What is the contribution of “pure” alpha/beta emitters to the total radiotoxicity in both materials?
How does this change with cooling time?

## Slide 17: Summary & conclusion
ActiWiz is an inhouse development originating from the need to calculate nuclide inventories in a highly optimized way
Provides targeted reporting for characterization and removes the complexity of general purpose MC simulations
Continuous benchmarking against FLUKA & experiments

## Slide 18
Thank you for your attention

## Slide 19: Analysis & reporting
Component criticality analysis: “which chemical element contributes in which proportion to clearance limits, H*(10), etc.”
***********************************************************************************************************
C O M P O N E N T C R I T I C A L I T Y A N A L Y S I S
***********************************************************************************************************
Compound: "inconel-0.25-Co", density 8.19 g/cm3
The following table shows how much each component of the compound material contributes
to the selected hazard quantity: H*(10) level
COBALT : 95.11% (weight fraction: 0.25%)
NICKEL : 3.45% (weight fraction: 53%)
TANTALUM : 0.59% (weight fraction: 0.01%)
IRON : 0.42% (weight fraction: 18.4%)
NIOBIUM : 0.21% (weight fraction: 5.2%)
CHROMIUM : 0.15% (weight fraction: 18.3%)

## Slide 20: Analysis & reporting
**************************************************************************************************************
(Q U A S I) - P U R E A L P H A & B E T A E M I T T E R S
**************************************************************************************************************
Selected hazard factor: IAEA clearance limits - Safety Standards RS-G-1.7 (2004)
Id rel. contribution to hazard t1/2 [s] decay info
--------------------------------------------------------------------------------------------------------------
H-3 67.5% 3.89097e+08 [ 100% beta-, ]
C-14 2.3% 1.79874e+11 [ 100% beta-, ]
Cl-36 0.251% 9.49863e+12 [ 1.9% beta+, 98.1% beta]
Mn-53 0.00868% 1.16129e+14 [ 100% beta+, ]
Fe-55 3.63% 8.63082e+07 [ 100% beta+, ]
...
--------------------------------------------------------------------------------------------------------------
Total contribution to hazard = 73.7%, which equals = 1.198378E-06 Bq/unit (93.5% of total activity)
--------------------------------------------------------------------------------------------------------------
The following chemical elements contributed to the hazard with 73.7% via (quasi) pure alpha/beta emitters:
CARBON - 0.0117% (weight fraction: 0.0025%)
IRON - 73.5% (weight fraction: 99.7%)
MANGANESE - 0.202% (weight fraction: 0.235%)
PHOSPHORUS - 0.0139% (weight fraction: 0.0115%)
SILICON - 0.00366% (weight fraction: 0.0035%)
SULFUR - 0.0078% (weight fraction: 0.00901%)
Example: ARMCO iron used for yokes 20 y irradiation @ SPS
20 y of cool-down

## Slide 21: Spoil activation study
Spoil activation assessment for future civil engineering works at the HiLumi LHC:
 | Shutdown 2016/17 (~3 months cooling time) |  | 
UPR | g spectrometry measurements | ActiWiz 3 | 
 |  | full | only g
concrete | 0.12 | 0.5 | 0.10
soil | 0.008 | 0.016 | 0.005
 | Shutdown 2016/17 (~3 months cooling time) |  | 
UPR | g spectrometry measurements | ActiWiz 3 | 
 |  | full | only g
concrete | 0.12 | 0.5 | 0.10
soil | 0.008 | 0.016 | 0.005
Ca-45 | 68%
Na-22 | 28%
S-35 | 2%
Ca-45 | 80%
Na-22 | 7%
Zn-65 | 3%
Fe-55 | 3%
S-35 | 1%
Mn-54 | 1%
Ca-45 is a pure b emitter: cannot be seen with g-spec
quantity of interest is the radiotoxicity = sum of activity over clearance limit
in 2016 some concrete wall & soil samples were taken and analyzed
particle fluence spectra calculated with FLUKA (detailed tunnel geometry)
C. Adorisio, S. Roesler, Induced activation studies for the LHC upgrade to High Luminosity LHC,
ARIA 2017 Workshop, Lund