## Slide 1: Status of the BDF Target Design ESS – CERN Meeting
Mike Parkin, Alvaro Romero Francia, Tina Griesemer, Damien Grenier, Christophe Yves Mucher, Steven S,, Jean-Louis Grenard, Marco Calviani, Giuseppe Mazzola, Luigi Esposito, Rui Franqueira Ximenes et al (SY-STI), Francesco Dragoni, Nikola Zaric, (EN-CV) Matthew Fraser (SY-ABT) on behalf HI-ECN3 Project
2024/09/20

## Slide 2: Content
BDF Target requirements
Water cooled target (CDR concept)
He cooled target (new proposal)
Conclusions & prospects
Questions to ESS

## Slide 3: Beam Intercepting devices towards ECN3
EHN1
EHN2
ECN3
SPS
TT22
TT21
LSS2
TT24
P4
TCC8
P4:6
P42
Other BIDS: Collimators, Masks, etc  To be defined
Target + beam windows
P42 commissioning Dump (TIDVG4)
T4 XTAX
TT20 TED
TBSE
TCSC
T4 Target
NA-CONS
HI-ECN3

## Slide 4: BDF/SHiP Target & Complex (Future ~ 2030)
New
Service Building
~ 500 – 700 m2
ECN3
Beam Dilution System
New
Access Shaft
(material only)
88 m2
TCC8
Existing
Access Shaft
48 m2
B918
B911
New Target Complex
containing the Beam Dump Target
13 x TZM blocks (580 mm)
5x W blocks (780 mm)
Baseline Design  To be improved during TDR
WP4
WP3
WP2
WP5+SHiP
WP4
WP6,WP7 +al.
350 kW-class Target

## Slide 5: BDF/SHiP Target
SPS Beam Dump Facility: Comprehensive Design Study, https://doi.org/10.23731/CYRM-2020-002
SHiP Experiment - Comprehensive Design Study report, https://cds.cern.ch/record/2704147
R. Jacobsson
Beam Dump Target / SHiP Target
  Fully absorbe all p+, maximize production of charm and beauty hadrons & re-absorption of pions, muons and kaons
High energy → production of charmed and beauty mesons
High ppp & POT → overcome small prod cross-section of extra rare events of hidden particles
High ρ, Z & A → Maximize p+ interaction
Shortest λ → Force absorption of K & π to reduce muon & neutrino background

## Slide 6: BDF Target
Target requirements
  Physics:
    high-Z material & with short interaction length
    Fully absorb SPS p+ beam
  Engineering:
    305kW power  cooling needs
    305kW power  temperature & thermal-induced stresses
  High nr of spills & POT  mechanical fatigue & radiation damage
Safety:
  High activation  Remote handling, waste disposal considerations, spallation/contamination products…
Baseline beam parameters of the BDF Target operation. https://doi.org/10.23731/CYRM-2020-002
~ 4.0×1019 p+/y
Very similar requirements to a neutron spallation target
Synergies with other labs are being pursued

## Slide 7: BDF Target baseline design
Baseline Design (CDR) – Water cooled, W + TZM cladded w/ Ta2.5W .
Pursued during the conceptual design phase
Prototype + test with beam + Post irradiation examination
Still some safety aspects to be addressed
Could be further optimized for physics
Alternative designs currently being studied in the TDR
Enclosed compact
Cu + W Target
Removes water from beam
Keeps physics performance
Reduces decay heat
Increases T and stress
W Helium cooled Target
Removes water from beam
Better physics performance
Reduces decay heat & residual stresses
Conceptually different system!
Other concepts: Baseline with W rolled material, Nb-cladded Target,…
https://doi.org/10.1103/PhysRevAccelBeams.22.113001

## Slide 8: BDF Target baseline design
Water-cooled, Ta-cladded TZM + W Core
  TZM: Absorbs most of the power. Higher strength, better creep resistance, higher recrystallisation temp wrt Mo.
  W: Good radiation damage resistance. Best for physics.
  Ta2.5W: To avoid corrosion-erosion of the core materials
  Cooling: 22 bar, 5 m/s, ~660l/min, ~305kW of heat.
Manufacturing
  Forged TZM and sintered W (single blocks)
  Diffusion bonding with cladding via Hot Isostatic Pressing
https://doi.org/10.1103/PhysRevAccelBeams.22.113001
Target Core with reasonable physics performance & that allows diluting (longitudinally) the energy deposition
13 x TZM blocks (Z=42, ρ=10.2g/cm3)
(580 mm)
5x W blocks (Z=74, ρ=19.3g/cm3)
(780 mm)
D250 mm
BDF Baseline Target Design

## Slide 9
Post Irradiation Examination
Design mostly validated but with few caveats
Prototype Beam tests
Validate manufacturing and test operation at identical temperatures & mechanical stresses.
Reduced diameter (80 mm) prototype.
Tested in 2018 on a dedicated slow extraction (SX) testbench in the T6 primary beam line in TCC2 at CERN. Total of 2.4 × 1016 p+
https://doi.org/10.1103/PhysRevAccelBeams.22.123001
BDF Baseline Target Prototype + PIE
I. Film Dosimetry
II. Metrology & Microscopy
V. Microstructural Characterization
III. Ultrasonic Testing
IV. Specimen Extraction
VI. Mechanical Characterization
VII. Thermal Characterization
Post-irradiation examination of a prototype tantalum-clad target for the Beam Dump Facility at CERN, T. Grisemer, R.F.Ximenes (to be published soon!)
Notes: Instrumentation (temperature and strain) of 4 most critical blocks
Total 14 hours of beam in 3 days → 2.4 × 1016 PoT

## Slide 10: In search of an alternative design Main motivations
Most of the shower develops on TZM and not on W  core could be further optimized for physics
Water in-beam promotes formation of radicals  safety concerns to be addressed or water removed
Decay heat on baseline target is considerable & driven by cladding. Possibility of LOCA (Loss Of Coolant Accident) poses a critical safety risk  Reduce Ta cladding
PIE revealed W quality to be poor  Look into more robust W supply
13 x TZM blocks
(580 mm)
5x W blocks
(780 mm)
BDF Target water cooling layout (20bar, 5m/s)
400GeV/c p+ beam4x1019 POT

## Slide 11: Alternative designs: Nb-cladded
Baseline Design (CDR) – Water cooled, W + TZM cladded w/ Ta2.5W .
Pursued during the conceptual design phase
Prototype + test with beam + Post irradiation examination
Still some safety aspects to be addressed
Could be further optimized for physics
Alternative designs currently being studied in the TDR
Enclosed compact
Cu + W Target
Removes water from beam
Keeps physics performance
Reduces decay heat
Increases T and stress
W Helium cooled Target
Removes water from beam
Better physics performance
Reduces decay heat & residual stresses
Conceptually different system!
Other concepts: Baseline with W rolled material, Nb-cladded Target,…
https://doi.org/10.1103/PhysRevAccelBeams.22.113001

## Slide 12: Nb-cladding R&D
Thermal diffusivity specimens
  Excellent thermal contact has been confirmed for all Niobium alloys (Nb, Nb1Zr, C103)
Tensile specimens
  Interface strength for Nb alloys higher for TZM than W
  TZM core :
    Ta foil + HIP: High increased the strength
    C103 did not bond without the foil
  W core
    Higher variation, but it seems no foil increases interface strength
SEM: Increase of successful diffusion bonding / maximum stresses
I. EBW of Capsules
II. Helium Penetrant Test
III. 1st HIPing Cycle (1200 °C)
VII. Thermal Characterization
IV. 2nd HIPing Cycle (1400 °C)
VI. Cutting & OM at interface
VIII. Mechanical Characterization
V. Ultrasonic Testing
*by courtesy of Bangor University
w/o foil + HIP:High
w/o foil + HIP:Low Ta foil + HIP:High
Ta foil + HIP:Low
W → Nb1Zr + no foil + HIP:High
TZM
W
TZM → C103 + Ta foil + HIP:High
UTS [MPa]
Nb-cladding R&D
Exploring diffusion bonding of niobium and its alloys with tungsten and a molybdenum alloy for high-energy particle target applications, T. Grisemer, R.F.Ximenes (to be published soon!)
However, long-lived Nb isotopes pose challenges for waste disposal

## Slide 13: Alternative designs: W Helium cooled Target
Baseline Design (CDR) – Water cooled, W + TZM cladded w/ Ta2.5W .
Pursued during the conceptual design phase
Prototype + test with beam + Post irradiation examination
Still some safety aspects to be addressed
Could be further optimized for physics
Alternative designs currently being studied in the TDR
Enclosed compact
Cu + W Target
Removes water from beam
Keeps physics performance
Reduces decay heat
Increases T and stress
W Helium cooled Target
Removes water from beam
Better physics performance
Reduces decay heat & residual stresses
Conceptually different system!
Other concepts: Baseline with W rolled material, Nb-cladded Target,…
https://doi.org/10.1103/PhysRevAccelBeams.22.113001

## Slide 14: BDF W Helium cooled Target
14
Helium cooled blocks (without cladding)
Removes the high stress regions of the baseline design (Ta cladding)
Allows higher surface block temperatures (no risk of boiling)
Removes radiological concerns with the water
All core material is W (good for physics)
- But HTC is lower
- New cooling system complexity and cost
 | ESS at 2012CDR | BDF | LBNF at 2023
Inlet Pressure | 3 bar | 16 bara | 4.5 bar
Swept vol. flow rate | 4.6m3/s | 0.13-0.15m3/s | 0.076m3/s
Target deposited heat | 3MW | 305kW | 35kW
BDF He system parameters | 
Thermal Power | 305 kW
Inlet Pressure | 16 bara
Pressure Drop | <2 bar (high estimate)
Mass flow | 345 – 400 g/s
Volume flow | 0.13 -0.15 m3/s
Inlet temperature | 30 °C
Outlet temperature | 200-170 °C
Heat transfer coefficient | 1000-2000 W/m2/K
Ø250mm
to
Ø362mm!
17 to 740 mm
Gaps 4mm
W
BDF Target. Coolant by Gaseous helium, ~200m/s.
3 or 4 channels in parallel.
P+

## Slide 15: BDF W Helium cooled Target
15
Operational conditions
18 x W blocks (~1.5mm)
Temperature (°C)
BDF operational conditions | 
Target design lifetime | 5 years
Max dpa | 1.6 to 1.2
Max He implantation | 220 to 143 appm
Max stresses | 150MPa
Max bulk temperature | 400°C
Max W-to-He surface Temperature | 350°C
Beam parameters | Same as for Baseline, except beam size
P+

## Slide 16: BDF W Helium cooled Target
16
Design approach
Cooling station & target have been considered together for system temperatures and pressures
Design approach has included Defining Design limits
  Stress
  Fatigue
  Block Temperature
  Surface temperature (e.g. limited oxidation)
  Irradiated properties
Applied these limits to target block position optimisation
Used safety margins >2 on irradiated (degraded) material properties at 2dpa. <2dpa expected)
Extrapolation and rule-of-thumb factor used to obtain irradiated fatigue limits due to lack of data
Whole target
Limited by Stresses
Limited by Surface Temperature
Limited by Stresses

## Slide 17: BDF W Helium cooled Target
17
Target Options being Considered
Beam Sigma & sweep radius
16 mm vs 8 mm (baseline)
50 mm sweep radius
Core geometry
Full 360 ° disks
45° 1/8th target slices
Helium Pressure
Recently moved to 16 bar due to compressor availability, size, cost and complexity
Benefits for stress and fatigue
Requires slightly larger diameter core for physics
To be seen if compatible with beam dilution system
1/8th target requires diagonal cuts to prevent shine path (effective but adds complexity)
Or offset cuts (less effective)
Beneficial for target pressure drops
Lower than CDR design at 22bar
Full target
1/8th target
Nominal gaps <0.5mm

## Slide 18
The Core blocks
W sheets, HIPed together with interlayers of ~50um Ta foil (or other – to be explored)
   Improved mechanical properties compared to Sintered blocks used for CDR.
Using W sheets thickness 10mm ±5mm
   As thick as reasonably possible with the best mechanical properties.
Ta interlayer foil
   builds on previous HIPing experience*
Options of joining being investigated:
  Hot Isostatic Pressing
  Vacuum Hot Press (used at SNS)
  Spark Plasma Sintering (used at SY)
  Tungsten Powder Injection Molding.
  Electron Beam Tungsten Rapid Prototyping
Drivers:
Must be clad for HIPing joining process
Don’t want cladding: high stresses at the cladding
Don’t want cladding: Ta produces lots of decay heat
Do want cladding at circumference: Compressive stresses beneficial to W sheets
Do want cladding : Protective layer against oxidation / corrosion-erosion
Capsule may be partially/fully machined away after HIPing.
No encapsulation
Full encapsulation
Circumferential encapsulation
Helium coolant
50um Ta interfoil (or other)
W Sheets
Ta capsule (or e.g. SS)
*“Application of hot isostatic pressing (HIP) technology to diffusion bond refractory metals for proton beam targets and absorbers at CERN, ” J. Descarrega et al.; Material Design and Processing Communications. 8 August 2019 https://doi.org/10.1002/mdp2.101
BDF W Helium cooled Target

## Slide 19: a
Ongoing Material Studies
Exact tests and number of tests currently being defined
Testing will be performed on
  The raw W sheets
  The joined blocks (similar to the baseline prototype after HIPing tests)
  The joined blocks post-beam (similar to the baseline prototype tests)
  In depth testing from 1 supplier & basic characterization from 2 more suppliers
- Raw W sheets
BDF W Helium cooled Target

## Slide 20: Prototype target design
Prototype target
To be constructed and tested in North Area T6 on the existing test stand base
Reproduce temperatures and magnitude & type of thermal-induced stresses
Post-beam testing of mechanical properties and interfaces will be performed
Potential to cross-check simulations
Coolant efficiency could be tested on a separate non-beam mock-up
If time allows, two targets will be tested:
  Static Helium concept** & actively cooled He concept
  3rd option: Water cooled concept (niobium cladding, copper sheets, copper external… TBD)
**In the event of no delay to the North Area long shutdown, the timescale is not possible to have a flowing helium circuit installed and commissioned before the prototype tests…
BDF W Helium cooled Target

## Slide 21: Prototype target design
Core ø50mm
W
Coolant: flowing water
Steel can
Static helium
600mm
Prototype target
Static Helium concept (baseline for now)
W in static Helium. Cooled with a water jacket
Block spacing defined to match maximum stresses and temperatures and stress type.
  Challenge with static gas. Requires a LONG cycle time = 7.2 minutes, with intensity 1.5e12 ppp.
Beam parameters considered: Beam σ 1mm to 3mm, Intensity 5e11 to 2e13 ppp
Mix of semicircle and full circle blocks
Semi-circle blocks better reproduce stress state of 1/8th target slices.
Full circle blocks better reproduce the stress –state of the 360° target.
BDF W Helium cooled Target

## Slide 22: Prototype target design
Prototype target
Static Helium concept (baseline for now)
BDF W Helium cooled Target
Temperature (°C)
Max P stress (MPa)
HTC 10
1.3e12ppp. 720s/c
P+

## Slide 23: Prototype target design
Outgassing
One of the main concerns into moving to a W He-cooled target operating at high temperature is the outgassing of radioactive species.
Being studied:
Shortlisted highest contributors in terms of total activity, LL and LA as computed by RP
Assume radioactive isotope as volatile if it makes one chemical compound which is reported as volatile (due to boiling or sublimation) below 500 °C
  Usually containing O, N, H (oxides, nitrates, nitrides, hydrides and hydroxides)
Some conflicting data, e.g. on W trioxide.
Other species of concern such as iodine which can make volatile molecules with Cobalt, Hafnium and Tantalum. ?
 Plan to execute offline oxidation tests
 Plan to execute irradiation and out-diffusion measurements
BDF W Helium cooled Target

## Slide 24: Conclusions & outlook
A water-cooled baseline design exists with a core of TZM and W.
Sound design, yet with potential for physics optimization and with some radiation protection caveats
W material quality used in the 2018 prototype was not good
Following HI-ECN3 project approval and start of TDR phase
Multiple alternative designs explored in view of mitigating water radiolysis, decay heat and improve physics performance.
He-cooled target most promising option. Being explored in detail.
Presently tackling
  Definition of core segmentation taking key metrics and safety margins
  Material R&D for the W base material and bonding of the assembly
  Detail design of a prototype to be tested with beam in 2025/26
  Design of the cooling station (Francesco and Nikola’s talks)
  Addressing Radiation Protection aspects (Claudia’s talk)
  Many other points to be addressed in the coming months

## Slide 25: Questions to ESS (1/2)
What safety factors (e.g. mechanical, thermal, cooling etc) have been chosen for the engineering studies of the target blocks?
What is the W material used at ESS and what quality assurance plan was adopted?
How has fatigue been assessed (both numerically and via testing)?
Are there erosion concerns?
Are there oxidation & spall concerns?
Is radiation damage and gas production a concern at ESS?
What radiochemistry is a concern (e.g. from volatile compounds from the irradiated W) and has been particularly addressed, and why?

## Slide 26: Questions to ESS (2/2)
How significant is decay heat and LOCA for ESS Target?
What are the redundancy systems and measures put in place for LOCA?
What instrumentation is used to monitor the target and its core ?
What design & manufacturing specifications have been adopted for the target assembly and that were mostly driven by the presence of a He coolant ?
Considering today’s status of the He-cooled pure W target for BDF, what recommendations can you provide?
Many thanks!

## Slide 28: WP3 – Target & BIDs: Planning (key dates)
TDR phase
TDR phase (main activities) – (2024-mid 2026)
Target (& BIDs) conceptual design followed by detailed design
Prototype(s) Target Design, construction and beam tests
Material studies, R&D and Procurement
Production phase – (2026 – 2030)
Detailed Design phase
Procurement & production of components and systems
Tests/dry-run, installation activities
Material tests/PIEs
Production phase
Commissioning & operation

## Slide 29: Enclosed compact Cu + W Target
29
Cu+W target :
Removes water from beam path (radiolysis)
Keeps physics performance
Reduces decay heat
Increases T and stress
beam
Cu-SS HIP bonding for the SPS internal dump (TIDVG5)

## Slide 30: Main Target developments in the coming months
Focus on W quality assurance
W via rolled products to ensure low porosity (low brittleness),and high mechanical properties
Material R&D on W to W bonding and characterization of interface strength
Further develop alternative target concepts, particularly He cooled option
Understand & design such He cooling system
Design Target core than can withstand higher temperatures and reduce mechanical stresses
Develop prototype Target(s) to be tested at CERN SX test-bench in 2025

## Slide 31: BDF – New ideas to be explored in 2024

## Slide 32: Ta2.5W cladding – LOCA
(Loss-of-Coolant Accident scenario) LOCA hypothetical scenario used as a criterion for assessing the safety of a nuclear installation during its design phase.
→ Strong implications on the classification of the facility.
Thermo-mechanical simulations to determine the temperature evolution of the target in a 2 years scenario after the accident.
Depending on the assumptions, T > 300 C may be reached for prolonged periods ((O)weeks)
Mena R., Ximenes R.F. and Calviani M. (2022), Loss-of-Coolant-Accident study for the Beam Dump Facility at CERN, NURETH-19 Conference

## Slide 33: Ta2.5W cladding – LOCA
Potentially degradation of the material through oxidation with LOCA.
→ Campaign to assess the onset for extensive oxidation and formation of volatile oxides
Thermogravimetric analyses (TGA) performed for Ta2.5W, TZM and W in the range of 400-800 C under active and inert atmospheres.
Visual inspection of the samples before and after oxidation for different temperatures.
Ta2.5W
TZM
W
Raw sample
800 C at 2 C/min
800 C at 40 C/min
400 C at 10C/min x 7 days
800 C at 2C/min
Inert
Atmosphere
(argon 6.0)
Active
Atmosphere
(50% argon: 50% air)
400 C
500 C
600 C
700 C
r1 = 10
r2 = 2
r3 = 40
[C/min]
r1 = 10
r2 = 2
r3 = 40
[C/min]
Notes: Small mass gain for Ta2.5W at 400C with inert argon (with some impurities)
Clear oxide layer at 500 C

## Slide 34: Nb-alloys cladding R&D
Presence of residual stresses (RS) during the manufacturing of the target blocks via Hot Isostatic Pressing (HIPing).
RS defines the onset for plastic deformation and eventually material failure
Purpose: quantify the RS in the BDF target blocks
Contour method* employed to measure the RS in the BDF target blocks. Ongoing FE model calibration.
* Prime, M. B., 2001, Cross-sectional Mapping of Residual Stresses by Measuring the Surface Contour After a Cut, Journal of Engineering Materials and Technology 123(2):162–168
Resulting left and right parts after EDM cutting (Top) Block 3 and (Bottom) Block 4
Average flatness measurements of the resulting surfaces
(Top) Block 3 and (Bottom) Block 4
The contour method and its different steps to obtain the residual stresses. Adapted from [StressMap 2018]
Residual stress

## Slide 35: BDF Target Prototype removal (2020)
Unplug-in  Transport to the bunker  Unscrew downstream flange  Instrumentation wire cut & flange removal  Extraction half-shells core assembly  Unscrew half-shells  Removal top half-shell & first glimpse of the target blocks
BDF target assembly

## Slide 36: BDF Target Prototype removal (2020)
Identification of the blocks and angular orientation with respect to the beam with a marker  Removal of the target blocks for the post irradiation examination (PIE) campaign  Storage of the extracted blocks in a shielded container

## Slide 37: NA62 in ECN3 (Today)
ECN3
B918
B911
TCC8
Existing
Access Shaft
48 m2
T10 target, K12 beamline and NA62 experiment to be dismantled in LS3
T10
Target
K12 beam line
T10
XTAX
Introduction to the BDF / HI-ECN3 Project - Discussion with JPARC T2K team

## Slide 38: BDF/SHiP Target & Complex (Future ~ 2030)
New
Service Building
~ 500 – 700 m2
ECN3
Beam Dilution System
New
Access Shaft
(material only)
88 m2
TCC8
Existing
Access Shaft
48 m2
B918
B911
New Target Complex
containing the Beam Dump Target
13 x TZM blocks (580 mm)
5x W blocks (780 mm)
Baseline Design  To be improved during TDR
WP4
WP3
WP2
WP5+SHiP
WP4
WP6,WP7 +al.
350 kW-class Target