## Slide 1
Surrogate Test Approaches: Enabling Capabilities for Predictive Testing Using Pulsed Lasers and Other Methods
Dale McMORROW,1 Joel Hales1,2, Adrian Ildefonso3,
Ani Khachatrian1, and Stephen Buchner1,2
1US Naval Research Laboratory, Washington, DC
2Amentum, Chantilly, VA
3Indiana University, Bloomington, IN
Distribution Statement A. Approved for public release; distribution is unlimited

## Slide 2
Outline
Where we’ve been
  PL SEE background and some examples
Where we’re going
  SEL screening approach
  ASSERT Program
    Pulsed focused X-ray
    Pulsed focused e-beam
Notes: No annotation necessary

## Slide 3
Pulsed Laser Single-Event Effects
Pulsed-laser SEE has been used for:
  Basic mechanisms studies – single transistors
  Sensitive node identification/characterization - circuits
  SEU mapping of sensitive areas
  Digital single-event transient characterization and mitigation
  Laser-induced latch-up screening/mitigation
  Analog single-event transient screening (ASETs)
  Hardened circuit (RHBD and RHBP) verification
  Dynamic SEE testing
  Complex circuit evaluation/error signature identification
  Experimental test setup verification
Notes: Description of advantages of using the pulsed laser for SEE studies

## Slide 4
Pulsed Laser Single-Event Effects
Common Underlying Theme:
  Spatial selectivity
Notes: Description of advantages of using the pulsed laser for SEE studies

## Slide 5
Taking Advantage of PL SEE Spatial Selectivity:
Sensitive Node Identification and SET Mapping.
Commercial PLL Charge Pump
Loveless, et al., IEEE TNS 57, 2933 (2010)
Loveless, et al., IEEE TNS 67, 99 (2020)

## Slide 6
Motivation: Need and Opportunity
NRL
Vanderbilt
Aerospace
JPL
LANL
Intel
Boeing
U. Saskatchewan
Allied Scientific
RTS
SEAKR
Pulsed-Laser Testing
Heavy-Ion Testing
LBNL
BNL
MSU
TAMU
Analog Devices
SNL
Renesas
UTD
APL
NGC

## Slide 7: Global Laser SEE Testing Facilities

## Slide 8
1.06 mm
Linear and Nonlinear Optical Absorption in Silicon
mm
1.3 mm
1.55 mm
Optical Absorption Spectrum of Silicon
m
Notes: Series of slides illustrating the differences between the charge deposition profile for single-photon and two-photon absorption. 590 nm.

## Slide 9
590 nm
Ec
Ev
Ec
Ev
1260 nm
+
-
-
-
-
-
-
-
1-Photon
2-Photon
Eg=1.1eV
+
-
630 nm
Two photons absorbed
By the material (silicon)
Simultaneously
Creates a single e-h pair
Optical Excitation of Carriers in Silicon
Single photon absorbed
By the material (silicon)
Creates a single e-h pair
Notes: Series of slides illustrating the differences between the charge deposition profile for single-photon and two-photon absorption. 590 nm.

## Slide 10: Practical Consideration: Front-Side vs. Backside Illumination
2w0
Front side
Sensitive volume
2w0
Backside
Sensitive volume
Microscope objective
Microscope objective
no3.5
substrate
Laser beam
Laser beam
Lewis, et al., IEEE TNS 48, 2193 (2001)

## Slide 11: 1064 nm Front Side vs. Backside Illumination SPA ASET Mapping – LM124
Plots illustrate the spatial distribution of the SET amplitude
Sensitive areas clearly identified
Effects of metalization evident
LM124
Front side
1064 nm
Backside
1064 nm
Lewis, et al., IEEE TNS 48, 2193 (2001))

## Slide 12
Spherical Lens vs. Axicon TPA Charge Generation in Silicon
Hales, et al., IEEE TNS 67, 81 (2020)
PL SEE Using Axicon -- Quasi-Bessel Beam (QBB)
Notes: No annotation necessary

## Slide 13
PL SEE Using Axicon -- Quasi-Bessel Beam (QBB)
Hales, et al., Optics Express 27, p37652 (2019)
Constant LET
Notes: No annotation necessary

## Slide 14
45 nm RHBD
PLL test
Pulsed Laser Single-Event Effects

## Slide 15
Pulsed Laser Single-Event Effects
High-speed SiGe test

## Slide 16
Size ratio of sensitive volume to charge profile
108
10-6
106
104
102
100
10-2
10-4
Bulk Diode
Bulk Transistor
CMOS SOI
16
Laser/Ion Correlation/Prediction:
Description of the Challenge
Technology diversity
  CMOS, HBT, Bulk, Epitaxial, SOI, III-V, Heterojunction, FinFET, etc.
Incident laser pulse parameters
    Instrument characterization and calibration (reproducibility)
    Laser pulse energy, spot size, pulse width
  Accurate modeling of the charge deposition

## Slide 17
17
  Two Examples of Spatial Selectivity

## Slide 18
Spatial Selectivity: Direct Measurement of SET
Pulses in Chains of Inverters
800 inverters, 130 nm partially depleted SOI
Ferlet-Cavrois, et al., IEEE TNS Dec. 2007; Dec 2008

## Slide 19
OUT
IN
4 rows of 200 inverters
Row1
Row2
Row3
Row4
Laser strike positions
1.2 µm
Ferlet-Cavrois, et al., IEEE TNS Dec. 2007; Dec 2008
Spatial Selectivity: Direct Measurement of SET
Pulses in Chains of Inverters

## Slide 20
SET width is shorter than 200 ps for laser strikes close to the chain output
OUT
IN
SOI
WN 0.3µm
Ferlet-Cavrois, et al., IEEE TNS
Dec. 2007; Dec 2008

## Slide 21
OUT
IN
SET width is shorter than 200 ps for laser strikes close to the chain output
Transient widths increase for laser strikes far from the chain output
SOI
WN 0.3µm
Ferlet-Cavrois, et al., IEEE TNS
Dec. 2007; Dec 2008

## Slide 22
OUT
IN
SET width is shorter than 200 ps for laser strikes close to the chain output
Transient widths increase for laser strikes far from the chain output
SOI
WN 0.3µm
Ferlet-Cavrois, et al., IEEE TNS
Dec. 2007; Dec 2008

## Slide 23
OUT
IN
SET width is shorter than 200 ps for laser strikes close to the chain output
Transient width gets very large close to the chain input (1.8 ns)
SOI
WN 0.3µm
Ferlet-Cavrois, et al., IEEE TNS
Dec. 2007; Dec 2008

## Slide 24
Propagation-Induced Pulse Broadening (PIPB)
Propagation-Induced Pulse Broadening
• 2 ps/inverter
SOI
WN 0.3µm
Ferlet-Cavrois, et al., IEEE TNS Dec. 2007; Dec 2008

## Slide 25: PIPB Implications
  Interpretation and significance of existing data
  SET mitigation approaches ($$)
  Test methodologies
Ferlet-Cavrois, et al., IEEE TNS Dec. 2007; Dec 2008

## Slide 26
The pulsed laser permits the rapid and accurate location of SEU and SEL sensitive regions of COTS parts with sub-micron precision
This example: two Resolver-to-Digital Converters were screened for latchup for a NASA space mission
DDC RDC19220
Latch-Up Screening of COTS Parts for Space Missions

## Slide 27: Latch-Up Screening of COTS Parts for Space Missions
The latch-up sensitive areas for one of the parts is shown here
Based solely on these laser results, this part was eliminated from consideration for this and future NASA missions
SEL sensitive areas in COTS RDC
Buchner, et al., TNS, 46, 1445 (1999).
(DDC RDC19220)

## Slide 28: Latch-Up Screening of COTS Parts for Space Missions
The latch-up sensitive areas for one of the parts is here
Based solely on these laser results, this part was eliminated from consideration for this and future NASA missions
The other part, it turned out, was latch-up free and, eventually, was deemed acceptable for the mission in question
Part Screening to Reject
SEL sensitive areas in COTS RDC
(DDC RDC19220)
Buchner, et al., TNS, 46, 1445 (1999).

## Slide 29: Latch-Up Screening of COTS Parts for Space Missions
Early example of laser/ion correlation
0.8 mm bulk technology node
This example:
        2.8 pJ latchup threshold (590 nm)
        1.4 pC deposited charge
        LETth: 8 MeV·cm2/mg
        HI LET threshold: 5-15 MeV·cm2/mg
Can SEL screening be quantitative?
Buchner, et al., TNS, 46, 1445 (1999).

## Slide 30
Current Focus
Laser/Ion correlation
-vs-
Laser-based prediction of HI LET

## Slide 31
Current Focus: Moving from Laser/Ion Correlation to Prediction
Correlation Approaches
  Rely on existing accelerator data on a given DUT to inform test conditions
  Parameters are chosen to reproduce the known heavy-ion responses
  Depending on the source, this parameter space can be large
  Much more difficult to achieve for emerging 3DHI technologies
Predictive Approaches
  Do NOT rely on pre-existing accelerator data
  Parameters are chosen to produce specified charge generation within the DUT
  Generates an equivalent LET
Heavy-ion testing
Pulsed-laser testing
Predict
Correlate
Notes: No annotation necessary

## Slide 32
Correlation Approach
D. McMorrow, et al., TNS, vol. 47, Jun, 2000.
Use for Measurements
Empirical Laser/Ion Correlation Approach
Functional Correlation
LET Prediction
Threshold Laser Energy
Threshold Ion LET

## Slide 33
Predictive Laser/Ion Approach
LET Calculation
Use laser focusing that resembles charge profile of an ion
Predictive Approach
Use for Measurements
J. M. Hales, et al., TNS, vol. 70, Apr, 2023.
Measured SETs for LM124

## Slide 34
PL SEE Using Axicon -- Quasi-Bessel Beam
Hales, et al., Optics Express 2019
Constant LET
Notes: No annotation necessary

## Slide 35
QBB transients measured prior to heavy-ion measurements
QBB tuned to LET = 59 MeV·cm2/mg
Heavy-ion measurements subsequently performed at BNL, tuned to LET = 59 MeV·cm2/mg
Worst case transients chosen and compared directly to QBB transients;
  No adjustable parameters
  No curve fitting
Agreement is exceptional
LM124 SET Prediction Using QBB
Notes: No annotation necessary

## Slide 36
Empirical Correlation for SEL LET Thresholds
Mixed-signal 180 nm bulk (Jazz) ASIC using TPA-based laser testing.
Heavy-ion measurements performed on ASIC. LETth = 0.9 MeV∙cm2/mg
Empirical correlation used to provide quantitative estimates of the LET threshold at various circuit locations in an ASIC
Big Story: this procedure quantified the SEL threshold dependence on design parameters -- follow-on ASIC design showed a 50-fold improvement in the SEL threshold compared to the original design
Hales, et al, TNS, 69, 429-435 (2022)

## Slide 37
Hales, et al, TNS, 69, 429-435 (2022)
Mixed-signal 180 nm bulk (Jazz) ASIC using TPA-based laser testing.
Heavy-ion measurements performed on ASIC. LETth = 0.9 MeV∙cm2/mg
Empirical correlation used to provide quantitative estimates of the LET threshold at various circuit locations in an ASIC
Big Story: this procedure quantified the SEL threshold dependence on design parameters -- follow-on ASIC design showed a 50-fold improvement in the SEL threshold compared to the original design
Anchor
Empirical Correlation for SEL LET Thresholds

## Slide 38
Careful characterization of laser parameters and validated optical modeling approaches ensure that laser-equivalent LET, or LETL, can be accurately determined
Calculational Laser/Ion Correlation (LIC) Approach

## Slide 39
Calculational LIC – Prediction of SEL Thresholds
Calculational approach uses measured experimental parameters and laser energy threshold to calculate LETL
Good agreement with LET values determined empirically
Bigger Story: Calculational estimates use laser testing only; approach holds promise as a predictive tool for SEL threshold determination
Hales, et al, TNS, 69, 429-435 (2022)

## Slide 40
CHALICE
CHALICE went Live on January 1, 2025 and is available to the radiation effects community on the nanoHUB website: https://nanohub.org/resources/chalice
Instruction manual on nanoHUB
Introduced at the 2024 SEE Symposium

## Slide 41
CHALICE
A. Ildefonso, SEE Symposium, 2024
CHALICE can be used to calculate the laser pulse energy needed for screening

## Slide 42
Accurate SET prediction in complex devices has been demonstrated
  SEL in mixed-signal ASIC using calculational approach
  SET in an operational amplifier using QBB
Investigation in wider variety of devices being targeted
Predictive Laser SEE – Current Status
Correlate
Heavy-ion testing
Pulsed-laser testing
Predict

## Slide 43
Current Focus:
Laser-based prediction, screening, and alternative sources

## Slide 44: Single-Event Latchup Screening
SEL screening is routinely used for part rejection in different laboratories to eliminate parts from consideration for space missions and to minimize the amount of heavy-ion testing required (NASA, JPL, NRL, TRAD, others)
  Standard approaches currently do not exist
In contrast, SEL screening is rarely used for part acceptance, but that landscape is changing
Our challenge: to develop standard, quantifiable procedures for the SEL screening process that can be adopted by space programs and used by the various laser test facilities (and trusted by PMs)

## Slide 45
PL SEL Screening: Goal and Risk Reduction
Minimizing the risk associated with PL SEL screening
To minimize the need for HI testing
Relieve stress on test infrastructure
Goal: Develop a PL screening approach that determines whether a DUT will undergo SEL when operating in a specified heavy-ion radiation environment
Choice of laser wavelength
Focused beam size
Scanning parameters
Choice of operating point (LETL)
Limited acceptance screening

## Slide 46
PL SEL Screening: Decision Tree (partial)
Includes decision points, specific testing approaches, and recommendations
Pathway depends explicitly on optical access options for the part

## Slide 47
PL SEL Screening: Approach
LETL
LET [MeV cm2 mg-1]
Negative / No SEL:
LETth > LETL
∞
Positive / SEL:
LETth < LETL
During testing, a part’s sensitivity to SEL depends on its LETth relative to the LETL
Note that screening is binary: it’s a pass/fail test
LETth – LET threshold of DUT
LETL – operational set point

## Slide 48
PL SEL Screening: Approach
Setting LETL = LETtar can lead to false positives and false negatives
Key goal for screening is to reduce false positives and eliminate false negatives
LET [MeV cm2 mg-1]
∞
LETL ± DLETL
True positives:
LETth < LETtar
False positives:
LETth > LETtar
True negatives:
LETth > LETtar
False negatives:
LETth < LETtar
LETtar
LETth – LET threshold of DUT
LETL – operational set point
DLETL – accuracy error of LETL
LETtar – target program metric

## Slide 49
LETL ± DLETL
PL SEL Screening: Acceptance
For back-side parts, setting LETL = LETtar could still lead to false negatives
Set LETL = LETtar + 3*DLETL to establish high likelihood of avoiding false negatives
LET [MeV cm2 mg-1]
LETtar
∞
True negatives:
LETth > LETtar
False negatives:
LETth < LETtar

## Slide 50
DARPA Microsystems Technology Office (DARPA MTO)
Kicked-off September 2024
“The ASSERT program seeks to develop novel, compact SEE test sources and techniques to enable the radiation-hardness characterization of advanced 3D components, inform new device designs and selection, update radiation-hardening-by-design (RHBD) rules, and validate new computational models and simulation tools. ASSERT sources will be used to characterize mixed-signal devices containing a multiplicity of materials including but not limited to silicon, GaAs, wide bandgap materials such as SiC and GaN, and emerging ultrawide bandgap materials such as cubic boron nitride, gallium oxide, and silicon nitride.”
**From DARPA ASSERT BAA
Advanced Sources for Single-Event Effects Radiation Testing (ASSERT)
Advanced Sources for Single-event
Effects Radiation Testing (ASSERT)

## Slide 51
**
Advanced Sources for Single-Event Effects Radiation Testing (ASSERT)
**From DARPA ASSERT BAA

## Slide 52
Additional Requirements**
Beam penetration through metallization and packaging without de-lidding, substrate thinning, backside illumination, etc.
Beam position accuracy ±1 μm at the surface of the DUT (Phase 2); ± 0.2 μm at 5 mm penetration into the DUT (Phase 3) [Note 1]
Maximum pulse width of 2 ps FWHM (full-width half max)
Pulse repetition frequency (PRF) of 1,000 Hz (minimum) [Note 2]
Overall system volume <61 m3 (i.e., the interior volume of a 40-foot shipping container (11.2 m × 2.2 m × 2.3 m) [Note 3]
Advanced Sources for Single-Event Effects Radiation Testing (ASSERT)
**From DARPA ASSERT BAA
Spatial selectivity enables fault isolation
ASSERT beam

## Slide 53
Pulsed-Laser SEE (PL SEE) testing techniques have been in use for decades
    Both qualitative and quantitative data have contributed to the field
    Decades-long history of source development (beam delivery, characterization, testing requirements, etc.)
    Correlation and Predictive capabilities have been relevant topics from the start
  Lasers cannot penetrate metal layers, limiting their utility for 3DHI technologies
  But... we can leverage lessons learned over decades of developing correlation and predictive testing approaches using PL to develop new sources better equipped to characterize 3DHI technologies
Advanced Sources for Single-Event Effects Radiation Testing (ASSERT)

## Slide 54
Advanced Sources for Single-Event Effects Radiation Testing (ASSERT)
Role of Independent Verification and Validation (IV&V) Team
  Serve as technical advisors to the DARPA Program Manager (PM)
  Evaluate technical reports and data to provide feedback to DARPA PM
  Select target DUTs that have a range of complexity and SEE types, and provide information to performers
  Acquire benchmark SEE data that will be provided as Government Furnished Information (GFI) to verify correlation metrics
  Determine protocols for assessing response agreement
Performers will be expected to
  Deliver designs, simulation results, experimental demonstrations and test data (if applicable) to the IV&V team

## Slide 55: ASSERT performers and approaches
Pulsed electrons (Northrop Grumman, NASA JPL)
Pulsed X-rays (RadiaBeam Technologies)
Precision dosimetry (SLAC National Accelerator Laboratory)
Nano-strip sensors for sub-micron resolution dosimetry and sub-ns bunch discrimination for high precision particle tracking
Prior work demonstrates pulsed electrons producing single-event transients in large-area photodiode
D. Nergui, et al., IEEE TNS 2020
D. Monahan, SEE/MAPLD 2024
G. Tzintzarov, SEE/MAPLD 2024
G. Tzintzarov, SEE/MAPLD 2023
Prior work demonstrates use of pulsed X-rays to generate SEEs in SiGe HBTs
Inverse Compton Scattering source will generate monochromatic, tunable high-energy X-rays (20-50 keV) in compact footprint
Spot size found to be critical in correlating electron SEEs to heavy ions
Thorlabs FD010
Distribution Statement A - Approved for Public Release, Distribution Unlimited
Notes: Upper Left: G. Tzintzarov, presented at 2023 SEE Symposium, available online (https://www.seemapld.org/archive.php)
Bottom Left: G. Tzintzarov, presented at 2024 SEE Symposium, not yet available online (https://www.seemapld.org/program.php#day2)
Upper Right: D. Nergui, Available online (https://ieeexplore.ieee.org/abstract/document/8933079)
Lower Right: D. Monahan, presented at 2024 SEE Symposium, not yet available online (https://www.seemapld.org/program.php#day2)

## Slide 56
PL SEE Desk Reference (2023)
Can be found at:
https://apps.dtic.mil/sti/citations/trecms/AD1204115
Accession Number: AD1204115
Or go to the DTIC Website and search:
“Pulsed Laser Single-Event Effects”

## Slide 57
PL SEE Testing – A Practical Desk Reference
SEE Testing with a Laser Beam – Guidelines
PL SEE Desk Reference (2023)

## Slide 58
Summary and Conclusions
Overview of PL SEE
Spatial selectivity – specific examples
Current status of SEE correlation and prediction
Interesting things moving forward
  Laser/ion correlation
  Advances in LET prediction
  Axicon-based SEE
  PL SEE Part Screening
  Alternative Sources for SEE
Notes: No annotation necessary