## Slide 1
IFAST – 4th Annual Meeting
WP9 Meeting – STFC update
6 GHz cavities: Closed and Open geometries

## Slide 2: Deposition of the 6 GHz closed cavities: NbTiN

## Slide 3: 6 GHz Cavity deposition facility
Central target material in the form of a rod.
The sample can be 50 mm Cu/wafer or 6 GHz cavity.
Heating stage consists of six 240 W halogen bulbs for substrate heating up to 700 oC.
An external coil capable of producing magnetic field of up 800 gauss, provides the magnetic field for the magnetron assembly.

## Slide 4: Target material choice for 6 GHz deposition
Niobium/Titanium stoichiometry for NbTiN films were adjusted by target material.
  Target 1: Nb rod with Ti wire.
  Target 2: Nb37Ti63 alloy tube.
  Target 3: Nb37Ti63 alloy tube with Nb wire.

## Slide 5: NbTiN from Nb rod with Ti wire
Test sample using the Nb rod with Ti wire.
Four point probe measurement (FPP) on sapphire test sample shows high Tc close to theoretical (~18 K).
SEM showed crystal grains on the order of 10s nm in size.
Positive results suggested a potential deposition method for SRF thin film and therefore a 6 GHz copper cavity was coated.
Deposition parameters: Pulsed DC Magnetron Sputtering
- 200 W Power
- 350 kHz Repetition rate
- 1.1 µs Duty Cycle
- 600 oC Substrate temperature
- Kr to N2 (2:1 ratio)
- 5x10-2 mbar pressure
1 mA

## Slide 6: NbTiN from Nb rod with Ti wire
Unfortunately, the cavity delaminated when inspected at INFN
Courtesy of D. Ford

## Slide 7: NbTiN from NbTi rod
Cu substrate
Sapphire Substrate
Test sample using the NbTi alloy rod.
SEM and EDS show a dense structure with uniform stoichiometry.
FPP measured a lower Tc of 14.98 K, most likely due to the high Ti content.
Adjustment to increase Nb content before cavity deposition.
Deposition parameters: Pulsed DC Magnetron Sputtering
- 200 W Power
- 350 kHz Repetition rate
- 1.1 µs Duty Cycle
- 600 oC Substrate temperature
- Kr to N2 (2:1 ratio)
- 5x10-2 mbar pressure
1 mA
Element | Atomic (%)
Ti | 65
Nb | 35

## Slide 8: NbTiN from NbTi rod with Nb wire
The NbTi alloy rod was wrapped in Nb wire to adjust Nb:Ti composition.
SEM and EDS continues to show a dense structure with a Nb:Ti ratio (62:38)
FPP on sapphire measured Tc of 17.68 K.
After these results a 6 GHz copper cavity was coated.
Deposition parameters: Pulsed DC Magnetron Sputtering
- 200 W Power
- 350 kHz Repetition rate
- 1.1 µs Duty Cycle
- 600 oC Substrate temperature
- Kr to N2 (2:1 ratio)
- 5x10-2 mbar pressure
Cu substrate
Sapphire substrate
1 mA
Element | Atomic (%)
Ti | 38
Nb | 62

## Slide 9: NbTiN from NbTi rod with Nb wire
The NbTi alloy rod was wrapped in Nb wire to adjust Nb:Ti composition.
SEM and EDS continues to show a dense structure with a Nb:Ti ratio (62:38)
FPP on sapphire measured Tc of 17.68 K.
After these results a 6 GHz copper cavity was coated.
Deposition parameters: Pulsed DC Magnetron Sputtering
- 200 W Power
- 350 kHz Repetition rate
- 1.1 µs Duty Cycle
- 600 oC Substrate temperature
- Kr to N2 (2:1 ratio)
- 5x10-2 mbar pressure
Cu substrate
Sapphire substrate

## Slide 10: NbTiN from NbTi rod with Nb wire (He)
The NbTi rod & Nb wire deposition was repeated with He as the process gas to adjust the sputtering dynamics.
SEM shows a different structure formation in the film and a lower Nb content by a few %.
FPP on sapphire measured Tc of 17.57 K with very sharp transition.
A 6 GHz copper cavity was coated.
Deposition parameters: Pulsed DC Magnetron Sputtering
- 200 W Power
- 350 kHz Repetition rate
- 1.1 µs Duty Cycle
- 600 oC Substrate temperature
- He to N2 (2:1 ratio)
- 5x10-2 mbar pressure
Cu substrate
Sapphire substrate
1 mA
Element | Atomic (%)
Ti | 42
Nb | 58

## Slide 11: Deposition of the 6 GHz split cavity

## Slide 12: 6 GHz Split Cavity
Progress on deposition on the split cavity has resumed as the cryogenic testing facility has been recommissioned - now reaching 2.8 K.
Latest tests have been conducted on cavity A: Which was electropolished by INFN.
Research plan:
Deposit Nb to be tested.
Deposit Nb3Sn thin film on top of Nb layer.
Cavity A: as received
Before installation in deposition system

## Slide 13: 6 GHz Split Cavity: Latest Nb deposition
Deposition parameters: HIPIMS
- 300 W Power
- 1000 Hz Repetition rate
- 100µs Duty Cycle
- 520 oC Substrate temperature
- Kr process gas
- 5x10-3 mbar Deposition pressure
Face 2
Heater stage uses 6 halogen bulbs to heat each face of the split cavity 520 oC.
Each face was deposited sequentially, 8 hours for each face.
Cavity A: Heated to 500oC
Cavity A: Nb layer deposited
Face 1

## Slide 14
6 GHz Split Cavity Tests
Latest result 38.3 μΩ a factor of two lower than previously deposited electropolished cavities.
Compared to previous the substrate temperature was increased by 100 oC.
Residual resistance is still an order of magnitude higher than expected.
Investigation into the cause of high residual resistance in the split cavities in ongoing.
Courtesy of D. Seal & N. Leicester
 | Rs, 4.2 K (μΩ)
Nb A 5 | 38.3
Nb B 1 | 70
Nb C 1 | 70
Nb A 1 | 131

## Slide 15: 6 GHz Open Cavity: Nb3Sn deposition
Deposition parameters: DC magnetron sputtering
- 50 W Power
- 520 oC Substrate temperature
- Kr process gas
- 5x10-3 mbar Deposition pressure
Unfortunately, during the first Nb3Sn deposition the heating failed after 20 hour.
The sample was vented, heater stage was fixed and both split cavity faces were redeposited on.
Each face was deposited sequentially, 24 hours for each face.
Cavity A: Nb3Sn deposition on face 1
Cavity A: Nb3Sn deposition on face 2

## Slide 16
Acknowledgements
C. Pira, O. Azzolini, R. Caforio, E. Chyhyrynets, D. Fonnesu, D. Ford, V. Garcia, G. Keppel, G. Marconato, A. Salmaso, F. Stivanello (LNL) M. Bertucci, R. Paparella (LASA)
O.B. Malyshev, R. Valizadeh, C. Benjamin, T. Sian, L. Smith, D. Seal
C.Z. Antoine, S. Berry, Y. Kalboussi, T. Proslier
D. Longuevergne, O. Hryhorenko,
S. Keckert, O. Kugeler, J. Knobloch
S. Prucnal, S. Zhou
X. Jiang, T. Staedler, A. Zubtsovskii
E. Seiler, R. Ries
A. Medvids, A. Mychko, P. Onufrievs
G. Burt, N. Leicester, S. Marks, D. Turner
W. Bradley, S. Simon
R. Berton, D. Piccoli, F. Piccoli, G. Squizzato, F. Telatin
A. M. Valente Feliciano
Associated Partners
Informal Partners
Notes: Replace this guidance text with your own bullet pointed content.
For further guidance please see https://www.bdadyslexia.org.uk/advice/employers/creating-a-dyslexia-friendly-workplace/dyslexia-friendly-style-guide

## Slide 17
Nb 3d
Ti 2p
N 1s
O 1s
461.1 eV
400.3 eV
530.9 eV
455.5 eV
397.8 eV
204.0 eV
206.8 eV
The X-ray photoelectron spectra indicate that the Nb, Ti, and N are in the form of a nitride.
The presence of oxygen is attributed to the sample's exposure to air and the formed oxide layer not fully removed from in situ cleaning.
NbTiN from NbTi rod with Nb wire (He)
Notes: Replace this guidance text with your own bullet pointed content.
For further guidance please see https://www.bdadyslexia.org.uk/advice/employers/creating-a-dyslexia-friendly-workplace/dyslexia-friendly-style-guide