## Slide 1: Beam Intercepting Devices at CERN Types, Challenges, Design, R&D and Operation
Antonio PERILLO MARCONE (SY-STI)
25th June 2025 Lecture 1/2

## Slide 2: Disclaimer
These lectures will present a phenomenological and broader approach in the design, construction and operation of beam intercepting devices, focusing on requirements, technologies and operational constraints
Dedicated Accelerator Schools (CAS, USPAS, JAS, etc.) are available to expand the calculation part

## Slide 3: Structure of the lectures
Lecture 1 will be focused on general concepts, definition and challenges in the design of beam intercepting devices
Lecture 2 will provide specific examples of advanced components recently built, in commissioning & in operation at CERN

## Slide 4: Acknowledgments
Many thanks to several colleagues for their contribution and material
M. Calviani, A. Lechner, C. Torregrosa, R. Ximenes, F.-X. Nuiry, L. Salvatore Esposito, R. Rossi, O. Aberle
And material from A. Bertarelli, P. Hurh, B. Riemer, M. Wohlmuther & many others

## Slide 5: Beam Intercepting Device – a possible definition
A beam intercepting device is a component that intercepts accelerated particle beams for diverse purposes, such as
Production of secondary particles (target)
Beam cleaning equipment (collimator)
Safe disposal (dump)
Protection of sensitive equipment (dumps, collimators)

## Slide 6
Safety function
Beam stoppers
Beam cleaning & control
Collimators
Scrapers
Beam dumps
Strippers
Slits
Physics
Particle producing targets

## Slide 7: Challenges to be faced (1/3)
Devices must be able to withstand operation and accident scenarios, whilst protecting sensitive equipment
Sometimes employed as “last line of defence” against component damage
Operational teams rely heavily on dependable components, whose failure often leads to long periods of downtime
BIDs are usually the most radioactive components in an accelerator complex (cool down, ALARA)
https://cerncourier.com/a/intercepting-the-beams/

## Slide 8: Challenges to be faced (2/3)
Operation in Ultra High Vacuum (10-10 mbar)
Movable parts with extremely high precision and tight geometrical tolerances (e.g., flatness, alignment)
High energy densities (several kJ/cm3/pulse)
High power densities (~MW/cm3)

## Slide 9: Challenges to be faced (3/3)
High beam kinetic energy (up 700 MJ)
High average deposited power (several hundreds of kW)
Physics requirements (sometimes implying materials with poor structural properties)
Impedance (especially for colliders)
Radiation damage – modification of thermo-physical and mechanical properties

## Slide 10: BIDs lifecycle
Lifecycle for the successful construction & operation of BIDs/Target Systems
Functional requirements
Conceptual design
R&D + prototype + testing
Advanced design
Procurement and construction
Operation / maintenance
Disposal
Commissioning
Lessons learnt at every step …

## Slide 11: Boundary conditions & constraints
Integration and localisation constraints (tunnels, alcoves, etc.)
Thermo-mechanical stability
Material damage (lifetime & reliability)
Operational availability
Safety for personnel and for machine
Handling, accessibility & maintenance considerations
Design is a complex and iterative process, which must satisfy multiple requirements with, in most cases, incomplete data to start with

## Slide 12: Boundary conditions & constraints
Warning:
Unclear functional requirements may later affect performances, safety, reliability/maintainability and inspectability
Initial cost estimate must be carefully thought albeit lack of clear specifications
Design is a complex and iterative process, which must satisfy multiple requirements with, in most cases, incomplete data to start with

## Slide 13: Knowledge of beam parameters impacting on BID
BID design parameters and constraints generally scale with particle peak intensity (e.g., protons per unit area)
Peak value can be highly dependent on the beam profile (e.g. gaussian, flat, or a combination, sweeps or rastered)

## Slide 14: Beam-matter interaction simulations
Following material Coulomb interactions during the cascade, atoms & molecules vibrate and therefore T increase!
In engineering terms: part of the energy is lost in the BID and converted into thermal energy (heat!) – this occurs almost instantaneously
Courtesy A. Lechner
Deposited energy (per unit volume)
[J cm-3]
Density [g cm-3]
Specific heat
[J g-1 K-1]
See presentation in this CAS by G. Lerner on 22/06
https://indi.to/6dFTv
Notes: In the adiabatic assumption, energy deposition shorter than diffusion time (e.g. microseconds)

## Slide 15: What are we talking about? SPS beam dump
A proton bunch has typical time duration of 1 ns
Pulses are constituted by bunches separated by tens of ns (25 ns)
Dumps (like targets) are made to sustain beam impacts repeatedly – in the case of SPS, every O(7.2) seconds
needs to be absorbed and dissipated!

## Slide 16: What are we talking about? LHC beam dump
Beam energy will be 6.8 TeV (6800 GeV) from 2022
Nb = 2748, with a bunch population up to 1.8x1011
This enormous energy is deposited in 89 ms
This is really a big value 
could melt 2.5 t of Cu
We will see tomorrow what are the effects of these quantities on large components and how to tackle them from an engineering standpoint

## Slide 17: Thermal behaviour of BIDs
After the pulse, the energy diffuses through the material and the peak temperature drops
After several repeated pulses, the temperatures will rise until a “pseudo steady state” is reached  quasi-static temperature profile
For a pulsed beam, energy is generally deposited in a target material in a very short time
https://doi.org/10.1103/PhysRevAccelBeams.24.093001

## Slide 18: Heat diffusion mechanisms – conduction
Almost all BIDs use conduction to remove heat from heated volume to surface for cooling
Conduction is diffusion of heat via random molecular and/or atomic interactions
1st interface graphite/CuCrZr
2nd interface CuCrZr/316LN
Heat flux
Heat conductivity

## Slide 19: Other (conventional) heat transfer methods
Convection
  Transfer heat from a surface into a fluid
  Motion of the fluid & diffusion inside fluid
Radiative cooling
  Via electromagnetic radiation  only effective at high T & DT
Convective boiling
  E.g., hypervapotron systems
  Not extensively employed in BIDs
emissivity
HTC = heat transfer coefficient
Stefan-Boltzmann constant
CNGS target

## Slide 20: Selection of cooling methods for BIDs
Several considerations add up in the selection – all are related to each other and must be considered at the same time & links to material selection:
Operational requirements (what is the average power?)
Cooling requirements (heat removal, operating temperature)
Robustness (what are the risk associated with the cooling media)
Chemical reactions between fluid and material (corrosion, erosion, radiolysis)
Safety (radiological and conventional, water vs. air)

## Slide 21: Basic mechanical property concepts
Young’s modulus describe a material stiffness (deformation for a given stress)
Material strength:
  Yield
  Ultimate
Relative deformation or change in shape and size of elastic or plastic nature under applied forces
We want typically BIDs to operate here
Notes: In general we would like to have materials with low Young’s modulus, since deformation is determined by DeltaT while stress is proportional to the Y modulus.
However, materials with low E also have low yield, so we must find a compromise for all applications.

## Slide 22: Finite Elements Methods for BIDs
Total stresses (force per unit area) inside a material can be generated by:
  Mechanical loads
  Thermal gradients (expansion)
  Geometrical constraints
In BIDs, the main source of stress is generally the non-uniform temperature distribution generated by beam impact
Analytical methods exist for simple shapes, but generally dedicated codes are used (ANSYS, COMSOL, etc.)

## Slide 23: Steps for Finite Element Modelling
Model setup
  Geometry (e.g., from CAD) & definition of material properties (mostly varying with temperature) & mesh generation (important step)
  Definition of loads (hence internal heat generation from MC codes) & boundary conditions
Thermal analysis (transient, steady-state…)
Structural analysis (static, dynamic)
Thermal-Structural coupling (complex analysis performed in some specific cases)

## Slide 24: Example of material response
Tmax=335°C
~0.07% plastic deformation
Tservice CuCrZr= 400°C
Yield strength= 280 MPa
Courtesy F.-X. Nuiry
CuCr1Zr absorbing block from 4th generation SPS beam dump (see tomorrow)

## Slide 25: Example of material response
Elastic stress waves travelling at the speed of sound in the materials
Density
Stiffness coefficient
Courtesy F.-X. Nuiry

## Slide 26: Dynamic regimes
BIDs for accelerators are generally designed to work in the elastic regime (deformation can recover)  reliability
Beam impact accidents (or even nominal operation) can provoke also permanent deformation of the component  plastic regimes (irreversible damage)
Sometimes the effect is much more catastrophic, if instantaneous power is high enough  quasi shockwave regime
Phys. Rev. Accel. Beams 22 013401 (2019)
Journal of Dynamic Behavior of Materials (2019) 5:266–295

## Slide 27: Palette of absorbing materials employed at CERN
BIDs requires a variety of different materials, characterised by largely different parameters – some generalities of employed materials are reported
Graphitic materials (and CfC)
1-1.8 g/cm3
Aluminium alloys
2.7 g/cm3
Titanium & alloys
4.5 g/cm3
(Stainless) steels
7.5-8 g/cm3
Low CTE, good thermal conductivity, low r, very high service T, exceptional robustness to beam impact
Light structural materials, good thermal conductivity, low Tm, poor properties at high T
Exceptional strength while light, low CTE, low thermal conductivity
“king” of structural materials, low thermal conductivity

## Slide 28: Palette of absorbing materials employed at CERN
Mo-alloys and TZM
10.2 g/cm3
CuCrZr1 & Glidcop®
8.9 g/cm3
Tantalum
16.6 g/cm3
Tungsten and alloys
18-19.3 g/cm3
Lead
11.3 g/cm3
Iridium
22.6 g/cm3
Very good heat conductivity, good strength and stability at high T
Reasonably low CTE, relatively good strength
Refractory metal, stable high, ductile, extreme corrosion resistance
Target material for neutron production, very low Tm, almost negligible strength
Target material for pbars, poor mech. performances, very high r
High r and related absorption power, alloyed-W has good machinability
Notes: Glidcop is a family of copper-based metal matrix composite (MMC) alloys mixed primarily with small amounts of aluminium oxide ceramic particles
The aluminum oxide particles block dislocation creep, which retards recrystallization and prevents grain growth; thus preserving the metal's strength at high temperatures. They also protect the metal against radiation damage.[3] On the other hand, they exclude the possibly of heat treatment or hot working of the worked parts.

## Slide 29: Figure of Merits
From: A. Bertarelli, Joint International Accelerator School (2014)
TSI = Thermal Stability Index
TRI = Thermomechanical Robustness Index

## Slide 30: Selection for absorbing materials for BIDs
Physics requirements
Functional reliability / integrity
Operational safety (for personnel and machine)

## Slide 31: Targets - Physics requirements
Different type of sources depending on experiments:
  “Point-like” source (e.g., antiproton production), very dense with small physical dimensions
  Massive target acting as dump (e.g., neutron production)
  Long, narrow target (e.g., neutrino production), low density but several nuclear inelastic lengths
  Refractory metals (e.g., RIB production), need to be heated “externally” to maximize effusion
  Fusion-like neutron sources (14 MeV) need for example deuterons on Li target
  Medical isotope production & harvesting (from U, water, etc.)
Constant iterations between physicists and engineers to find the right compromise between availability/reliability and physics output

## Slide 32: Functional reliability / integrity
BIDs not to get damaged under load!
Strength, fatigue, cooling performance
Erosion, corrosion, wear
High temperature, high strain-rate performance
Complexity, repairability, repeatability, Quality Assurance
  If special materials are employed, make sure it is available 5/10/15 years later (e.g. for refurbishments/replacements)

## Slide 33: Operational safety
Safety critical components vs. replaceable components
  Some components in a target facility are replaceable, hence expected to fail at a certain rate, posing little safety risk (e.g., pbar target)
  Some components are part of a safety matrix (especially for personnel protection) (e.g., beam stoppers)
  QA and conservative choices should be increased for safety critical components
  Safety critical components should be “damage tolerant”, especially in the case of off-normal events. In these cases, ductility (ability to plastically deform without fracture) is highly desirable

## Slide 34: Radiation protection considerations
Radiation protection considerations are essential in the design iteration of beam intercepting devices – impact on
  Operation – for intervention, exposure to personnel, downtime
  Radioactive waste - long-term disposal & design must (start to) be part of the items to think to from the very beginning
General principles (when possible!):
  Low activation materials (e.g., low-Co stainless steels)
  Toxic materials to be avoided (beryllium, Pb)
  Safe disposal

## Slide 35: Ultra High Vacuum design for BIDs
As for other components that are installed in the machine’s Ultra High Vacuum, BIDs must also comply to requirements of UHV
Additional challenges for BIDs are generated by:
  Movable parts, no lubrification allowed  not compatible with UHV
  High temperatures during beam impact  increase outgassing
  Use of graphitic materials  tendency to absorb and release gasses (outgassing issues)
QA steps and careful control of design processes is a fundamental aspects of BIDs design, construction and reliable operation

## Slide 36: Ultra High Vacuum design for BIDs
Vacuum criteria
Leak tightness
(e.g. 1·10-10 mbar∙l∙s-1)
Contamination
(hydrocarbons, CO/CO2, higher Z – from cleaning or poor design)
Outgassing (from internal components)
(e.g. threshold 10-7 mbar∙l∙s-1)
Virtual leaks (e.g. trapped pockets of gas)
(< 5∙10-9 mbar∙l∙s-1)

## Slide 37
Residual Gas Analysis spectrum for a collimator jaw
  48 hours at room T after a bake-out cycle at 250°C
Gas-rates normalized to H2 and respective limits for different gas species
CO2
CO
CH4
H2O

## Slide 38: Beam impact experimental testing and validation
Validation of design often include the possibility of testing components or integral devices under beam impact
Sometimes devices and materials operate at the extreme – uncharted territory of temperature and stress (where EOS are not available)
Existing material constitutive models at extreme conditions are limited and mostly drawn from military research (e.g. Ta, Ir).
Dedicated tests allows for numerical vs. experimental cross-check

## Slide 39: Integral and material testing at CERN HiRadMat facility
440 GeV/c, up to 288 bunches, 1.3*1011 ppb
Pulse length: 5 ns – 7.2 ms
Beam radius: 0.25 mm – 4 mm
Dedicated facility for studying the impact of intense pulsed beams on materials
J. Phys.: Conf. Ser. 1350 012162

## Slide 40: Application of HiRadMat to antiproton production
Efficient pbar production requires maximizing interaction in a short distance
AD-T core made of Ir (22.3 g/cm3), 3 mm diameter, 55 mm length
2000 ºC in 0.43 ms
Antiprotons
HORN
TARGET CORE
Phys. Rev. Accel. Beams 19, 073402 (2016)
Extreme dynamic response!

## Slide 41: Relevance of post-irradiation examination
Irradiated AD-target (2000-2008), 1.6*1019 POT
ESTIMATED DPA
Upstream face
Mid face
Iridium core is an amalgam of broken, melted & re-solidified fragments
Cracks in the graphite matrix also observed

## Slide 42: Application of HiRadMat to antiproton production
Target Core made of 10x Ta rods (un-annealed) 8 mm ⌀ by 16 mm in length
Embedded in a matrix made of compressed layers of Expanded Graphite (EG)
Encapsulated in Ti-6V-4Al e-beam welded container
Phys. Rev. Accel. Beams 21, 073001 (2018)
x49 pulses impacted (ΔTmax/pulse = 1800 ºC)
Reliance on post-irradiation examination

## Slide 43: Post Irradiation Examination of Ta-irradiated sample
Neutron Tomography @PSI (NEUTRA)
Phys. Rev. Accel. Beams 21, 073001 (2018)
European Journal of Mechanics / A Solids 85 (2021) 104149
Target opening and slicing cores at CERN
Observation of spalling voids
Tensile pressure shall be kept <2-3 GPa to avoid void nucleation

## Slide 44: Application of HiRadMat to antiproton production New target design
Air cooled target
Sliced core, with different diameter and length
Matrix of different graphitic materials
Courtesy C. Torregrosa

## Slide 45: Application of HiRadMat to antiproton production New target design – tested at HiRadMat
Courtesy C. Torregrosa

## Slide 46: Application of HiRadMat to antiproton production Some results
Ø3 mm
Extensive Longitudinal cracks
Material displacement along the face
Longitudinal cracks in the isostatic-graphite matrix!
Courtesy C. Torregrosa

## Slide 47: Application of HiRadMat to antiproton production Some results
Good behaviour of advanced materials
TFGR W-TiC in two different configurations
Courtesy C. Torregrosa

## Slide 48: Long-term radiation damage
Irradiation of materials by particles causes microstructural defects (atomic displacements & transmutation products)  in turn creates macroscopic effects
Related to:
  Ionizing energy losses/heating (i.e. electron stopping power)
  Non-ionizing energy losses (energy transfer to atomic nuclei  displacement damage)
  Gas production (mostly due to protons, 2H, 3H, 3He and alphas stopping in the target)
Additional variable to consider in the design of beam intercepting devices, especially targets and beam windows

## Slide 49: Long-term radiation damage Thermo-physical effects
Embrittlement, creep, sweeling, fracture toughness reduction, thermal and electrical resistivity reduction, CTE, young’s modulus, transmutation products, etc.
Dependent on particle type, energy and rate of irradiation
S. A. Malloy, et al., Journal of Nuclear Material, 2005. (LANSCE irradiations)
N. Maruyama and M. Harayama, “Neutron irradiation effect on … graphite materials,” Journal of Nuclear Materials, 195, 44-50 (1992)
10x reduction at 0.02 DPA

## Slide 50: Displacement per Atom
Is a measure of the amount of radiation damage in irradiated materials
  For example, 3 DPA means each atom in the material has been displaced from its site within the structural lattice of the material an average of 3 times
Displacement damage can be induced by all particles produced in the hadronic cascade, including high energy photons, albeit on a smaller scale  directly related to energy transfers to atomic nuclei
Does not account for thermal annealing after the initial cascade and subsequent recombination
NB: it cannot be measured, only estimated via Monte Carlo codes (FLUKA, MARS, PHITS, etc.)

## Slide 51: How can we test materials?
Proton beam
Cooling water
Target basket
110 MeV
93 MeV
30 MeV (C-slot)
68 MeV
RbCl 1
RbCl 2
Courtesy K. Doyhun (BNL) & N. Solieri (CERN)
BLIP irradiation @Brookhaven National Laboratory
Capsules containing graphitic materials irradiated at 0.1 DPA

## Slide 52: Challenges of post-irradiation examination
Irradiation capsule are extremely radioactive, need a dedicated hot-cell and expertise to handle the samples
Ta2.5W samples
Mo-coated MoGR samples
Mo-coated CfC sample
Preliminary results indicate good adhesion of Mo-coating on graphitic materials, with hardening of bulk

## Slide 53: Challenges for the future
Courtesy A. Lechner

## Slide 54: Conclusions
Beam Intercepting Devices are multi-physics, multi-expertise systems combining challenging requirements
Reliable construction depends on a delicate balance of different requirements and constraints
Operational experience is a key aspect in the feedback loop – example of CERN’s devices in Lecture 2