## Slide 2: Outline
1. Requirements
2. Brandt model (cos-theta)
3. Bean model (block coil)
4. Open points

## Slide 3: Requirements
Estimation of the hysteretic losses
Block coil
Cos-theta coil
Bean model
Brandt model
Requirements
Brandt model
Bean model
Open points

## Slide 4
Implementation of Brandt Model in MATLAB for REBCO magnetization effect

## Slide 5: Quadrature points “qp” in Matlab
Inside each block of the magnet, a grid of quadrature points was built;
Each point is characterized by a value of sheet current density (A/m).
Requirements
Brandt model
Bean model
Open points

## Slide 6: Inizialization
a uniform current distribution was supposed to flow inside the magnet
(i.e. same value of for each ).
The magnetic flux density value was calculated in each quadrature point.
Requirements
Brandt model
Bean model
Open points

## Slide 7: Critical sheet current
For each the value of critical sheet current density has been calculated taking into account both the intensity and the direction of .
For each tape was calculated the mean critical sheet current density , useful to implement Brandt Formula.
,
Requirements
Brandt model
Bean model
Open points

## Slide 8: Brandt Formula
To calculate the new sheet current density for each by the following formula
where
the values of for each tape must be obtained
(and ).
N.B. the parameter if , while if
qp 1
qp 2
qp 3
qp 4
qp 5
qp n
…
Requirements
Brandt model
Bean model
* self-field versus field contribute

## Slide 9: b, w values
perpendicular magnetic field averaged along the tape (.
Requirements
Brandt model
Bean model
Open points
Digitare l'equazione qui.

## Slide 10: Iteration process
Iteration n
100
1
The new value of sheet current density obtained by the Brandt formula will generate a new field map that will generate a new sheet current distribution .
The process must be iterated several times until convergence is achieved.
Requirements
Brandt model
Bean model
Open points

## Slide 11: Magnetization calculation
Once the convergence in current distribution is achieved, the magnetization and the hysteretic loss produced inside each tape is calculated by the following formulas*:
,
The total loss at each current value is obtained by
considering the contibution of each tape.
*general formula for magnetization:
, with
Hysteretic Losses
Requirements
Brandt model
Bean model
Open points

## Slide 12: Field, Current, Losses
CURRENT DISTRIBUTION (J/Jc)
HYSTERETIC LOSSES (P)
MAGNETIC FIELD (B)
Requirements
Brandt model
Bean model
Open points
P(W/m)

## Slide 13: References
https://en.wikipedia.org/wiki/Biot-Savart_law
E. H. Brandt and M. Indenbom, “Type-ii-superconductor strip with current in a perpendicular magnetic field” ,
Physical review B, vol. 48, no. 17, p. 12893, 1993.
https://en.wikipedia.org/wiki/Magnetic_moment
Requirements
Brandt model
Bean model
Open points

## Slide 14
Estimation of the hysteretic losses in SC layer via Brandt Model

## Slide 15: Goals
Although the loss mechanism is of a resistive nature, the resistance is highly nonlinear, with the results that the loss per cycle is independent of the cycle time.
Hysteretic losses = red area between the two curves.
Problem: we do not know the trend of the curves.
We can estimate hysteretic losses by circumscribing the hysteresis losses with a rectangle.
We are only interested in the ramping phase of the magnet  we can only consider half rectangle.
Requirements
Brandt model
Bean model
Open points

## Slide 16: Goals
: peak-to-peak amplitude of oscillating field
: amplitude of field oscillation which just penetrates to the centre of the sample (penetration field)
: magnetization
: fully penetrated magnetization
We have to calculate:
Without the presence of transport current (
With the presence of transport current
Requirements
Brandt model
Bean model
Open points

## Slide 17: Studied configuration
1
2
3
x
N° double pancakes | N° tapes (m/m)
1 | 1048 (524+524)
2 | 1048 (524+524)
3 | 1080 (540+540)
Tot | 3176
Requirements
Brandt model
Bean model
Open points

## Slide 18: Assumptions with
Ramp oscillation
Bean model:
  Current density: 0 or
  Penetration of the external field with constant gradient
External field perpendicular to the broad face
Requirements
Brandt model
Bean model
Open points

## Slide 19: Magnetization
Definition:
  where: = magnetic moment
Cross product:
Magnetization (with for Bean model):
if
if
Requirements
Brandt model
Bean model
Open points

## Slide 20: Magnetization (M)
We take into account a factor 2 for the “closure at infinity” (to take the end of the magnet into account):
Requirements
Brandt model
Bean model
Open points

## Slide 21: Peak-to-peak amplitude
We assume that the value of the peak-to-peak amplitude of oscillating field is equal to the average field inside the SClayer (slab)
Requirements
Brandt model
Bean model
Open points

## Slide 22: Hysteretic losses
Hysteretic losses per unit volume = red area:
Requirements
Brandt model
Bean model
Open points

## Slide 23: Hysteretic losses
Hysteretic losses per unit length :
Requirements
Brandt model
Bean model
Open points

## Slide 24: Assumptions with
Ramp oscillation
Bean model:
  Current density: 0 or
  Penetration of the external field with constant gradient
External field perpendicular to the broad face
Requirements
Brandt model
Bean model
Open points

## Slide 25: Magnetization
Definition:
  where: = magnetic moment
Cross product:
Magnetization (with for Bean model):
if
if
Requirements
Brandt model
Bean model
Open points

## Slide 26: Magnetization (M)
We take into account a factor 2 for the “closure at infinity” (to take the end of the magnet into account):
Requirements
Brandt model
Bean model

## Slide 27: Magnetization (M)
We determine the value as a function of transport current  we balance the currents:
Requirements
Brandt model
Bean model
Open points

## Slide 28: Magnetization (M)
We substitute the value of in the total magnetization expression:
Same expression as in the case with
Requirements
Brandt model
Bean model
Open points

## Slide 29: Peak-to-peak amplitude
We assume that the value of the peak-to-peak amplitude of oscillating field is equal to the average field inside the Sc layer (slab)
Requirements
Brandt model
Bean model
Open points

## Slide 30: Hysteretic losses
Hysteretic losses per unit volume = red area:
Same expression as in the case with
Requirements
Brandt model
Bean model
Open points

## Slide 31: Hysteretic losses
Hysteretic losses per unit length :
Same expression as in the case with
Requirements
Brandt model
Bean model
Open points

## Slide 32: Results
Block coil with Bean model
Cos-theta with Brandt model
Q | Value | U.M.
 | 527.52 | kJ/m
 | 651.6 | kJ/m
Q | Value | U.M.
 | 527.52 | kJ/m
 | 651.6 | kJ/m
Q | Value | U.M.
 | 36 | kJ/m
Q | Value | U.M.
 | 36 | kJ/m
Results referred to the entire cross section (not a quarter!)
Results referred to the entire cross section (not a quarter!)
Requirements
Brandt model
Bean model
Open points

## Slide 33: Open points
Goal: draw conclusions
Do these values constitute a problem from a cryogenic point of view ?
Considering the workforce and time schedule, does it make sense to further investigate the hysteretic losses ?
Is there a maximum time limit for the ramp phase of the magnet ?
Requirements
Brandt model
Bean model
Open points

## Slide 34: How we implemented the method in Ansys
We apply a uniform engineering current density to each pancake in ANSYS.
We extrapolate the field map.
We create a path of 100 points corresponding to each SC layers (for simplicity of calculation, we divide the thickness of each pancake by the number of SC layers).
We know the field distribution  we can calculate the average field inside each SC layer
1
2
3
x
We must calculate each parameter of the following formula:
Calculation of

## Slide 35: How we implemented the method in Ansys
We can use the critical current density fit
  We calculate the critical current density for each SC layer with the previously calculated average field values.
Calculation of
We must calculate each parameter of the following formula:
Requirements
Brandt model
Bean model
Open points

## Slide 36: How we implemented the method in Ansys
We know the cross section of the SC layer.
Calculation of
We must calculate each parameter of the following formula:
Requirements
Brandt model
Bean model
Open points

## Slide 37: How we implemented the method in Ansys
We can use the critical current density fit
  We calculate the critical current density for each SC layer with the previously calculated average field values.
Calculation of
We must calculate each parameter of the following formula:
Requirements
Brandt model
Bean model
Open points

## Slide 38: How we implemented the method in Ansys
We know the engineering current density and the filling factor of the tape (from geometric consideration)
We can calculate the transport current density in each SC layer
Calculation of
We must calculate each parameter of the following formula:
Requirements
Brandt model
Bean model
Open points