## Slide 1: Future challenges for radiation hard materials in HEP experiments
Nicola Pacifico

## Slide 2
[Old] Motivation: the HL-LHC radiation environment
Inner Pix:~ 10 MGy, 1017 neq/cm2
Outer Pix:~ 1 MGy, 1016 neq/cm2
Outer Tracker: ~ 0.1 MGy, 1014 neq/cm2
An unprecedented radiation level for HEP experiments
Significant performance degradation expected from radiation damage for
  Sensors
  Electronics
  Mechanics / services
Inadequate existing data con radiation performance of many custom or commercial materials => new tests were required on many materials.

## Slide 3
Motivation: radiation damage in materials
Radiation damage mechanisms | 
Ionization damage | Displacement damage
Conductors/semiconductors: | All materials:
Totally recoverable | Typically not recoverable at room temperature Macroscopic effects on structural properties are usually noticeable at relatively high fluences (~>1018 n/cm2) Electrical properties in semiconductors affected at doping concentration levels (~>1010 n/cm2)
Insulators: | 
Not recoverable In polymers: degradation of polymeric chains Charging up of passivations | 

## Slide 4
Present rationale
In current (LS3) scenarios
Ionization damage overwhelming in polymers
Logistic limitations in destructive testing of activated materials (after hadron irradiation)
Gamma irradiation only viable option (for systematic testing)

## Slide 5: Common test standards
Standard | Test structure | Quantity
ASTM D1002 | Single lap joints | Apparent lap shear strength
ISO 25217 | Double cantilever beams | Mode 1 fracture energy
ASTM D638 | Dogbones | Tensile properties
ASTM D5740 | Cast discs/ sandwiches | Apparent thermal conductivity

## Slide 6: Materials of interest (categories):
Adhesives (epoxies, impregnations glues, thermally conductive glues, tapes)
Encapsulants
Thermally conductive interfaces
Connectors
Cables
CFRP or Carbon Foam structure
… and more as they come…

## Slide 7
Testing materials: Irradiation facilities

## Slide 8: Aging/irradiation tests: some considerations
Most reliable scenario: irradiation in “free spots” in experimental caverns
Pros: - radiation field reflects the “real” one
- comes for “free”
Cons: - long irradiation times (years) – planning often doesn’t allow this - environment can be tricky (standard atmosphere, no humidity control)
- samples can be accessed only during shutdowns
Realistically achievable scenario: irradiation in dedicated high rate facilities
Pros: - short irradiation turn-over times (suitable e.g. for R&D) possibility
Cons: - accelerated aging can be not fully representative of “real” aging
(there is evidence of dose rate dependence of degradation on some materials) - necessary to control temperature and ozone formation
- can be expensive

## Slide 9: Specialized irradiation facilities
Type | Field characteristics | Application
> GeV protons | High dose rate, small sample size (~cm^2) or scanning table (with lower effective dose rate). Close approximation of “real” usage conditions in HEP. Significant sample activation. | Small material samples, active and passive electronics, small prototypes (up to 10x10 cm2).
~100 MeV Pions | Medium dose rate, small sample size or scanning table. Close approximation of “real” usage conditions in HEP. Significant sample activation, limited availability (no specialized facility, mostly piggybacking on HEP experiments) | Small material samples, active and passive electronics, small prototypes (up to 10x10 cm2).
Synchrotron light sources | Extremely high instantaneous dose rate, on small volumes. No activation. Suitable for specialized detector irradiation studies. | Small detectors, active and passive electronics. Highly localized irradiation (beam size ~10 um)
(examples, mentioned for completeness, but not pertinent to this talk)

## Slide 10: Standard irradiation facilities
Type | Field characteristics | Application
~20-70 MeV protons (cyclotrons, synchrotrons) | High dose rate, small sample size (~cm^2) or scanning table (with lower effective dose rate). Significant bragg peak – dose tuning difficult for different samples. Combination of displacement and ionization damage | Active and passive electronics, small prototypes (up to 10x10 cm2).
~10 MeV neutrons | High dose rate, medium sample size, good irradiation uniformity, no direct ionizing energy loss. | Material samples, active and passive electronics, small prototypes (up to 10x10 cm2).
Gamma (60Co or 137Cs) | High instantaneous dose rate, on large volumes. No activation. Very good radiation uniformity. | Material samples, active and passive electronics.
~5-10 MeV electrons | Very high instantaneous dose rate, large areas can be scanned quickly, limited penetration depth. | Small (thin) samples, active and passive electronics
Comprehensive list of irradiation facilities at https://irradiation-facilities.web.cern.ch/

## Slide 11: Choice of the irradiation facility
TANSTAAFL: “There ain’t no such thing as a free lunch” (R. A. Heinlein)
TANSTAAIIF: There ain’t no such thing as an “ideal” irradiation facility.
* Note: only 20-70 MeV proton sources are considered – the few (worldwide) GeV proton sources cannot handle a material characterization campaign.
Field | Gamma | Protons * | Neutrons | Electrons | Mixed
Large volume irradiation |  |  |  |  | 
Reasonable irradiation time |  |  |  |  | 
Representative radiation field |  |  |  |  | 
Lack of material activation |  |  |  |  | 
Irradiation depth uniformity |  |  |  |  | 

## Slide 12: FCC & Future Scenarios

## Slide 13: Future needs - fields
FCC enter the hadron fluence range where displacement damage cannot be overlooked anymore (approaching the dpa range)
Solutions:
  2-stage campaigns (e.g. gamma + neutrons)
  Mixed field irradiations
  BUT
  Displacement damage from neutrons is different from charged hadrons (damage cluster topology)
  ⇒Mixed field irradiations preferred

## Slide 14
(charged) hadrons irradiation ⇒ significant activation
Destructive tests will produce atmospheric contaminants (radioactive particles)
Tests can only be performed without major overhead if an on-site facility is available
Requirements:
  Hot cell with:
    Tensile / compression test stations (+ manpower)
    Climate control
    Radioactive waste disposal direct access
Future needs - infrastructures

## Slide 15: Conclusions
Irradiation needs will likely be shifting towards mixed field irradiation facilities for most exposed components.
A major point of concern is the availability of testing infrastructure (+ specialized manpower allocated) at the mixed field facility itself
This represents a major change in paradigm from the previous net separation between irradiation facilities and testing facilities.