## Slide 1: Cryogenics for superconducting devices Philippe Lebrun
JUAS Course 2
25 February 2025

## Slide 2: Contents
Introduction: cryogens & superconductors
Cryogenic fluids and materials
Refrigeration & liquefaction
Heat transfer & thermal insulation
Thermal screening with cold vapour
References

## Slide 3: Characteristic temperatures of cryogens
Cryogen | Triple point [K] | Normal boiling point [K] | Critical point [K]
Methane | 90.7 | 111.6 | 190.5
Oxygen | 54.4 | 90.2 | 154.6
Argon | 83.8 | 87.3 | 150.9
Nitrogen | 63.1 | 77.3 | 126.2
Neon | 24.6 | 27.1 | 44.4
Hydrogen | 13.8 | 20.4 | 33.2
Helium | 2.2 (*) | 4.2 | 5.2
(*): l Point

## Slide 4: Useful range of liquid cryogens & critical temperature of superconductors
Nb-Ti
Nb3Sn
Mg B2
YBCO
Bi-2223

## Slide 5: Cooling of superconducting devices
LHe 1.9 K
SCHe 4.5 K
LIN ~70 K
LHe 4.2 K

## Slide 6: Contents
Introduction: cryogens & superconductors
Cryogenic fluids and materials
Refrigeration & liquefaction
Heat transfer & thermal insulation
Thermal screening with cold vapour
References

## Slide 7: Properties of cryogens compared to water
Property |  | He | N2 |  | H2O
Normal boiling point | [K] | 4.2 | 77 |  | 373
Critical temperature | [K] | 5.2 | 126 |  | 647
Critical pressure | [bar] | 2.3 | 34 |  | 221
Liq./Vap. density (*) |  | 7.4 | 175 |  | 1600
Heat of vaporization (*) | [J.g-1] | 20.4 | 199 |  | 2260
Liquid viscosity (*) | [mPl] | 3.3 | 152 |  | 278
(*) at normal boiling point |  |  |  |  | 

## Slide 8: Vaporization of normal boiling cryogens under 1 W applied heat load
Cryogen | [mg.s-1] | [l.h-1] (liquid) | [l.min-1] (gas NTP)
Helium | 48 | 1.38 | 16.4
Nitrogen | 5 | 0.02 | 0.24
Let be the enthalpy of the fluid
At constant pressure with

## Slide 9: Specific heat of helium and materials [up to 20 K]

## Slide 10: Specific heat of helium and materials [up to 300 K]

## Slide 11: Amount of cryogens required to cool down 1 kg iron
Using | Latent heat only | Latent heat and enthalpy of gas
LHe from 290 to 4.2 K | 29.5 litre | 0.75 litre
LHe from 77 to 4.2 K | 1.46 litre | 0.12 litre
LN2 from 290 to 77 K | 0.45 litre | 0.29 litre
Assuming perfect heat exchange between iron and the fluid

## Slide 12: Contents
Introduction: cryogens & superconductors
Cryogenic fluids and materials
Refrigeration & liquefaction
Heat transfer & thermal insulation
Thermal screening with cold vapour
References

## Slide 13: Basic thermodynamics of refrigeration First Principle
First Principle (energy conservation) for a closed thermodynamic system
  heat received by system
  work received by system
  change of internal energy of system
  change of macroscopic kinetic energy of system (usually negligible)
Internal energy
  kinetic energy of particles in system
  potential energy of particles in system ( 0 for ideal gas)
To cool (reduce T) a system, need to lower
  Remove heat  heat exchanger
  Remove work  expansion engine or turbine
  If , increase  expansion without motor work in Joule-Thomson valve, works only for non-ideal gases and in limited temperature domain

## Slide 14: Brazed aluminium plate heat exchanger

## Slide 15: Cryogenic turbo-expander

## Slide 16: Joule-Thomson inversion temperatures
Cryogen | Maximum inversion temperature [K]
Helium | 43
Hydrogen | 202
Neon | 260
Air | 603
Nitrogen | 623
Oxygen | 761
While air can be cooled down and liquefied by JT expansion from room temperature, helium and hydrogen need precooling down to below inversion temperature by heat exchange or work-extracting expansion (e.g. in turbines)
Isenthalps in T-S diagram can have positive or negative slope, i.e. isenthalpic expansion can produce warming or cooling
 inversion temperature

## Slide 17: Two-stage Claude cycle

## Slide 18: Claude-cycle helium refrigerators/liquefiers Air Liquide & Linde

## Slide 19
Process cycle & T-S diagram of LHC 18 kW @ 4.5 K cryoplant

## Slide 20
LHC 18 kW @ 4.5 K helium cryoplants
33 kW @ 50 K to 75 K
23 kW @ 4.6 K to 20 K
41 g/s liquefaction
4 MW compressor power
C.O.P. 220-230 W/W @ 4.5 K
Air Liquide
Linde

## Slide 21: ITER 25 kW @ 4.5 K helium refrigerator

## Slide 22: Oil-injected screw compressor

## Slide 23: Compressor station of LHC 18 kW@ 4.5 K helium refrigerator

## Slide 24: Basic thermodynamics of refrigeration Second Principle
First principle (Joule)
Second principle (Clausius)
Hence
This equation can be written in three different ways
introducing entropy defined by
where is called the Carnot factor
introducing exergy defined by
(= for reversible process)

## Slide 25: Minimum refrigeration work
Consider the extraction of 1 W at liquid helium temperature 4.5 K, rejected at room temperature 300 K
The minimum refrigeration work is
In practice, the most efficient helium refrigerators have an efficiency of about 30% with respect to the Carnot limit

## Slide 26: Contents
Introduction: cryogens & superconductors
Cryogenic fluids amd materials
Refrigeration & liquefaction
Heat transfer & thermal insulation
Thermal screening with cold vapour
References

## Slide 27: Second-principle thermodynamics at low temperature
Minimum refrigeration work to extract heat at temperature with ambient temperature
At low temperature
 entropy is a good measure of the cost of cryogenic refrigeration
strategies minimizing improve cryogenic design
  Thermal insulation and heat load management
  Thermal shielding and heat interception at higher temperature
  Efficient cooling scheme, matched to system cooling requirements

## Slide 28: Cryogenic design strategies
T device
Q device
Ln T
Ln Q
Increasing S
Q shield
T shield
Shielding, heat interception
T refri
Q refri
Cooling scheme
Insulation

## Slide 29: Non-linear heat transfer to liquid cryogens Pool boiling nitrogen
~ 1.5 105 W/m2

## Slide 30: Non-linear heat transfer to liquid cryogens Pool boiling helium
104 W/m2

## Slide 31: Heat conduction in solids
Fourier’s law
Thermal conductivity [W/m.K]
Integral form
Thermal conductivity integral [W/m]
Thermal conductivity integrals for standard construction materials are tabulated
A

## Slide 32: Thermal conductivity integrals of selected materials [W/m]
From vanishingly low temperature up to | 20 K | 80 K | 290 K
OFHC copper | 11000 | 60600 | 152000
DHP copper | 395 | 5890 | 46100
1100 aluminium | 2740 | 23300 | 72100
2024 aluminium alloy | 160 | 2420 | 22900
AISI 304 stainless steel | 16.3 | 349 | 3060
G-10 glass-epoxy composite | 2 | 18 | 153

## Slide 33: Non-metallic composite support post with heat intercepts
5 K cooling line (SC He)
Aluminium strips to thermal shield at 50-75 K
Aluminium intercept plates glued to G-10 column

## Slide 34: Thermal radiation
Wien’s law
  Maximum of black-body power spectrum
Stefan-Boltzmann’s law
  Black body
  with
  «Gray» body
  with surface emissivity
  Between «gray» surfaces at temperatures and
  with function of and geometry of facing surfaces

## Slide 35: Emissivity of technical materials at low temperatures
 | Radiation from 290 K Surface at 77 K | Radiation from 77 K Surface at 4.2 K
Stainless steel, as found | 0.34 | 0.12
Stainless steel, mech. polished | 0.12 | 0.07
Stainless steel, electropolished | 0.10 | 0.07
Stainless steel + Al foil | 0.05 | 0.01
Aluminium, as found | 0.12 | 0.07
Aluminium, mech. polished | 0.10 | 0.06
Aluminium, electropolished | 0.08 | 0.04
Copper, as found | 0.12 | 0.06
Copper, mech. Polished | 0.06 | 0.02

## Slide 36: Residual gas conduction
Two different regimes, depending upon the relative values of heat transfer distance and mean free path of gas molecules
Viscous regime
  At higher pressure
  Classical conduction
  Thermal conductivity independant of pressure
Molecular regime
  At lower pressure
  Kennard’s law
  Heat transfer proportional to pressure, independant of spacing between surfaces
  depends on gas species
  Accommodation coefficient depends on gas species, and geometry of facing surfaces

## Slide 37: Multi-layer insulation (MLI)
Complex system involving three heat transfer processes
  With reflective layers of equal emissivity,
  Due to parasitic contacts between layers, increases with layer density
  due to residual gas trapped between layers, scales as in molecular regime
  Non-linear behaviour requires layer-to-layer modeling
In practice
  Typical data available from (abundant) literature
  Measure performance on test samples

## Slide 38: Typical heat fluxes at vanishingly low temperature between flat plates [W/m2]
Black-body radiation from 290 K | 401
Black-body radiation from 80 K | 2.3
Gas conduction (100 mPa He) from 290 K | 19
Gas conduction (1 mPa He) from 290 K | 0.19
Gas conduction (100 mPa He) from 80 K | 6.8
Gas conduction (1 mPa He) from 80 K | 0.07
MLI (30 layers) from 290 K, pressure below 1 mPa | 1-1.5
MLI (10 layers) from 80 K, pressure below 1 mPa | 0.05
MLI (10 layers) from 80 K, pressure 100 mPa | 1-2

## Slide 39: Cross-section of LHC dipole cryostat

## Slide 40: LHC cryostat heat inleaks at 1.9 K
Measured
He property tables
LHC sector (2.8 km)
On full LHC cold sector (2.8 km)
- Measured 560 W, i.e. 0.2 W/m
- Calculated 590 W, i.e 0.21 W/m

## Slide 41: Contents
Introduction: cryogens & superconductors
Cryogenic fluids and materials
Refrigeration & liquefaction
Heat transfer & thermal insulation
Thermal screening with cold vapour
References

## Slide 42: Vapour cooling of cryostat necks and supports with perfect heat transfer
Assuming perfect heat transfer between solid and vapour, i.e.
specific heat of vapour
thermal conductivity of support
can be calculated by numerical integration for
  different cryogens
  different values of aspect ratio
  different values of vapour flow

## Slide 43: He vapour screening of stainless steel neck between 300 K and 4 K

## Slide 44: Vapour cooling of cryostat necks and supports in self-sustained mode
A particular case of gas cooling is the self-sustained mode, i.e. the vapour flow is generated only by the residual heat reaching the bath
Then
with latent heat of vaporization
Given the general equation
The variables can be separated and integration yields
The denominator of the integrand acts as an attenuation factor of the thermal conductivity

## Slide 45: Reduction of heat conduction by self-sustained helium vapour cooling
Effective thermal conductivity integral from 4 to 300 K | Purely conductive regime [W.cm-1] | Self-sustained vapour-cooling [W.cm-1]
ETP copper | 1620 | 128
OFHC copper | 1520 | 110
Aluminium 1100 | 728 | 39.9
Nickel 99% pure | 213 | 8.65
Constantan | 51.6 | 1.94
AISI 300 stainless steel | 30.6 | 0.92

## Slide 46: Vapour cooling of cryostat necks and supports with imperfect heat transfer
Introducing efficiency of heat transfer between solid and vapour ()
The steady-state heat balance equation becomes
This non-linear equation needs to be solved by numerical integration

## Slide 47: Vapor-cooled current leads
The (imperfect) heat transfer between solid and vapour can be written
Introducing electrical resisitivity , the steady-state heat balance equation reads
Assuming the material follows the Wiedemann-Franz-Lorenz (WFL) law
with
The aspect ratio can be chosen for minimum heat inleak , and the minimum heat inleak does not depend on the material

## Slide 48: Heat load of optimized current lead
Material obeying
the WFL law
Minimum residual
heat load
1.04 W/kA
Uncooled
47 W/kA

## Slide 49: Beating the WFL law: HTS current leads
The WFL law essentially states that good electrical conductors are also good thermal conductors
Efficient current leads need good electrical conductors with low thermal conductivity
Superconductors are bad thermal conductors with zero resisitivity
 Build current lead with superconductor up to temperature as high as possible, i.e. use HTS
HTS
Copper

## Slide 50: HTS vs. normal conducting current leads
Type |  | Resistive | HTS (4 to 50 K) Resistive (above)
Heat into LHe | [W/kA] | 1.1 | 0.1
Total exergy consumption | [W/kA] | 430 | 150
Electrical power from grid | [W/kA] | 1430 | 500

## Slide 51: Take-home facts
Helium is the only practical cryogen for cooling LTS
Liquid nitrogen is a convenient fluid for precooling and thermal screening
Specific heat of helium is orders of magnitude higher than that of solid materials at low temperature
Cryogenic helium refrigerators and liquefiers have an efficiency not higher than 30% of the Carnot cycle: cryogenic refrigeration is energy costly
Proper cryogenic design should aim at minimizing entropy generation, by reducing parasitic heat in-leaks, temperature differences and pressure drops
Heat transfer processes at low temperature show non-linearities and strong variations w.r. to their values at room temperature
Helium vapour has a high cooling potential for heat interception in cryostat thermal screens, necks, supports and current leads

## Slide 52: Some references Books
K. Mendelssohn, The quest for absolute zero, McGraw Hill (1966)
R.B. Scott, Cryogenic engineering, Van Nostrand, Princeton (1959)
G.G. Haselden, Cryogenic fundamentals, Academic Press, London (1971)
R.A. Barron, Cryogenic systems, Oxford University Press, New York (1985)
B.A. Hands, Cryogenic engineering, Academic Press, London (1986)
S.W. van Sciver, Helium cryogenics, Plenum Press, New York (1986, 2nd edition 2012)
K.D. Timmerhaus & T.M. Flynn, Cryogenic process engineering, Plenum Press, New York (1989)
J.G. Weisend (ed.), The handbook of cryogenic engineering, Taylor & Francis, Philadelphia (1998)
J.G. Weisend (ed.), Cryostat design: case studies, principles and engineering, Springer, Switzerland (2016)

## Slide 53: Some references Reports & Proceedings
Ph. Lebrun, An introduction to cryogenics, CERN-AT-2007-01 (2007) http://cdsweb.cern.ch/record/1012032?ln=en
Proceedings of CAS School on Superconductivity and Cryogenics for Particle Accelerators and Detectors, Erice (2002)
  U. Wagner, Refrigeration
  G. Vandoni, Heat transfer
  Ph. Lebrun, Design of a cryostat for superconducting accelerator magnet
  Ph. Lebrun & L. Tavian, The technology of superfluid helium
  http://cdsweb.cern.ch/record/503603?ln=en
Proceedings of CAS School on Superconductivity for Accelerators, Erice (2013)
  P. Duthil, Basic thermodynamics
  P. Duthil, Material properties at low temperatures
  A. Alekseev, Basics of low-temperature refrigeration
  B. Baudouy, Heat transfer and cooling techniques at low temperature
  V. Parma, Cryostat design
  Ph. Lebrun & L. Tavian, Cooling with superfluid helium
  https://cds.cern.ch/record/1507630?ln=en
Proceedings of ICEC, CEC/ICMC and IIR Cryogenics conferences

## Slide 54: Phase diagram of helium