## Slide 2
Vacuum Systems
Slot 5
V. Baglin
CERN TE-VSC, Geneva
https://indico.cern.ch/event/1470062/timetable/?view=standard#day-2025-02-17

## Slide 3
Outline
Cryo-pumping
Adsorption isotherms
Synchrotron radiation

## Slide 4: Why cryo-vacuum matters?
Explanation of beam induced background in ATLAS during November 2024 …

## Slide 5
1. Cryopumping

## Slide 6
Saturated Vapour Pressure
Pressure over liquid or gas phase (many monolayers condensed)
Follows the Clausius-Clapeyron equation: Log Psat = A – B/T
For a smooth surface:
4.2 K

## Slide 7: Desorption probability
The desorption probability, p, of a molecule is a function of the binding energy, E and the temperature, T (first order desorption, Frenkel 1924). The surface coverage, θ, varies like :
The desorption process is characterized by the sojourn time,  :
For large E and small T, the molecule remains onto the surface : CRYOPUMPING
For some combination of E and T, the molecule is desorbed (bake out)
(ν0 ~ 1013 Hz, k = 86.17 10-6 eV/K)

## Slide 8: Sojourn time at cryogenic temperature
E(eV) | 1.9 K | 4.2 K | 50 K | 70 K
0.01 | 1 106 years | 0.1 s | 1 ps | 0.5 ps
0.02 | ∞ | 3 103 years | 10 ps | 2 ps
0.15 | ∞ | ∞ | 130 s | 6 ms
0.21 | ∞ | ∞ | 5 years | 130 s
0.3 | ∞ | ∞ | 1 104 years | 12 years
Cryosorption occurs up to ~ 100 K
Superfluid He
Liquid He
~LN2 (77K)
1 eV/k =
11,604.5 K

## Slide 9: Sojourn time - Physisorbed molecules
Physisorption occurs:
    below 23 K for binding energies < 0.1 eV
    below 50 K for binding energies < 0.2 eV
    below 70 K for binding energies < 0.3 eV
1 year
20
50
70

## Slide 10: A Natural Warm Up of a St. Steel Cold Bore

## Slide 11: Cryopumping regimes/mechanisms
Physisorption
Sub-monolayer coverage : attractive force (van der Waals) between a gas molecules and a material
Binding energy for physical adsorption
H2 from 20 to 85 meV for smooth and porous materials respectively
1 h sojourn time at 5.2 K and 26 K for smooth and porous materials resp.
Condensation
For thick gas coverage, only forces between gas molecules
Energy of vaporisation 9 to 175 meV for H2 and CO2 resp.
1 h sojourn time at 2.8 K and 53.4 K for H2 and CO2 resp.
 sub-monolayers quantities of gas can be physisorbed at their boiling temperature
(ex : H2 boils at 20.3 K and a bake-out above 100 ºC removes water)
Cryotrapping
Use of an easily condensable carrier (e.g. Ar) to trap molecules with
a high vapor pressure gas (e.g. He, H2)

## Slide 12: Sticking probability/coefficient
Probability : 0 <  < 1
ν collision (impingement) rate (molecules.s-1.cm-2)
Function of the gas specie, surface condition, surface coverage, temperature of gas and surface
Pumping speed
i.e :  multiplied by the conductance of a surface
A = area sample (m2); <v>=MB averag. veloc.
J.N. Chubb et al. Vacuum/vol 15/number 10/491-496
J.N. Chubb et al. J. Phys. D, 1968, vol 1, 361
H2 at 300 K incident onto a surface at 3.1 K
H2 and CO at 4.2 K :
  SH2 = 5.3 ℓ.s-1·cm-2
  SCO = 1.4 ℓ.s-1·cm-2

## Slide 13: Capture factor, Cf
The capture factor takes into account the geometry of the system :
Baffle in a cryopump
Holes in the electron shield of the LHC beam screen
 | 1 | 2 | 3 | 4
0.1 | 0.48 | 0.26 | 0.39 | 0.43
1 | 0.68 | 0.36 | 0.51 | 0.57
A.A. Krasnov. Vacuum 73 (2004) 195-199
Cf ~ 0.3
R. Haefer. J. Phys. E : Sci. Instrum., Vol 14, 1981, 273-288

## Slide 14: LHC Beam Screen hole’s Pumping Speed
Operating temperature ~ 15 K : molecule’s kinetic energy is accommodated to the vacuum chamber walls, T = 15 K
Transparency, t=4.4%, Capture factor, Cf=0.5
Horizontal width 4,6 cm
  Specific surface area A = 1445 cm2/m
Assume P = 2 10-9 mbar (1015 H2/m3) at 15 K, what is the quantity, Q, of gas pumped per m?
1 mbar ℓ at 15 K  G= 6.4 1020 molecules
At LHC design pressure, ~ monolayers per s per m are pumped on the cold bore
 | H2 | CH4 | CO | CO2
ℓ/s/m at 15 K | 316 | 112 | 84 | 67
Cold-bore at 1.9 K

## Slide 15: Thermal transpiration
What is the pressure (gas density) in a cryogenic tube?
  Vacuum gauges are usually located at room temperature to reduce heat load and have more accessibility
For small aperture, the impingment rate, n, is conserved at the cold / warm transition
Since the average velocity scales like √T
Pressure scaling
Density scaling
T2 (K) | 4.2 | 77
P1/P2 | 8 | 2
T1 (K) = 300 K
In practice:

## Slide 16: Pressure measurement in a cryogenic machine
What and how is the pressure measured by a gauge located at room temperature for a given gas density in the LHC beam screen at 15 K?
n (H2/m3) (year) | 1 1015 (design) | 2.25 1013 (2015) | 2.5 1012 (2018)
P at 15 K (mbar) | 2 10-9 | 5 10-11 | 5 10-12
P at RT (mbar) | 1 10-8 | 2 10-10 | 2 10-11
BS

## Slide 17
2. Adsorption isotherms

## Slide 18: Adsorption isotherm
Measurement, at constant temperature, of the equilibrium pressure for a given gas coverage, θ
Varies with:
molecular species
surface temperature (under 20 K only H2 and He)
surface nature
gas composition inside the chamber
...
Models :
Henry’s law for low surface coverage
DRK (Dubinin, Radushkevich and Kaganer) for metallic, glass and porous substrate. Valid at low pressure. Good prediction with temperature variation
BET (Brunauer, Emmet and Teller). Multi-monolayer description
α = exp (ΔE/kT) >>1

## Slide 19
Saturated Vapor Pressure
Pressure over liquid or gas phase (many monolayers condensed )
Follows the Clausius-Clapeyron equation: Log Psat = A – B/T
For a smooth surface:
4.2 K

## Slide 20
H2 Adsorption Isotherm on Stainless Steel
Qo = one monolayer
C. Benvenuti, R. Calder, G. Passardi
J.Vac.Sci. 13(6), Nov/Dec 1976, 1172-1182
The vapor pressure increases when increasing the adsorption of gas up to a few monolayers (~ 1015 molecules/cm2)
The vapor pressure saturates when several monolayers of gas are adsorbed
The pressure level of the saturation is a function of the temperature

## Slide 21: H2 adsorption isotherm on stainless steel
A condensation cryopumps allows to pump large quantities of H2 at 2.3 K.
CERN ISR condensation cryopump operated with liquid He at 2.3 K (50 Torr on the He bath)
C. Benvenuti et al. Vacuum, 29, 11-12, (1974) 591

## Slide 22: LHC and HL-LHC cold bores
Operating at 1.9 K are modern integrated and distributed condensation cryo-pumps !!!
The Large Hadron Collider:
A marvel of Technology by L. Evans
Open Access book
Availlable at CERN Document Server
The High Luminosity
Large Hadron Collider
by O. Brüning & L. Rossi
Open Access book
https://doi.org/10.1142/13487
1.9 K cold bore
60-80 K
Beam screen

## Slide 23: H2 adsorption isotherms from 8 to 20 K
The surface capacity strongly decreases when increasing the surface temperature
Stainless steel
DRK description
D = 3125 eV-2
Θm = 7 1014 H2/cm2
F. Chill et al. PAC’2015, Richmond, USA, 2015.

## Slide 24: He adsorption isotherm from 1.9 to 4.2 K
Sub-monolayer range
Approaches Henry’s law at low coverage
The isotherms are well described by the DRK model
θm ~ 1.3 1015 H2/cm2
Stainless steel
E. Wallén. J.Vac.Sci.A 15(2), Mar/Apr 1997, 265-274.

## Slide 25
H2 Isotherms for Industrial Surfaces
G. Moulard, B. Jenninger, Y. Saito, Vacuum 60 (2001) 43-60
Identification of two types of adsorption sites with:
1) high energy (pores, defects)
2) low energy (flat surface).

## Slide 26: Cryosorbing materials
Large capacity
Large pumping speed
Large temperature working range (up to ~ 30 K)
e.g. activated charcoal used for cryopumps
Capacity ~ 1022 H2/g i.e. 1021 monolayers (P. Redhead, Physical basis of UHV,1968)
Sticking coefficient ~ 30 % at 30 K (T. Satake, Fus. Tech. Vol 6., Sept. 1984)
used for cryopanels held at 20 K
COMMERCIAL CRYOPUMP

## Slide 27: RHIC, Brookhaven, USA
RHIC’s solution: anticipate leaks !!
RHIC use sorption pumps based on 300 g of activated charcoal.
They are located every 30 m to mitigate He leaks and to pump H2
Test in a 480 m long sector at 4.4 K
RHIC interconnect
H.C. Hseuh, Proc. PAC 1999
H.C. Hseuh, E. Wallén.
J.Vac.Sci.A 16(3), May/Jun 1998, 1145-1150.

## Slide 28: Cryo-vacuum: Summary
Gas can be physisorbed for very long period on cryogenic surfaces
The sticking coefficient characterises the pumping speed of a surface
The capture coefficient characterises the pumping speed of a device
At cryogenic temperature, thermal transpiration correction shall be applied
The vapour pressure is the equilibrium pressure as a function of gas coverage
When saturated (many monolayers), the vapour pressure follows the Clausius-Clapeyron law
Adsorption isotherms depend very much on the conditions
Some material can be porous so to adsorb many monolayers of gas without reaching the saturated vapour pressure: cryosorbers

## Slide 29
3. Synchrotron radiation

## Slide 30
In a synchrotron, charged particles can radiate light by synchrotron radiation
This effect can be used for diagnostics purposes
CERN Control Centre LHC beams SR displays
Particles lose energy by synchrotron radiation  should be compensated by RF system
Beam emittance shrinks upon emission of synchrotron radiation (damping wigglers)
Power is dissipated on the machine elements: power density , W/mm2, can be extremely HIGH!
Molecules are desorbed from the vacuum chamber wall due to synchrotron radiation
Synchrotron radiation: visible light

## Slide 31
Synchrotron Radiation
A charged particle which is accelerated generate radiation (magnetic bremsstrahlung)
The power of the centripetal radiation is larger than the longitudinal radiation (factor )
For a relativistic particle, the radiation is highly peaked (opening angle ~ 1/ )
The radiation energy range from infrared to gamma rays: from meV to MeV
The SR theory dated from 1950, Schwinger (USA), Sokolov and Ternov (URSS)
K. Hübner, CAS 1984, CERN 85-19
R.P. Walker, CAS 1992, CERN 94-01
A. Hofmann, CAS 1996, CERN 98-04
L. Rivkin, CAS 2008
References :
1/g
B
g=relativistic factor

## Slide 32
Magnetic rigidity:
Critical energy
The critical energy split the power spectrum in two equals parts
~ 88 % of the emitted photons have an energy lower than the critical energy

## Slide 33
Dissipated power
The average power emitted by the beam per unit of length is
Electrons :
Protons:
For the total dipole radiation power dissipated around the ring, multiply by 2 p r
Protons generate a lot less SR compared to electrons because there is a 1/m04 dependency in the formula for the radiated power, where m0 is the mass of the radiating particle. Protons are 1836 times heavier than electrons, so the reduction factor is ~8.8·10-14
1836 = ratio of proton to electron mass

## Slide 34
The photon flux per unit of length is given by :
Electrons :
Protons:
Linear photon flux
Example 1:
ESRF-1 (Grenoble):
(high-energy
light source)
r = 23.366 m
I = 200 mA
E = 6 GeV
ec = 20.503 keV
F = 6.604 1018 ph/s/m
P = 6.692 kW/m
1/g = 82.5 mrad  0.82 mm @10 m
Example 2:
LHC (CERN):
(high-energy proton storage ring)
r = 2784 m
I = 584 mA
E = 7 000 GeV
ec = 44 eV
F = 1 1017 ph/s/m
P = 0.2 W/m
1/g = 134 mrad  1.34 mm @10 m

## Slide 35
LHC SR Spectrum : from IR to UV
With nominal parameters : 7 TeV and 585 mA
2010, 2011, 2012 and 2015 spectra
450 GeV
7 TeV
Key parameter: photodesorption yield

## Slide 36
LEP SR spectrum: harder spectrum, X-rays & gamma rays
LEP: electron-positron collider; was installed in the (now) LHC tunnel before LHC; same circumference (26.8 km)
Example 3:
LEP (CERN):
(high-energy
COLLIDER)
r = 2963 m
I = 4 mA
E = 100 GeV (up to 104)
ec = 748.6 keV 
F = 1.736·1016 ph/s/m
P = 0.642 kW/m
1/g = 5.11 mrad  0.511 mm @100 m

## Slide 37
 |  | Soleil | KEK-B |  | LEP |  |  | LHC | 
 |  |  | LER | HER | Inj. | 1 | 2 | Inj. | Col.
Particle |  | e- | e+ | e- | e- | e- | e- | p | p
Beam current | mA | 500 | 2600 | 1100 | 3 | 3 | 7 | 584 | 584
Energy | GeV | 2.75 | 3.5 | 8 | 20 | 50 | 96 | 450 | 7000
Bending radius | m | 5.36 | 16.31 | 104.46 | 2962.96 |  |  | 2784.302 | 
Power | W/m | 14 030 | 20 675 | 5 820 | 0.8 | 30 | 955 | 0 | 0.2
Critical energy | eV | 8 600 | 5 800 | 11 000 | 6 000 | 94 000 | 660 000 | 0 | 44
Photon flux | photons/m/s | 3 1019 | 7 1019 | 1 1019 | 3 1015 | 7 1015 | 3 1016 | 7 1015 | 1 1017
Dose at 3000 h | photons/m | 4 1026 | 8 1026 | 1 1026 | 3 1022 | 7 1022 | 3 1023 | 7 1022 | 1 1024
In LEP, and all synchrotron light sources, the evacuation of the power is an issue
The LHC operates at 7 TeV with ~ 0.6 A. Power evacuation is an issue for the cryogenic system (1 kW/arc), due to the low Carnot efficiency at low temperature
The critical energy varies from a few 10 eV to 660 keV. Strongly bound molecules can be desorbed
The photon flux is large, so large gas load. Adequate dimensioning of the effective pumping speed is required
The annual integrated photon dose is large. Implications on gas reduction and radiation (next lecture)
SR impact on different type of machines …

## Slide 38
(C. Herbeaux et al.)
… heavy consequences on design
A complex vacuum chamber design with a light extraction path, pumping and instrumentation ports and power absorbers (crotch)
Stainless steel
NEG coated, in-situ baked to 180ºC
e-
e-
SR fan
B

## Slide 39
Soleil « crotch » power absorber: Water cooled copper (Glidcop) (256 W/mm2)
A sawtooth profile is machined in order to distribute the SR power on a wider area
SOLEIL Design
(C. Herbeaux et al.)
… heavy consequences on design
SR fan
e-

## Slide 40
LEP Design
(CERN LEP Vacuum group)
… heavy consequences on design
Antechamber and distributed NEG pumping, water cooling and lead shielding
SR fan
molecule
NEG strip:
30 mm wide (27 active)
Both sides pump
Stick. Coeff:
~ 0.1 (CO, CO2, N2)
~ 0.05 (H2)

## Slide 41
LHC Design
(CERN LHC Vacuum group)
Courtesy N. Kos CERN TE/VSC
Courtesy N. Kos CERN TE/VSC
… heavy consequences on design
Perforated Cu colaminated beam screen to intercept the SR power protecting the 1.9 K cold bore and to allow a distributed pumping

## Slide 42: Synch. Rad. Summary
The photon fan generated by relativistic particles moving in a magnetic field is known as synchrotron radiation
The spectrum of synchrotron radiation is described with high precision by well know analytical formulae
Synchrotron radiation depends strongly on the mass of the radiating particle: for equal beam energy electrons generate much more SR than protons
The SR fan is generated in the local plane of the orbit within a narrow cone
The presence of synchrotron radiation must be considered in the design phase, since it can lead to heating problems and large photon-induced desorption yields
The power and flux carried by the SR fan can be large: vacuum components must be designed in such a way to cope with this.
In “extreme” cases (e.g. LEP or FCC-ee), the critical energy of the SR spectrum can be so high to present a formidable challenge in terms of radiation shielding and radioprotection

## Slide 43
Some References
C. Benvenuti, Molecular surface pumping: cryopumping, Cern Accelerator School, Vacuum technology, CERN 99-05
V. Baglin, Cold/sticky systems, Cryo-pumping and vacuum systems, Cern Accelerator School, Vacuum in accelerators, CERN 2007-03 & CERN ACC-2023-009
The physical basis of ultra-high vacuum, P.A. Redhead, J.P. Hobson, E.V. Kornelsen. AVS.
Capture pumping technology, K. Welch, North Holland.
Cryopumping, theory and practice, R. Haefer, R. Clarendon press.
Design and modelling of UHV systems of particle accelerators, O. Malyshev, Wiley.
Some Journals Related to Vacuum Technology
Journal of vacuum science and technology A and B
Vacuum

## Slide 44
Thank you for your attention !!!