## Slide 2
Vacuum Systems
Slot 6
V. Baglin
CERN TE-VSC, Geneva
https://indico.cern.ch/event/1470062/timetable/?view=standard#day-2025-02-17

## Slide 3
Outline
Photon induced molecular desorption
Vacuum instability and ion stimulated desorption
Particle losses and heavy ions stimulated desorption

## Slide 4
1. Photon induced
molecular desorption

## Slide 5
The interaction of photons (light) with matters produce the desorption of neutral gases inside the vacuum system
The photon stimulated desorption (PSD) of physisorbed (meV) or chemisorbed (eV) molecules can be direct or non-direct
The identified transmitters are photoelectrons, secondary electrons and phonons
The photon stimulated molecular desorption is a function of the nature of the material, its temperature, its surface state, and of the photon energy and the angle of irradiation.
No model exists, therefore in-situ qualification of the material is required for the design of a future machine.
Photodesorption

## Slide 6
The photodesorption process is linked to the production of photoelectrons and secondary electrons
Photoelectrons contribute to the gas load by ESD
The oxide and carbon layers are believed to be the source of gas
The diffusion of atoms into the solid and their recombination at the surface plays a role
O. Gröbner et. al. EPAC 1992
J. Gómez-Goñi et al. JVSTA 12(4) Jul/Aug 1994, 1714
T. Kobari et al Proc .of Vacuum Design of Synch Light Sources Conference, Argonne, 1990
Photodesorption: present understanding

## Slide 7
Beam cleaning during the first period of LEP
O. Gröbner. Vacuum 43 (1992) 27-30
C. Herbeaux, Journée thématiques RTVide, décembre 2014
SOLEIL
Dynamic pressure due to PSD
The dynamic pressure decreases by several orders of magnitude with photon dose: “photon conditioning”
The photon desorption yield is characterised by ηphoton
With beam P ~ 10-10 Torr
With beam P ~ 2 10-9 mbar
Dynamic pressure:

## Slide 8: Photo-desorption yield measurement
V. Baglin et al. EPAC 1998, Stockholm, Sweden.
SR light is extracted from a dipole magnet to irradiate the test chamber at ~ 11 mrad
SR fan is vertically collimated therefore photon flux < 4 eV are attenuated
The gas load is measured by the throughput method via a conductance (72.5 ℓ/s for N2)
A wire and a collector are biased for current measurement to estimate the photon reflectivity and photoelectron yield
J. Gómez-Goni et al. J. Vac. Sci. Technol. A 12(4), Jul/Aug 1994, 1714
With G = 2.5 1019 molecules/mbar.ℓ at RT

## Slide 9: CERN EPA Synchrotron Light Facility 42 - 1999
The LEP Pre-Injector as a multipurpose facility, J-P. Potier, L. Rinolfi, EPAC 1998, Stockholm, Sweden, 1998

## Slide 10
C. Herbeaux et. al. EPAC 2008, Genoa, Italy
O. Gröbner et al.
J.Vac.Sci. 12(3), May/Jun 1994, 846-853
Cu baked at 150°C
The hydrogen desorption is characterised by a diffusion process: a = 0,5
M. Andritschky et al., Vacuum 38 (8-10), 933, (1988)
a ~ 0.9-1.3
Conditioning under photon irradiation
Typical desorption yield range: from 10-3 molecule/photon to 10-6 when conditioned
NEG coated SS activated at 180°C

## Slide 11
C. Herbeaux et al. JVSTA 17(2) Mar/Apr 1999, 635
Unbaked stainless-steel
3.75 keV
Gas | H2 | CH4 | H2O | CO | CO2 | Total
molecules/cm2 x 1015 | 8.1 | 0.2 | 1.1 | 2.8 | 2.2 | 14.4
Gas load
The total desorbed quantity amounts to 15 monolayers for an unbaked system
Unbaked stainless-steel
3.75 keV

## Slide 12
At low energy, the photoelectric effect dominates: linear trend until ~ 5 keV
Above a few 100 keV, Compton diffusion dominates and produce a cascade of energetic recoil electrons with a diffusion of secondary photons
J. Gómez-Goñi et al. JVSTA 12(4) Jul/Aug 1994, 1714
150°C bake-out
O. Gröbner. CAS 99-15
Evolution with critical energy

## Slide 13
2. Vacuum instability and ion
stimulated desorption

## Slide 14
A lesson from history
1965
7 MCHF
Oct.
1971

## Slide 15
Vacuum Instability : the Effect
In circular machine with large proton current :
    Intersecting Storage Rings (routine 40 A, record 57 A), LHC (0.6 A)
First documented pressure bump in the ISR E. Fischer/O. Gröbner/E. Jones RUN8: 18/11/1970
Beam current stacking to 1 A
Pressure increases to 10-6 Torr (x 50 in a minute)
Beam losses

## Slide 16: Intersecting Storage Rings
August 1971
L: 4 1030 to 1.4 1033 Hz/cm2
62 GeV in center of mass
30-40 A (until 57 A)
50-60 h fills (10 h turn over)

## Slide 17
The mechanism of vacuum instability
When the beam current approach the critical current, the pressure increases to infinity
Quasi stationary long tube (C=0)
Origin are ions produced by beam gas ionisation
Reduction of the effective pumping speed, Seff

## Slide 18
O. Gröbner, CERN 99-05
LHC beam current (A)
Varies with the material, the ion energy and ion species
Several units of molecules can be desorbed by ions  Sputtering
Baked
stainless steel
A.G. Mathewson, CERN ISR-VA/76-5
N2+
A.G. Mathewson, CERN ISR-VA/76-5
Unbaked
stainless steel
N2+
5 keV, Baked
G. Hulla, PhD Thesis, Vienna Tech. U, 2009
He+, Ne+, Ar+, Kr+, Xe+
H2+, CH4+,C2H4+, C2H6+
CO+,N2+,CO2+
0.2-0.5 keV
Ion desorption yield

## Slide 19
A conditioning is observed but at high dose, some ions can be implanted !
G. Hulla, PhD Thesis, Vienna Tech. U, 2009
7 keV, Cu Baked, Ar+
G. Hulla, PhD Thesis, Vienna Tech. U, 2009
7 keV, Cu Baked, CO+
In the LHC : the maximum flux is about 3 108 ions/(cm2.s) i.e. a dose of 3 1015 ions/(cm2.year)
In the LHC, there is no “beam” conditioning under ion bombardment
Conditioning and implantation

## Slide 20
A lesson from history - Epilogue

## Slide 21
ISR Remedy
Beam cleaning being negligible:
  Increase number of pumps
  Reduce outgassing using 300°C bakeout
  Perform ex-situ Ar/O2 glow discharge cleaning with in-situ bakeout
 ηICrit increased to ~ 60 A and the machine could reached 57 A and 2×10-12 Torr!
M. Jacob and K. Johnsen, CERN 84-13, 1984
A.G. Mathewson, CERN ISR-VA/76-5

## Slide 22
Vacuum Instability in J-Parc?
J-Parc Rapid Cycling Synchrotron (RCS), Main Ring (MR) injector
RF shielded (Cu stripes with capacitors) ceramic chambers in dipoles and quadrupoles and Ti chambers for straights
Probable signature of Ion Stimulated Molecular Desorption
J. Kamiya et al., JPS Conf. Proc. , 011023 (2021)

## Slide 23
3. Particle losses
and
heavy ion stimulated desorption

## Slide 24
Loss of ions from a beam leads to large pressure increases: 10-8 …10-5 mbar!
W. Fischer et. al. EPAC 2002, Paris, France
110 bunches, Au79+,
9.9 GeV/u
W. Fischer et. al. EPAC 2006, Edinburgh, Scotland
3 109, Au79+, 9.9 GeV/u
1, 2 & 3 mrad
RHIC

## Slide 25
Surface effect (except diffusion H2) due to a thermal activation
M. Bender et al. , NIM B 267 (2007) 885-890
Xe29+, 1.4 MeV/u, Perpendicular
Temperature of atomic Cu subsystem after Xe impact
300° C
Desorbed particles per Xe per dt
« Inelastic thermal spike model » : a temperature map coupled to the thermal desorption model
Mecanism

## Slide 26
E. Mahner et al. ,
Phys. Rev. ST Accel. Beams 6, 013201 (2003)
Desorption yields range from 20 – 20 000 molecules per ion
The desorption is determined by the energy given to the electrons (electronic stopping force)
Pb53+, 4. 2 MeV/u, 14 mrad
The desorption induced by the electrons is the responsible mechanism
L. Prost et al. , PRL 98, 064801 (2007)
High energy ions

## Slide 27
Located in the LHC arcs around IP2 to intercept lead beams with modified charge produced at the interaction point: Pb81+ instead of PB82+
W jaws
HL-LHC ions collimator
TCLD
TCLD & LEN Bypass
Courtesy S. Redaelli, F. Savary
Installed during LS2: 2019-2021

## Slide 28: Slot 7 summary
In accelerators, the circulating beam can contribute to stimulate molecular desorption
Those phenomenon can lead to much larger gas load than the thermal outgassing rate
     « Dynamic pressure »
Photon stimulated desorption originates from SR
Ion stimulated desorption originates from beam gas ionisation and can lead to vacuum instability
Particle losses may trigger beam dumps / other unwanted phenomena

## Slide 29
Thank you for your attention !!!

## Slide 31
Some References
Cern Accelerator School, Vacuum technology, CERN 99-05
Cern Accelerator School, Vacuum in accelerators, CERN 2007-03
Cern Accelerator School, Vacuum for particle accelerators, Glumslov, June 2017
The physical basis of ultra-high vacuum, P.A. Redhead, J.P. Hobson, E.V. Kornelsen. AVS.
Scientific foundations of vacuum technique, S. Dushman, J.M Lafferty. J. Wiley & sons.
Les calculs de la technique du vide, J. Delafosse, G. Mongodin, G.A. Boutry. Le vide.
Vacuum Technology, A. Roth. Elsevier Science
Foundations of vacuum science and technology, Ed by J.M. Lafferty. J. Wiley & sons.
Vacuum in Particle Accelerators: Modelling, Design and Operation of Beam Vacuum Systems, O. Malyshev. Wiley VCH.
Some Journals
Journal of Vacuum Science and Technology
Vacuum
Applied Surface Science
Nuclear Instruments and Methods
Physical Review Accelerator and Beams