## Slide 1: 2025 Joint Universities Accelerator School Exercise on Superconducting Magnets Case study
Paolo Ferracin
  (pferracin@lbl.gov)
Lawrence Berkeley National Laboratory (LBNL)

## Slide 2: Case study introduction
Goal: outline design of a superconducting magnet
  Apply the theory explained during lectures to a practical case
  Solve a case study using analytical formulas, “back of the envelope” calculation, plots, data, etc. provided during the presentations
    From the superconducting material to the full magnet
  Understand physics and reasoning behind design options
    General dimensions, orders of magnitude of different parameters
Superconducting material
Superconducting strand
Superconducting cable
Superconducting coil
Superconducting magnet

## Slide 3: Case study
11 T Nb3Sn dipole for the LHC collimation upgrade
Second long shutdown: increase of collimation efficiency
  New collimation units
  Some 8.3 T Nb-Ti dipoles replaced by 11 T Nb3Sn dipoles
  FNAL/CERN collaboration
14.3 m
Nb-Ti 8.3 T
5.5 m
Nb3Sn 11 T
5.5 m Nb3Sn
5.5 m Nb3Sn
1 m Collimator

## Slide 4: Case study
11 T Nb3Sn dipole for the LHC collimation upgrade
  Introduction
    The second phase of the LHC collimation upgrade will enable proton and ion beam operation at nominal and ultimate intensities.
    To improve the collimation efficiency by a factor 15–90, additional collimators are foreseen in the room temperature insertions and in the dispersion suppression (DS) regions.
    To provide longitudinal space of about 3.5 m for additional collimators, a solution based on the substitution of a pair of 5.5-m-long 11 T dipoles for several 14.3-m-long 8.33 T LHC main dipoles (MB) is being considered.
  Goal
    Design a Nb3Sn superconducting dipole with an 60 mm aperture and a operational field (80% of the current limit Iss) at 1.9 K of 11 T.

## Slide 5: Case study
11 T Nb3Sn dipole for the LHC collimation upgrade

## Slide 6: Case study
11 T Nb3Sn dipole for the LHC collimation upgrade
  Questions
    Determine and plot critical curves (Jsc vs. B) for Nb3Sn and Nb-Ti at 1.9 K
    Determine coil filling factor (J0 /Jsc ratio or Anon-Cu_cable/Ainsulated_cable)
    Compute load-line (Jsc vs. B) for a
      Sector coil (60) with constant current density
    Determine coil size, operational (80% of Iss ), conditions, “short-sample” conditions, and margins
      w
      jsc_ss , jo_ss , Bbore_ss , Bpeak_ss
      jsc_op, jo_op , Bbore_op , Bpeak_op
      T, jsc , Bpeak margins
    Compare “short sample”, “operational” conditions and margins if the same design uses Nb-Ti superconducting technology with the same coil size w
    Determine e.m forces Fx and Fy and the accumulated stress on the coil mid-plane in the operational conditions
    Evaluate dimension of collars, iron yoke, and shrinking cylinder, assuming that the support structure is designed to reach 90% of Iss

## Slide 7: Case study
11 T Nb3Sn dipole for the LHC collimation upgrade
  Question
    Determine and plot critical curves (Jsc vs. B) for Nb3Sn and Nb-Ti at 1.9 K

## Slide 8: Nb-Ti and Nb3Sn Critical surfaces
The critical surface defines the boundaries between superconducting state and normal conducting state in the space defined by temperature, magnetic field, and current densities.
The surface, determined experimentally, can be fitted with parameterization curves.
Nb-Ti
Nb3Sn

## Slide 9: Measurements of the conductor critical current
The critical current of a conductor is measured by winding a sample of the wire around a sample holder.
To avoid premature quenching induced by Lorentz forces during ramping, the wire must be well supported
  Stycast glue may be used to constrain the wire around the holder
In case of Nb3Sn wires, a sample holder made of titanium is used.
Once the wire is cooled-down and placed in a given magnetic field, the current is increased until the transition occurs.

## Slide 10: Nb-Ti parameterization curve (LHC dipole)
Nb-Ti parameterization
  Temperature and field dependence of BC2 and TC are provided by Lubell’s formulae:
  where BC20 is the upper critical flux density at zero temperature (14.5 T), and TC0 is critical temperature at zero field (9.2 K)
  Temperature and field dependence of Jc is given by Bottura’s formula
  where JC,Ref is critical current density at 4.2 K and 5 T (3000 A/mm2) and CNb-Ti (27 T), Nb-Ti (0.63), Nb-Ti (1.0), and Nb-Ti (2.3) are fitting parameters.
a

## Slide 11: Nb3Sn parameterization curve (typical values for HEP magnets)
Nb3Sn parameterization
  Temperature, field, and strain dependence of Jc is given by Summers’ formula
  where Nb3Sn is 900 for  = -0.003, TCom is 18 K, BC20m is 27.6 T, and CNb3Sn,0 is a fitting parameter equal to 43100000000 AT1/2mm-2 for a Jc=2900 A/mm2 at 4.2 K and 12 T.
  Assume  = 0.000

## Slide 12: Parameterization curves
References
  M.S. Lubell, “Empirical scaling formulas for critical current and critical fields for commercial NbTi,” IEEE Trans. Magn., Vol. MAG-19 No. 3, pp. 754–757, 1983.
  L. Bottura, “A practical fit for the critical surface of NbTi,” IEEE Trans. Appl. Supercond., Vol. 10, No. 1, pp. 1054–1057, 2000.
  L.T. Summers, M.W. Guinan, J.R. Miller and P.A. Hahn, “A model for the prediction of Nb3Sn critical current as a function of field, temperature, strain and radiation damage,” IEEE Trans. Magn., Vol. 27, No. 2, pp. 2041–2044, 1991.

## Slide 13: Nb-Ti and Nb3Sn critical curves at 1.9 K

## Slide 14: Case study
11 T Nb3Sn dipole for the LHC collimation upgrade
  Question
    Determine coil filling factor (J0 /Jsc ratio or Anon-Cu_cable/Ainsulated_cable)

## Slide 15: Superconducting cables and coils

## Slide 16: J0 /Jsc ratio
The cable design parameters are:
  Number of wires Nwire
  Wire diameter dwire
  Cable mid-thickness tcable
  Cable width wcable
  (Cu/non-Cu) ratio
  Insulation thickness
  Pitch angle
    To be neglected in this comp.

## Slide 17: J0 vs. Jsc
Cu to non-Cu ratio: 1.2

## Slide 18: J0 vs. Jsc

## Slide 19: Case study
11 T Nb3Sn dipole for the LHC collimation upgrade
  Question
    Compute load-line (Jsc vs. B) for a
      Sector coil (60) with constant current density
    Determine coil size, operational (80% of Iss ), conditions, “short-sample” conditions, and margins
      w
      jsc_ss , jo_ss , Bbore_ss , Bpeak_ss
      jsc_op, jo_op , Bbore_op , Bpeak_op
      T, jsc , Bpeak margins
    Compare “short sample”, “operational” conditions and margins if the same design uses Nb-Ti superconducting technology with the same coil size w

## Slide 20: Short sample and operational current
Short sample current
  The critical current is measured in few different conditions of temperature and field. By fitting the data with known parameterizations, the entire critical surface can be reconstructed.
If the magnet reaches the maximum current computed through the intersection of the measured critical surface and the load line, i.e. Imax = Iss, one can declare victory (at least from the quench performance point of view).
If the magnet maximum current Imax is lower that Iss , the quench performance is expressed in term of fraction of short sample (Imax/Iss).
Usually magnets are designed to operate at Iop = 0.8 Iss or below.

## Slide 21: Computation of the load line Approximations of practical winding cross-sections
Sector coil
  Current density J = J0 (A per unit area) on a a sector with a maximum angle  = 60º for a dipole

## Slide 22: Approximations of practical winding cross-sections

## Slide 23: Computation of the load line Approximations of practical winding cross-sections
Sector coil
  Current density J = J0 (A per unit area) on a a sector with a maximum angle  = 60º for a dipole
  Where, Bbore is the bore field, j0 is overall current density and w is the coil width
  “Less ideal” case
    Bpeak = Bbore· ~1.04
    “Not so perfect” field quality
      b3 = 0
With a w/r of 30/30 = 1 1.04
Bpeak/Bbore
L. Rossi, E. Todesco, “Electromagnetic design of superconducting quadrupoles”, Phys. Rev. ST Accel. Beams 9 (2006) 102401.

## Slide 24: Computation of the load line Sector coil
Bbore_op = 11 T
Bbore_ss = Bbore_op /0.8 = 13.75 T
Bpeak_ss = Bbore_ss· 1.04 = 14.3 T

## Slide 25: Computation of the load line Sector coil
Bbore_op = 11 T
Bbore_ss = Bbore_op /0.8 = 13.75 T
Bpeak_ss = Bbore_ss· 1.04 = 14.3 T
From the critical curve
  jsc_ss = 2460 A/mm2
Therefore
  w = 25.25 mm
Results
  jsc_ss = 2460A/mm2
  jo_ss = jsc_ss * λ = 786 A/mm2
  Bbore_ss = 13.75 T
  Bpeak_ss = 14.3 T
  jsc_op = 1965 A/mm2
  jo_op = jsc_op * λ = 629 A/mm2
  Bbore_op = 11 T
  Bpeak_op = 11.44 T
  jsc_margin = 2140 A/mm2
  Bpeak_margin = 4 T
  Tmargin = 6.7 K

## Slide 26: Nb3Sn vs. Nb-Ti Sector coil
Nb-Ti parameters
w = 25.25 mm
Results
  jsc_ss = 1660 A/mm2
  jo_ss = jsc_ss * λ = 532 A/mm2
  Bbore_ss = 9.3 T
  Bpeak_ss = 9.7 T
  jsc_op = 1330 A/mm2
  jo_op = jsc_op * λ = 425 A/mm2
  Bbore_op = 7.45 T
  Bpeak_op = 7.74 T
  Jmargin = 1370 A/mm2
  Bmargin = 2.5 T
  Tmargin = 2.1 K

## Slide 27: Comparison

## Slide 28: Case study
11 T Nb3Sn dipole for the LHC collimation upgrade
  Question
    Determine e.m forces Fx and Fy and the accumulated stress on the coil mid-plane in the operational conditions with sector coil approximation

## Slide 29: E.m. forces and stresses
The e.m. forces in a dipole magnet tend to push the coil
  Towards the mid plane in the vertical-azimuthal direction (Fy, F < 0)
  Outwards in the radial-horizontal direction (Fx, Fr > 0)
Tevatron dipole
HD2

## Slide 30: E.m. forces and stresses
LHC dipole at 0 T LHC dipole at 9 T
Usually, in a dipole or quadrupole magnet, the highest stresses are reached at the mid-plane, where all the azimuthal e.m. forces accumulate (over a small area).
Displacement scaling = 50

## Slide 31: E.m. forces and stresses Sector coil approximation
For a dipole sector coil, with an inner radius a1, an outer radius a2 and an overall current density jo , each block (quadrant) see
  Horizontal force outwards
  Vertical force towards the mid-plan
  In case of frictionless and “free-motion” conditions, no shear, and infinitely rigid radial support, the forces accumulated on the mid-plane produce a stress of

## Slide 32: E.m. forces and stresses Sector coil approximation
In the operational conditions (Bbore_op = 11.0 T)
  Fx (quadrant) = +2.29 MN/m
    Fx (total) = +4.60 MN/m = 460 t/m
  Fy (quadrant) = -2.10 MN/m
The accumulates stress on the coil mid-plane is

## Slide 33: Comparison

## Slide 34: Case study
11 T Nb3Sn dipole for the LHC collimation upgrade
  Question
    Evaluate dimension of collars, iron yoke, and shrinking cylinder, assuming that the support structure is designed to reach 90% of Iss

## Slide 35: Support structure Collars
Collars were implemented for the first time in the Tevatron dipoles.
Since then, they have been used in all but one (RHIC) the accelerator magnets and in most of the R&D magnets.
They are composed by stainless-steel or aluminum laminations few mm thick.
By clamping the coils, the collars provide
  coil pre-stressing;
  rigid support against e.m. forces (it can be self-supporting or not);
  precise cavity (tolerance  20 m).
L. Rossi, [1]
MJB Plus, Inc., [2]
Tevatron
SSC
LHC

## Slide 36: Support structure Collars
Collaring procedure
  Collars are pre-assembled in packs (several cm long) and placed around the coil.
    The collar laminations are divided in “short” and “long”.
  Since the uncompressed coil is oversized with respect to the collar cavity dimension, at the beginning of the collaring procedure the collars are not locked (open).
  The coil/collar pack is then introduced into a collaring press.
  The pressure of the press is increased until a nominal value.
  Collars are locked with keys, rods or welded, and the press released.
  Once the collaring press is released, the collar experience a “spring back” due to the clearance of the locking feature and deformation.

## Slide 37: Support structure Collars
Collaring of a dipole magnet
Collaring of a quadrupole magnet

## Slide 38: Dimension of the support structure Collars
We assume a 25 mm thick collar
  Images not in scale

## Slide 39: Without iron yoke

## Slide 40: With iron yoke
The iron yoke thickness can be estimated with

## Slide 41: Dimension of the yoke
The iron yoke thickness can be estimated with
Therefore, being
  Bbore = 12.2 T (at 90% of Iss )
  r = 30 mm and
  Bsat = 2 T
we obtain
  tiron = ~190 mm

## Slide 42: Support structure Shell (or shrinking cylinder)
The cold mass is contained within a shell (or shrinking cylinder).
The shell constitutes a containment structure for the liquid Helium.
It is composed by two half shells of stainless steel welded around the yoke with high tension (about 150 MPa for the LHC dipole).
  With the iron yoke, it contributes to create a rigid boundary to the collared coil.
If necessary, during the welding process, the welding press can impose the desired curvature on the cold mass.
  In the LHC dipole the nominal sagitta is of 9.14 mm.

## Slide 43: Support structure Shell (or shrinking cylinder)

## Slide 44: Support structure Shell (or shrinking cylinder)
The shell tension provided by the welding may contribute to the overall support of the collared coil.
An often (SSC, LHC) implemented approach is the line-to-line fit.
  When the yoke is put around the collared coil, a gap (vertical or horizontal) remains between the two halves; this gap is due to the collar deformation induced by coil pre-stress.
  After welding, the shell tension closes the gap, and good contact is provided between yoke and collar.
  After cool-down, despite the higher thermal contraction of the collared coil with respect to iron, the gap remain closed (high rigidity), and the collared coil in good contact with the yoke.
Aluminum spacer may be used to control the yoke gap.

## Slide 45: Dimension of the support structure
We assume that the shell will close the yoke halves with the same force as the total horizontal e.m. force at 90% of Iss
We assume an azimuthal shell stress after cool-down of
  shell = 200 MPa

## Slide 46: Dimension of the support structure
We assume that the shell will close the yoke halves with the same force as the total horizontal e.m. force at 90% of Iss
  Fx_total = Fx_quadrant * 2 = +6.8 MN/m
Assuming an azimuthal shell stress after cool-down of
  shell = 200 MPa
The thickness of the shell is
  tshell = Fx_total /2/1000/ shell ~ 17 mm

## Slide 47: Comparison