## Slide 1: Conductor and Cable Summary and Comparison of MQXFB08 Witness Sample Results
S. C. Hopkins, J. Fleiter, T. Boutboul (TE-MSC-LSC)
Technical Meeting to Review Coils for MQXFB08, 6 November 2024

## Slide 2: Cable and Coil Overview
Coil | Cable 1 | Cabling Report | HT | Witness Report | Cable NCRs | Strand Contract 2 | Billets
CR148 | H16OC0455A | 3091621 | 822 | 3185366 | - | F663/Am4 (9) F663/Am5 (31) | AO08S00399 (9) AO08S00615 (9) AO08S00619 (9) AO08S00629 (4) AO08S00639 (9)
CR149 | H16OC0409A | 2772479 | 830 | 3185367 | - | F663/Am3 (2) F663/Am4 (31) F663/Am5 (7) | AO08S00283 (8) AO08S00308 (7) AO08S00444 (8) AO08S00476 (8) AO08S00625 (7) AO08S99116 (2)
CR150 | H16OC0412A | 2774489 | 837 | 3185368 | - | F663/Am4 (21) F663/Am5 (19) | AO08S00561 (11) AO08S00569 (10) AO08S00598 (10) AO08S00613 (9)
CR151 | H16OC0414A | 2791624 | 844 | 3185369 | - | F663/Am5 (40) | AO08S00593 (11) AO08S00597 (11) AO08S00599 (9) AO08S00601 (9
1 MQXF cable specification, EDMS 1863790 2 MQXF wire specification, LHC-MQXF-CI-0001, EDMS 1419924

## Slide 3: Nonconformities
NCRs affecting the cable are summarised below
  Insulated cables
    NCRs concerning strand pop-ups for CR148, CR149 and CR150, not treated further in this presentation
  Witness samples (coil heat treatments)
    No indication of a significant performance impact from minor coil HT NCRs for CR148 and CR149
Coil | HT | Cable NCRs | NCRs Implicating Cable | Coil HT NCRs
CR148 | 822 |  | 3093358 | 3129199
CR149 | 830 |  | 2811007 | 3138474
CR150 | 837 |  | 3017026, 3132312 | 
CR151 | 844 |  |  | 

## Slide 4: Testing Anomalies
For CR148 and CR150, the maximum cabling degradation evaluated from witness samples is reported as exceeded the 5 % specification:
  For CR148:
    Anomalous value for strand 13 at 14.5–15 T only: mean for strand 13 is 4.1 %, in specification
    Also in specification for other witness samples and original cable qualification
  For CR150:
    Higher degradation value is for strand 11 only: excluding this strand, average degradation is ~2 %
    This might suggest slight degradation of the test piece; but Ic is nevertheless within the Ic band
For CR149, Ic data for strand 6 were included in the evaluation only at 4.3 K due to a testing issue in the first cooldown
  Retests at 1.9 K were successful, but not considered in the report due to the possibility of an Ic increase on the second cooldown
  Ic is comparable to strand 7; calculation of margin is not significantly affected
For CR150, extracted sample WE06 was degraded, probably due to sample damage
  Excluded from analysis
  No correlation with furnace position, so not caused by heat treatment anomalies
For CR151, measurement could not be performed at 1.9 K, so coil short sample limits are reported only at 4.5 K
  The values have been estimated by scaling (next slide) and are in the normal range
  Samples will be remeasured at 1.9 K for confirmation (expected by the end of November); note that as this is a second cooldown, the Ic may be slightly increased

## Slide 5: CR151 Performance at 1.9 K
Ic parameters for the witness samples at 1.9 K have been estimated assuming the typical temperature scaling for MQXF wire
T (K) | Bc2 (T) | Cmin (A·T) | Cavg (A·T) | Cmax (A·T)
1.9 | 28.6 | 54210 | 55759 | 58443
4.3 | 25.8 | 46082 | 47399 | 46981
At 1.9 K | Ic,SS (A) | Iop/Ic,SS (%)
Min | 22488 | 73.2%
Avg | 22664 | 72.7%
Max | 22957 | 71.7%
With those values, margin at 1.9 K would be 26.8 %

## Slide 6: Load Line Margin
Large margin on load line of ~26 %
  Consistent in mean and spread with recent coils

## Slide 7: Estimated Coil RRR
Large RRR margin
Connection side (CC) has higher RRR
All values within the range of other recent coils

## Slide 8: Effect of HT/Furnace on Round Wire Ic
Ic of virgin witness samples (building 180) – Ic of virgin qualification samples (building 163)
Ic consistently slightly higher for witness samples (HT in building 180) than qualification samples (HT in building 163)
In a consistent range for recent coils

## Slide 9: Cabling Degradation of Ic
Cabling degradation of Ic is within the 5 % specification for qualification samples of all coils
Mean cabling degradation is also <5 % for witness samples
  Except the CR150, for which degradation values are available for only two strands, one of which shows anomalously high degradation
  Excluding this outlier, mean
Otherwise, consistent and conforming degradation as assessed from witness samples across all recent production, both at 1.9 K and 4.3 K
Excluding outliers above: mean cabling degradation ~3 %
MQXFB08

## Slide 10: Summary
Cable data in specification for all coils
  Excluding anomalous cabling degradation for two potentially damaged extracted strand samples
  Lack of Ic data at 1.9 K for one coil, but scaling suggests performance in the normal range
Good consistency between recent coils, and data in a comparable range to MQXFB02-07
Systematic differences remain between small (building 163) and large (building 180) HT furnaces, and in RRR between CC and CoC

## Slide 11: Thank you for your attention!