## Slide 1: D1 / Quench Protection Heater Power Supply Status
Tatsushi NAKAMOTO, KEK
On behalf of CERN-KEK Collaborations for D1 and DQHDS for HL-LHC
CERN-KEK Committee, 19th Meeting, Nov. 26, 2024

## Slide 2: Acknowledgement
KEK (in particular)
M. Sugano, K. Suzuki, Y. Arimoto, R. Ueki, Y. Ikemoto, H. Kawamata,
N. Okada, R. Okada, H. Ohhata, A. Terashima, K. Tanaka, N. Ohuchi, T. Ogitsu.
Univ. of Tokyo
N. Kimura.
CERN (in particular)
E. Todesco, J. C. Perez, H. Prin, D. Duarte Ramos, C. Scheuerlein,
H. G. Gavela, G. Willering, F. Mangiarotti, L. Fiscarelli.
D. Carrillo, E. Nowak, M. Pojer, D. Wollmann.
Hitachi
M. Yanagisawa, A. Yokogi, H. Togashi, T. Tahara, T. Chiba.
Fusac Technologies
T. Ichihara.

## Slide 3: Japanese Contribution to HL-LHC: D1, DQHDS
Beam separation dipole (D1): 7 units x 7m long cold masses
  Design study of D1 for HL-LHC within the framework of the CERN-KEK collaboration since 2011.
  150 mm single aperture, 35 Tm (5.6 T x 6.3 m), Nb-Ti technology.
  Development 2-m long model magnets (3 units) at KEK
  1 full-scale prototype cold mass (LMBXFP)
  6 series cold masses (LMBXF1-6)
Quench heater power supply (DQHDS)
  4 units of pre-series
  626 units of series production
IP

## Slide 4: Powering test of D1 series production magnets at KEK

## Slide 5: Current status of MBXF / LMBXF
 | Prototype | Series production (in order of production sequence) |  |  |  |  | 
 | MBXFP1 | MBXF1 | MBXF5 | MBXF2 | MBXF3 | MBXF6 | MBXF4
Magnet assembly |  |  |  |  |  |  | 
Cold test at KEK |  |  |  |  | Test is underway |  | 
Cold mass assembly |  |  |  |  |  |  | 
Delivery of completed cold-mass to KEK |  |  |  |  |  |  | 
Transport to CERN |  |  |  |  |  |  | 
Horizontal test at CERN |  |  |  |  |  |  | 
MBXF5
MBXF2
LMBXFP1
LMBXF1

## Slide 6: Items of cold powering test at KEK
Check of electrical integrity by a Hi-pot test at cold
Training
  Up to the ultimate current
  Identification of quench start location by quench antennas
  Training memory
  Current-holding test at the ultimate current for 4h
Magnetic field measurement
  Field quality at the magnet center
  Integrated field quality
Joint resistance
RRR measurement

## Slide 7: Dual operation of refrigerators
During CD1 of MBXF5, we had a trouble with the warm turbine of #4 refrigerator.
  CD2 of MBXF5 after TC was postponed.
Cooling test of dual operation of the #4 refrigerator and #2 liquefier was conducted in April 2024. Sufficient total liquefaction ability of 490 L/h was confirmed.
Cooling down of MBXF2 was performed with such a dual operation.
20 m long LHe transfer line connecting #2 and #4 systems.
#4 Refrigerator/Liquefier for Test Stand
180 L/h, 2400 L dewar
Manufactured by Teisan/Air Liquide in 1987
New cold box in 2007
#2 Liquefier (Primary)
400 L/h, 5000 L dewar
LINDE LR280 in 2014
Mandatory to supply LHe to users at KEK.

## Slide 8: Training Quenches
All series magnets reached the ultimate current.
The 2nd cycle for MBXF5 was postponed due to malfunction of the test facility of KEK.
Good training memory in MBXF1 and MBXF2.
Successful current-holding for 4h at the ultimate.
 Stable operation of the magnets
Cold mass
4h
4h
4h
at CERN
 | 1st cycle |  | 2nd cycle | 
 | Nominal | Ultimate | Nominal | Ultimate
MBXFP1 | 3 | – | 3 | –
MBXF1 | 2 | 7 | 0 | 0
MBXF5 | 4 | 9 | TBC | TBC
MBXF2 | 10 | 18 | 0 | 1
Number of quenches
Acceptable training performance
TC: Thermal cycle
Due to a trouble of refrigerator

## Slide 9: Quench start locations
Quench start locations were changed during the training.  No weak point.
All quenches at a low current took place at LE, which is a common nature of MBXF.
Arrangement of quench antennas
LE
Top
Bottom
RE
Not identified
Balance voltage
TC
TC
TC
Signals detected by quench antennas

## Slide 10: Current dependence of integrated multipoles
The field quality of series production magnets is predictable by OPERA 3D simulations.
Ramp-up
Ramp-down
Ramp-up
Ramp-down

## Slide 11: Integrated multipoles at the nominal current (I=12.11 kA)
Series
Prototype
Good reproducibility in integrated field quality among the series production magnets.
in KEK cryostat
in KEK cryostat
Fine-tuning by modification
of coil cross-section from prototype
to series magnets
0.25
0.16
-12.54
-4.13
-5.49
-6.81
-4.72
0.19
0.54
0.14
0.13
-0.15
-0.14
-0.10
6.44
1.35
1.18
0.53
0.63
0.10
0.16
0.03
-0.03
-0.06
-0.00
-0.50
-0.62
-0.65
-0.75
0.38
0.01
0.23
0.08
0.16
-0.00
0.77
0.13
0.14
0.08
-0.07
0.02
0.02
-0.01
0.010.00
-0.12
-0.20
-0.10
-0.17
-0.14
-2.53
-3.73
-1.11
-1.12
-0.28
1.97
1.91
2.00
1.89
1.65
-0.52
-0.59
0.33
0.40
0.02
-0.12
-0.08
-0.13
-0.20
-0.15
0.17
0.33
0.13
0.02
-0.08
0.18
0.27
0.24
0.19
0.13
0.12
0.04
0.17
0.08
0.00
0.01
0.06
0.02
-0.00
-0.03
0.09
0.06
0.08
0.05
0.01
0.05
0.06
0.02
0.03
0.02

## Slide 12: Flash Report: Cold Test of MBXF3
Cooling of MBXF3 started Nov. 8.
A campaign of training quenches started at the Nov. 20.
The test will continue until the end of Dec. 2024.
CD2 of MBXF5 which was postponed due to malfunction of the refrigerator will be performed in March 2025.

## Slide 13: Powering test of prototype at SM18

## Slide 14: Horizontal powering test of LMBXFP1 at CERN
MBXFP1 cold mass (LMBXFP1) was assembled into a cryostat at CERN.
The first powering test for MBXF cold mass with a horizontal cryostat.
The items to be checked in the horizontal test.
  Training memory for the cold mass including newly designed bus leads.
  Field quality including the influence of the magnetic LHC cryostat.
  Long-time operation: current-holding test at the ultimate for 8 hours.
  Endurance test: 500 powering cycles between 1 kA and 12.11 kA.
G. Willering, Gaëlle Ninet, Franco Mangiarotti, Piotr Rogacki, Lucio Fiscarelli
https://indico.cern.ch/event/1379959/
EDMS 3015584

## Slide 15: Training Quenches of LMBXFP1
Cold mass
at CERN
Magnet at KEK
End cover
End plate
Bus lead
Splice
box
The quench current reached the ultimate current in the second cycle.
Current-holding at the ultimate current for 8h was also successful.
500 powering cycles between 1 kA and 12.11 kA could be stably completed.
 The bus leads newly designed by KEK was validated.
Training memory should be checked in the series production magnets.
Bus lead
8h

## Slide 16: Magnetic design considering an effect of LHC cryostat
The effect of the LHC cryostat made of magnetic iron was considered in the magnetic design.
The magnet cross-section was optimized so that the field quality was controlled within the target after the cold mass was assembled into the LHC cryostat.
Offset estimated from OPERA 3D simulation: Db3=+6.1 units, Db5=+0.3 units
The validity of this design strategy was checked in LMBXFP1 for the first time.
Iron pit
LHC cryostat
• Vertical SS cryostat at KEK
• Iron pit surrounding the cryostat
• The magnet is off-centered by 150 mm
• LHC cryostat made of magnetic iron
• The off-center of the magnet with respect to
the cryostat is neglected.
Test at KEK
Test at CERN

## Slide 17: Field quality at the nominal current of LMBXFP1
Measurement by KEK KEK cryostat (MBXFP1) |  |  | Measurement by CERN LHC cryostat (LMBXFP1) |  | 
Field integral (B1) |  | 34.935 Tm | Field integral (B1) |  | 35.188 Tm
n | bn integral (unit) | an integral (unit) | n | bn integral (unit) | an integral (unit)
2 | 0.25 | -2.52 | 2 | 0.27 | 0.88
3 | -12.54 | 1.96 | 3 | -5.44 | 1.95
4 | 0.19 | -0.52 | 4 | 0.05 | 0.12
5 | 6.43 | -0.12 | 5 | 6.68 | -0.19
6 | 0.10 | -0.08 | 6 | 0.05 | 0.00
7 | 0.38 | 0.18 | 7 | 0.35 | 0.20
8 | 0.01 | 0.11 | 8 | 0.04 | 0.15
9 | 0.77 | 0.01 | 9 | 0.76 | 0.00
10 | 0.02 | 0.09 | 10 | 0.04 | 0.10
11 | -0.12 | 0.05 | 11 | -0.13 | 0.07
12 | -0.02 | 0.02 | 12 | 0.03 | 0.03
13 | -0.76 | 0.00 | 13 | -0.73 | 0.05
14 | -0.08 | -0.06 | 14 | 0.00 | 0.00
15 | -1.22 | -0.01 | 15 | -1.18 | 0.03
The field quality of LMBXF cold mass
with the LHC cryostat can be well predicted
from the field quality of the magnet measured
at KEK.
The proposed magnetic design is valid.
Note that the cross-section of LMBXFP1 was not fully optimized.
Fine-tuning has been applied to the series production magnets.
Shift of bn by the LHC cryostat
Simulation: +6.1uits
Measurement: +7.1units
Integrated b3
Integrated b5
Simulation: +0.27uits
Measurement: +0.25units

## Slide 18: Prediction of integrals of b3 and b5 for series production cold mass with LHC cryostat
The field quality can be expected within the acceptance criteria for the series production cold masses with the LHC cryostat.
b3 integral (unit) | Measurement by KEK with KEK cryostat | Prediction for cold mass with LHC cryostat | Acceptance criteria
MBXF1 | -4.13 | 1.97 | b3 integral <±2.9 units
MBXF5 | -5.49 | +0.61 | b3 integral <±2.9 units
MBXF2 | -6.81 | -0.71 | 
b5 integral (unit) | Measurement by KEK with KEK cryostat | Prediction for cold mass with LHC cryostat | Acceptance criteria
MBXF1 | 1.35 | 1.62 | b3 integral <±1.5 units
MBXF5 | 1.18 | 1.45 | 
MBXF2 | 0.53 | 0.80 | b3 integral <±1.5 units
Db3=+6.1 units
Db5=+0.27 units
At the nominal current

## Slide 19: Status of D1 Series Production and Tests
LMBXFP1
  Horizontal powering test at CERN was completed.
  The cold mass was accepted by CERN.
  Installation to IT String was done in Nov, 2024.
LMBXF1
  The cold mass was completed and delivered to KEK at March 2024.
  The cold mass is expected to be delivered to CERN in the week of December 9.
MBXF5
  The trouble of a the refrigerator forced to stop the cold test (CD2) after T.C.
  Plan of CD2 in early 2025, after the cold test of MBXF3.
MBXF2
  Final assembly of the cold mass is underway at Hitachi.
  Completion will be in June 2025.
MBXF3
  The magnet was nearly completed in August, but the delivery to KEK has been delayed due to the NC (cut of voltage tap wires).
  Delivery to KEK was on Oct. 28 and the cold powering test is currently underway.
MBXF6
  Two coils (LT-5, LB-5) were already wound but the collaring will be only possible in December due to an issue of resources in Hitachi.
MBXF4
  Coil winding is planned in early 2025.
LMBXF1
LMBXFP1 in IT-String

## Slide 20: Status of D1 Series Production and Tests
LMBXFP1
  Horizontal powering test at CERN was completed.
  The cold mass was accepted by CERN.
  Installation to IT String was done in Nov, 2024.
LMBXF1
  The cold mass was completed and delivered to KEK at March 2024.
  The cold mass is expected to be delivered to CERN in the week of December 9.
MBXF5
  The trouble of a the refrigerator forced to stop the cold test (CD2) after T.C.
  Plan of CD2 in early 2025, after the cold test of MBXF3.
MBXF2
  Final assembly of the cold mass is underway at Hitachi.
  Completion will be in June 2025.
MBXF3
  The magnet was nearly completed in August, but the delivery to KEK has been delayed due to the NC (cut of voltage tap wires).
  Delivery to KEK was on Oct. 28 and the cold powering test is currently underway.
MBXF6
  Two coils (LT-5, LB-5) were already wound but the collaring will be only possible in December due to an issue of resources in Hitachi.
MBXF4
  Coil winding is planned in early 2025.
LMBXF1
LMBXFP1 in IT-String

## Slide 21: Status of D1 Series Production and Tests
LMBXFP1
  Horizontal powering test at CERN was completed.
  The cold mass was accepted by CERN.
  Installation to IT String was done in Nov, 2024.
LMBXF1
  The cold mass was completed and delivered to KEK at March 2024.
  The cold mass is expected to be delivered to CERN in the week of December 9.
MBXF5
  The trouble of a the refrigerator forced to stop the cold test (CD2) after T.C.
  Plan of CD2 in early 2025, after the cold test of MBXF3.
MBXF2
  Final assembly of the cold mass is underway at Hitachi.
  Completion will be in June 2025.
MBXF3
  The magnet was nearly completed in August, but the delivery to KEK has been delayed due to the NC (cut of voltage tap wires).
  Delivery to KEK was on Oct. 28 and the cold powering test is currently underway.
MBXF6
  Two coils (LT-5, LB-5) were already wound but the collaring will be only possible in December due to an issue of resources in Hitachi.
MBXF4
  Coil winding is planned in early 2025.
LMBXF1
LMBXFP1 in IT-String

## Slide 22: Status of DQHDS

## Slide 23: Status of Quench Heater Power Supply (DQHDS)
4 unit of DQHDS pre-series were delivered to KEK in March 2024 and sent to CERN for performance qualification. The pre-series units were successfully validated and accepted in July.
Visit of production lines at the producer (Nichicon) by KEK with a remote connection of CERN experts was conducted on Oct. 16.
  The green-light to start the series production was sent to Nichicon.
264 units of the series production will be delivered by March 2025 (JFY2024).
The remaining 362 units will be delivered in JFY 2025.
Pre-series DQHDS
Visit of production lines