## Slide 1
Mon 27th January 2025
Faculty of Natural Sciences
Hall 413 B - Tirana
Optical and Interferometric Methods for Material Characterization
and Dimensional Analysis
Giovanni Pappalettera

## Slide 4
ENROLLED STUDENT WITH
2.980 WOMEN AND 132
FOREIGN STUDENTS
DEPARTMENTS
PROFESSORS and RESEARCHERS
184 WOMEN
NON TEACHING STAFF
126 WOMEN
POLITECNICO DI BARI IN NUMBERS
TERRITORIAL
SEATS

## Slide 5
MECHANICS, MATHEMATICS and MANAGEMENT DEPARTMENT
SEAL of EXCELLENCE DEPARTMENT
2018-2022
2023-2027
A recognition given by the Italian
Ministry of University and Research
Selecting among 800 University
Department
Best Ranking in the Industrial Area

## Slide 6: Teaching Offer
Bachelor
Master
Aerospace Systems Engineering(TA)
Mechanical Engineering
Post Lauream
PhD
Mechanical and Energetic Engineering (DRIME)
PhD
Engineering and Aerospace Systems(DRISA)
Mechanical Engineering
Energetic Engineering
Industrial and Naval Systems Engineering
(TA)
Management Engineering
Management Engineering
Mechanical Engineering
PhD
Management Engineering (DRIG)

## Slide 8
Stress and Strain
Stress
Strain
Apply Load
Measure
Deformation
Get Stress/Strain
Curve

## Slide 9
Strain Measurement: Strain Gauge
Dimensional variation of the strain gauge change its resistivity
Wheatstone Bridge

## Slide 10
Strain Gauges limitations
Aluminum foam stringered panel
PU foam
Corrosion onset
CFRP Composite
PCB Board

## Slide 11
Why optical Methods?
No contact
No destructive
High resolution
High sensitivity
Which optical Methods?
Speckle Interferometry
Moirè Methods
Fringe Projection Methods
Digital Holography
Shearography
Photoelasticity
DIC
…..
Interferometric Implementation
Non Interferometric Implementation
Every time we are looking for:

## Slide 12
I
Interferometric Methods
I
I
Mobile Mirror
Mirror
I
Constructive
Destructive
Intermediate
Arm 1
Arm 2

## Slide 13
Speckle Methods
2
2
P
2
P
?
Intensity?
Constructive/Destructive
?
Intensity?
Constructive/Destructive
Randomly determined

## Slide 14
Principle of Fringe Analysis
Basic idea is the relationship between phase in the pattern and the quantity to be measured
Fringes Generated by Laser Interference
This express the light wavefront at a given instant t
Phase can be express as a function of the travelled path h(x,y)
h

## Slide 15
Fringes Generated by Laser Interference
Let’s suppose now to have two wavefront and let’s call them reference and test
Let’s make them interfere on a surface
Leading to an intensity
Principle of Fringe Analysis

## Slide 16
Principle of Fringe Analysis
Where
We can set
We get the fundamental equation of the fringe analysis

## Slide 17
Principle of Fringe Analysis
Background
Contrast
Phase

## Slide 18
Principle of Fringe Analysis
How I can extract the phase? PHASE SHIFTING
Three Step Phase Shifting

## Slide 19
Principle of Fringe Analysis: one application
1 DPSS, =532 nm, P=25 mW laser source
1 CCD camera 640x480 ;
1 Electronically controlled cutter
1 Precision Translational stage
1 Compressed air cleaning system
1 PC
Speckle is a noise on the fringe pattern

## Slide 20
Grid 1
Grid 2
All the methods allowing to exploit this effect, overlapping even electronically these two grids are called
moiré
Moiré Principle
Notes: In questa slide mostriamo il principio fondamentale su cui sono basate le tecniche moiré. Sovrapponendo due griglie sfasate si generano delle frange la cui frequenza varia al variare dello spostamento relativo. Questo principio può essere declinato in varie maniere a seconda dello specifico set-up.

## Slide 21
Moiré Principle

## Slide 22
Geometric Moiré
Interferometric Moiré
Reflection Moiré
Shadow moiré
u=pNx
v=pNy
In plane displacement
w=KpNz
Out of plane displacement
Moiré Method

## Slide 23
p
P’
p’=(dp)/(d±p)
d=moiré fringes distance
Moiré Method

## Slide 24
Plane moiré
Shadow Moiré
Moiré Method

## Slide 25
u=pNx
Interferometric Moiré
Moiré Method

## Slide 26
Fringe Projection Methods
If I subtract two phase map on the object and on the phase plane I get this:
Similar Triangles

## Slide 27
DIC

## Slide 28
DIC

## Slide 29
DIC
Foam Iosipescu
Stress Concentration Airbus
Clear Aligners
Iosipescu FOAM

## Slide 30
DIC

## Slide 31
DIC

## Slide 32
DIC

## Slide 33
DIC
C(5,5,1,1)=0
Perfect Match!

## Slide 34
DIC
C(5,5,1,1)=0
Best Match!

## Slide 35
DIC

## Slide 36
DIC current challenges and Machine Learning
Improve Computational Time going toward real time evaluation
Reduce error in calculating strain from displacement
Manage with issue at high deformation up to paint breaking
Ru Yang, Yang Li, Danielle Zeng, Ping Guo, Deep DIC: Deep learning-based digital image correlation for end-to-end displacement and strain measurement. Journal of Materials Processing Technology, 302, 2022

## Slide 37
DIC current challenges and Machine Learning
Three ideas:
Two separate net for Displacement and Strain
Displacement and Strain Calculated in the incremental way
Accumulated displacement is used to update the ROI

## Slide 38
DIC current challenges and Machine Learning
Using an encoder decoder architecture and
Giving two input images (reference and
calculation) you have:
Two displacement fields
Three strain fields

## Slide 39
DIC current challenges and Machine Learning
Notes: Pytorch

## Slide 40
Calculated Strain Error
Max: 5.93%
Avg: 0.24 %
Strainnet Error
Max: 0.11 %
Avg: 0.018 %
Error in Strain Determination is reduced
But still not proved to manage large deformation at once
DIC current challenges and Machine Learning

## Slide 41
DIC current challenges and Machine Learning
Higher accuracy both on displacement and
Strain with respect to VIC-2D software
Other comparison can be done in terms of
Calculation time
When applied to a sequence of 189 images
The net time for VIC 2D software was 27 s
Time for Deepnet was 2.35 s
https://github.com/RuYangNU/Deep-Dic-deep-learning-based-digital-image-correlation

## Slide 42
ESPI current challenges and Machine Learning
Wenbo Jiang, Tong Ren, Qianhua Fu Zeng, Deep Learning in the Phase Extraction of Electronic Speckle Pattern Interferometry. Electronics, 13(2), 2024
Denoising is a process which is slowing
the measurement chain
When dealing with complex fringe pattern
Global optimum denoising can hyde some
Local features
Poor generalization

## Slide 43
Ground Truth
SOOPDE
WFF
BL Hilbert L2
FDD NET
MDD NET
Xu, M.; Tang, C.; Hong, N.; Lei, Z. MDD-Net: A generalized network for speckle removal with structure protection and shape preservation for various kinds of ESPI fringe patterns. Opt. Lasers Eng. 2022, 154, 107017.
Higher Contrast
Higher Denoising
Better shape Preservation
Notes: Windows Frame Fourier
Oriented Partial Differential equation

## Slide 44
Thank You For Your Attention!
giovanni.pappalettera@poliba.it