## Slide 1: PSI Roadmap towards High-Field Magnets
HFM Annual Meeting 2025
D. Araujo, B. Auchmann, A. Brem, T. Michlmayr, A. Stampfli and C. Müller
A. Haziot and E. Ravaioli (CERN)
This work was performed under the auspices of and with support from the Swiss Accelerator Research and Technology (CHART) program.
February 11, 2025

## Slide 2
CHART2 Stress-Management R&D
Composite
Characterization
and Modeling
Powered Samples
Coil Demonstrator
Subscale Magnets
Intermediate Field
Demonstrator
Courtesy, X. Kong,
Prof. Tervoort and J. Eijnden
Courtesy, S. Otten and J. Eijnden
subscale stress-managed
common coil 1
subscale stress-managed
common coil 2 - ESC
Stress-managed asymmetric
common coil 1 – SMACC1
Courtesy, R. Gupta
BigBOX2: Stress-Managed
Coil Demonstrator Under
High-Magnet Field

## Slide 3
CHART2 Stress-Management R&D
Composite
Characterization
and Modeling
Powered Samples
Coil Demonstrator
Subscale Magnets
Intermediate Field
Demonstrator
Courtesy, X. Kong and
J. Eijnden
Courtesy, S. Otten and J. Eijnden
subscale stress-managed
common coil 1
subscale stress-managed
common coil 2 - ESC
Stress-managed asymmetric
common coil 1 – SMACC1
Courtesy, R. Gupta
BigBOX2: Stress-Managed
Coil Demonstrator Under
High-Magnet Field

## Slide 4
CHART2 Stress-Management R&D
Composite
Characterization
and Modeling
Powered Samples
Coil Demonstrator
Subscale Magnets
Intermediate Field
Demonstrator
Courtesy, X. Kong and
J. Eijnden
Courtesy, S. Otten and J. Eijnden
subscale stress-managed
common coil 1
subscale stress-managed
common coil 2 - ESC
Stress-managed asymmetric
common coil 1 – SMACC1
Courtesy, R. Gupta
BigBOX2: Stress-Managed
Coil Demonstrator Under
High-Magnet Field
This Presentation

## Slide 5
Agenda
Stress-managed coil demonstrator under high-magnet field (BigBOX2)
Subscale Stress-Managed Common Coil Magnet (subscale SMCC1)
Validation of ESC protection system (subscale SMCC2)
Stress-Managed Asymmetric Common Coil Magnet (SMACC1)
Outlook for CHART2 2025 developments and tests

## Slide 6: BigBOX: Stress-Managed Coil Demonstrator Under High-Magnet Field
Assessing coil performance: Nb3Sn degradation, load line fraction and coil training behavior
Validating technologies: pre-load free coil, interface conditions, impregnation systems, stress-managed structure and ceramic insulation coating
DCC17 Magnet
BigBOX and DCC17
Stress-Managed Coil and DCC Integration designed and manufactured at PSI
Testing campaign
Cable manufactured at LBNL

## Slide 7: BigBOX1: Manufacturing Steps and Results
Winding Impregnation (Wax)
Electrical Tests Integration
6 times power-up to short sample limit without training
D. M. Araujo et al., “Assessment of Training Performance, Degradation and Robustness of Paraffin-Wax Impregnated Nb3Sn Demonstrator Under High Magnetic Field,” IEEE Trans. Appl. Supercond., vol. 34, no. 5, pp. 1–8, Aug. 2024, doi: 10.1109/TASC.2024.3368995.
Test Results: courtesy R. Gupta, P. Joshi and M. Kumar

## Slide 8: From BigBOX1 to BigBOX2
Peak field of 12.3 T
Peak of Stress of 170 MPa
BigBOX2: powering in two direction (assessment of degradation) and Impregnation System: filled paraffin Wax comparable to BOX 7 and 8.
BigBOX1: powered in a single direction
Impregnation system: paraffin wax
BigBOX2 was manufactured and delivered to BNL in 2024
BigBOX2 is scheduled to be tested in March 2025

## Slide 10: Subscale Stress-Managed Common Coil Magnet (subscale SMCC1)
Stress-managed common coil concept
Validating manufacturing processes and technologies: re-use of tooling from winding to the final assembly, layer to layer splicing, impregnation system, ceramic coating
Outer
pad
Inner
pad
End
plate
Rods
Coils
Magnet Concept, design and manufacturing by PSI
Heat Treatment of 2 of 4 coils and testing campaign
Cable manufactured at LBNL

## Slide 11: Subscale Stress-Managed Common Coil Magnet (subscale SMCC1)
Stress-managed coil: Nb3Sn manufacturing steps
D. Araujo et al., “Subscale Stress-Managed Common Coil Design,” IEEE Transactions on Applied Superconductivity, vol. 34, no. 5, pp. 1–5, Aug. 2024, doi: 10.1109/TASC.2024.3360220.

## Slide 12: Subscale Stress-Managed Common Coil Magnet (subscale SMCC1)
Test Results courtesy G. Willering, et al.
D. Araujo et al., “Manufacturing and Testing of the First Nb3Sn Subscale Stress-Managed Common Coil: 2-in-1 Dipole Magnet Developed at the Paul Scherrer Intitute,” IEEE Transactions on Applied Superconductivity, 2025.
Test campaign started in May 2024

## Slide 14: Validation of ESC protection system (subscale SMCC2)
Copper coils winding trials
Blank assembly of subscale SMCC2
Subscale SMCC1
4 x stress-managed Nb3Sn coils
Energy Extraction
Subscale SMCC2
+ 4 x stress-managed Cu coils
Energy Shift Coupling (ESC)
E. Ravaioli, A. Verweij, and M. Wozniak, “Energy shift with coupling (ESC): a new quench protection method,” Supercond. Sci. Technol., Jan. 2025, doi: 10.1088/1361-6668/ada833.

## Slide 16: Stress-Managed Asymmetric Common Coil Magnet (SMACC1)
Asymmetric Common Coil concept
D. Araujo et al., “Electromechanical Design of Nb3Sn Stress-Managed Asymmetric Common-Coils,” IEEE Transactions on Applied Superconductivity, 2025.
Common-coils
Double
pancake
racetracks
Apertures
Combined with stress-managed common coil concept

## Slide 17: Cable, Magnet Parameters and Cross-section
Dext shell = 740 mm
Shell thickness = 35 mm
Cooling channels and rod holes d = 40 mm
Horizontal pad and non-magnetic pole
iron pole and yoke
Shell, keys and coil formers
Outer vertical pad
Type | High-Field | Low-Field
Wire type | Nb3Sn RRP® 162/169 | Nb3Sn RRP® 78/91
CERN Wire Denomination | DEM-1.1 | ERMC-0.7
N wire x dia in mm | 21 x 1.1 | 34 x 0.7
Cu/nCu | 0.9 | 1.2
Bare Cable dimensions in mm | 12.74 x 2.06 | 12.74 x 1.31
Insulation thickness in mm | 0.155 | 0.155
Length Availability | - | 400 m
Cable Originally Designed for | R2D2 | -
Design based on existent cable
B0 in T | Bpeak in T | Top in K | % Margin | Iop in kA
12.0 | 12.6 (+5%) | 1.9 | 24.1 | 12.9
13.0 | 13.7 | 1.9 | 17.1 | 14.1
14.0 | 14.7 | 1.9 | 10.0 | 15.3
15.4 | 16.2 | 1.9 | 0 | 17.0
List of parameters provided in the annex
Field quality: -10 to + 15 units on the cross-section from 1 to 12 T

## Slide 18: Stress-Managed Asymmetric Common Coil Magnet (SMACC1)
Progress on the engineering design, courtesy T. Michlmayr

## Slide 19: Stress-Managed Asymmetric Common Coil Magnet (SMACC1)
keys
bladder
& support plates
Nb3Sn – ReBCO tapes Splices trials, cold measurements performed at PSI
Design and Tests of SMACC1 bladders at PSI
Strain-gauges validation on the subscale SMCC1 magnet. Trials, validation through thermal cycles and measurements during the test campaign at CERN performed by PSI
SMACC1 Winding trials
Progress on R&D: A. Stampfli, C. Müller, T. Michlmayr, A. Brem and D. Araujo
+ Impregnation Trials
+ Electrical Integrity Studies
+ …

## Slide 21: Outlook for CHART2 2025 Developments and Tests
Test and analysis of BigBOX2 (in collaboration with BNL/US-MDP)
Complete the manufacturing of 4 subscale SMCC copper coils and assembly of subscale SMCC2
Subscale SMCC2 test at CERN
SMACC1 Engineering Design (conceptual design review took place in January 2025)
Manufacturing of SMACC1 Coils

## Slide 23
CHART2 Stress-Management R&D
Composite
Characterization
and Modeling
Powered Samples
Coil Demonstrator
Subscale Magnets
Intermediate Field
Demonstrator
Courtesy, X. Kong and
J. Eijnden
Courtesy, S. Otten and J. Eijnden
subscale stress-managed
common coil 1
subscale stress-managed
common coil 2 - ESC
Stress-managed asymmetric
common coil 1 – SMACC1
Courtesy, R. Gupta
BigBOX2: Stress-Managed
Coil Demonstrator Under
High-Magnet Field

## Slide 24: SMACC1 2D Magnetic Parameters
SMACC1 2D | Mag length of 1 m | Mag length of 14.3 m |  | High field layers | Low field layers
B0 in T | 12.0 |  | Insulated reacted conductor area in mm2 | 2954 | 4367
Bpeak 12 T in T* it includes the self-field contribution | 12.8 |  | Weq in mm2 | 20.1 | 19.1
I12 T in kA | 12.66 |  | Jsc12 T in A/mm2 | 1205 | 2129
Emag 12 T in M | 1.6 | 22.9 | Jcu 12 T in A/mm2 | 1339 | 1774
L in mH Differential self inductance | 18.6 | 266 | Joverall 12 T in A/mm2 includes insulation | 411 | 603
Loadline margin in % at 1.9 K | 23.1 |  |  |  | 
Fxmag 12 T in MN/m | 8.66 |  |  |  | 
Fymag 12 T in MN/m | 0.56 |  |  |  | 

## Slide 25: Magnet Parameters: number of turns and coil unit length
SMACC1 cross-section
Layers | 1 | 2 | 3/4
Cable Type | High-field | High-field | Low-field
Number of turns | 9 | 39 | 52/52
*Coil unit length in m | ~15 | ~75 | ~95
1 2 3 4
*Computed with a straight section of **446.6 mm
**Max possible straight-section given the cable available.

## Slide 26: Magnet Parameters: Load line and yoke field map

## Slide 27: 3D Magnetic Analysis Field Quality
12-T
2D x 3D