## Slide 1
WP2.1 - Progress on ReBCO Tape Research at KIT
Bernhard Holzapfel, Nadja Bagrets, Ruslan Popov Institute for Technical Physics, Karlsruhe Institute of Technology, HFM annual meeting 2024,
12.02.2025

## Slide 2: Content
WP2.1- R&D on accelerator grade HTS REBCO conductors
Motivation
KC4 Equipment Status
Coated Conductor Depositions and Characterization
Next steps

## Slide 3: REBCO Coated Conductor Application Areas
Fusion
FCL
NMR/MRI
Rotating machines
AC/DC cables
Transformer
FCC
Power Applications
Magnets
Rotating Machines
Notes: Due to their outstanding properties, coated conductors are promising candidates for many application areas: magnets, fusion, accelerator and others, power applications, rotating machines.

## Slide 4: Current Status and Challenges of Coated Conductors
Coated Conductors are available on an industrial scale, but costs remain an issue
Beyond Jc there exist a number of open development areas, which need to be improved (yield, mechanical issues, thin conductors, electromechanical properties of full conductor, ac losses) and combined
Each application requires different and specific CC properties/architectures (e.g. magnetic field, temperature, ac-properties, stabilization, mechanical properties, insulation)
New scientific ideas often require just a few 100 m of very specific CC, not easily available from commercial vendors, since industry needs to focus on just a few CC variants to enable economic production
There exists currently no company independent public research institution in Europe, which is able to bridge the gap between small scale basic materials research on PLD-based CC and larger scale industrial synthesis, being able to deliver 100 m+ class, tailored, high quality Coated Conductors on demand

## Slide 5: KC4: KIT-CERN Collaboration on Coated Conductor
Both power applications as well as magnet applications are targeted
Focus on R&D CC issues, not on low cost CC production
KC4 is part of the Helmholtz R&D Programm „Materials and Technologies for the Energy Transition“ at KIT
KC4 is part of the High Field Accelerator Magnets R&D Programm at CERN
Third party R&D projects towards tailored CC synthesis for specific applications will be become possible based on an HTS CC open foundry concept
Long length filamentization and ROEBEL cable fabrication will be feasible
KIT and CERN established a joint, open HTS CC synthesis Lab, which will bridge the gap between small scale materials research on CC and larger scale component requirement of tailored, high quality full Coated Conductor architectures in sufficiently long length

## Slide 6: Timeline of KIT-CERN Collaboration
Baseline R&D Operation (< 25% capacity use)
KIT/ITEP
CERN
CERN
Tailored R&D and demonstration operation
KIT/ITEP
2022
2023
2024
2027
I-A Installation
I-B Commissioning
I-C Performance demonstration
I-D Baseline R&D operation
HTS CC Open Lab/Foundry
Third Parties
KIT ITEP
CERN
t.b.c
Intermediate 20 m length scale
Extension to 100m+ length scale

## Slide 7: KC4: Baseline R&D Topics
Investigate scaling laws to transfer small scale PLD materials development results towards larger scale Coated Conductor production systems
Address specific Coated Conductor architectures needed for the R&D program at CERN and KIT
Investigate and improve electromechanical properties of full coated conductor architectures (mechanical stability, interface resistance, thermal properties,….)
Evaluate in-line quality control systems
Establish accelerated materials development concepts

## Slide 8: KC4 Coated Conductor Synthesis Steps
180µm
A : substrate cleaning/polishing USP/USR-F/USR-B/POL
B : IBAD Buffer deposition ABAD
C : PLD Buffer deposition HEX600+PLD300/600
D : PLD SC deposition HEX600+PLD300/600
E : Ag- coating Tacoma–M/MET-F
F : O2- loading Tacoma-O/BEL-F
G : Cu-plating PLA
e.g. TapeStar
A
B
C
D
E
F
G
b > 12mm (foils)
b < 12mm (tapes)
+ characterization (structural, electrical, mechanical)
(
)

## Slide 9: BRUKER HTS R&D-line equipment Transferred to KIT:
Tape processing equipment with different substrate handling concepts (batch and reel-to-reel R2R processes) including stabilization
PLD600
Batch vacuum coating
PLD600
substrate drum
R2R electroplating
ABAD vacuum coater

## Slide 10: Core KC4 Lab space
Transfered Bruker equipment list
USR-F* substrate cleaning
USP* tape spooling
USR-B* reel-to-reel substrate cleaning
POL* substrate polishing
ABAD IBAD deposition
HEX 600 tape handling
PLD300 PLD
PLD600 long length PLD
Takoma-M Ag-coating
Takoma-O O-loading
MET-F Ag-coating
BEL-F O-loading
PLA* Cu-plating
TapeStar* Jc-characterization
*: equipment located in other ITEP labs
ITEP wide > 500 m2 lab space dedicated to KC4

## Slide 11: Current Project Status (intermediate 20 m length scale)
180µm
Cleaning
ABAD
Buffer
SC
Ag
O
Cu

## Slide 12: Status Deposition Runs
Short length (0,5 m; 0,5, 1, 2 µm) experiments to optimize/check deposition conditions for regular Y123 coatings, and coatings with artificial pinning centres are processing routinely
Intermediate length depositions (15 m) with lateral movement. Good Ic homogeneity over the length is demonstrated
IBAD MgO tapes from Faraday, SUNAM, HTS and Shanghai SC under investigation - LMO and CeO buffer layer termination of IBAD MgO tapes
Establishment of (routine) characterization procedures
  - 77 K, sf full width Ic characterization
  CryoScan homogeneity check
  Tapestar Ic characterization
  Optional mechanical characterization, interlayer resistance measurements
  Optical characterization
  - X-ray characterization (PhD Kai Walter) - fast LT, high field Jc measurement so far missing (request for collaboration)

## Slide 13: Intermediate lengths: Ic homogeneity over the length
Using the transport calibration factor of 1,6 these Ic values correspond to an Ic > 300 A over the first, quite defect free 10 m tape length, and Ic > 240 A for 15 m tape length

## Slide 14: Short samples: Ic for 1-2 m HTS thickness, 12 mm width

## Slide 15
Wider tapes (Joint CERN project „HIGHEST“ - I.FAST Innovative Fund)
30 mm wide IBAD MgO CC
40 mm wide ABAD YSZ CC
4cm tape width
Jc distribution across 4 cm wide CC
Worldwide first realization of 30 and 40 mm wide Coated Conductors within Highest project

## Slide 16: High field, low temperature Jc characterization tests for YBCO and YBCO with BZO
High field, low temperature Jc characterization tests on small patterned bridges for PPMS setup
BZO nanocolumns can pin the vortices along their entire length, therefore, compared to pristine YBCO, 2-3-fold increase in the low-temperature and high-field Jc is achieved for these tapes. This result is in line with best laboratory results worldwide.
Correlation with small scale PLD experiments

## Slide 17
Characterization examples Jc anisotropy characterization for YBCO and BZO doped YBCO
B ‖ c
B ‖ ab

## Slide 18: Interfacial resistance studies
Tape ID | CTL (mm) | Rb (n*cm2)
S2303_016 (variation over the width) | 0,109 0,106 0,108 | 12,45 11,83 12,21
S2401_001 (variation along the length) | 0,090 0,105 | 16,39 22,28
S2401_002 (variation along the length) | 0,113 0,121 0,104 0,111 | 18,93 21,88 15,99 18,47
S2303_019 A | 0,660 | 606
S2303_019 B | 0,185 | 44
KC4 tapes show low variation in CTL and barrier resistance along the length and over the width. Compared to commercial HTS tapes, these parameters are relatively low
Further experiments are running to investigate the influence of humidity and hydrogen on the barrier resistance value

## Slide 19: Mechanical characterization – tensile load
Ic after application of 0.1% tensile strain
Ic-values are measured on two short samples of same tape
Tensile strain of 0.1% applied at 77 K
Samples are cut to remove damage from extensometer tips
Ic-values measurement repeated for shortened samples
Result: Ic change is within 1%: 195.64 A to 194.68 A and 200.62 A to 198.8 A (that can be within measurement uncertainty and scattering along the length)

## Slide 20: Characterization examples – compressive load
I-V curves of the sample S2303-014_1 before and after applying a compressive transversal load of 100 MPA over an area of 180 mm2 at RT
Pressure punch

## Slide 21: Further mechanical characterization steps:
Jc under tensile stress/strain
Tensile machine gripping
Current joints
Voltage contacts
Pressure punch
Current joints
Voltage contacts
Jc under compressive stress
Jc under delaminating stress

## Slide 22: Next steps
Discussion and decision of joint characterization efforts
- required repeat of deposition parameter tests for various buffers, SC stoichiometries
- increasing tape lengths >100 m
- electro-mechanical properties measurements
- achievement RfO for second PLD system PLD300 (The laser system is operational and currently the final steps are under way to finish the commissioning phase)
- further transfer small scale PLD experiments on production of tapes
- investigation of factors influencing intrinsic electrical properties

## Slide 23
KIT KC4 Team

## Slide 24: BRUKER HTS BHTS’s process chain
The standard processing route for the BHTS coated conductors consists of …
  … stainless steel substrate polishing and cleaning
  … YSZ buffer layer coating by vacuum deposition (ABAD)
  … Ceria and YBCO layer coating by vacuum deposition (PLD)
  … Ag shunt layer coating by vacuum deposition (evaporation) and Ag layer annealing in O2 atmosphere
  … Cu encapsulation by plating
  … final inspection and quality check of the HTS tapes
180µm
Typical HTS layer stack
Idealized sketch of the BHTS process chain

## Slide 25
Critical Current Density characterization at low T, high field
Ic-measurements at low temperatures and high fields were performed at CERN by Aisha Saba and Giovanni Succi on 4 mm wide tapes which were laser cut at KIT.
the IV-curves of the sample at 10 T for different contacted tape areas
The Ic value for the relevant BIIc sample is 170 A, which corresponds to an engineering critical current density of JE = 850 A/mm2, which meets the deliverable threshold.
The measured field dependence of Ic at 4,2 K
Ic value >1000 A at zero field, and engineering critical current density of 937 A/mm2 at 10 T and 4 K
B ‖ c
B ‖ c