## Slide 1
Anna Kario1, Herman ten Kate1, Simon Otten1, Jorick Leferink1, Sander Wessel1, Cansu Topaloglu1, Mark Smithers1, Mohammed Abdul Rasheed1, Melissa Goodwin1, Daniel Davis2, David Larbalestier2, Ulf Trociewitz2, Tengming Shen3, Amalia Ballarino4, 1 University of Twente, 2 NHFML, 3 LBNL, 4 CERN
Critical Current Reduction by Transverse Pressure in Bi-2212 Rutherford cables up to 300 MPa at 11 T / 4.2 K

## Slide 2: Motivation: Transverse Stress in dipole magnets
80 to 110 MPa level azimuthal stress expected in Bi-2212 based dipole magnet designs
Apart from one early date test (2000), there were no recent test data existing on cables
Experimental data on stress limits for recent Bi-2212 cables are needed.
Zlobin et al. (2023) https://doi.org/10.1109/TASC.2023.3264165
Zlobin et al. (2022) https://doi.org/10.1109/TASC.2022.3158635
104 MPa peak stress
80 MPa peak stress
96 MPa peak stress
Garcia Fajardo et al. (2022) https://doi.org/10.1109/TASC.2023.3264788
Results are also highly relevant for high-field solenoids under high radial compressive load!

## Slide 3
Wire and Cable properties of the 4 samples
0.8 mm
Wire layout
Bi-2212 in Ag matrix
0.8 mm diameter
55 x 18 filaments
Image by Zhang et al. (2018)
Rutherford cable
17 strands
58 mm twist pitch
Size 7.8 mm x 1.4 mm
Mullite or alumina sleeve
LBNL1109
No. | sample | powder | insulation
1 | LBNL1109 | Engi-mat LXB103 | Mullite sleeve
2 | LBNL2002 | Engi-mat LXB156 | Mullite sleeve
3 | LBNL1109 | Engi-mat LXB103 | Nextel pure alumina
4 | LBNL2002 | Engi-mat LXB156 | Nextel pure alumina
Image by Zhang et al. (2018)

## Slide 4
Heat treatment in furnace at NHMFL
U-shape for press experiment
OPHT at 50 bar in 1 bar oxygen
~890°C at melting
Vacuum impregnation at UT
CTD-101K at 60°C at 0.7 mbar
Cured for 5 hour at 110°C and 16 hour at 125°C
Flat surface
condition achieved
allowing even transverse pressure.
Sample heat treatment and impregnation
45 mm
M Matras 2016, PhD thesis

## Slide 5
Transverse Pressure Facility
Cable sample in U-shape
Pressure on ≈ 45 mm straight cable section
Impregnated surface of the sample
Current supplied by 50 kA sc. transformer
Background field by 11 T solenoid magnet
Pressure of up to 250 kN generated by a set of repulsing coils
Allowing stress levels up to 300 MPa
In 4.2 K boiling helium bath
Accuracies: ΔIc/Ic ≈ ±1% & Δσt/σt ≈ ±4%.
50 kA transformer
Sample holder
11 T solenoid
Press coils

## Slide 6
Virgin cable Ic(Ba) - Curves of all 4 samples
At 11 T /4.2 K and 10 MPa transverse stress: Ic ranges 1500 to 5000 A and n from 9 to 17
Same results expected but, a significant difference between the samples in both Ic and n!
Cable 1
Cable 2
Cable 3
Cable 4
Cable 1
Cable 2
Cable 3
Cable 4

## Slide 7
Why ? Comparison to witness strands
Note: witness strands and cables are not from the same powder/wire batches
Witness strands of samples 2 and 3 reached about expected performance (900 to 1000 A/mm2 at 5T/4.2K)
Witness strands of cables 1 and 4 show roughly half this performance
Whole wire/cable critical current densities at 4.2 K and 5 T applied field
Ic of witness strands and cable samples clearly correlate, strongly pointing at the powder/wire batch/heat treatment conditions as the cause….
Cable 1
Cable 2
Cable 3
Cable 4

## Slide 8
Sample 2
T = 4.2 K
Ba = 11 T
Critical current vs. transverse stress
Transverse stress test: No reversibility seen!
Measurement sequence:
  10 MPa - 20 MPa
  10 MPa - 30 MPa
  10 MPa - 40 MPa
  etc.
Example Sample 2, representative for ALL samples measured.
Main observation:
Loaded curve = unloaded curve (within fraction of systematic measurement error)
There is NO significant reversible effect observed in any sample!
Meaning: Ic reduction through Bc2 suppression due to lattice deformation is not visible, not significant.

## Slide 9
Transverse stress test: Ic (P) or I/Ic(P)
Samples 3,4,6 reach 5% degradation above 130 MPa; Sample 5 at 80 MPa, but highest Ic !!
For a magnet with <150 MPa, cable 5 is the best conductor, even when degrading faster!
Just considering I/Ic is misleading.
Critical current vs. transverse stress
Normalized critical currents
Cable 1
Cable 2
Cable 3
Cable 4
95%
Cable 1
Cable 2
Cable 3
Cable 4

## Slide 10
Microstructure: flavor of defects
10
Here and there broken filaments, heavily distorted shape; not enough for 40 - 60% degradation.
Sample-1 200 MPa 92%
Sample-3 250 MPa 56%
Sample-2 300 MPa 40%
Tomography of cable at ¾ wire height.
Long voids inside, along the wire.
Sample-2

## Slide 11
Conclusion
Unique transverse pressure data on 4 Bi-2212 cable samples up to 300 MPa
Factor 3 difference found in cable critical currents (likely caused by differences in powder and wire batches, cabling, heat treatment)
5% degradation level is at 80 (high-Ic cable) to 200 MPa (lower-Ic cable).
Only 1 to 5% Ic reduction, and saturating, observed in all samples when cycling between 10 and 200 MPa and up to 200 cycles (good).
Contrary to Nb3Sn, in Bi-2212 all changes in critical current are irreversible!
No cause for large degradation found in the microstructure at filament level.