## Slide 1: Demonstrator of metal-insulated REBCO high field magnet coils
CEA-CERN HFM collaboration W2-11 agreement on HTS MI racetracks developments
Thibault Lécrevisse (CEA) on behalf of CEA team
Amalia Ballarino (CERN)
T. Lécrevisse
C. Genot
E. Benoist
G. Lenoir
A. Blondelle
A. Caunes
E. Pepinter
T. Barabe
B. Maloeuvre
S. Somson
M. Durochat

## Slide 2: 1. Agreement Status : Development main phases
KE5647
Start: 01/04/2023
End: 31/03/2025
31/05/2025
Phase 3:
« EuCARD v3 »
MI cold bore 14 T+ magnet
Phase 2:
« EuCARD v2 »
Magnet MI 14 T+
Phase 1:
Racetrack MI (2-5 T)
(Ongoing activity at Irfu)
140 mm
600 mm
Metal Insulated for :
Costs / risks reduction
Conductor and design limit exploration
Compact 14 T+ REBCO mock-ups

## Slide 3: 1. Agreement Status : Phase 1 axes
Modeling
PEEC-R
3D FEM
R&D / Characterization
Electrical connections
Radial thermal conductivity
MI Racetrack fabrication, assembly and tests
Winding & assembly
Test and analysis

## Slide 4: 2. Mechanical structure
Cooling
&
Current leads
Electrical
connections : Copper-Copper with Indium
140 mm mechanical structure
G10 Insulation

## Slide 5: 2. Fabrication and short Racetracks assembly first tests
Single MI racetrack (RT)
Racetracks fabrication
Inner / outer copper rings
8 MI racetracks fabricated  3 used (RT 5, 7, 8)
Double Racetracks stack (DRT 78)
DRT mechanical structure
Double Racetracks assembly
3 Cernox
Text
Tmid
Tint
1 Arepoc Hall probe
VTs

## Slide 6: 2. Two DRT tested at 77 K and 4.2 K
Racetrack #7
Racetrack #8
damaged
DRT78 (quench simulation benchmark)
Ic, tape (77 K, s.f.) = 199 A
133 turns
Ic, tape (77 K, s.f.) = 229 A
134 turns
Shanghai Superconductor Technology (SST), 4 mm wide and 74-78 µm thick
Co-winding of :1 REBCO tape with a 30 µm thick Durnomag®
53 m of single 4 mm tape per Racetrack
Racetrack #7
Racetrack #5
DRT75 (performance benchmark)
Ic, tape (77 K, s.f.) = 229 A
134 turns
Ic, tape (77 K, s.f.) = 278 A
137 turns
First tested assembly :
RT8 voluntary degraded by local heating during fabrication
6 Quenches
Second tested assembly :
Bottom RT7 from DRT78 assembly
8 Quenches
REBCO tape provided and characterized by CERN

## Slide 7: 2. DRT75 magnetic design
Loadline estimation with Gui-RAT @ 670 A
RT 7
RT 5
With redistribution
W/o redistribution
RT 7
RT 5
Bpeak @ 670 A : 8.2 T
Bcenter @ 670 A : 3.6 T
Est. Current limit around 980 -1460 A (RT7)

## Slide 8: 2. DRT75 tests
Self-Field Double Racetracks Tests
77 K Saclay
4.2 K Grenoble (Institut Néel)
04-14/11/2024
Current limitation
Magnetic Field generation
Protection
Next slides will focus on :

## Slide 9: 2. DRT75 tests : Quench and current limitation
DRT75 : test example
Quench protection by Power Supply voltage limitation (0.9 V)
Quench #1
Pre-quench
Quench : voltage grow
Voltage limitation : current decay
Quench
#1
Quench
#2
Quench
#3
Reached 2.7 T @ 670 A
8 quenches @ > 1600 A/mm² (in the winding pack)
Lower magnetic field (< 3.6 T) and quench current (< 980-1460 A)

## Slide 10: 2. DRT75 tests : Magnetic Field generation
DRT75 : Magnetic induction non linearity
Good
Issue
About 650 mT missing @ 500 A (23.5%)
About 980 mT missing @ 670 A (26.7%)
Cannot explain the difference
Quench #2
 WHY ?
MI  bypassing current ?
 Only about 15 mT (5 A/s) and 30 mT (10 A/s)
 Field decay blow 1 mT @100 mV (quench)
1
2
3
Magnetization ?
 Only a few mT

## Slide 11: 2. DRT75 tests : Hall probe issue
Arepoc Hall probe issue ?  comparison of AREPOC 2258 with an AREPOC 2256 and AST 244T @77 K
New campaign with few calibrated sensors (remaining Arepoc and new AST 244T) (Planned week 10-2025)
  Arepoc 2558 sensor got broken during transfer to a different setup  no correlation above 0.3 T available
3rd charging
No difference between sensors
Linear coefficient adjusted
AREPOC 2258 diverged from other sensors
RT7 test at 77 K, SF

## Slide 12: 2. DRT75 tests : Quench current / protection
Quench and protection ?
RT5
Locally burned parts
Post mortem analysis ongoing (Metallography, Tomography X)
Origins ?
Magnetization or/and mechanics ?  (in winding pack) but locally ?
Poor cooling (G10 contact) ?
J/Jc
A-formulation 2D model : 2 Racetracks / 130 turns / 25 elements in width / 3 µm HTS layer / 670 A in 10 s
Magnetization and mechanical effect study ongoing
8 quenches at almost the same current (670 A / 1600 A/mm²)
Only 48-65 % of expected current
Localized burned parts in mid-plane for both RT

## Slide 13: 2. Exploring « long » racetracks
*Dummy Accelerator Racetrack for Development
Target 600 mm long straight part (possibilities up to 900 mm with winding machine)
600 mm DARD* winding
Ongoing (started 17/01/2025)
140 mm RT5
DARD1
DARD2
Expected Week 7-8
600 mm structure

## Slide 14: 3. Conclusion
Short MI Racetrack : a nice way for learning
  Fabrication
  DRT assembly
  Tests setup
  High Je quench protection (>1600 A/mm²)
  Magnetic field generation to confirm (2.7 T or 3.6 T ?)
  Current limitation to understand
What next (S1 2025) ?
New run of RT and DRT measurement @4.2 K
 Comparison with numerical models
“long” MI Racetrack
  600 mm dummy copper MI Racetracks
What next ?
SC “long” Racetrack fabrication
RT tests at 77 K
DRT assembly and test at 77 K
DRT transfer to CERN (May 2025)

## Slide 15: Thank you for your attention
T. Lécrevisse : thibault.lecrevisse@cea.fr
12/02/2025
15
Any questions

## Slide 16: 2. Activities overview : Integrated electrical connection
Integrated electrical connections
Pressed
contact
Integrated current leads
Copper Ring : Bulk or soldered tape
Copper – Copper with or w/o Indium
With or w/o graphene
Effect of pressure
Effect of copper roughness
Mechanical cycles
Thermal cycles (77 K)
Optimize the contact resistance and evaluate the required contact area for each application
For now about 0.8 µΩ.cm² with Indium w/o graphene
   200 nΩ on our samples
4 copper rings stacked together with Vtap to evaluate its resistivity
Test of evolution of contact resistivity in compressive testing machine @77 K
Current leads
Compressive plate
Sample