## Slide 1
This work was performed under the auspices of and with support from the Swiss Accelerator Research and Technology (CHART) program, http://chart.ch.
Towards REBCO HFMs
at PSI/CHART
D. Araujo, B. Auchmann, A. Brem, M. Duda, J. Kosse, C. Lindner, T. Michlmayr, H. Rodrigues, D. Sotnikov, A. Stampfli
HFM Annual Meeting, CERN, 10-12 February, 2025
HFM
High Field Magnets
Programme

## Slide 2: Contents: Setup and Initial Canvassing at PSI

## Slide 3
Setup

## Slide 4: Infrastructure
Coating line.
Flat-coil winding table, two spools.
Cryogen-free test station up to 2 kA
Winding table for non-planar coils.

## Slide 5: NI Coils
inside
Courtesy: H. Garcia Rodigues, J. Kosse, M. Duda
May 2022

## Slide 6
15 T in 72 mm warm bore
15 K conduction-cooling
Solid-state (Pb) thermal buffer
5 coils from 12 mm ReBCO, 110 mm ID 21 T peak field
target
HTS no-insulation positron-capture solenoid, to demonstrate positron source with 10x increased yield wrt. state of the art. Manufacturing/commissioning in 2024/25. Experiment at PSI’s SwissFEL 2025/26
Synergies: FCCee Injector Study: P3 experiment (PSI Positron Production)
Coil technology licensed from
Courtesy: M. Duda, H. Garcia Rodigues, J. Kosse, T. Michlmayr
https://iopscience.iop.org/article/10.1088/1361-6668/ada9d3/pdf

## Slide 7: BabyHTS: AC loss model-validation coils
Courtesy: Dmitry Sotnikov
Coil name | Cable | Inner diameter, Twisting, mm | Inner diameter, Former, mm | Outer diameter, limit, mm | Insulation between windings, mm
blueBerry | 4 mm single tape | 17 | 20 | 30 | 0.6
greyBerry4d | 4 mm soldered 2-stack | 17 | 20 | 40 | 0.6
greyBerry12 | 12 mm single tape | 57 | 60 | 70 | 0.6
Paper insulation → double pancake start → winding → v-taps → leads
✘
✔︎
✔︎

## Slide 8: BabyHTS: AC loss model-validation coils
Courtesy: Anna Kario, Simon Otten and Thomas Hanhart
AC loss measurements at University of Twente via amplitude and phase shift measurement with two lock-in amplifiers.
Applied current is AC with frequency from 0.1 Hz to 20 Hz, with amplitudes up to 100 A.
greyBerry4d
Tape: 4mm
Turns: 20
P_max = 0.28W
greyBerry12
Tape: 2x12mm
Turns: 14
P_max = 0.73W

## Slide 9: BabyHTS: AC loss model-validation coils
Courtesy: Simon Otten and Thomas Hanhart
Critical current measurement done on both pancakes separately.
Matches Robinson database with factor 0.8: 150 A for measurement and 145 A for model.
Measured in University of Twente
Critical current validation in FEM

## Slide 10: BabyHTS: AC loss model-validation coils
Courtesy: Simon Otten, Thomas Hanhart and Dmitry Sotnikov
Numerical models resolve the REBCO layer and homogenized the other metal layers (Hastelloy, silver, copper).
Agreement to measurements is good for 4-mm 2-stack and 12-mm 1-stackcable.
Note: fully homogenized model inaccurate and divergent.

## Slide 11: HTS Modeling WG Benchmark
ROXIE  COMSOL , Quanscient, Racoon (LBE)
Qualify models and tools with the HFM HTS Modeling WG
All based on homogenization per tape stack.
Results by: J. van Nugteren, S. Sorti, and D. Sotnikov
11.02.25
Paul Scherrer Institute PSI
11
Screening-current and -loss calculation
Screening current density [A/m2]
Power density [W/m, integrated over cable x-sec]
ROXIE

## Slide 12
Initial Canvassing

## Slide 13: First Goal: HTS subscale
Re-use subSMCC coil design and structure for REBCO magnet (6-8 tapes).
SMCC magnet with apertures for field quality measurements.
  Accuracy, stability, reproducibility
Experimental and numerical protection studies
  EE, CLIQ, ESC
Protection study under way to determine cable layout
Coil manufacturing in Q2’25.
Nb3Sn subSMCC

## Slide 14: Towards winding, insulating, and soldering a tape-stack cable.
Soldered REBCO insulated tapes-stack cable.
  multiple soldered 2-stacks from FFJ, soldered together in-winding with pressure and heat source (induction, hot-air blower), tbd.
  Fall-back: dry stack of soldered 2-stacks.
Courtesy: Christian Lindner

## Slide 15: Towards winding, insulating, and soldering a tape-stack cable.
Soldered REBCO insulated tapes-stack cable.
  multiple soldered 2-stacks from FFJ, soldered together in-winding with pressure and heat source (induction, hot-air blower), tbd.
  Fall-back: dry stack of soldered 2-stacks.
Courtesy: Christian Lindner

## Slide 16: REBCO Block-Coil Dipole Scaling Exercise
As expected, AC losses grow non-linearly with field due to larger field sweep and growth in coil-size.
In this study (for which all previous caveats and assumptions apply) AC losses increase 4-fold from 14 to 20 T.
Initial results indicate that losses decrease mildly towards lower temperatures.

## Slide 17: ReBCO FCC-hh Dipole Scaling Exercise
Analogue study for scaling with temperature (5-30 K) for constant 14 T bore field indicates weak scaling of AC losses, notable cost increase.

## Slide 18: Conclusion
PSI has entered the canvassing phase, attempting to implement soldered tape-stack cables in a stress-managed structure to address questions of mechanics and reproducibility.
Numerical tools are being developed and need validation.
Canvassing efforts need to be accompanied by model-based extrapolations to full scope of HFM HTS goals.