## Slide 2
KEK Progress on
Nb3Sn conductors
Michinaka SUGANO
KEK
On behalf of Japanese and CERN collaborators

## Slide 3: Outline
Collaborative work between KEK and CERN on the development of Nb3Sn conductor aiming for higher Jc (1st phase)
New collaborative work on the development of high performance Nb3Sn conductor (2nd phase)
  Research structure
  Tasks for KEK
  Approaches to achieve the tasks
  Current status

## Slide 4
Achievements in the collaborative work in the 1st phase

## Slide 5: 1st phase of Nb3Sn conductor development program
KEK and CERN signed the MoU regarding the collaborative work on high performance Nb3Sn wires for FCC in 2016.
This 1st phase of R&D program lasted until 2022.
Two Japanese wire manufacturers, JASTEC and Furukawa Electric, joined the program.
JASTEC selected Distributed-Tin (DT) process, while Furukawa Electric chose Nb-tube process.

## Slide 6: Target specifications for the 1st phase
Improvement in non-Cu Jc towards 1500 A/mm2 at 4.2 K, 16 T was prioritized.
The interim target was set to be 1000 A/mm2 at 4.2 K, 16 T.
Parameter | Ultimate target | Stage 1 | Stage 2
Wire diameter (mm) | ~1 | ~1 | ~1
Cu/non-Cu ratio | ~1 | ~1 | ~1
Non-Cu Jc (4.2 K, 16 T) (A /mm2) | ≥ 1500 | ≥ 1000; aim 1200 | ≥ 1500
µ0ΔM (1 T, 4.2 K) (mT) | ≤ 150 |  | 
deff (µm) | ≤ 20 | ≤ 60 | ≤ 60
RRR | ≥ 150 | ≥ 150 | ≥ 150
Unit lengths / km | ≥ 5 |  | 
Cost | 5 EUR / kA m |  | 

## Slide 7: DT wires developed by JASTEC
Multi Nb module (pure Nb)
Mono core of Sn (Sn-Ti alloy)
Nb common barrier
Cu stabilizer outside the barrier
Cross-section of DT wire (before Heat treatment)
Nb
Nb
Sn
Sn
Φ1.0 mm
Improvement in Sn diffusion
Ternary additive elements
Strategies for higher Jc

## Slide 8: Shortening the Sn diffusion distance
A reduction in the Sn diffusion distance improves
non-Cu Jc by 28% (1025 A/mm2 at 4.2 K, 16 T).
Magnetic field (T)
SEM images of A15 area far from Sn core in longer and shorter Sn diffusion distances.
Shorter Sn diffusion distance
Longer Sn diffusion distance
4.2K, Ec=0.1µV/cm
Sample A
Sample C
Sn diffusion distance (Ld) was reduced by drawing down the f0.8 wire
Ld
Ld
Ld
14
15
16
17
18
19
20

## Slide 9: Ternary additive element
Controlling Ti content in Sn core leads to an improvement in Jc at 16 T.
Magnetic field (T)
4.2K, Ec=0.1µV/cm
non-Cu Jc =
1137 A/mm2 at 16T
Ld=48 mm
Ld=32 mm
Sn diffusion
distance
R. Flükiger, Cryogenics 48 (2008) 293-307
0.55wt%
0.44wt%
0.38wt%
Ti content: C > D > E
Ti content in matrix
14
15
16
17
18
19

## Slide 10: The highest non-Cu Jc in DT wires in the 1st phase
Non-Cu Jc of 1100 A/mm2 at 4.2 K, 16 T was achieved in Trial 3 wires, exceeding the interim target of 1000 A/mm2.
 | T1-A | T1-B | T1-C | T3-A | T3-B
Wire diameter (mm) | 0.80 | 0.74 | 0.64 | 0.80 | 0.80
Sn diffusion distance (µm) | 60 | 58 | 48 | 32 | 32
Ti ratio (wt%) | 0.55 | 0.55 | 0.55 | 0.48 | 0.35
Non Cu JC ( A/mm2 )@16T | 800 | 930 | 1025 | 1137 | 1032
1.4 times higher
before this R&D
Magnetic field (T)
14
15
16
17
18
19
non-Cu Jc (A/mm2)

## Slide 11: Effective filament diameter (deff)
Significant flux jump in the initial wire (Trial 1) was strongly suppressed in Trial 3 with high non-Cu Jc.
The calculated deff was ~55 mm corresponding to two modules.
 The interim target of deff ≤ 60 μm was confirmed to be satisfied.
• The magnetization curves were measured at CERN to evaluate the effective
filament diameter.
Trial 1
Trial 3A
 | Trial 1 | Trial 3A
Diameter (mm) | 0.7 | 0.8
deff (µm) | 267 | 54.5
non-Cu Jc (A/mm2) | 930 | 1137
0.8 mm
Magnetization curves
Single
module

## Slide 12: Tolerance against transverse stress of Trial 3 wires
Irreversible Ic degradation starts at around 150 MPa
 Promising stress tolerance
Origin of Ic change
  Mode II: Plastic deformation of the metal matrix
  Mode III: Crack propagation across the wire
Transverse
compression
Normalized critical current
Transverse compressive stress (MPa)
Irreversible Ic degradation
Mode II
Mode III
M. Nakamoto, M. Sugano, IEEE TAS (2023).

## Slide 13
New collaborative work to develop the high performance Nb3Sn wires
(2nd phase)

## Slide 14: 2nd phase of Nb3Sn conductor development program
KEK and CERN signed the MoU (KE6084) to start new collaborative work over three years since August 2024.
HFM WP1.15 – KEK collaboration for development of advanced high-field Nb3Sn conductor
Contact person
  CERN: Thierry Boutboul
  KEK: Michinaka Sugano

## Slide 15: Structure
CERN
T. Boutboul
S. Hopkins
A. Devred
KEK
M. Sugano
T. Ogitsu
JASTEC
Furukawa
Electric
NIMS
N. Banno
Tohoku Univ.
S. Awaji
• Discussion of specs
• Order of fabrication
of trial wires
• Directing R&D
• Characterization
• Technical
suggestion
• In-depth
characterization
Consultation
Consultation
Fundamental
R&D
Technical
discussion
Mini-workshop
held in Oct, 2024

## Slide 16: Tasks for KEK
There are three main tasks for KEK.
  Task 1: Industrialization of Distributed-Tin (DT) Nb3Sn wires
  Task 2: Reinforcement of Nb3Sn wire
  Task 3: Enhancement of the Jc of Nb3Sn wire
Task 1 has the highest priority.

## Slide 17: Task 1: Industrialization of Distributed-Tin (DT) Nb3Sn wires
JASTEC DT wire with non-Cu Jc > 1100 A/mm2 (4.2 K, 16 T) had a workability issue. The most important item to realize is production with a longer piece length of this wire.
Targets for Task 1 (2024 Aug – 2026 Aug)
  non-Cu Jc(4.2 K, 16 T) > 1100 A/mm2
  Wire diameter=0.85 mm
  Cu/non-Cu ratio > 1.1
  Effective filament diameter < 50 mm
  RRR after the wire reaction > 150
  The target piece length > 250 m

## Slide 18: Approaches to Task 1
Strategies to improve in the workability of JASTEC DT wire
  Controlling the hardness of Nb modules
    Heat treatment of multifilamentary Nb wires before assembling with Sn cores
    Comparison between Nb raw materials from different suppliers
  Enhancing the hardness of Sn alloy
  DT wires with Cu-Zn matrix

## Slide 19: Task 2: Reinforcement of Nb3Sn wire
Aiming for mechanical reinforcement against transverse compressive stress
Targets for Task 2 (2024 Aug – 2027 Aug)
  Develop and validate methods to reinforce Nb3Sn wires
  non-Cu Jc(4.2 K, 16 T) > 1000 A/mm2
  Wire diameter=0.85–1.1 mm
  Cu/non-Cu ratio > 1.1
  Effective filament diameter < 50 mm
  RRR after the wire reaction > 150
  The target piece length > 100 m

## Slide 20: Approaches to Task 2
Proof-of-principle for mechanical reinforcement measures
  DT wires with Cu-Zn matrix (JASTEC-NIMS technology)
  Cu-Nb reinforcement (Furukawa-Tohoku Univ. technology)
Banno et al, IEEE TAS 34 (2024) 8400505.
Cu-matrix
Cu-Zn matrix
Cu-Zn matrix DT wire
Cu-Nb reinforcement wire
Cu-Nb reinforce bronze-processed Nb3Sn wire
Cu-Nb reinforced DT wires
Cu-Nb
(reinforcer)

## Slide 21: Task 3: Enhancement of the Jc of Nb3Sn wire
Aiming for improvement in non-Cu Jc towards 1500 A/mm2 at 4.2 K, 16 T
Targets for Task 3 (2024 Aug – 2027 Aug)
  Develop and validate methods to enhance non-Cu Jc of Nb3Sn wires towards 1500 A/mm2 (4.2 K, 16 T)
  The highest achievable Jc
  Wire diameter=0.85–1.1 mm
  Cu/non-Cu ratio > 1.1
  Effective filament diameter < 50 mm
  RRR after the wire reaction > 150
  The target piece length > 100 m

## Slide 22: Approaches to Task 3
Pursuing the possibility of Jc improvement for DT wires with Cu-Zn matrix
Fundamental research to improve Jc in NIMS
  Influence of Ti-doping site
Banno et al, IEEE TAS 30 (2020) 6000705.
Cu-matrix
DT wires
Cu-Zn matrix
DT wires
Ti-doping to Sn or Cu
Ti-doping to Nb
Banno, Superconductivity 6 (0203) 100047.

## Slide 23: Current status
KEK submitted to CERN the plan for Task 1 as Deliverable1.1 in October 2024.
JASTEC started to fabricate trial wires for Task 1. The item to check first is the effect of controlling the hardness of Nb modules for better workability.
KEK just started to discuss the development strategies for Task 2 and 3 with Furukawa Electric.
NIMS is conducting fundamental research for Task 3. The findings will be incorporated into the trial wires which JASTEC will fabricate.

## Slide 24: Conclusions
New collaborative work between KEK and CERN started in August 2024 to develop the advanced high-field Nb3Sn conductors.
Two Japanese wire manufacturers, JASTEC and Furukawa Electric, have joined this program. NIMS and Tohoku Univ. have also participated as academic partners.
The most prioritized task is the industrialization of DT wires. JASTEC has started fabrication of the first trial wires for Task 1.
Plans for the other two main tasks of mechanical reinforcement and improving Jc will also be defined by July 2025. Once the plan is submitted to CERN, fabrication of the trial wires for Task 2 and 3 will be started.