## Slide 1: Composite beam pipes for the FCC
Rodrigo José da Silva (RJS), PhD ORCiD 0000-0001-8016-3165 R&D Engineer at CERN EP-DT
DRD8 collaboration meeting
Supported by
16-20 June 2025
Bristol – UK

## Slide 2: Beam pipe definition
RJS | Composite beam pipes for the FCC
Beam pipe
Supports
End flanges
Joints
Interaction point
DRD8 collaboration meeting
Notes: Let’s start with some outline on why we want to implement CFRP for cryostat.
The main drive is the overall reduction in material budget compared to current aluminium designs, thanks to CFRP higher radiation length (higher particles transparency). From preliminary studies, the reduction can reach up to 60% comparing CFRP against Aluminium sandwich structure cylinders
Not copy of industry
RnD follow existing development and tune/develop adaptable

## Slide 3: General requirements and challenges
ALICE – LS2 Central beam pipe
⌀ 60 mm, Wall thickness 0.8 mm
Beryllium ( ̴ 35 cm radiation length)
Radiation length
Thickness
Stiffness
Secondary or primary vacuum
Energy preserved
Secondary or primary vacuum
Transparency
Buckling resistance
Keep mechanical integrity
Radiation environment
Leak tightness
Permeability
Thickness
Can we consider CFRP pipes?
DRD8 collaboration meeting
RJS | Composite beam pipes for the FCC
Notes: Let’s start with some outline on why we want to implement CFRP for cryostat.
The main drive is the overall reduction in material budget compared to current aluminium designs, thanks to CFRP higher radiation length (higher particles transparency). From preliminary studies, the reduction can reach up to 60% comparing CFRP against Aluminium sandwich structure cylinders
Not copy of industry
RnD follow existing development and tune/develop adaptable

## Slide 4: Non-Evaporable Getter (NEG) and manufacturing viability
Cu/Ni
Be
NEG
CFRP
Transparency: 0.4 mm CFRP (+ 5 µm coating) ≈ 0.8 mm Be
CFRP
DRD8 collaboration meeting
RJS | Composite beam pipes for the FCC
Notes: Let’s start with some outline on why we want to implement CFRP for cryostat.
The main drive is the overall reduction in material budget compared to current aluminium designs, thanks to CFRP higher radiation length (higher particles transparency). From preliminary studies, the reduction can reach up to 60% comparing CFRP against Aluminium sandwich structure cylinders
Not copy of industry
RnD follow existing development and tune/develop adaptable

## Slide 5: Work in progress
Assessing CFRP properties pre and post radiation exposition
Cu/Ni coating deposition on the CFRP pipes (assessing quality)
NEG deposition on the CFRP pipes (assessing quality)
Vacuum testing (leak tightness)
Additional investigation on manufacturing (can we go with even thinner pipes?)
Buckling SF ≈ 17
[90/+30/-30/90]
0.4 mm thickness
DRD8 collaboration meeting
RJS | Composite beam pipes for the FCC
Notes: Let’s start with some outline on why we want to implement CFRP for cryostat.
The main drive is the overall reduction in material budget compared to current aluminium designs, thanks to CFRP higher radiation length (higher particles transparency). From preliminary studies, the reduction can reach up to 60% comparing CFRP against Aluminium sandwich structure cylinders
Not copy of industry
RnD follow existing development and tune/develop adaptable

## Slide 6: To the most critical case: primary vacuum
1st case: CFRP at the interaction point
2nd case: full CFRP (including flanges)
3rd: full CFRP (except at the collision point)
Interaction point
(thinner wall)
DRD8 collaboration meeting
RJS | Composite beam pipes for the FCC
Other sections
(thicker wall)
Notes: Let’s start with some outline on why we want to implement CFRP for cryostat.
The main drive is the overall reduction in material budget compared to current aluminium designs, thanks to CFRP higher radiation length (higher particles transparency). From preliminary studies, the reduction can reach up to 60% comparing CFRP against Aluminium sandwich structure cylinders
Not copy of industry
RnD follow existing development and tune/develop adaptable

## Slide 7: Joints: CFRP - metal
DRD8 collaboration meeting
RJS | Composite beam pipes for the FCC
Notes: Let’s start with some outline on why we want to implement CFRP for cryostat.
The main drive is the overall reduction in material budget compared to current aluminium designs, thanks to CFRP higher radiation length (higher particles transparency). From preliminary studies, the reduction can reach up to 60% comparing CFRP against Aluminium sandwich structure cylinders
Not copy of industry
RnD follow existing development and tune/develop adaptable

## Slide 8: Secondary vacuum: double-wall central chamber (FCC ee)
Vertex detector
Beam pipe
DRD8 collaboration meeting
RJS | Composite beam pipes for the FCC
Notes: Let’s start with some outline on why we want to implement CFRP for cryostat.
The main drive is the overall reduction in material budget compared to current aluminium designs, thanks to CFRP higher radiation length (higher particles transparency). From preliminary studies, the reduction can reach up to 60% comparing CFRP against Aluminium sandwich structure cylinders
Not copy of industry
RnD follow existing development and tune/develop adaptable

## Slide 9: Secondary vacuum: double-wall central chamber (FCC ee)
PARAFFIN
INLET
PARAFFIN
OUTLET
Heat load on central vacuum chamber ̴ 58 W
Double-wall AlBeMet
DRD8 collaboration meeting
RJS | Composite beam pipes for the FCC
Notes: Let’s start with some outline on why we want to implement CFRP for cryostat.
The main drive is the overall reduction in material budget compared to current aluminium designs, thanks to CFRP higher radiation length (higher particles transparency). From preliminary studies, the reduction can reach up to 60% comparing CFRP against Aluminium sandwich structure cylinders
Not copy of industry
RnD follow existing development and tune/develop adaptable

## Slide 10: Secondary vacuum: double-wall central chamber (FCC ee)
External wall:
CFRP candidate
Heat load on central vacuum chamber ̴ 58 W
DRD8 collaboration meeting
RJS | Composite beam pipes for the FCC
Notes: Let’s start with some outline on why we want to implement CFRP for cryostat.
The main drive is the overall reduction in material budget compared to current aluminium designs, thanks to CFRP higher radiation length (higher particles transparency). From preliminary studies, the reduction can reach up to 60% comparing CFRP against Aluminium sandwich structure cylinders
Not copy of industry
RnD follow existing development and tune/develop adaptable

## Slide 11: Secondary vacuum: IRIS
Vertex detector
TRANSLATIONAL MOTION
Retractable Tracker Petals
CFRP candidate
DRD8 collaboration meeting
RJS | Composite beam pipes for the FCC
ROTARY MOTION
Notes: Let’s start with some outline on why we want to implement CFRP for cryostat.
The main drive is the overall reduction in material budget compared to current aluminium designs, thanks to CFRP higher radiation length (higher particles transparency). From preliminary studies, the reduction can reach up to 60% comparing CFRP against Aluminium sandwich structure cylinders
Not copy of industry
RnD follow existing development and tune/develop adaptable

## Slide 12: Questions?
DRD8 collaboration meeting
rjs.phd@cern.ch
RJS | Composite beam pipes for the FCC
Notes: Let’s start with some outline on why we want to implement CFRP for cryostat.
The main drive is the overall reduction in material budget compared to current aluminium designs, thanks to CFRP higher radiation length (higher particles transparency). From preliminary studies, the reduction can reach up to 60% comparing CFRP against Aluminium sandwich structure cylinders
Not copy of industry
RnD follow existing development and tune/develop adaptable