## Slide 1
Summary of measurements after first irradiation of HPK samples
19th RD50 Workshop
21-23 November 2011 CERN
Joachim Erfle
University of Hamburg
On behalf of the CMS Tracker Collaboration
Notes: 1

## Slide 2: Overview
introduction to the HPK-campaign
results of first irradiations
    dark current
    effective doping concentration
    signal collection
conclusions
courtesy of A. Dierlamm, KIT
Notes: 2

## Slide 3: Goals of the HKP-campaign
The main challenges of the HL-LHC will be:
    higher radiation damage
    higher occupancy
therefore we want to find the best suiting material and layout for the coming tracking sensors.
To achieve that we investigate a large variety of materials and structures that are irradiated and measured.
The first step is to check, if at low fluences everything is compatible with available data. After that we will go to higher fluences.

## Slide 4: Wafer overview
structure | to study
diodes | material
baby strip sensor | reference design / material
baby with integrated pitch adapter | design
pixel sensor | reference Design / material
multigeometry pixel | layout parameters
multigeometry strips | layout parameters
baby strixel | design
teststructures | process parameters
Notes: 4

## Slide 5: Material
material | thinning method | active thickness | physical thickness
FZ | deep diffusion | 120,200,300 μm | 320 μm
FZ | --- | 200 μm | 200 μm
FZ | handling wafer | 120 μm | 320 μm
MCz | --- | 200 μm | 200 μm
Epi | handling wafer | 50,100 μm | 320 μm
of each material there are 3 different types:
  n-type (N)
  p-type with p-stop (P)
  p-type with p-spray (Y)

## Slide 6: Material characteristics of thin FZ: deep diffusion
Concentration profile from CV-curve:
front
320-N µm
120-N µm
120-P µm
Diodes behave like parallel-plate capacitors
→ measure capacitance vs voltage to determine depletion depth and charge carrier concentration
Deep diffusion influences effective doping
J. Erfle, UHH
J. Erfle, UHH

## Slide 7: Irradations
neutrons: 1 MeV (TRIGA Reactor Ljubljana)
protons: 25 MeV (Karlsruhe Synchrotron)
radius | protons Φeq [cm-2] | neutrons Φeq [cm-2] | total Φeq [cm-2] | active thickness
40 cm | 3 ∙ 1014 | 4 ∙ 1014 | 7 ∙ 1014 | ≥ 200 μm
20 cm | 1 ∙ 1015 | 5 ∙ 1014 | 1.5 ∙ 1015 | ≥ 200 μm
15 cm | 1.5 ∙ 1015 | 6 ∙ 1014 | 2.1 ∙ 1015 | ≥ 200 μm
10 cm | 3 ∙ 1015 | 7 ∙ 1014 | 3.7 ∙ 1015 | ≤ 200 μm
5 cm | 1.3 ∙ 1016 | 1 ∙ 1015 | 1.4 ∙ 1016 | < 200 μm
courtesy of S. Müller, KIT
HL-LHC: Lint=3000 fb-1

## Slide 8: Volume current versus fluence:
currents match expected value from M.Moll‘s thesis within the uncerntainties.
-> dose measurements are ok.
currents are measured after annealing of 10 min@ 60°C at 0°C and scaled to 20°C
J. Erfle, UHH
neutrons
neutrons
protons
protons

## Slide 9: Volume current versus fluence: Baby sensors
courtesy of A. Nürnberg, KIT
First Baby sensors show higher currents than diodes
-> maybe a surface effect?
currents are measured after annealing of 10 min@ 60°C at -20°C and scaled to 20°C
neutron irradiated Baby sensors

## Slide 10: Annealing behaviour of dark current
measurements are performed at 0°C and scaled to 20°C
the annealing of alpha matches the expected curve from M.Moll‘s thesis.
p@3E14
results for neutron irradiation coming soon
J. Erfle, UHH
80°C

## Slide 11: Neff for different materials / irradiations
n-type
protons
neutrons
capacitances are measured at 0°C, 1KHz after annealing of 10min@60°C
J. Erfle, UHH
J. Erfle, UHH
the FZ and the MCz n-type materials are type-inverted after neutron or proton irradiation.

## Slide 12: Neff for different materials / irradiations
n-type
p-type
protons
neutrons
capacitances are measured at 0°C, 1KHz after annealing of 10min@60°C
J. Erfle, UHH
J. Erfle, UHH
J. Erfle, UHH
J. Erfle, UHH
MCz: lowest increase in Neff.

## Slide 13: Time resolved charge collection measurement with Transient Current Technique (TCT) TCT curves show type inversion
FZ320P
FZ320N
not type inverted
type inverted
unirradiated
p@3E14
courtesy of T. Pöhlsen, UHH
courtesy of T. Pöhlsen, UHH
- holes
- electrons
U=300V
U=600V
courtesy of J. Lange
Laser: 672 nm, red
type inversion of FZ and MCz n-type materials is confirmed by TCT.
capacitances are measured at 0°C, 1KHz after annealing of 10min@60°C

## Slide 14: Annealing beaviour of Neff
Neff changes of FZ320N typical for type inverted material. FZ320P behaviour looks similar but is not type inverted: not completely understood yet.
measurements are performed at 0°C (1KHz)
unirradiated
p@3E14
J. Erfle, UHH
unirradiated
FZ320P
FZ320N
80°C

## Slide 15: Signal of FZ320P baby sensor, after p@3E14
signal induced by a 90Sr source, readout by ALiBaVa
Vdepl
courtesy of K. Hoffman, KIT
CCE of FZ320 p-type is about 87% at p@3E14, compared to non-irradiated
measurements are performed at -20°C

## Slide 16: CCE of diodes, after p@3E14
p-type:
hole
collection
n-type:
electron
collection
infrared laser
red laser, front injection
p-type
n-type
measurements are performed at 0°C and 600V, with 20ns integration time
unirradiated
courtesy of T. Pöhlsen, UHH
courtesy of T. Pöhlsen, UHH
courtesy of J. Lange
infrared laser: CCE is about 90%
electrons only: CCE ~ 85%, holes collection only: CCE ~ 67%

## Slide 17: Conclusions and outlook
CMS silicon measurement campaign is gaining speed, analysis tools are up and running
Trying to understand material properties in detail
Comparison shows currents as expected -> dose measurement ok
Neff compared before and after irradiation
CCE with baby sensors and diodes investigated
More irradiations to come
Full annealing studies to be done
Notes: 17

## Slide 18: Backup

## Slide 19: CCE of FZ320 after proton irradiation
measurements are performed at 0°C
courtesy of T. Pöhlsen

## Slide 20: TCT pulses – p-type
FZ200P
FZ320P
MCZ200P
not type inverted
courtesy of T. Pöhlsen
courtesy of T. Pöhlsen
courtesy of T. Pöhlsen
300V
600V
250V
measurements are performed at 0°C, using a red laser

## Slide 21: TCT pulses – n-type
FZ200N
FZ320N
MCZ200N
type inverted
measurements are performed at 0°C, using a red laser
courtesy of T. Pöhlsen
courtesy of T. Pöhlsen
courtesy of T. Pöhlsen
200V
300V
300V

## Slide 22: Interstrip capacitance on teststructure after neutron and proton irradiation
Interstrip capacitance also is stable
measurements are performed at -20°C, 1MHz
courtesy of M. Bernard-Schwarzz, HEPHY
TS_CAP_AC
low
low
high
courtesy of M. Bernard-Schwarzz, HEPHY
Bias

## Slide 23: Interstrip resistance on teststructure
measurements are performed at -20°C
unirradiated
courtesy of M. Bernard-Schwarzz, HEPHY
GOhm
TS_CAP_DC
interstrip resistance in unirradiated material is pretty good.
courtesy of M. Bernard-Schwarzz, HEPHY
Bias
V

## Slide 24: Strip structures: measurement of basic properties
measurements are performed at -20°C, (1kHz)
courtesy of M. Bernard-Schwarz, HEPHY
material | unirradiated | p@3E14 | n@4E14
aluminum | 22 ± 2 mOhm/sq | 20 ± 1 mOhm/sq | 22 ± 1 mOhm/sq
poly | 3.7 ± 0.8 kOhm/sq | 3.9 ± 1 kOhm/sq | 4 ± 1.2 kOhm/sq
p+ | 120 ± 10 Ohm/sq | 160 ± 10 Ohm/sq | 120 ± 10 Ohm/sq
n+ | 29 ± 2 Ohm/sq | 26 ± 6 Ohm/sq | 28 ± 2 Ohm/sq
characteristic | unirradiated | p@3E14
coupling capacitance | 43.4 ± 1.8 [pF/cm] | 44.4 ± 0.7 [pF/cm]
dielectric breakdown | 249 ± 2 [V] | 244 ± 6 [V]
Basic properties don‘t change at these fluences

## Slide 25: Interstrip resistance on TS
measurements are performed at -20°C
unirradiated
proton irradiated
neutron irradiated
interstrip resistance on teststructures drops from >200GOhm to <200MOhm after irradiation
courtesy of M. Bernard-Schwarzz, HEPHY
courtesy of M. Bernard-Schwarzz, HEPHY
courtesy of M. Bernard-Schwarzz, HEPHY
resistances on baby sensors in similar range
GOhm
MOhm
MOhm

## Slide 26: oxygen content
material | bulk resistivity | oxide concentration
FZ320P | 3-8 | 3,50E+016
FZ200P | 3-8 | 3,00E+017
FZ120P | 3-8 | 5,00E+017
FZ320N | 1.2-2.4 | 1,80E+016
FZ200P | 1.2-2.4 | 3,00E+017
FZ120P | 1.2-2.4 | 5,00E+017
MCZ200P | >2 | 3,75E+017
MCZ200N | >0.5 | 3,00E+017

## Slide 27: fluence computed from data with a fixed alpha
neutrons, 4E14
protons, 2.9E14
neutrons, 1E14
protons, 1.1E14
currents are measured at 0°C and scaled to 20°C

## Slide 28: interstrip resistance on baby sensor
FZ320P
FZ320N
proton irradiated
neutron irradiated
proton irradiated
interstrip resistance drops on baby sensors from >100GOhm to >100MOhm
measurements are performed at -20°C
courtesy of K. Hoffmann
courtesy of M. Bernard-Schwarz
courtesy of M. Bernard-Schwarz