## Slide 1: Field quality of HCQQXF_SC002-FL000001 (LMQXFA01 type Q3, with MQXFA03 and MQXFA04)
MAB meeting 20/01/2025
L. Fiscarelli

## Slide 2: Performed tests
At 1.9 K
  Field quality with Rotating Coils
    Machine cycles and Stair-step cycles
  Integrated gradient and alignment with Stretched wire
    Nominal current with both in series, low current for individual powering
At ambient temperature
  Longitudinal scan with Rotating Coil

## Slide 3: Rotating coils at 1.9 K
Anticryostat flange
Longitudinal center
Shaft too short to cover at the same time both magnets
Two measurement positions
Cycles repeated twice

## Slide 4: Main field and magnetic length
Current | A | 16230 |  |  |  | 
 |  | A03 | A04 | Integral |  | 
CERN |  |  |  |  |  | 
Integrated gradient | T | 559.53 | 559.62 | 1119.15 | SSW | 1119.03
Central gradient TF | T/m/kA | 8.1790 | 8.1828 |  |  | 
Lm | m | 4.215 | 4.214 |  |  | 
Nodal distance | m | 4.770 |  |  |  | 
FNAL |  |  |  |  |  | 
Integrated gradient | T | 559.70 | 559.95 | 1119.60 |  | 
Difference | units | 8 | 1 | 4 |  | 
Nodal distance | m | 4.772 |  |  |  | 
Difference | mm | -2 |  |  |  | 

## Slide 5: Field quality
Harmonics are given in units at the reference radius of 50 mm

## Slide 6: TF vs current - ramp-up of machine cycle

## Slide 7: Harmonics vs current - ramp-up of machine cycle

## Slide 8: Harmonics vs current - ramp-up of machine cycle

## Slide 9: Magnetic common axis (1.9 K)

## Slide 10: Relative magnetic axis (ambient temperature)

## Slide 11: Relative alignment – data from AUP

## Slide 12: Field direction
Relative angle measured at ambient temperature:
1.99 mrad

## Slide 13: Conclusions
Transfer function of the two magnet is within 5 units
In agreement with results from AUP (~5 units)
Results of field quality are confirmed as well:
  Only a8 slightly out of expected range (-1 units for MQXFA04)
Magnetic axis
  Common axis measured at 1.9 K
  Relative axis measured only at ambient temperature
  Relative angle at the limit (2.0 mrad)