## Slide 1
Charge collection studies of
65 nm CMOS MAPS
for ALICE ITS3
S. Perciballi* on behalf of ALICE
*Università di Torino, stefania.perciballi@unito.it
6th Allpix Squared User Workshop 2025 – Amsterdam 7-9 May

## Slide 2: ALICE Inner Tracking System (ITS2)
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
properties of the quark-gluon plasma produced in heavy-ion collisions
low momentum (≲1 GeV/c) particle reconstruction
ITS2 first large-area (∼10 m2 ) silicon tracker → MAPS
ALPIDE chip: TowerJazz 180 nm CMOS imaging process
Main characteristics:
7 layers of MAPS (3 inner - 4 outer barrel)
close to interaction point (23 mm)
single point resolution ∼ 5µm (pixel ∼ 29×27 µm2)
low material budget: 0.36% X0/X
fast readout:
    Pb-Pb collisions at 50 kHz (ITS1: 1 kHz)
    p-p at 400 kHz
2
The ALICE upgrade for Run3

## Slide 3: ITS3 – truly cylindrical wafer-scale MAPS tracker
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
3
Layout:
3 layers → replace ITS2 Inner Barrel
beam pipe inner radius (to 16 mm with 500 μm thickness)
closer to the beam pipe 23 mm → 18 mm
Technology:
65 nm CMOS from TPSCo (Tower Partners Semiconductor):
    300 mm wafer-scale chips, fabricated using stitching
thinned down to 50 µm
    flexible (bent to target radii)
mechanically held by carbon foam ribs with low density and high thermal conductivity
Benefits:
extremely low material budget: 0.09% X0/X per layer
homogeneous material distribution

## Slide 4: MAPS in the 65 nm CMOS technology
STANDARD
MODIFIED
MODIFIED WITH GAP
Process modification for fully depleted sensor:
  standard → ALPIDE like design
  modified → completely depleted
  modified with gap → increase the lateral field to speed up the charge collection process
4
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
MLR1: Multi Layer Reticle 1 → first submission in the TPSCo 65 nm technology
Charge Collection Speed
Charge Sharing
APTS
CE65
DPTS

## Slide 5: APTS-OA characterization setup
APTS (Analogue Pixel Test Structure) – OA (Operational Amplifier)
5
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
matrix sizes: 4×4
pixel pitch: 10 µm
4 inner pixels read out by the Oscilloscope → Sampling rate 40 GS/s
12 outer pixels read out by a custom made proximity board → Sampling rate 4 MS/s
→ preserve timing information
Measurements with a 55Fe X-ray source

## Slide 6: APTS-OA: waveform analysis
6
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
Details can be found in https://doi.org/10.1016/j.nima.2024.169896
Waveform parameters:
t0: minimum of signal derivative
baseline: average over 2.5 ns, at 15 ns before t0
underline: average over 2.5 ns, at 15 ns after t0
Amplitude: difference between baseline and underline
Fall time: time difference between 50% and 10% of the signal amplitude

## Slide 7: Charge Collection with 55Fe
Charge collection mainly by diffusion
7
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
STANDARD
MODIFIED
Charge collection mainly by drift
Reverse bias equal to -2.4V

## Slide 8: Charge Collection with 55Fe on modified sensors
8
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
MODIFIED
MODIFIED WITH GAP
It presents a slower component
in charge collection
It presents one main component
in charge collection
Reverse bias equal to -2.4V

## Slide 9: Charge Collection with 55Fe on modified sensors
9
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
MODIFIED
MODIFIED WITH GAP
It doesn’t change much with reverse bias
it becomes increasingly faster with reverse bias
Reverse bias equal to -4.8V

## Slide 10: Simulations: Pixel Geometry
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
Doping Profiles are covered by Non-Disclosure Agreement
The doping profiles shown in this presentation give comparable results to the proper doping profiles
MODIFIED WITH GAP
10
low dose n
n+
p-
p+
p-well
p-well

## Slide 11: TCAD Mesh
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
11
mesh = 0.1x0.1x0.1 µm3
12 µm of sensor depth
3D TCAD simulation
Mesh cut
Final mesh to be exported into AllPix2
Weighting potential evaluation
Notes: 3D TCAD simulation of a 2x2 pixel matrix of 10 µm pitch:
Finer mesh in one pixel corner (0.1x0.1x0.1) µm3
Simulating only 12 µm of the sensor depth to reduce computational time
From TCAD Mesh to AllPix2:
Mesh cut to consider only the corner pixel with finer mesh
Weighting Potential: 2 TCAD simulations of a 2x2 matrix with Vel of 0.4V and 0.41V → the weighting potential is calculated as the potential difference for each grid point
Final mesh exported into AllPix2
AllPix2 can reproduce the mesh for a full pixel and repeat it for the entire pixel matrix that we want to consider - field_mapping = ‘PIXEL_QUADRANT_I’’

## Slide 12: AllPix2 Flow
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
12
Mesh Converter
Simulation of 55Fe X-ray source
AllPix2 simulation
Pulse analysis
Notes: Mesh Converter: used to convert TCAD mesh into a mesh that can be imported into AllPix2 → the number of divisions must be ~ equal to the mesh in TCAD divisions = 50 50 120 xyz = x y z
Simulations of 55Fe X-Ray source using a macro: the physical process is completely simulated from the photon impinging on the sensor to the collected charge by the electrode
AllPix2 simulation: a 4x4 pixel matrix is simulated
Pulse analysis: the same analysis method is used both for the experimental data and the pulses collected by the simulation. For each event, the amplitude and fall time are extracted and the pixel coordinates are saved.

## Slide 13: AllPix2 Simulations – Modified with Gap
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
13
Simulations
Data
Simulation

## Slide 14: AllPix2 Simulations – Modified
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
14
Simulations
Data
Simulation

## Slide 15: AllPix2 Simulations Results
Electrode
Electrode
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
15
Fall time versus amplitude from the simulation: by separating the fast and slow component it is possible to obtain the conversion points in the sensor

## Slide 16: Fast Tail
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
16
One event animation of the fast tail population: the signal reaches almost the final amplitude after 500 ps
Electric Field [V/cm]

## Slide 17: Slow Tail
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
17
One event animation of the slow tail population: the signal reaches almost the final amplitude after 1.25 ns
Electric Field [V/cm]

## Slide 18: Charge Collection Speed
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
A linear trend is observed for the slow tail events at times less than 200 ps, not changing with reverse bias: this is due to the diffusion contribution (isotropic and independent to reverse bias) in the first part of the charge collection process.
By comparing charge collection at different reverse biases, it is possible to observe that the fast tail events don’t undergo significant differences, when changing reverse bias, while a decrease of charge collection speed is observed in the slow tail events.
18

## Slide 19: Conclusions
An unexpected behavior was observed on the modified with gap sensor with the 55Fe source
Some simulations using approximated doping profiles were made to fully understand the data
Even if approximate doping profiles were used, the experimental results can be reproduced
From the simulations, it can be established that this behavior is due to a feature of the electric field
These results and simulations helped to better understand sensors performance
The experimental data and the simulation results were confirmed using the proper doping profiles
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
19

## Slide 20: Thank you!
20
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
6th Allpix Squared User Workshop

## Slide 21: Tail Conversion Points
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
21
Electrode
Fall time versus amplitude from the simulation: by separating the fast and slow component it is possible to obtain the conversion points in the sensor

## Slide 22: Charge Collection with 55Fe
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
Increasing Vreverse bias
MODIFIED
MODIFIED WITH GAP
22

## Slide 23: MLR1 Test Structures
MLR1: Multi Layer Reticle 1 → first submission in the TPSCo 65 nm technology
APTS (Analogue Pixel Test Structure)
DPTS (Digital Pixel TS)
CE65 (Circuit Exploratoire)
aim: explore different pixel designs
matrix sizes: 4×4
pixel pitch: (10, 15, 20, 25) µm
Two types of output drivers:
Source follower (APTS-SF)
Operational Amplifier (APTS-OA) → preserve timing information
aim: study pixel matrix uniformity
matrix sizes: 64x32, 48x32
pixel pitch: 25, 15 μm
aim: study in-pixel discrimination
matrix sizes: 32×32
pixel pitch: 15 µm
6th Allpix Squared User Workshop 2025 – S. Perciballi / 7-9 May
23