## Slide 1: MCBXF test results MCBXFB05 – June 2024 MCBXFA1 – September 2024 MCBXFB06 – December 2024
Gerard Willering
Franco Mangiarotti, Lucio Fiscarelli, Piotr Rogacki, Jerome Feuvrier, Michael Boczan, Jean-Luc Guyon. Many thanks to all involved.
Test plan reference:
MCBXFA: EDMS 2801912
MCBXFB: EDMS 2783919
Test report reference:
MCBXFB05: EDMS 3123996
MCBXFA1: EDMS 3162193
MCBXFB06: EDMS 3221448 (no document yet)
WP3 meeting – 15 January 2025

## Slide 2: MCBXFB05

## Slide 3
MCBXFB05
HCMCBXFB012-E9000005
Reception tests at 2000 V: Passed
On insert in air at 300 K before cool down 1 at 200 V: Passed
Cool down 1 at 1.9 K before powering at 1000 V: Passed
Cool down 1 at 1.9 K after powering at 1000 V: Passed
Cool down 2 at 1.9 K before powering at 1000 V: Passed
Cool down 2 at 1.9 K after powering at 1000 V: Passed
HV insulation tests
Performed tests are inner dipole vs (outer dipole + ground) and outer dipole vs (inner dipole + ground)

## Slide 4
MCBXFB05 powering
Cool down 1
Individual powering one quench in inner dipole.
Combined powering: 6 quenches were registered in one angle in one of the quadrants to reach the ultimate operation space. Afterwards all powering tests showed stable operation.
Cool down 2
Individual powering without quench
Combined powering: All powering was stable to ultimate current.

## Slide 5
MCBXFB05 powering overview
Cool down 1 powering overview with the indication of the 6 quenches.
Cool down 2 powering overview

## Slide 6
MCBXFB05 resistances

## Slide 7: MCBXFA1

## Slide 8
MCBXFA1
HCMCBXFA011-E9000001
Reception tests at 2000 V: Passed
On insert in air at 300 K before cool down 1 at 200 V: Passed
Cool down 1 at 1.9 K before powering at 1000 V: Passed
Cool down 1 at 1.9 K after powering at 1000 V: Passed
Cool down 2 at 1.9 K before powering at 1000 V: Passed
Cool down 2 at 1.9 K after powering at 1000 V: Passed
HV insulation tests
Performed tests are inner dipole vs (outer dipole + ground) and outer dipole vs (inner dipole + ground)

## Slide 9
MCBXFA1 powering
Cool down 1
Individual powering: without quench.
Combined powering: One quench outside nominal perimeter
Cool down 2
Individual powering without quench
Combined powering: All powering was stable to ultimate current.

## Slide 10
MCBXFA1 powering overview
Cool down 1 powering overview with the indication of the quench.
Cool down 2 powering overview

## Slide 11
MCBXFA1 resistances

## Slide 12: MCBXFB06

## Slide 13
MCBXFB06
HCMCBXFA011-E9000001
Reception tests at 2000 V: Passed
On insert in air at 300 K before cool down 1 at 200 V: Passed
Cool down 1 at 1.9 K before powering at 1000 V: Passed
Cool down 1 at 1.9 K after powering at 1000 V: Passed
Cool down 2 at 1.9 K before powering at 1000 V: Passed
Cool down 2 at 1.9 K after powering at 1000 V: Passed
HV insulation tests
Performed tests are inner dipole vs (outer dipole + ground) and outer dipole vs (inner dipole + ground)

## Slide 14
MCBXFA1 powering
Cool down 1
Individual powering: without quench.
Combined powering: Two quenches outside nominal perimeter
Cool down 2
Individual powering without quench
Combined powering: One quench outside nominal perimeter

## Slide 15
MCBXFA1 powering overview Cool down 1
Cool down 1 powering overview with the indication of the two quenches.
Due to issues with the powering, only one 1-hour holding current test was done.

## Slide 16
MCBXFA1 powering overview Cool down 2
Cool down 2 powering overview with the indication of the one quench.
Additional holding current tests were performed, with 4 time 4 hours and 2 times 8 hours. All without quench.

## Slide 17
MCBXFB06 resistances
The room temperature resistance was measured, but during SC to normal transition the measurement could not be done. Therefore Table 2 only shows the room temperature resistance.

## Slide 18
Conclusions powering performance of MCBXF magnets tested vertically in 2024
For MCBXFB05, MBXFA1 and MCBXFB06:
Very good training performance in first and second cool down
All instrumentation OK.
All HV insulation tests passed
All holding current tests passed (1st CD: 2 times 4 hours and 2 times 1 hour, 2nd CD 4 times 4 hours). Additional holding current tests were performed up to 2*8 hours duration for MCBXFB06.

## Slide 19: Magnetic measurements By Lucio Fiscarelli and Piotr Rogacki

## Slide 20: MCBXFA01 – Field quality
All harmonics are within requirements

## Slide 21: MCBXFB05 – Field quality
All harmonics are within requirements, except for the b3 in combined powering at 2/2.5 Tm

## Slide 22: MCBXFB06 – Field quality
All harmonics are within requirements, except for the b3 in combined powering at 2/2.5 Tm

## Slide 23
Measurements at room temperature on MCBXFB magnets

## Slide 24: b3 - MCBXFB06 vs MCBXFB03

## Slide 25: Remarks on magnetic field characteristics
For MCBXFA01, all harmonics are within requirements for all powering configurations
For MCBXFB05 and MCBXFB06
The Transfer Function (TF), compared to previous magnets, is
    within ±20 units in individual powering,
    within ±30 units in combined powering.
Harmonics are within requirements except for the b3 in combined powering 2/2.5 Tm (±22 units).
The change of b3 (+5 units) measured at warm on B05/B06 with respect to previous magnets is confirmed by the measurements at cold. This, added to the saturation, contributes to the larger value of the b3.