## Slide 1
BOND 14T
Design Status
Ariel Haziot
E. Fernandez Mora, J. Ferradas Troitino, S. Izquierdo Bermudez, N. Peray, J.C. Perez, and E. Todesco
December 19th, 2024

## Slide 2
Introduction
BOND in the framework of HFM:
BOND stands for BlOck coil Nb3Sn Dipole
Block-type coils with flared ends – 14 T bore field (50 mm aperture) with ≈ 20 % load line margin at 14 T and 1.9 K.

## Slide 3
Outline
BOND Single Aperture
  Baseline - Magnetic design
  Baseline - Mechanical model
  Baseline - Engineering
  Alternative 40x1.1 design
BOND Double Aperture
  Baseline - Magnetic design
  Baseline - Mechanical model

## Slide 4
BOND Single Aperture
Baseline - Magnetic Design

## Slide 5
BOND single – Baseline parameters
Cable: 44 x 1.1 mm
Conductor parameters |  | 
Strand diameter | (mm) | 1.10
Layout |  | RRP 162/169
Effective filament diameter | (µm) | 64
Jc at 4.2 K and 16 T | (A/mm2) | 1200
Cu/NonCu ratio |  | 0.9
No. of strands in cable |  | 44
Bare cable thickness | (mm) | 1.91
Bare cable width | (mm) | 26.20
Bare cable thickness (reacted) | (mm) | 1.99
Bare cable width (reacted) | (mm) | 26.46
Insulation thickness | (mm) | 0.15
Insulated cable width (reacted) | (mm) | 26.76
Insulated cable thickness (reacted) | (mm) | 2.29
Astrand | (mm2) | 0.950
Asc | (mm2) | 0.500
Acu | (mm2) | 0.450
23
29
1.15 mm
0.5 mm
Interlayer
Midplane
50 mm
Aperture

## Slide 6
BOND single – Baseline parameters
Coil dimensions

## Slide 7
BOND single – Baseline parameters
Iron dimensions
60.295
50
85.295
135
87.92
R=20
R=270
R=24
X0: 45 Y0: 195
142.92
140
20
15
20

## Slide 8
BOND single – Baseline magnetic design
2D magnetic (ROXIE)
Overall Parameters |  | 
Aperture | (mm) | 50
Field | (T) | 14.00
Field integral | (T m) | 16.17
Magnetic length | (m) | 1.16
Coil length | (m) | 1.40
Number of apertures | (adim) | 1
Distance between apertures | (mm) | -
Yoke outer diameter | (mm) | 540
Shell outer diameter | (mm) | 640
Cable data |  | 
Material |  | Nb3Sn
Process |  | RRP
No. strands | (adim) | 44
Strand diameter | (mm) | 1.100
Cu/NonCu | (adim) | 0.9
RRR | (adim) | 150
Bare cable thickness (R) | (mm) | 1.99
Bare cable width (R) | (mm) | 26.460
Insulation thick radial (5 Mpa) | (mm) | 0.150
Insulated cable surface | (mm2) | 61.28
Filling factor | (adim) | 0.359
Coil design |  | 
Insulated cable surface (one aperture) | (mm2) | 12746
Equivalent coil width | (mm) | 56.9
Coil efficiency | (T mm / A) | 0.00074
N. layers | (adim) | 2
N. turns/pole | (adim) | 52
Cable length/pole | (m) | 153
Operational parameters |  | 
Current (Inom) | (kA) | 20.255
Peak Field | (T) | 14.75
Short sample current @ 1.9 K | (kA) | 25.300
Short sample current @ 4.5 K | (kA) | 22.560
Short sample field @ 1.9 K | (T) | 17.91
Short sample field @ 4.5 K | (T) | 16.15
j overall | (A/mm2) | 331
j strand | (A/mm2) | 484
j superconductor | (A/mm2) | 920
Loadline fraction @1.9 K | (%) | 80.1
Loadline fraction @4.5 K | (%) | 89.8
Stored energy/m | (MJ/m) | 1.030
Inductance/m | (mH/m) | 4.60
Stored energy | (MJ) | 1.45
Field quality |  | 
Harmonic b2 @ Inom | (10-4) | 0.00
Harmonic b3 @ Inom | (10-4) | 8.80
Harmonic b4 @ Inom | (10-4) | 0.00
Harmonic b5 @ Inom | (10-4) | 6.60
Harmonic b7 @ Inom | (10-4) | 1.96
Protection |  | 
Coil energy density | (J/mm3) | 0.081
j copper | (A/mm2) | 1023
Temperature margin @ 1.9 K | (K) | 4.13
Time margin | (ms) | 91
Hot spot Temperature | (K) | 108
Mechanics |  | 
Forces x ( per quadrat) | (MN/m) | 6.027
Forces y ( per quadrat) | (MN/m) | -2.688
Force z (per head) | (MN) | 0.966

## Slide 9
BOND single – Baseline magnetic design
2D magnetic (ROXIE)

## Slide 10
BOND single – Baseline magnetic design
2D magnetic (ROXIE)

## Slide 11
BOND single – Baseline magnetic design
3D magnetic (ROXIE)
3D parameters |  | 
Flared end curvature radius | (mm) | 750/803
Flared end angle | (º) | 5
Flared end straight part | (mm) | 250/248
Flared end length | (mm) | 402
Straight section length | (mm) | 600
Pad length | (mm) | 600
Iron yoke length | (mm) | 1400
Iron yoke
Iron pads
Field at center: 14.12 T
Field integral: 16.17 T.m
Magnetic length: 1.15 m

## Slide 12
BOND single – Baseline magnetic design
3D magnetic (Opera)
B peak
Chart: Z [m]
Field at center: 14.11 T
Field integral: 16.22 T.m
Magnetic length: 1.15 m
Courtesy of E. Fernandez Mora

## Slide 13
Chart: Current [A]
| 100 | 1012.75 | 2025.5 | 3038.25 | 4051 | 5063.75 | 6076.5 | 7089.25 | 8102 | 9114.75 | 10127.5 | 11140.25 | 12153 | 13165.75 | 14178.5 | 15191.25 | 16204 | 17216.75 | 18229.5 | 19242.25 | 20255
Bond single 2D | 0.94 | 0.9355 | 0.93312 | 0.91931 | 0.90018 | 0.8768 | 0.85499 | 0.83562 | 0.81802 | 0.80143 | 0.785 | 0.76927 | 0.7555 | 0.74357 | 0.73316 | 0.72402 | 0.71593 | 0.70871 | 0.70225 | 0.69642 | 0.69115
Bond single 3D Roxie | 0.93 | 0.93113 | 0.89854 | 0.85404 | 0.81832 | 0.78782 | 0.76096 | 0.73912 | 0.73004 | 0.72192 | 0.70801 | 0.69662
Bond single 3D Opera | 0.93506 | 0.93506 | 0.93506 | 0.93204 | 0.91707 | 0.89735 | 0.87345 | 0.8519 | 0.83362 | 0.81782 | 0.80315 | 0.78938 | 0.77648 | 0.76423 | 0.75267 | 0.74212 | 0.73266 | 0.72422 | 0.71666 | 0.70985 | 0.7037 | 0.69812 | 0.69678 | 0.69303 | 0.68838
BOND single – Baseline magnetic model
Transfer function

## Slide 14
BOND Single Aperture
Baseline - Mechanical Model

## Slide 15
BOND single – Baseline mechanical model
Introduction to mechanical model
Al-cylinder based mechanical structure – Bladder and Key loading procedure
Bonded coil components. Frictional contacts anywhere else (µ = 0.2)
Isotropic material properties
Criteria
Use same modelling assumptions as MQXF, which we know well
Target similar coil peak stress limits at warm/cold as MQXF:
  RT below 110 - 120 MPa
  CD below 150 MPa
Maintain an average contact pressure > 5 MPa
All components below yield limits: SVM or S1 at cold for brittle materials
Spacer in Stainless to improve cooling
Courtesy of J. Ferradas Troitino

## Slide 16
BOND single – Baseline mechanical model
Results summary
Coil stresses
Coil contact pressure
Stress limits in the structure
Coil displacements
Coil longitudinal strain
Coil is below stress limits:
σVM < 120 MPa at RT
σVM < 150 MPa at cold
Roughly: εz < 2000 µstr
All components below yield limits (SVM or S1 for brittle materials)
Average contact pressure > 5 MPa during powering
Coil and pole displacements
< 0.1 mm during powering
Courtesy of J. Ferradas Troitino

## Slide 17
Warm (Peak: 71 Mpa)
Cold (Peak: 150 Mpa)
Field (Peak: 132 Mpa)
BOND single – Baseline mechanical model
Equivalent stress on coil
Contact pressure at 14 T
Courtesy of J. Ferradas Troitino

## Slide 18
Forces from Opera 3D model
  Total force imported:
  Fx = 3.7 MN (5.3 MN/m)*
  Fy = -1.5 MN (-2.13 MN/m)*
  Fz = -0.27 MN (-1.079 MN total)
Temporary endplate (100 mm thick)
No lateral contact with the wedge.
Endpusher only against the coils.
* Assuming 700 mm length
1522.9 mm / 2
1400 mm / 2
600 mm / 2
Isotropic coil material model (same as 2D)
Same horizontal interference as 2D (650µm horizontal), 50µm for the vertical one
BOND single – Baseline mechanical model
3D mechanical model (Ansys)
Courtesy of J. Ferradas Troitino

## Slide 19
BOND single – Baseline mechanical model
3D mechanical model (Ansys)
Warm (Peak: 66 Mpa)
Cold (Peak: 159 Mpa)
Field (Peak: 122 Mpa)
Courtesy of J. Ferradas Troitino

## Slide 20
BOND Single Aperture
Baseline - Mechanical Model

## Slide 21
BOND single – Baseline engineering
Engineering design on-going
Courtesy of N. Peray

## Slide 22
BOND single – Baseline engineering
Tooling for reaction and impregnation under development
Reaction
Impregnation
Courtesy of N. Peray

## Slide 23
BOND Single Aperture
40x1.1 mm – Alternative option

## Slide 24
BOND single – 40x1.1 mm option
40 x 1.1 mm parameters
Conductor parameters |  | 
Strand diameter | (mm) | 1.10
Layout |  | RRP 162/169
Effective filament diameter | (µm) | 64
Jc at 4.2 K and 16 T | (A/mm2) | 1200
Cu/NonCu ratio |  | 0.9
No. of strands in cable |  | 40
Bare cable thickness | (mm) | 1.91
Bare cable width | (mm) | 23.81
Bare cable thickness (reacted) | (mm) | 1.99
Bare cable width (reacted) | (mm) | 24.05
Insulation thickness | (mm) | 0.15
Insulated cable width (reacted) | (mm) | 24.35
Insulated cable thickness (reacted) | (mm) | 2.29
A strand | (mm2) | 0.950
A sc | (mm2) | 0.500
A cu | (mm2) | 0.450
23
29
3.0 mm
2.0 mm
Interlayer
Midplane
Same 50 mm aperture
Same coil pack dimension as baseline
Adjustment of coil position to optimize field quality
50 mm
Aperture

## Slide 25
Bond single - 40x1.1 mm magnetic design
2D magnetic (ROXIE)
Overall Parameters |  | 
Aperture | (mm) | 50
Field | (T) | 14.00
Field integral | (T m) | 16.17
Magnetic length | (m) | 1.16
Coil length | (m) | 1.40
Number of apertures | (adim) | 1
Distance between apertures | (mm) | -
Yoke outer diameter | (mm) | 540
Shell outer diameter | (mm) | 640
Cable data |  | 
Material |  | Nb3Sn
Process |  | RRP
No. strands | (adim) | 40
Strand diameter | (mm) | 1.100
Cu/NonCu | (adim) | 0.9
RRR | (adim) | 152
Bare cable thickness (R) | (mm) | 1.99
Bare cable width (R) | (mm) | 24.050
Insulation thick radial (5 Mpa) | (mm) | 0.150
Insulated cable surface | (mm2) | 55.76
Filling factor | (adim) | 0.359
Coil design |  | 
Insulated cable surface (one aperture) | (mm2) | 11598
Equivalent coil width | (mm) | 53.5
Coil efficiency | (T mm / A) | 0.00073
N. layers | (adim) | 2
N. turns/pole | (adim) | 52
Cable length/pole | (m) | 153
Operational parameters |  | 
Current (Inom) | (kA) | 19.915
Peak Field | (T) | 14.83
Short sample current @ 1.9 K | (kA) | 24.283
Short sample current @ 4.5 K | (kA) | 21.657
Short sample field @ 1.9 K | (T) | 17.95
Short sample field @ 4.5 K | (T) | 15.95
j overall | (A/mm2) | 357
j strand | (A/mm2) | 524
j superconductor | (A/mm2) | 995
Loadline fraction @1.9 K | (%) | 82.0
Loadline fraction @4.5 K | (%) | 92.0
Stored energy/m | (MJ/m) | 2.194
Inductance/m | (mH/m) | 4.64
Stored energy | (MJ) | 3.07
Field quality |  | 
Harmonic b2 @ Inom | (10-4) | 0.00
Harmonic b3 @ Inom | (10-4) | 6.70
Harmonic b4 @ Inom | (10-4) | 0.00
Harmonic b5 @ Inom | (10-4) | 4.23
Harmonic b7 @ Inom | (10-4) | 1.17
Protection |  | 
Coil energy density | (J/mm3) | 0.095
j copper | (A/mm2) | 1106
Temperature margin @ 1.9 K | (K) | 4.00
Time margin | (ms) | 76
Hot spot Temperature | (K) | 112
Mechanics |  | 
Forces x ( per quadrat) | (MN/m) | 5.926
Forces y ( per quadrat) | (MN/m) | -2.651
Force z (per head) | (MN) | 

## Slide 26
Bond single - 40x1.1 mm magnetic design
2D magnetic (ROXIE)

## Slide 27
Bond single - 40x1.1 mm
2D magnetic (ROXIE)

## Slide 28
Bond single - Alternative options
2D magnetic (ROXIE)
Coil design |  | Baseline | 40x1.1
Insulated cable surface (one aperture) | (mm2) | 12746 | 11598
Equivalent coil width | (mm) | 56.9 | 53.5
Coil efficiency | (T mm / A) | 0.00074 | 0.00073
N. layers | (adim) | 2 | 2
N. turns/pole | (adim) | 52 | 52
Cable length/pole | (m) | 153 | 153
Relative conductor difference to baseline | (%) | 0 | 9.0
Operational parameters |  |  | 
Current | (kA) | 20.255 | 19.915
Peak Field | (T) | 14.75 | 14.83
Short sample current @ 1.9 K | (kA) | 25.300 | 24.283
Short sample current @ 4.5 K | (kA) | 22.560 | 21.657
Short sample field @ 1.9 K | (T) | 17.91 | 17.95
Short sample field @ 4.5 K | (T) | 16.15 | 15.95
j overall | (A/mm2) | 331 | 357
j strand | (A/mm2) | 484 | 524
j superconductor | (A/mm2) | 920 | 995
Loadline fraction @1.9 K | (%) | 80.1 | 82.0
Loadline fraction @4.5 K | (%) | 89.8 | 92.0

## Slide 29
Bond single - Alternative options
Discussion
Coil design |  | Baseline | 40x1.1
Insulated cable surface (one aperture) | (mm2) | 12746 | 11598
Equivalent coil width | (mm) | 56.9 | 53.5
Coil efficiency | (T mm / A) | 0.00074 | 0.00073
N. layers | (adim) | 2 | 2
N. turns/pole | (adim) | 52 | 52
Cable length/pole | (m) | 153 | 153
Relative conductor difference to baseline | (%) | 0 | 9.0
Operational parameters |  |  | 
Current | (kA) | 20.255 | 19.915
Peak Field | (T) | 14.75 | 14.83
Short sample current @ 1.9 K | (kA) | 25.300 | 24.283
Short sample current @ 4.5 K | (kA) | 22.560 | 21.657
Short sample field @ 1.9 K | (T) | 17.91 | 17.95
Short sample field @ 4.5 K | (T) | 16.15 | 15.95
j overall | (A/mm2) | 331 | 357
j strand | (A/mm2) | 484 | 524
j superconductor | (A/mm2) | 920 | 995
Loadline fraction @1.9 K | (%) | 80.1 | 82.0
Loadline fraction @4.5 K | (%) | 89.8 | 92.0
Pros
cable production at CERN
less conductor
  9 %
  ~3 km of strand for BOND Double
more interlayer spacings
  3 mm at midplane, 1.5 mm at interlayer
Cons
cable to be developed
less margin
  ~2 % (92% shortsample at 4.5K)

## Slide 30
BOND Double Aperture
2D Magnetic design

## Slide 31
Bond Double
From Single to Double
V1: Straight from single with central pad -> too high stress at the corner
V2: Introduction of:
  4 pieces yoke,
  optimized central pad with SS master
  extra rod hole
V1
V2

## Slide 32
Bond Double
Magnetic field quality optimization
Gap = 10 mm
Gap = 15 mm
Gap = 20 mm
Full gap
Open
Close

## Slide 33
BOND Double – Baseline parameters
Iron dimensions
R=24
X0: 125 Y0: 195
60.295
50
85.295
135
87.92
R=20
140
20
15
20
142.92
125
200
20
105
R=24
X0: 0 Y0: 195
R=340

## Slide 34
BOND Double – Baseline magnetic design
2D magnetic (ROXIE)
Overall Parameters |  | 
Aperture | (mm) | 50
Field | (T) | 14.00
Field integral | (T m) | 16.17
Magnetic length | (m) | 1.16
Coil length | (m) | 1.40
Number of apertures | (adim) | 2
Distance between apertures | (mm) | 250
Yoke outer diameter | (mm) | 680
Shell outer diameter | (mm) | 780
Cable data |  | 
Material |  | Nb3Sn
Process |  | RRP
No. strands | (adim) | 44
Strand diameter | (mm) | 1.100
Cu/NonCu | (adim) | 0.9
RRR | (adim) | 150
Bare cable thickness (R) | (mm) | 1.99
Bare cable width (R) | (mm) | 26.460
Insulation thick radial (5 Mpa) | (mm) | 0.150
Insulated cable surface | (mm2) | 61.28
Filling factor | (adim) | 0.359
Coil design |  | 
Insulated cable surface (one aperture) | (mm2) | 12746
Equivalent coil width | (mm) | 56.9
Coil efficiency | (T mm / A) | 0.00077
N. layers | (adim) | 2
N. turns/pole | (adim) | 52
Cable length/pole | (m) | 153
Operational parameters |  | 
Current (Inom) | (kA) | 19.590
Peak Field | (T) | 14.72
Short sample current @ 1.9 K | (kA) | 24.581
Short sample current @ 4.2 K | (kA) | 21.904
Short sample field @ 1.9 K | (T) | 18.00
Short sample field @ 4.2 K | (T) | 16.25
j overall | (A/mm2) | 320
j strand | (A/mm2) | 468
j superconductor | (A/mm2) | 890
Loadline fraction @1.9 K | (adim) | 0.797
Loadline fraction @4.2 K | (adim) | 0.894
Stored energy/m | (MJ/m) | 2.064
Inductance/m | (mH/m) | 10.00
Stored energy | (MJ) | 2.89
Field quality |  | 
Harmonic b2 @ Inom | (10-4) | -8.12
Harmonic b3 @ Inom | (10-4) | 11.55
Harmonic b4 @ Inom | (10-4) | -0.07
Harmonic b5 @ Inom | (10-4) | 6.37
Harmonic b7 @ Inom | (10-4) | 1.89
Protection |  | 
Coil energy density | (J/mm3) | 0.081
j copper | (A/mm2) | 989
Temperature margin @ 1.9 K | (K) | 4.13
Time margin | (ms) | 104
Hot spot Temperature | (K) | 106
Mechanics |  | 
Forces x ( per quadrat) | (MN/m) | 6.107
Forces y ( per quadrat) | (MN/m) | -2.531
Force z (per head) | (MN) | 

## Slide 35
BOND Double – Baseline magnetic design
2D magnetic (ROXIE)

## Slide 36
BOND Double – Baseline magnetic design
2D magnetic (ROXIE)

## Slide 37
BOND Double Aperture
2D Mechanical model

## Slide 38
BOND Double – Baseline mechanical model
Mesh, contacts and symmetries
bonded
sliding
interference
coupled
symmetry

## Slide 39
Warm
Cold
Field
BOND Double – Baseline mechanical model
Displacement plots
Horizontal key interference: 0.8 mm
Vertical key interference: 0.03 mm
Central key interference: 0.8 mm

## Slide 40
BOND Double – Baseline mechanical model
Coil equivalent stress
Warm (Peak: 65 MPa)
Cold (Peak: 133 MPa)
Field (Peak: 150 MPa)
Horizontal key interference: 0.8 mm
Vertical key interference: 0.03 mm
Central key interference: 0.8 mm

## Slide 41
BOND Double – Baseline mechanical model
Stress on structural parts

## Slide 42
BOND Double – Baseline mechanical model
Coil equivalent stress
Interference (0.8 mm) already high
Not enough contribution from the shell at cooling
Need for a thicker shell
Iron becomes the limiting factor
Shell: 50 mm
Shell: 80 mm

## Slide 43
BOND Double – Baseline mechanical model
Coil equivalent stress
Warm (Peak: 83 MPa)
Cold (Peak: 152 MPa)
Field (Peak: 162 MPa)
Horizontal key interference: 0.8 mm
Vertical key interference: 0.03 mm
Central key interference: 0.8 mm

## Slide 44
BOND Double – Baseline mechanical model
Stress on structural parts

## Slide 46
Parameters for coil optimization

## Slide 47
Parameters for field homogeneity